Table S1 Macroscopic phenotypes of twelve corn (Zea mays L.) cultivars.

| Cultivar | Dry Weight (g) | Height (cm) | Diameter (mm) |
| --- | --- | --- | --- |
| CF 22 | 150.15±16.82 | 354.48±0.71 | 23.52±0.68 |
| DK 301 | 110.24±5.21 | 270.52±17.68 | 23.93±1.52 |
| FY 968 | 139.08±11.48 | 332.52±17.68 | 20.72±2.25 |
| JA 588 | 143.92±32.88 | 342.50±20.51 | 21.8±0.028 |
| JL 327 | 102.56±23.89 | 256.51±4.95 | 16.28±2.16 |
| KXA 4574 | 111.35±1.63 | 271.54±30.41 | 21.21±1.61 |
| LH 1 | 141.79±6.07 | 335.49±6.36 | 22.38±2.99 |
| SN 211 | 140.99±21.43 | 320.53±10.61 | 22.29±1.57 |
| SY 801 | 122.58±7.65 | 278.00±21.21 | 18.07±2.04 |
| XY 335 | 137.77±7.38 | 323.75±3.89 | 21.35±0.53 |
| YH 2 | 151.90±15.06 | 351.00±9.90 | 22.29±0.014 |
| ZX 618 | 124.94±1.98 | 298.50±4.95 | 16.45±2.33 |

Table S2 Reducing sugar yields for each region of DK 301 and YH 2.

| Cultivar | Part | Reducing sugar yield (%) |
| --- | --- | --- |
| DK 301 | Leaf | 33.22±0.60a |
|  | Sheath | 19.30±0.40b |
|  | Rind | 37.47±1.26c |
|  | Pith | 38.80±0.15d |
| YH 2 | Leaf | 23.32±0. 32e |
|  | Sheath | 19.92±0. 12b |
|  | Rind | 16.09±0.19g |
|  | Pith | 25.97±0.80g |

The data labeled by the different superscripts (a–g) were different from each other (p<0.05).

Table S3 Physical-chemical properties for each regions of various DK 301 sample.

| Part | Physical properties |  |  |  | Chemical properties |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | CrI | DP | CD(nm) | DO/DB | Cel (%) | NDS (%) | H-Cel (%) | Lig (%) | Ash (%) |
| Leaf | 23.89±0.92a | 474.42±10.74a | 17.70±1.70a | 0.84±0.015a | 39.76±1.08a | 21.70±1.20a | 27.20±1.56a | 7.99±0.12a | 3.23±0.12a |
| Sheath | 36.18±0.051b | 746.39±0.46b | 14.19±0.04b | 0.74±0.01b | 35.08±0.31b | 4.68±0. 50b | 41.42±0.50b | 16.23±0.478b | 2.25±0.090b |
| Rind | 42.06±0.97c | 761.75±10.22b | 10.10±0.80c | 1.29±0.02c | 45.65±0.31c | 15.28±0.52c | 20.77±1.26c | 13.88±0.39c | 4.18±0.066c |
| Pith | 23.57±0.27a | 351.76±2.66c | 18.65±0.65a | 1.73±0.01d | 40.79±0.04a | 14.71±1.17c | 33.51±1.10d | 7.54±0.11a | 2.52±0.12d |

The data labeled by the different superscripts (a–d) within the same column were different from each other (p<0.05). NDS: neutral detergent soluble; H-Cel: hemicelluloses; Cel: cellulose; ASL: acid soluble lignin; AIL: acid insoluble lignin.

Table S4 Physical-chemical properties for each regions of various YH 2 sample.

| Part | Physical properties |  |  |  | Chemical properties |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | CrI | DP | CD (nm) | DO/DB | Cel (%) | NDS (%) | H-Cel (%) | Lig (%) | Ash (%) |
| Leaf | 44.35±1.68a | 726.82±2.89a | 19.80±0.40a | 1.30±0.0058a | 26.14±0.81a | 19.80±1.05a | 31.74±0.74a | 20.59±1.93a | 1.69±0.24a |
| Sheath | 35.54±0.13b | 706.02±0.49b | 13.85±0.35b | 0.73±0.0058b | 36.81±0.15b | 5.28±0.57b | 37.36±1.03b | 15.19±0.76b | 5.28±0.049b |
| Rind | 55.39±0.12c | 1124.75±2.66c | 10.15±0.35c | 0.83±0.01c | 31.57±1.18c | 11.64±0.085c | 23.79±0.59c | 26.44±1.82c | 6.27±0.035c |
| Pith | 33.96±1.76b | 457.01±3.90d | 13.50±0.50b | 1.70±0.01d | 29.73±1.16d | 16.53±1.43d | 29.02±1.99d | 21.65±0.62a | 2.27±0.031d |

The data labeled by the different superscripts (a–d) within the same column were different from each other (p<0.05). NDS: neutral detergent soluble; H-Cel: hemicelluloses; Cel: cellulose; ASL: acid soluble lignin; AIL: acid insoluble lignin.