Phosphorus-Doped NiFe Electrodes for Stable Alkaline Seawater Electrolysis at Industrial Current Densities: Facile Synthesis and Mechanistic Insights

Wei Wang*, Zhibo Ren, Peng Liu, Chang Zhang, Tao Wang, Fan Wang, Xupeng Yan, Weiqi Guo, Zhan Wu , Jinyi Wang*

Huaneng Clean Energy Research Institute, Beijing, 102209, China.

* Corresponding Author

Email: w_wang@qny.chng.com.cn; jy_wang@qny.chng.com.cn

Figure

Fig. S1 SEM images of NiFe-NF1

Fig. S2 OER activity of PNiFe NF, NiFe NF and nickel foam (NF) in 30 wt% KOH and 20 wt% NaOH + 0.5 M NaCl electrolyte

Fig. S3 CV curves at different sweep rates of the electrode in 30 % KOH + 0.5 M NaCl solution: (a)NF, (b)NiFe-NF, (c) PNiFe-NF.

Table

Tab. S1 The electrochemically active surface area of NF, NiFe-NF, and P-NiFe-NF electrodes in 30 % KOH + 0.5 M NaCl solution

| ECSA(cm2) | NF | NiFe-NF | P- NiFe-NF |
| --- | --- | --- | --- |
| 30% KOH+0.5M NaCl | 54.25 | 90.25 | 156.00 |

Tab. S2 The concentration of ions in natural seawater

| Ions | K+ | Ca2+ | Mg2+ | Na+ | Cl- | SO42- |
| --- | --- | --- | --- | --- | --- | --- |
| Concentration (mg/L) | 324 | 335 | 1072 | 10117 | 17171 | 2290 |

# References:

1.	Liu, P.;  Wang, J.;  Wang, X.;  Liu, L.;  Yan, X.;  Wang, H.;  Lu, Q.;  Wang, F.; Ren, Z., A superhydrophilic NiFe electrode for industrial alkaline water electrolysis. Int. J. Hydrog. Energy 2024, 49, 285-294.