Supplementary Information

Preparation of Al2TiO5 ceramic fibers and thermal expansion, insulation, and strength of ZrO2-Al2TiO5 fiberboards

Wei Liu, Yongshuai Xie, Zhezhe Deng, Ying Peng, Jianhong Dong, Ze Zhu, Dehua Ma, Luyi Zhu*, Guanghui Zhang, Xinqiang Wang

State Key Laboratory of Crystal Materials, School of Crystal Materials, Shandong University, Jinan 25010, P.R. China

*Corresponding author: Luyi Zhu, *E-mail: zhuly@sdu.edu.cn

Fig. S1. Crystal structure of Al2TiO5.

Fig. S2. Macroscopic image of PAAT precursor fibers.

Table S1. The assignments of the FT-IR spectral peaks of PAAT precursor and Al2TiO5 fibers heat-treated at different temperatures

| Wavenumber/cm-1 | Assignment |
| --- | --- |
| 3441 | H-O str. |
| 2956, 2922 | CH3 str. |
| 2852 | CH2 str. |
| 1627 | C=O antisym. str. |
| 1532 | C=C antisym. str. |
| 1453 | C=O sym. str. |
| 1381 | CH3 rock |
| 1289 | C-H sym. def |
| 1029 | C-H rock |
| 936 | C-C str. |
| 780, 706, 659 | Al-O str. |
| 609, 560 | Ti-O str. |

Fig. S3. 1H NMR spectra of PAAT precursor.

Table S2. Attribution of chemical shift peaks in 1H NMR spectra

| Alphabetical order | Chemical shift (ppm) | Assignment |
| --- | --- | --- |
| a | 0.99 | -CH3 in C6H15N⸱HCl |
| b | 1.06 | -CH3 in C2H5OH |
| c | 1.88 | -CH3 in CH3OH |
| d | 1.97 | C-N in C6H15N⸱HCl |
| e | 2.09 | -CH3 in Acac- |
| f | 2.51 | DMSO-D6 |
| g | 2.86 | Al-OH |
| h | 3.17 | -CH3 in CH3OH |
| i | 3.37 | -OH in H2O |
| j | 3.44 | Ti-OH |
| k | 4.11 | -OH in CH3OH |
| l | 5.51 | -CH in CH3OH |

Fig. S4. XPS spectra of PAAT precursor, (A) C1s, (B) O1s, (C) Al2p, (D) Ti2p.

The surface elemental composition and valence states of PAAT precursor fibers were determined by XPS spectra, as shown in Fig. S4. The surface of the precursor fibers containd C, O, Al and Ti elements. Simultaneously, the fine structure of the four elements was analyzed. The three peaks of C1S energy spectrum are located at 288.27, 286.39 and 284.57 eV respectively, which can be attributed to C=O, C-O and C-C (Fig. S4A). The fitting peaks of O1s energy spectrum (Fig. S4B) were C-O, M (Al, Ti)-OH and M (Al, Ti)-O, and the binding energies were 532.12, 531.41 and 529.77 eV, respectively. The peak of element Al2p (Fig. S4C) appeared at 74.31 eV and was attributed to Al (III). The binding energy of Ti2p1/2 and Ti2p3/2 were 463.8 and 458.15 eV, respectively, which were attributed to Ti (IV) (Fig. S4D).

Fig. S5. Molecular structures of (A) Aluminium acetylacetonate; (B) Titanium acetylacetonate.

Fig. S6. (A) The flexural strength and fracture deflection curves of ZAT fiberboards. (B) The bending stress-displacement curves of ZAT fiberboards.

Table S3. Testing results of thermal shock resistance of samples

| The sample | Number of thermal shock resistance | Apparent morphology after thermal shock |
| --- | --- | --- |
| ZAT-0 | 1 | Instant splitting |
| ZAT-1 | 4 | After 4 times fracture |
| ZAT-2 | 10 | Cracking after 10 times |
| ZAT-5 | 29 | Cracking after 29 times |
| ZAT-8 | 51 | Slight flaking after 51 times |

Fig. S7. (A) Schematic of the infrared imaging test device. (B) Time-dependent temperature profile of the center point on the cold surface. (C) Infrared image of the hot surface of Al2TiO5 fibers (2 mm thick) heated at 1265ºC and the illustration is an optical photograph subjected to a butane torch flame. (D-E) Infrared image of the cold surface of Al2TiO5 fibers, (D)after 60 s, (E) after 180 s.