Table 1 Materials used in this study

| No. | Product | Manufacturer | Properties |  |  |  |  | Structure |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Form | Density@ 25 ºC | Solubility in water | M.Wt. | Conc. |  |  |
| 1 | Nonylphenol 9 ethoxylate C33H60O10 | DOW | Transparent viscous liquid | 1.055g/cm3 | Soluble | 616.82 | 100% |  |  |
| 2 | Demtrol 1010 |  | Transparent viscous liquid | 1.01g/cm3 | Sparingly soluble | 2000 Da | 100% |  | propylene oxide/ethylene oxide (PO/EO) polyol block |
| 3 | Demtrol 1015 |  | Transparent viscous liquid | 1.02 g/cm3 | Slightly soluble | 5700 Da | 100% |  |  |
| 4 | Demtrol 1020 |  | Transparent viscous liquid | 1.01g/cm3 | low solubility | 4000 DA | 100% |  |  |
| 5 | Demtrol 1115 |  | Transparent viscous liquid | 1.02 g/cm3 | Slightly soluble | 6100 Da | 100% |  |  |
| 6 | C-A | Champion X | Pale yellow viscous liquid | 0.9746 g/cm3 | Dispersable | - | >50% |  | Mixture of ionic and nonionic surfactants dissolved in naphtha |
| 7 | B-A | Baker Hughes | Pale yellow liquid | 0.9236 g/cm3 | Dispersable | - | >50% |  | Mixture of ionic and nonionic surfactants dissolved in naphtha |
| 8 | B-B | Baker Hughes | Pale yellow liquid | 0.9244 g/cm3 | Dispersable | - | >50% |  |  |
| 9 | PEG 600 mono Oleate | Alpha | Pale yellow liquid | 0.895 g/cm3 | Dispersable | 864.5 | >97% |  | (C27H86 O14.5) |
| 12 | PEG 600 di Caprylate | Alpha | Transparent viscous liquid | 0.99 g/cm3 | Dispersable | 843.0 | >97% |  | (C42H82O16) |
| 13 | PEG 600 phthalate | Alpha | Pale yellow liquid | 1.53g/cm3 | Dispersable | 739 | >90% |  | C8H4O3 |
| 14 | Tween 80 | Alpha | Transparent viscous liquid | 1.12g/cm3 | Dispersable | 600 | >90% |  | C26H56O7.5 |
| 15 | Tween 20 | Alpha | Pale yellow liquid | 1.10 g/cm3 | soluble | 1,227 g/mole | >90% |  | C58H114O26 |
| 16 | Benzalkonium chloride | Alpha | Semi Solid | 0.98 g/cm3 | Miscible | 339.99 g/mol | 97.8% |  | C21H38ClN |
| 17 | Sodium xylene sulfonate | Alpha | Transparent liquid | 1.20 g/cm3 | soluble | 208.21 g/mole | 40% |  | C8H9NaO3S |
| 18 | Dodecyl benzene sulfonic acid | Alpha | Dark brown viscous liquid | 1.05 g/cm3 | Dispersable | 326.49 g/mole | 90% |  | C18H30O3S |
| 18 | N,N-Bis(2-hydroxyethyl) dodecanamide | Alpha | Pale yellow liquid | 0.99 g/cm3 | Soluble | 287.43 g/mole | 99% |  | C16H33NO3 |