Supporting Information (SI)

Effects of Hemicellulose on Recycling Performance of Paper Based on Sisal fibers

Shaoliu Qin1, 2, Yian Chen2, *, Shenming Tao2, Cunzhi Zhang2, Xingzhen Qin1, *, Pan Chen3, *, Haisong Qi2,

1 School of Chemistry and Chemical Engineering, Guangxi University, Nanning, 530004, China.

2 State Key Laboratory of Pulp and Paper Engineering, South China University of Technology, Guangzhou, 510641, China.

3 Department of Materials Engineering, Beijing Institute of Technology, Beijing, 100081, China.

Corresponding Author

*E-mail: xzhqin2009@163.com.

*E-mail: chenyian@scut.edu.cn.

*E-mail: panchen@bit.edu.cn

Table S1 The chemical composition of sisal holocellulose fiber

| Type | Glucose content (%) | Xylose contenta (%) | Lignin content (%) | Minerals and others (%) |
| --- | --- | --- | --- | --- |
| Holocellulose-0 | 76.81 | 10.17 | 7.54 | 5.48 |
| Holocellulose-1 | 76.34 | 10.09 | 7.97 | 5.60 |
| Holocellulose-2 | 76.13 | 10.12 | 7.90 | 5.85 |
| Holocellulose-3 | 76.43 | 9.94 | 7.77 | 5.86 |
| Holocellulose-4 | 76.20 | 10.09 | 7.93 | 5.78 |
| Holocellulose-5 | 78.16 | 9.60 | 6.97 | 5.27 |
| Celulose-0 | 62.39 | 7.91 | 5.81 | 23.89 |
| Celulose-1 | 72.51 | 8.46 | 4.47 | 14.56 |
| Celulose-3 | 59.69 | 7.96 | 4.48 | 27.87 |
| Celulose-5 | 65.29 | 8.14 | 4.46 | 22.11 |

a Polyxylose is mainly element in sisal hemicellulose.

Fig. S1 XRD curves of holocellulose (A) and cellulose (B) papers after different rounds of recycling processes.