Supplementary information

A Molecular Fence Catalyst for CO2 Hydrogenation to CO with High Activity and Durability

Weige Su1, Syed Jalil Shah2, Xu Fan1, Changhao Li1, Xuehui Jia1, Jianhua Chen1, Zhongxing Zhao1,*, Zhenxia Zhao1,*

1Key Laboratory of New Low-carbon Green Chemical Technology, Education Department of Guangxi Zhuang Autonomous Region, State Key Laboratory of Featured, Metal Materials and Life-cycle Safety for Composite Structures, School of Chemistry and Chemical Engineering, Guangxi University, Nanning, 530004, China.

2Zhengzhou Research Institute, Harbin Institute of Technology, Zhengzhou, Henan 450000, China.

E-mail: zhaozhenxia@gxu.edu.cn; zhaozhongxing@gxu.edu.cn

Reagents

Cupric Nitrate (Cu(NO3)2, AR, Maclin)

Ammonia Solution (NH3·H2O, 28 wt.%, Sinopharm Chemical Reagent Co., Ltd)

Brij-58 (C16H33(OCH2CH2)nOH, AR, Aladdin Reagent Co., Ltd)

Tetraethyl Orthosilicate (C6H14O, AR, Aladdin Reagent Co., Ltd)

Cyclohexane (C6H12, AR, Aladdin Reagent Co., Ltd)

Isoamyl Alcohol (C5H12O, AR, Aladdin Reagent Co., Ltd)

LUDOX HS-30 Silica Solgel (SiO2·H2O, 30 wt.%, Grace)

Sodium Aluminate (NaAlO2, AR, Aladdin Reagent Co., Ltd)

Sodium Bromide (NaBr, AR, Maclin)

Sodium Hydroxide (NaOH, AR, Sinopharm Chemical Reagent Co., Ltd)

Ultrapure Water (H2O, AR, Laboratory Prepared)

1-Methylpyrrolidine (C5H11N, AR, Aladdin Reagent Co., Ltd)

Copper (II) Acetylacetonate (C10H14CuO4, AR, Aladdin Reagent Co., Ltd)

Ethanol (C2H6O, AR, Aladdin Reagent Co., Ltd)

Catalyst preparation

Synthesis of Cu@SiO2. Cu@SiO2 was prepared by a modified reported method from the literature1. Briefly, 3.37 g of Brij-58 was dissolved in 15 mL of cyclohexane in a 50 mL sample bottle at 50 °C under stirring. Then, 0.4 mL of copper nitrate solution (2 M) was added to form a reverse microemulsion system. After 1 hour of stirring, 1 mL of ammonium hydroxide was added dropwise, followed by 2 g of tetraethyl orthosilicate after 30 minutes. The silica coating proceeded for 2 hours, after which 15 mL of isopropanol was added to demulsify the microemulsion. The mixture was centrifuged to obtain the precipitate, which was dried in a vacuum oven at 70 °C for 12 hours. The dried powder was then calcined at 500 °C in an air stream to remove organic species. During calcination, the temperature was increased slowly at a rate of 1 °C per minute to avoid the formation of quartz phases and to prevent the rapid diffusion of decomposition gases, which could create excessive meso-porosity. Eventually, the product Cu@SiO2 was reduced at 773 K for 3 hours under a 30 mL/min flow of 5% H2 in N2.

Transformation of Cu@SiO2 to Cu@mMOR. Cu@mMOR was prepared via a 1-methylpyrrolidine (NMP)-assisted crystallization method. In a typical preparation, 500 mg of Cu@SiO2 was mixed with sodium aluminate (0.513 g), sodium bromide (1.28 g), aqueous sodium hydroxide (8.6 g, 30 wt.%), and deionized water (66.37 g) in a homogenizer at a high speed of 20000 rpm to form a uniform solution. The purpose of this step was to enable the pre-adsorption of Na+ on the Cu@SiO2 interface. Then, 23.3 g of silica sol and 6 g of the structure-directing agent NMP were slowly added dropwise to this uniform solution. The purpose of adding NMP was to accelerate the crystallization of the MOR framework. Next, the mixture was kept at 60 °C and stirred for 6 hours to form a uniform gel. Subsequently, the gel was transferred to a 150 mL Teflon-lined autoclave for hydrothermal crystallization at 170 °C. After 4 days of heating, the solid product was separated by centrifugation, washed with deionized water, and then dried overnight at 120 °C. The sample was then calcined at 550 °C for 8 hours to remove the organic components. Eventually, the calcined sample was subjected to ion exchange with 0.1 M ammonium chloride solution, followed by air calcination and H2 reduction at 500 °C to obtain Cu@mMOR.

Synthesis of mMOR. Typically, the preparation of mMOR was similar to that of Cu@mMOR. The main difference was that Cu@SiO2 was not added, and the amount of silica sol was adjusted according to the XRF result of Cu@SiO2.

Synthesis of Cu/mMOR via Modified Impregnation Method. As a comparison material, Cu/mMOR was prepared via a modified impregnation method. To increase the presence of more Cu species on the catalyst surface, copper (II) acetylacetonate with a larger molecular size was used as the Cu source. In a typical procedure, copper (II) acetylacetonate was first dissolved in an appropriate amount of ethanol to prepare a uniform solution. Subsequently, mMOR powder was impregnated with this solution and ultrasonically dispersed in a sealed glass bottle for 30 minutes. The excess solvent in the mixture was then removed by rotary evaporation. Finally, the solid powder was calcined at 500 °C for 4 hours and subsequently reduced by H2 at 500 °C to obtain the Cu/mMOR sample.

Catalyst characterization

X-ray diffraction (XRD)

XRD patterns were collected via a Rigaku diffractometer (Cu Kα radiation, λ = 1.5418 Å). The working voltage and current were set to 30 kV and 30 mA, respectively. Diffraction patterns were recorded in the 2θ range of 10° to 60°, with a scanning rate of 10° per minute.

High-resolution transmission electron microscopy (HRTEM)

HRTEM images were obtained using a 2100 Plus TEM (JEOL) with energy-dispersive X-ray spectroscopy (EDS) at 200 kV. Particle size analysis was performed using ImageJ2. The d-spacing values were analyzed with Digital Micrograph software.

X-ray photoelectron spectra (XPS)

XPS was measured on a Thermo Scientific K-Alpha instrument with an Al Kα X-ray source (hν = 1486.6 eV). The binding energies were referenced against adventitious carbon C (1s) at 284.8 eV3. Prior to XPS measurements, the sample powder was pressed into a disc, reduced in hydrogen at 350 °C for 2 hours, and transferred to an XPS sample holder in a glove box.

N2 adsorption-desorption isotherms

The textural properties of the catalysts were determined by N2 adsorption-desorption isotherms measured on a Micromeritics ASAP 2020 instrument at −196 °C. Prior to measurements, each sample was degassed under a vacuum at 300 °C for 4 hours to eliminate moisture. The specific surface areas were calculated via the Brunauer–Emmett–Teller (BET) method from the adsorption isotherm in the relative pressure range of 0.05–0.254. Microporous surface area and pore volume were obtained via the t-plot method and the pore size distribution was analyzed via the BJH method5, 6.

X-ray Fluorescence Spectrometer (XRF)

The elemental composition of the samples was measured by an XRF on an ARL Perform' X (Thermo Fisher Scientific). XRF measurements were conducted at six different points on each sample, with an analysis time of 300 seconds per point, totaling 1800 seconds per sample.

NH3 temperature-programmed desorption (NH3-TPD)

NH3-TPD was conducted via a TP-5080 chemisorption analyzer (Tianjin Xianquan). 100 mg of the catalyst (20–40 mesh) was placed in the middle of a quartz tube. Prior to analysis, the samples were outgassed under a He flow at 300 °C for 2 hours and then cooled to 150 °C. The samples were then saturated with NH3 under a flow of 15 vol% NH3 (balanced with helium) for 30 minutes. Subsequently, He gas (30 mL/min) flowed over the catalyst at 150 °C for 30 minutes to remove physically adsorbed NH3. The TPD profiles were recorded by a thermal conductivity detector (TCD) as the samples were heated from 150 to 650 °C at 10 °C/min in He flow. All gas flow rates were maintained at 30 mL/min.

CO2 temperature-programmed desorption (CO2-TPD)

CO2-TPD was also performed on the TP-5080 chemisorption analyzer (Tianjin Xianquan). The experimental procedure of CO2-TPD was similar to that of NH3-TPD, except that NH3 was replaced with a CO2-He mixture (15% CO2).

H2 temperature-programmed desorption (H2-TPD)

H2-TPD was also performed on the TP-5080 chemisorption analyzer (Tianjin Xianquan). The experimental procedure of H2-TPD was similar to that of NH3-TPD, except that NH3 was replaced with an H2-N2 mixture (10% H2). To enhance the TCD's detection sensitivity for H2, the reference gas was switched from He to N2 due to the greater thermal conductivity difference with H2.

The content of spillover H* in H2-TPD is calculated as Eq. (1):

|  |  | (1) |
| --- | --- | --- |

In this equation, Si and SH2, standard correspond to the thermal conductivity detector (TCD) peak area of spillover H* and H2 standard. The nH2, standard is determined by the volume of the quantitative loop. The mcatalyst represents the mass of the catalyst.

H2 temperature-programmed reduction (H2-TPR)

The reducibility of the as-calcined samples was determined by H2-TPR on a TP-5080 chemisorption analyzer (Tianjin Xianquan). 100 mg of as-calcined sample was pretreated at 350 °C for 1 hour in N2 flow to remove surface impurities, then cooled to room temperature. Subsequently, the sample was heated in a 10% H2/N2 flow to 450 °C at a ramp rate of 10 °C/min. The H2-TPR profiles were recorded using a thermal conductivity detector (TCD). All gas flow rates were set at 30 mL/min.

N2O-H2 temperature-programmed reduction (N2O-H2-TPR)

N2O-H2-TPR experiments were conducted via a TP-5080 chemisorption analyzer (Tianjin Xianquan). First, a 100 mg sample was pretreated in N2 at 450 °C for 1 hour, followed by reduction in 10% H2/90% N2 at 450 °C for 2 hours, and then cooled to 90 °C under N2. Next, 10% N2O/90% N2 was introduced at 90 °C for 1 hour to oxidize surface Cu0 to Cu+. Subsequently, the sample was conducted in 10% H2/90% N2 by heating from 150 °C to 450 °C and maintaining at 450 °C for 1 hour. All gas flow rates were set at 30 mL/min.

H2–D2 isotope exchange

H2–D2 isotope exchange was conducted via a modified TP-5080 chemisorption analyzer (Tianjin Xianquan), with online detection by a quadrupole mass spectrometer (BSD-MASS) connected through a heated transfer line. Typically, 50 mg of catalyst was pre-reduced under H2 flow at 350 °C for 1 hour, then purged with Ar at the same temperature for 1 hour. After cooling to 100 °C, a mixture of 50% H2 and 50% D2 was introduced. The temperature was then increased to 600 °C at 10 °C/min, with H2, HD, and D2 signals recorded in the outlet gas. All gas flow rates were set at 30 mL/min.

The content of HD in the HD exchange test is calculated as Eq. (2):

|  |  | (2) |
| --- | --- | --- |

In this equation, VH2 represents the gaseous hourly space velocity (GHSV) of H2 feed gas. The XH2 is the conversion rate of H2 after reaction, which is determined by the mass spectrum (MS) signal of H2. The mcatalyst represents the mass of the catalyst.

Infrared spectroscopy after pyridine adsorption (Pyridine-IR)

Pyridine-IR was performed with a Nicolet 5700 spectrometer. The sample was weighed and pressed into a self-supporting wafer of 2 cm2. Next, the sample was pretreated from 20 °C to 450 °C in an air stream at a flow rate of 100 mL/min and a heating rate of 2 °C/min. Then, the sample was degassed at 200 °C for 1 hour before recording the initial IR spectrum. After cooling to 150 °C, the sample was exposed to a pyridine pressure of 1.5×10−3 bar for 5 minutes, followed by degassing for 1 hour. Finally, the temperature was increased from 150 °C to 450 °C at a rate of 10 °C/min, and the IR spectrum was recorded once the temperature stabilized.

The concentration of various acid sites was calculated as Eq. (3) or Eq. (4)7:

|  |  | (3) |
| --- | --- | --- |
|  |  | (4) |

In this equation, C represents the concentration of BAS or LAS, the unit of which is mmol/g catalyst. The IA represents the integrated area of the BAS or LAS band (cm-1). In addition, the R and W represent the radius (cm) and weight (mg) of the catalyst disk, respectively.

In situ diffuse reflectance infrared Fourier transform spectroscopy (DRIFTS)

DRIFTS were recorded on an INVENIO S infrared spectrometer (Bruker) equipped with a liquid nitrogen-cooled MCT detector and an in situ high-temperature chamber. The catalyst sample was reduced at 600 °C under hydrogen for 30 minutes, then purged with Ar at 20 mL/min for 30 minutes. After purging, the background spectrum was collected in the wavenumber range of 400-4000 cm−1 with 32 scans, recorded as 0 minutes. Next, a 10% CO2-90% Ar gas mixture was introduced at a flow rate of 40 mL/min, and spectra were collected every 2 minutes for the first 10 minutes. The gas was then switched to a 20% H2-80% Ar mixture at the same flow rate, and spectra were collected every 2 minutes for the next 10 minutes. Finally, a 10% CO2-20% H2-70% Ar mixture was introduced at a flow rate of 40 mL/min, and spectra were collected every 2 minutes, with additional spectra collected at 45 and 60 minutes.

X-ray absorption spectroscopy (XAS)

XAS measurements, including X-ray absorption near-edge structure (XANES) and extended X-ray absorption fine structure (EXAFS), at the Cu K-edge were performed at the TPS-44A1 beamline at the National Synchrotron Radiation Research Center (NSRRC) in Taiwan. The electron beam energy was set to 3.0 GeV, with a pair of channel-cut Si (111) crystals serving as the monochromator. The collected EXAFS data were processed with the ATHENA module within the IFEFFIT software package8. Data processing involved subtracting the post-edge background from the total absorption and normalizing it to the edge-jump step. The k2-weighted χ(k) data for the Cu K-edge were then Fourier transformed to real (R) space through a Hanning window (dk = 1.0 Å−1) to isolate contributions from various coordination shells. Quantitative structural parameters around the central atoms were determined through least-squares fitting, utilizing the ARTEMIS module of the IFEFFIT software package. For Wavelet Transform analysis, the χ(k) data exported from ATHENA were imported into the Hama Fortran code. The parameters were as follows: R range, 0 - 6 Å; k range, 0 - 12 Å−1; k weight; and Morlet function with κ = 10, σ = 2 was used as the mother wavelet to provide the overall distribution9.

Kinetic isotope effect (KIE)

KIE experiment was performed with a temperature-programmed reactor equipped with an online mass spectrometer BSD-MASS. About 50 mg of catalyst was placed into a TPD glass tube and secured with quartz wool. The reactor was heated to 600 °C at a rate of 10 °C/min in an Ar flow and held for 1 hour to remove adsorbed species from the catalyst surface. The system was then cooled to 300 °C. Subsequently, a CO2/H2/Ar gas mixture (CO2/H2/Ar = 5/10/85) was introduced, and the outlet gas signals (m/z = 2, 18, 28, 36, 44) were recorded online via the mass spectrometer. The temperature was ramped at a rate of 10 °C/min to 600 °C and held for 0.5 hours. This procedure was repeated with a CO2/D2/Ar gas mixture (CO2/D2/Ar = 5/10/85), recording the effluent gas signals (m/z = 4, 20, 28, 36, 44). The data from both experiments were compared to determine the KIE values. All gas flow rates were controlled at 30 mL/min.

The value of KIE in the kinetic isotope effect is calculated as Eq. (5):

|  |  | (5) |
| --- | --- | --- |

In this equation, rCO,H and rCO,D respectively represent the rate of CO formation in CO2/H2 and CO2/D2, which are determined by the mass spectrum (MS) signal of CO.

Computational details

Density Functional Theory (DFT)

DFT calculations were carried out using the Vienna Ab-initio Simulation Package (VASP)10. The exchange-correlation energy was described by the Perdew-Burke-Ernzerhof (PBE) functional within the generalized gradient approximation (GGA)11. The projector-augmented wave (PAW) method was employed to account for core-valence interactions12. The DFT+U method was applied to Cu, with a U-J value of 4 eV13, 14. An energy cutoff of 480 eV was set for plane wave expansions, and a 3×3×1 Monkhorst-Pack grid was used to sample the Brillouin zone. A vacuum space of 15 Å was applied above the surfaces to avoid periodic interactions. Structural optimizations were performed until the energy convergence reached 1.0×10-6 eV and the force convergence reached 0.02 eV/Å. Transition states were identified using the climbing image nudged-elastic-band (CI-NEB) method, with a convergence criterion set at 0.05 eV/Å15.

The Gibbs free energy change (ΔG) for each step was calculated via the formula:

|  |  | (6) |
| --- | --- | --- |

Where ΔE is the electronic energy difference obtained from DFT calculations, ΔZPE is the zero-point energy difference, T is the temperature (873.15 K), and ΔS is the entropy change. The ZPE was calculated via16:

|  |  | (7) |
| --- | --- | --- |

The TS values for adsorbed species were calculated from vibrational frequencies via17:

|  |  | (8) |
| --- | --- | --- |

Ab initio molecular dynamics (AIMD)

Ab initio molecular dynamics (AIMD) simulation of CO2 diffusion in Cu@mMOR was carried out using the Vienna Ab initio Simulation Package (VASP)10. The simulations were conducted within the canonical (NVT) ensemble, utilizing the Nosé thermostat to maintain temperature stability, with a time step of 1 fs18, 19. A plane-wave energy cutoff of 350 eV was employed. Long-range interactions were described using the DFT-D3 (BJ) method20. The electronic energy convergence criterion was set to 10-5 eV.

Ab initio molecular dynamics (AIMD) simulation of H2O-assisted hydrogen spillover in Cu@mMOR was carried out using the CP2K Package21. The AIMD simulation was performed within the canonical (NVT) ensemble, employing the Nosé-Hoover thermostat to maintain temperature control, with a time step of 0.5 fs at 873 K18, 19. The energy cutoff and relative cutoff were set at 500 Ry and 60 Ry, respectively. The DZVP basis set with GTH pseudopotentials was used for all elements to ensure an accurate description of electronic interactions22. Dispersion interactions were accounted for using the Grimme-D3 method throughout all calculations20.

Catalytic Reaction Test

The catalytic reaction tests for the reverse water-gas shift (RWGS) reaction were conducted in a mixed bed reactor with an internal diameter of 14 mm and a length of 300 mm in downflow mode. To prevent temperature fluctuations due to exothermic and endothermic reactions, a mixture of 20 mg of catalyst (120 mesh) and 300 mg of quartz sand (100 mesh) was placed in the reactor and supported between quartz wool. The catalyst was exposed to a CO2/H2 flow. The reaction was carried out at 600 °C, 0.1 MPa, CO2/H2 = 1/2, and a GHSV of 270 L gcat−1 h−1, unless otherwise specified. The outlet light gases (CO, CH4, and CO2) were analyzed online via an Agilent 7820A gas chromatograph (GC) equipped with a TCD and a PoraPak Q column (Agilent G3591-70010).

The conversion of CO2 (XCO2) and selectivity to CO (SCO) were calculated as follows:

|  |  | (9) |
| --- | --- | --- |
|  |  | (10) |

At which, the NCO2,in is the molar quantity of CO2 fed into the reactor, while NCO,out and NCO2,out are the molar quantities of CO and CO2 in the outlet gas, respectively.

All results were obtained with a carbon mole balance greater than 95%.

Supplementary Figure 1 | The surface-interface properties of Cu@SiO2. (a) DRIFTS, (b) zeta potential, (c) charge density difference contour plot, (d) charge density difference curve, and (e) work function of Cu@SiO2. The cyan and yellow parts in charge density difference contour plot represented charge depletion and accumulation, respectively. The H, Cu, O, and Si atoms are depicted in misty-rose, blue, red, and orange, respectively.

As shown in Supplementary Figure 1a, Cu@SiO2 exhibited a sharp Si-OH vibration peak, a small Cu-O peak, and an intense peak assigned to Si-O-Si1, 23, 24. These peaks indicated that the surface of Cu@SiO2 is rich in Si-OH groups, which not only bond with Cu to form a heterojunction interface but also serve as adsorption sites. In Supplementary Figure 1b, Cu@SiO2 displayed a more significant negative charge compared to pure SiO2 spheres, suggesting that its surface can adsorb cations via strong electrostatic force. Moreover, the DFT simulation showed that the heterojunction interface between Cu and SiO2 can result in obvious charge transfer (Supplementary Figure 1c). As seen in the charge density difference curve of Supplementary Figure 1d, Cu can transfer a large number of electrons to SiO2 through the interface, resulting in the latter exhibiting a negative charge, which is consistent with the experimental results of zeta potential. Based on the calculated work function (Supplementary Figure 1e), the work function of Cu was lower than that of SiO2, indicating that electrons are more easily transferred from the surface of Cu25. Thus, Cu@SiO2 could accumulate Na+ around its surface during the in situ crystallization process due to electrostatic adsorption. Since Na+ was the structure-directing agent for 5-member rings (1.6 Å) and 8-member rings (3.9 Å)26-29, which were prone to nucleate and grow around Cu. Taking into account the ionic radius of Na+ being 1.02 Å30, the occupation of Na+ in the 8-member rings and smaller pores prevent CO2 (3.4 Å) from passing through, thereby forming a fence.

Supplementary Figure 2 | The crystal structure of various catalysts. XRD patterns of Cu@mMOR, Cu/mMOR, mMOR, and Cu@SiO2.

Supplementary Figure 3 | The surface elemental distribution of various catalysts. XPS survey patterns of Cu@mMOR, Cu/mMOR, and Cu@SiO2.

As seen in Supplementary Figure 3, XPS survey patterns showed the presence of Na element in Cu@mMOR but not in Cu/mMOR, indicating that a small amount of Na+ remained during proton exchange. These residual Na+ ions may potentially further enhance the CO2 capture capacity of Cu@mMOR.

Supplementary Figure 4 | The surface Cu distribution in various catalysts. Cu 2p XPS patterns of Cu@mMOR, Cu/mMOR, and Cu@SiO2.

As present in Supplementary Figure 4, the Cu 2p XPS patterns for various catalysts revealed that surface Cu species consist of Cu0 and Cu+ without the appearance of Cu satellite peaks, implying that Cu2+ was fully converted to Cu0 and Cu+ in these three catalysts31.

Supplementary Figure 5 | The textural structure of various catalysts. (a) N2 isothermal adsorption-desorption curves and (b) pore size distributions of Cu@mMOR, Cu/mMOR, mMOR, and Cu@SiO2.

Supplementary Figure 6 | The valence and local structure of Cu@SiO2. The (a) XANES spectra, (b) FT-EXAFS spectra, and (c) WT-EXAFS spectra of Cu@SiO2.

Supplementary Figure 7 | The defect variation of confined Cu species before and after crystallization. The Raman spectra of Cu@mMOR and Cu@SiO2.

Supplementary Figure 8 | The acid content and acidity of various catalysts. NH3-TPD patterns of Cu@mMOR, Cu/mMOR, mMOR, and Cu@SiO2.

As seen, all acid sites of catalysts were divided into three regions based on the NH3 desorption temperature: weak acids (blue, below 250°C), medium acids (green, between 250 and 350°C), and strong acids (red, exceeding 350°C)32. Additionally, the quantity of acid sites was determined via the titration of desorbed NH333.

Supplementary Figure 9 | The acid strength distributions of Brønsted acid sites and Lewis acid sites in various catalysts. (a) Pyridine-IR patterns, (b) the strong Brønsted acid sites percentage, (c) the Brønsted acid sites distribution, and (d) the Lewis acid sites distribution of Cu@mMOR, Cu/mMOR and mMOR.

In pyridine-IR, the vibration band of pyridine with Brønsted acid sites (BAS) and Lewis acid sites (LAS) was at 1540 cm-1 and 1450 cm-1, respectively7. Emphatically, pyridine chosen as a probe could only detect the acid sites in 12-member-ring channels of mMOR due to its molecular size (0.65×0.70 nm) larger than other cages of mMOR34. As seen in Supplementary Figure 9a, the corresponding acid amounts in three catalysts were calculated via the integrated peak areas of various acid sites. Clearly, these peaks' intensity decreased with temperatures, and the residue peak at 450 °C represents the strong acids35. Their amounts and ratios of BAS and LAS were columned in Supplementary Fig. 9b-d. For Cu/mMOR, more BAS was maintained with a similar strong BAS ratio to mMOR. Moreover, the LAS amount was slightly increased in Cu/mMOR rather than the decrease in Cu@mMOR, indicating that more Cu species existed on the catalyst surface to form new LAS36.

Supplementary Figure 10 | The effect of O charge density in various catalysts by Cu species. The XPS O 1s spectra of Cu@mMOR, Cu/mMOR, and mMOR.

To verify the hypothesis that electron transfer enhances BAS acidity, the O 1s XPS spectra of various catalysts were performed and presented in Supplementary Figure 10. The O 1s XPS spectra were divided into three peaks: 533.0 eV (orange) for Si-O-Si bonds, 531.0-532.5 eV (green) for Si-O-Al bonds, and around 530.0 eV (purple) for Cu-O bonds37-40. Pristine mMOR showed peaks at 533.0 eV (Si-O-Si) and 532.2 eV (Si-O-Al). Cu@mMOR exhibited peaks at 532.8 eV (Si-O-Si), 531.5 eV (Si-O-Al), and 529.7 eV (Cu-O). Cu/mMOR had peaks at 533.0 eV (Si-O-Si), 531.9 eV (Si-O-Al), and 530.0 eV (Cu-O). The lower binding energy of Si-O-Al in Cu@mMOR (531.5 eV) indicated higher electron density compared to Cu/mMOR and pristine mMOR.

Supplementary Figure 11 | The RWGS kinetic of various catalysts. Arrhenius plot of Cu@mMOR, Cu/mMOR and Cu@SiO2. The data were tested at the conditions of 0.1 MPa, 270 L h-1 gcat-1 and CO2/H2 = 1/2.

Supplementary Figure 12 | The CO2 adsorption behavior of various catalysts. The CO2-TPD profiles of Cu@mMOR, Cu/mMOR and mMOR.

CO2 binding capacity on various catalysts was evaluated via CO2-TPD and shown in Supplementary Figure 12. As seen, pristine mMOR showed no obvious CO2 desorption peaks in the range of 150-600 °C while Cu@mMOR presented a clear peak at 231 °C for CO2 desorption. Differently, Cu/mMOR showed no CO2 desorption peaks before 450 °C but had a suspected signal of CO2 dissociative adsorption beyond 500 °C41, 42. It can be speculated that these encapsulated Cu in Cu@mMOR significantly enhanced mMOR to capture CO2 without dissociating them, confirming the successful fabrication of an isolation layer for Cu nanoparticles.

Supplementary Figure 13 | The systemic energy and temperature of CO2 diffusion and adsorption within mMOR during the AIMD simulation. The (a) potential energy fluctuation and (b) temperature fluctuation of CO2 diffusion and adsorption within mMOR during 20 ps (20000 fs) simulation.

To ensure the dynamic stability of the AIMD simulation of CO2 diffusion and adsorption within mMOR, we investigated the fluctuation states of potential energy and temperature during the 20 ps simulation. As seen, the potential energy and temperature both exhibited a steady trend indicating that the simulation system was stable and self-driven43.

Supplementary Figure 14 | The dynamic tracking on CO2 diffusion and adsorption within Cu@mMOR. The real-time distance between C and Na during AIMD simulation.

To understand the dynamics of CO2 diffusion and adsorption within Cu@mMOR, we analyzed the real-time distance between C and Na during AIMD simulation. The distance between C and Na fluctuated significantly within the first 10 ps, indicating that CO2 diffused freely in the mMOR channel. After 10 ps, the distance between C and Na remained steady at 3.4 Å, suggesting that CO2 was adsorbed by the Na site in the channel44.

Supplementary Figure 15 | The C-O vibration simulation for CO2 during AIMD. The simulated IR spectrum of CO2 in Cu@mMOR by calculating velocity autocorrelation function.

To investigate the C-O vibration of CO2 after adsorption in Cu@mMOR, we simulated its IR spectrum via the VASPKIT tool45. As displayed in Supplementary Figure 15, distinct vibrational peaks appeared around 1350 and 2300 cm-1, respectively. The former peak was attributed to C-O symmetric stretching vibration, and the latter peak corresponded to C-O asymmetric stretching vibration46. Typically, symmetric stretching vibrations cannot induce a dipole moment change in linear CO2, resulting in observing a distinct signal in the IR spectrum difficulty. Based on the simulated IR spectrum, the symmetry of CO2 decreased after adsorption, indicating CO2 was activated in the Na site of Cu@mMOR during the simulation. To ensure the accuracy of our AIMD simulation, the simulated IR spectrum was further compared with the CO2-DRIFTS of Cu@mMOR (Supplementary Figure 25). By comparison, the simulated spectrum showed high similarity with our experimental result, validating the reliability of our AIMD simulations.

Supplementary Figure 16 | The H2 adsorption behavior of various catalysts. The H2-TPD profiles of Cu@mMOR and Cu/mMOR.

The chemical adsorption and dissociation behaviors of H2 on Cu@mMOR and Cu/mMOR were estimated via H2-TPD tests. As observed in Supplementary Figure 16, all of these profiles were divided into two regions, assigning to the H* (chem-adsorbed H) on Cu (< 150 ºC) and the spillover H* species (> 150 ºC)47. Both of these two catalysts exhibited very similar H* capture properties on the Cu surface but a great discrepancy in H* spillover. The spillover H* signal curve in Cu@mMOR mainly presented two peaks at 292 and 400ºC, assigning to H* spillover from Cu to the interfacial region and to the mMOR48, 49. Moreover, its total amount of spillover H* from their peak area (Eq. 1) was about 28.7 μmol/g, 20.5 times higher than that of Cu/mMOR (1.4 μmol/g). It suggested that Cu@mMOR showed dramatically stronger H2 dissociation and spillover behavior than Cu/mMOR. This may mainly be attributed to its interfacial defect sites which could intensify electron transfer capacity with the aid of Cu vacancies and the acidity of BAS50.

Supplementary Figure 17 | The atomic model of Cu clusters with various Cu vacancies concentrates. The optimized structures of (a1) Cu13, (b1) Cu13 + Cu11O6 and (c1) Cu13 + Cu9O6. The geometries of intermediates and transition states involved in the H2 dissociation over (a2-4) Cu13, (b2-4) Cu13 + Cu11O6, and (c2-4) Cu13 + Cu9O6. The H, O, Cu, and Si atoms are depicted in misty-rose, red, blue, and orange, respectively.

Three Cu cluster models with different Cu vacancy concentrations were established, which were shown in Supplementary Figure 17 after structural optimization. Firstly, the typical nanocluster model of Cu13 was located on the MOR (100) plane (Supplementary Fig. 17a), representing the Cu species without vacancies. To construct cluster models with different Cu vacancy concentrations, similar size Cu2O clusters (Cu12O6) were first established. Subsequently, Cu12O6 was reduced by removing one Cu+ and three Cu+ to form the Cu11O6 and Cu9O6 clusters, respectively. Finally, these clusters together with Cu13 formed new clusters in low-level and high-level Cu vacancies.

Supplementary Figure 18 | The charge transfer of Cu clusters with various Cu vacancies concentrates during H2 dissociation. The charge density difference contour plots and Bader charge of (a) Cu13, (b) Cu13 + Cu11O6, and (c) Cu13 + Cu9O6.

To investigate the mechanism of H2 dissociation, charge density difference contour plots are shown in Supplementary Figure 18. The cyan and yellow parts represented charge depletion and accumulation, respectively. The cutoff of the density-difference iso-surface was 0.003 eA-3. As demonstrated, H2 dissociated via homolytic dissociation on the Cu cluster without vacancies. When Cu vacancies were introduced, H2 underwent heterolytic dissociation, producing an H+ and an H-. As the concentration of Cu vacancies increased, the charge density difference between the H+ and H- became more pronounced. These results indicated that Cu vacancies induced molecular polarization of the H2, causing a shift in bonding electrons and accelerating H-H bond cleavage, which consequently enhanced the H2 dissociation capability of the Cu clusters51.

Supplementary Figure 19 | The DOS distribution of Cu clusters with various Cu vacancies concentrates. The total density of states for the models of Cu13, Cu13 + Cu11O6, Cu13 + Cu9O6 and pristine mMOR.

To understand the effect of Cu vacancies on the electronic structure of Cu clusters, the total density of states analysis is provided in Supplementary Figure 19. In the total density of states, the Fermi level separated the valence band from the conduction band, and the upper and lower parts of the patterns represented electrons with different spin states. As shown, mMOR demonstrated a band gap near the Fermi level, indicating that the pristine mMOR was not favorable for electron transport52. After loading the Cu clusters, the total density of states exhibited a broad metallic band near the Fermi level, suggesting that the Cu clusters can significantly enhance electron transport within the catalyst53. With the increasing concentration of Cu vacancies, the bandwidth near the Fermi level expanded, promoting more electron transfer between the Cu clusters and the mMOR framework.

Supplementary Figure 20 | The diffusion kinetics of hydrogen spillover. The kinetic isotope effect patterns of Cu@mMOR and Cu/mMOR.

Supplementary Figure 21 | The variation of OH groups in Cu@mMOR during reaction. The partial enlarged view of CO2/H2-DRIFTS profiles of Cu@mMOR.

As seen in Supplementary Figure 21, the -OH stretching vibration of BAS (3620 cm-1) and hydrous clusters (3620-3760 cm-1) exhibited an obvious variation, which was attributed to H* spillover54, 55. Owing to the strong adsorption to the H2O56, the H* in the BAS continuously formed hydrous clusters with the product H2O at the reaction beginning (0-6 min). Subsequently, the delocalization of hydrous clusters accelerated the diffusion of H* in the channels of MOR, boosting Cu to provide positive feedback of higher H* dissociation and H* donation57. It could contribute to the dramatic rise of H* signals at 8 min, nevertheless which declined rapidly at 10 min due to the H* consumption of reaction. Eventually, H* and hydrous clusters ended the induction period and reached a dynamic equilibrium (20-30 min), at which free H* was less and H(H2O)* was the most.

Supplementary Figure 22 | The systemic energy and temperature of H2O-assisted spillover within Cu@mMOR during the AIMD simulation. The (a) potential energy fluctuation and (b) temperature fluctuation of H2O-assisted spillover within Cu@mMOR during 10 ps (10000 fs) simulation.

Supplementary Figure 23 | The dynamic behavior of H2O-assisted hydrogen spillover in Cu@mMOR. The radial distribution function g(r)OH and estimated mean effective potential energy path for spillover on Cu@mMOR.

As depicted in Supplementary Figure 23, the O-H bond distribution function displayed a distinct peak at ~1.0 Å, representing the O-H bond of H2O58. Notably, the value of g(r) was more than 0 at ~1.3 Å, reflecting the proton exchange between H2O and H3O+ 59. The free energy barrier of H2O-assisted hydrogen spillover was estimated via V(r) = -RTln(g(r)), where g(r) is the radial distribution function of the O-H bond60. As calculated, the free energy barrier of H2O-assisted hydrogen spillover was 0.29 eV, which was significantly lower than the reported barrier (0.4~0.8 eV) for direct hydrogen spillover61. Thus, H2O was favorable for accelerating the hydrogen spillover from Cu to other sites in Cu@mMOR.

Supplementary Figure 24 | The variation of chemical groups in various catalysts during the CO2 adsorption period. The CO2-DRIFTS profiles of Cu@mMOR and Cu/mMOR.

To directly prove the Cu catalytic mechanism, pure CO2-DRIFTS was also given in Supplementary Figure 24. The species corresponding to each infrared peak were identified by references62-64. Only an adsorbed CO2 peak at about 1345 cm-1 was observed in the CO2-DRIFTS, which was evident that separated Cu species could not directly convert CO2 to CO in Cu@mMOR.

Supplementary Figure 25 | The construction of the CO2 hydrogenation site model for Cu@mMOR. Model of MOR shell in Cu@mMOR after structure optimization. The O, Na, Al, and Si atoms are depicted in red, purple, pink, and orange, respectively.

As displayed in Supplementary Figure 25, the mMOR (100) plane with Na sites was used to represent the CO2 reduction site. First, the CIF file of the standard MOR zeolite was downloaded from the IZA structure database, and the (100) plane was selected as the substrate. Subsequently, two Al sites were selected within the 12-membered ring channels of MOR based on the literature and Na+ ions were placed nearby65. Finally, the model was structurally optimized.

Supplementary Figure 26 | The reaction processes of the formate pathway and carboxyl pathway on Cu@mMOR. The geometries of (a) CO2*, (b) CO2* + H*, (c1, d1) formate pathway, (c2, d2) carboxyl pathway, (e) CO* + OH* and (f) CO* + H2O* in the RWGS reaction of Cu@mMOR. The H, C, O, Na, Al, and Si atoms are depicted in misty-rose, black, red, purple, pink, and orange, respectively.

As shown in Supplementary Figure 26, the RWGS reaction could follow two pathways, each involving steps such as CO2 adsorption, hydrogen spillover to the vicinity of CO2, formation of hydrogenated intermediates, decomposition of intermediates into CO, and secondary hydrogenation. The two pathways differed only in the step of hydrogenated intermediate formation, with the other steps being essentially identical. To distinguish the differing parts, the steps of the formate pathway were highlighted with red boxes and arrows, while those of the carboxyl pathway are indicated with green boxes and arrows in the figure.

Supplementary Table 1 | Total elemental distribution of Cu@mMOR, Cu/mMOR, Cu@SiO2, and mMOR.

| Element (wt.%) | mMOR | Cu@SiO2 | Cu/mMOR | Cu@mMOR |
| --- | --- | --- | --- | --- |
| Cu | - | 7.8 | 4.1 | 3.2 |
| Na | 0.1 | - | 0.1 | 1.2 |
| Al | 5.0 | - | 4.6 | 5.2 |
| Si | 42.4 | 44.9 | 39.1 | 39.6 |

Supplementary Table 2 | Pore textual parameters of Cu@mMOR, Cu/mMOR, Cu@SiO2, and mMOR from N2 adsorption-desorption isotherms.

| Catalyst | SBET (m2 g−1) | Smicro (m2 g−1) | Smicro/SBET (%) | Vt (cm3 g−1) | Vmicro (cm3 g−1) |
| --- | --- | --- | --- | --- | --- |
| Cu@mMOR | 427.1 | 423.5 | 99.2 | 0.17 | 0.16 |
| Cu/mMOR | 310.7 | 303.3 | 97.6 | 0.13 | 0.11 |
| Cu@SiO2 | 112.0 | 34.0 | 30.3 | 0.08 | 0.01 |
| mMOR | 530.1 | 519.4 | 98.2 | 0.20 | 0.19 |

Supplementary Table 3 | EXAFS fitting of various samples.

| Sample | Shell | CNa | R(Å)b | σ2 (Å2)c | ΔE0(eV)d | R factor (%) |
| --- | --- | --- | --- | --- | --- | --- |
| Cu foil | Cu-Cu | 12* | 2.52±0.013 | 0.0058 | 7.01±0.39 | 0.5 |
| Cu2O | Cu-O | 2* | 1.90±0.012 | 0.0049 | 7.01±1.57 | 0.5 |
| CuO | Cu-O | 4* | 1.92±0.016 | 0.0059 | 3.19±0.70 | 0.6 |
|  | Cu-Cu | 4* | 2.93±0.023 | 0.0065 | 6.71±1.52 |  |
| Cu@mMOR | Cu-O | 4.0±0.2 | 1.89±0.023 | 0.0056 | 2.82±0.88 | 1.5 |
|  | Cu-Cu | 2.0±0.3 | 2.61±0.003 | 0.0068 | 5.63±1.61 |  |
| Cu/mMOR | Cu-O | 3.8±0.2 | 1.93±0.008 | 0.0048 | 3.71±1.41 | 0.6 |
|  | Cu-Cu | 9.1±0.5 | 2.54±0.028 | 0.0072 | 7.07±3.91 |  |
| Cu@SiO2 | Cu-O | 3.6±0.2 | 1.94±0.024 | 0.0028 | 1.88±0.83 | 0.9 |
|  | Cu-Cu | 10.1±0.4 | 2.54±0.011 | 0.0084 | 7.25±1.84 |  |

aCN, coordination number; bR, the distance between absorber and backscatter atoms; cσ2, Debye-Waller factor to account for both thermal and structural disorders; dΔE0, inner potential correction; R factor indicates the goodness of the fit. During the fitting process, the amplitude reduction factor S02 was fixed to 0.8, according to the experimental EXAFS fit of Cu foil by fixing CN as the known crystallographic value. Fitting range: 3.0 ≤ k (/Å) ≤ 12 and 1.5 ≤ R (Å) ≤ 3.2 (Cu foil); 3.0 ≤ k (/Å) ≤ 11.0 and 1.0 ≤ R (Å) ≤ ~2.8 (Sample X). A reasonable range of EXAFS fitting parameters: 0.700 < Ѕ02 < 1.000; CN > 0; σ2 > 0 Å2; ΔE0 < 10 eV; R factor < 0.02.

Supplementary Table 4 | Comparison between Cu-based catalysts in this work and other reported Cu-based catalysts for RWGS reaction.

| Catalyst | XCO2a (%) | SCOb (%) | STYCOc (mmol gcat-1 h-1) | Stability (h) | Reaction conditions | Reference |
| --- | --- | --- | --- | --- | --- | --- |
| Cu@mMOR | 49.1 | 99.2 | 1957 | 788 | 270 L gcat-1 h-1, 600 °C, H2/CO2 = 2/1 | This work |
| Cu@mMOR | 41.1 | 99.6 | 3290 | - | 540 L gcat-1 h-1, 600 °C, H2/CO2 = 2/1 | This work |
| Cu/mMOR | 29.6 | 96.8 | 1151 | 45 | 270 L gcat-1 h-1, 600 °C, H2/CO2 = 2/1 | This work |
| Cu/mMOR | 18.2 | 90.3 | 1321 | - | 540 L gcat-1 h-1, 600 °C, H2/CO2 = 2/1 | This work |
| Cu@SiO2 | 33.6 | 97.8 | 1011 | 90 | 270 L gcat-1 h-1, 600 °C, H2/CO2 = 2/1 | This work |
| Cu@SiO2 | 26.1 | 96.5 | 2024 | - | 540 L gcat-1 h-1, 600 °C, H2/CO2 = 2/1 | This work |
| CuSiO-Ⅰ | 9.8 | 100 | 2583 | 45 | 3000 L gcat-1 h-1, 600 °C, H2/CO2/N2 = 2/1/2 | Ref.66 |
| CFNP09 | 12.0 | 99.5 | 533 | 100 | 200 L gcat-1 h-1, 600 °C, H2/CO2 = 1/1 | Ref.67 |
| 4Cu-Al2O3 | 47.0 | 100 | 2098 | 40 | 300 L gcat-1 h-1, 600 °C, H2/CO2 = 2/1 | Ref.68 |
| 15CuCe | 50.0 | 100 | 2232 | 240 | 400 L gcat-1 h-1, 600 °C, H2/CO2 = 3/1 | Ref.69 |
| Cu/β-Mo2C | 38.8 | 99.2 | 1717 | 40 | 300 L gcat-1 h-1, 600 °C, H2/CO2 = 2/1 | Ref.70 |
| Cu/LaTiO2 | - | - | 124 | 540 | 15 L gcat-1 h-1, 600 °C, H2/CO2 = 2/1 | Ref.71 |
| Cu-Ce/CDC | 50.0 | 100 | 64 | 80 | 23.8 L gcat-1 h-1, 600 °C, H2/CO2/N2 = 4/1/3.3 | Ref.72 |
| Cu/Ce0.9Zr0.1Ox | 57.0 | 100 | 115 | 110 | 30 L gcat-1 h-1, 550 °C, H2/CO2/N2 = 12/3/5 | Ref.73 |
| 5Cu/LaFeO3 | 33.6 | 100 | 360 | 18 | 72 L gcat-1 h-1, 600 °C, H2/CO2/N2 = 1/1/1 | Ref.74 |
| Y2O3/Cu | 45.6 | 99.9 | 1854 | 100 | 400 L gcat-1 h-1, 600 °C, H2/CO2/N2 = 69/23/8 | Ref.75 |

aXCO2, conversion rate of CO2; bSCO, selectivity of CO; cSTYCO, space-time yield of CO.

Supplementary Movie 1 | A 20 ps AIMD simulation for the CO2 diffusion and adsorption within Cu@mMOR

As shown in the Supplementary Movie 1, the elements were color-coded for clarity: Si in yellow, O in red, C in aqua green, Na in blue, and Al in pink. Each movie frame represented a 1 ps progression in the dynamical process. In the initial stage (0-10 ps), CO2 molecule continuously moved through the channel of mMOR. In the later stages (10-20 ps), CO2 gradually stabilized near the Na+ site, representing CO2 was captured and activated by the Na+ site.

Supplementary Movie 2 | A 10 ps AIMD simulation for H2O-assisted spillover within Cu@mMOR

As shown in the Supplementary Movie 2, the elements were color-coded for clarity: Si in yellow, O in red, H in white, Cu in light green, and Al in pink. Each movie frame represented a 0.5 ps progression in the dynamical process. Initially, H* bound with H2O molecules to be H3O* and migrated from the Cu site into the channel. Subsequently, H* underwent continuous exchange among H2O molecules. Notably, as the H3O* approached the mMOR framework, it transferred H* to the framework O, realizing the H*spillover from the Cu site to mMOR. Then, H* could be re‐coordinated by H2O, re‐entering a state of dynamic exchange within the channels to spill the farther locations. Collectively, these processes indicated that H2O molecules promoted the H* spillover, which benefited CO2 reduction in Cu@mMOR.

References

1.	Ge, Y. et al. Highly efficient Pt decorated CoCu bimetallic nanoparticles protected in silica for hydrogen production from ammonia–borane. ACS Sustain. Chem. Eng. 5, 1675-1684 (2017).

2.	Schneider, C. A., Rasband, W. S. & Eliceiri, K. W. NIH image to ImageJ: 25 years of image analysis. Nat. Methods 9, 671-675 (2012).

3.	Greczynski, G. & Hultman, L. Referencing to adventitious carbon in X-ray photoelectron spectroscopy: can differential charging explain C 1s peak shifts? Appl. Surf. Sci. 606, 154855 (2022).

4.	Brunauer, S., Emmett, P. H. & Teller, E. Adsorption of gases in multimolecular layers. J. Am. Chem. Soc. 60, 309-319 (1938).

5.	Lippens, B. C. & de Boer, J. H. Studies on pore systems in catalysts: V. the t method. J. Catal. 4, 319-323 (1965).

6.	Barrett, E. P., Joyner, L. G. & Halenda, P. P. The determination of pore volume and area distributions in porous substances. I. computations from nitrogen isotherms. J. Am. Chem. Soc. 73, 373-380 (1951).

7.	Emeis, C. A. Determination of integrated molar extinction coefficients for infrared absorption bands of pyridine adsorbed on solid acid catalysts. J. Catal. 141, 347-354 (1993).

8.	Ravel, B. & Newville, M. ATHENA, ARTEMIS, HEPHAESTUS: data analysis for X-ray absorption spectroscopy using IFEFFIT. J. Synchrotron Radiat. 12, 537-541 (2005).

9.	Rehr, J. J. & Albers, R. C. Theoretical approaches to X-ray absorption fine structure. Rev. Mod. Phys. 72, 621-654 (2000).

10.	Kresse, G. & Furthmuller, J. Efficient iterative schemes for ab initio total-energy calculations using a plane-wave basis set. Phys. Rev. B 54, 11169-11186 (1996).

11.	Perdew, J. P., Burke, K. & Ernzerhof, M. Generalized gradient approximation made simple. Phys. Rev. Lett. 77, 3865-3868 (1996).

12.	Kresse, G. & Joubert, D. From ultrasoft pseudopotentials to the projector augmented-wave method. Phys. Rev. B 59, 1758-1775 (1999).

13.	Anisimov, V. I., Aryasetiawan, F. & Lichtenstein, A. I. First-principles calculations of the electronic structure and spectra of strongly correlated systems: the LDA+U method. J. Phys.: Condens. Matter 9, 767-808 (1997).

14.	Xue, M., Nakayama, M., Liu, P. & White, M. G. Electronic interactions of size-selected oxide clusters on metallic and thin film oxide supports. J. Phys. Chem. C 121, 22234-22247 (2017).

15.	Henkelman, G., Uberuaga, B. P. & Jónsson, H. A climbing image nudged elastic band method for finding saddle points and minimum energy paths. J. Chem. Phys. 113, 9901-9904 (2000).

16.	Norskov, J. K. et al. Origin of the overpotential for oxygen reduction at a fuel-cell cathode. J. Phys. Chem. B 108, 17886-17892 (2004).

17.	Bendavid, L. I. & Carter, E. A. CO2 adsorption on Cu2O(111): a DFT+U and DFT-D study. J. Phys. Chem. C 117, 26048-26059 (2013).

18.	Komatsugawa, H. & Nose, S. Nonequilibrium structural changes of a viscoelastic liquid under oscillatory shear: a molecular dynamics study. Phys. Rev. E 53, 2588-2594 (1996).

19.	Hoover. Canonical dynamics: equilibrium phase-space distributions. Phys. Rev. A: Gen. Phys. 31, 1695-1697 (1985).

20.	Grimme, S., Ehrlich, S. & Goerigk, L. Effect of the damping function in dispersion corrected density functional theory. J. Comput. Chem. 32, 1456-1465 (2011).

21.	VandeVondele, J. et al. Quickstep: fast and accurate density functional calculations using a mixed gaussian and plane waves approach. Comput. Phys. Commun. 167, 103-128 (2005).

22.	VandeVondele, J. & Hutter, J. Gaussian basis sets for accurate calculations on molecular systems in gas and condensed phases. J. Chem. Phys. 127, 114105 (2007).

23.	Kiviaho, J., Niemelä, M. K., Reinikainen, M. & Pakkanen, T. A. TPR and FT-IR studies on carbonyl cluster derived Co-Ru/SiO2 catalysts. Appl. Catal., A 149, 353-372 (1997).

24.	Agarwal, A., Rimer, J. D. & Palmer, J. C. Water structure and dynamics near the surfaces of silicalite-1. J. Phys. Chem. C 127, 23887-23896 (2023).

25.	Liu, T. et al. Improving interfacial electron transfer via tuning work function of electrodes for electrocatalysis: From theory to experiment. J. Phys. Chem. C 123, 28319-28326 (2019).

26.	Itabashi, K., Kamimura, Y., Iyoki, K., Shimojima, A. & Okubo, T. A working hypothesis for broadening framework types of zeolites in seed-assisted synthesis without organic structure-directing agent. J. Am. Chem. Soc. 134, 11542-11549 (2012).

27.	Mallette, A. J., Shilpa, K. & Rimer, J. D. The current understanding of mechanistic pathways in zeolite crystallization. Chem. Rev. 124, 3416-3493 (2024).

28.	Lee, S.-H. et al. Synthesis, characterization, and catalytic properties of zeolites IM-5 and NU-88. J. Catal. 215, 151-170 (2003).

29.	Kubu, M. & Přech, J. Transformation of analcime into IMF structure during the synthesis of IMF zeolite. Micropor. Mesopor. Mat. 206, 121-126 (2015).

30.	Shannon, R. D. Revised effective ionic radii and systematic studies of interatomic distances in halides and chalcogenides. Acta Cryst. A 32, 751-767 (1976).

31.	Daniel, J. E. et al. Investigating Cu-site doped CuSbS nanoparticles using photoelectron and electron paramagnetic resonance spectroscopy. J. Phys. Chem. C 128, 13888-13899 (2024).

32.	Cai, K. et al. Influence of acid strength on the reactivity of dimethyl ether carbonylation over H-MOR. ACS Sustain. Chem. Eng. 7, 2027-2034 (2019).

33.	Niwa, M., Suzuki, K., Isamoto, K. & Katada, N. Identification and measurements of strong Brønsted acid site in ultrastable Y (USY) zeolite. J. Phys. Chem. B 110, 264-269 (2006).

34.	Cao, K. P. et al. Insights into the pyridine-modified mor zeolite catalysts for DME carbonylation. ACS Catal. 10, 3372-3380 (2020).

35.	Wang, H. L. & Xin, W. Y. Surface acidity of H-Beta and its catalytic activity for alkylation of benzene with propylene. Catal. Lett. 76, 225-229 (2001).

36.	Benaliouche, F., Boucheffa, Y. & Thibault-Starzyk, F. In situ FTIR studies of propene adsorption over Ag- and Cu-exchanged Y zeolites. Micropor. Mesopor. Mat. 147, 10-16 (2012).

37.	Tsuji, M. et al. Factors affecting microscopic basicity of silicate glasses from the perspective of O1s binding energy. Steel Res. Int. 95, 2300383 (2024).

38.	Huang, M., Adnot, A. & Kaliaguine, S. Cation-framework interaction in alkali-cation-exchanged zeolites: an XPS study. J. Am. Chem. Soc. 114, 10005-10010 (1992).

39.	Hong, S. B. & Camblor, M. A. SiO- defects in as-synthesized pure-silica and aluminosilicate sodalites. Chem. Mater. 9, 1999-2003 (1997).

40.	Sreedharan, R., Mohan, M., Saini, S., Roy, A. & Bhattacharjee, K. Intermediate Cu-O-Si phase in the Cu-SiO2/Si(111) system: growth, elemental, and electrical studies. ACS Omega 6, 23826-23836 (2021).

41.	Azambre, B., Collura, S., Trichard, J. M. & Weber, J. V. Nature and thermal stability of adsorbed intermediates formed during the reaction of diesel soot with nitrogen dioxide. Appl. Surf. Sci. 253, 2296-2303 (2006).

42.	Yang, T. et al. Surface orientation and pressure dependence of CO2 activation on Cu surfaces. J. Phys. Chem. C 124, 27511-27518 (2020).

43.	Liu, J.-C. et al. Metal affinity of support dictates sintering of gold catalysts. J. Am. Chem. Soc. 144, 20601-20609 (2022).

44.	Parkes, M. V., Greathouse, J. A., Hart, D. B., Sava Gallis, D. F. & Nenoff, T. M. Ab initio molecular dynamics determination of competitive O2 vs. N2 adsorption at open metal sites of M2(dobdc). Phys. Chem. Chem. Phys. 18, 11528-11538 (2016).

45.	Wang, V., Xu, N., Liu, J.-C., Tang, G. & Geng, W.-T. VASPKIT: a user-friendly interface facilitating high-throughput computing and analysis using VASP code. Comput. Phys. Commun. 267, 108033 (2021).

46.	Coenen, K., Gallucci, F., Mezari, B., Hensen, E. & van Sint Annaland, M. An in-situ IR study on the adsorption of CO2 and H2O on hydrotalcites. J. CO2 Util. 24, 228-239 (2018).

47.	Miller, J. T. et al. Hydrogen temperature-programmed desorption (H2-TPD) of supported platinum catalysts. J. Catal. 143, 395-408 (1993).

48.	Ren, K., Jia, F., Zhang, C., Xing, E. & Li, Y. Ni as the promoter on hydrogen spillover for better hydrogenative regeneration on Pt/Y based catalysts. Fuel 335, 127047 (2023).

49.	Lee, K. et al. Engineering nanoscale H supply chain to accelerate methanol synthesis on ZnZrOx. Nat. Commun. 14, 819 (2023).

50.	Zhu, Q. et al. Enhanced CO2 utilization in dry reforming of methane achieved through nickel-mediated hydrogen spillover in zeolite crystals. Nat. Catal. 5, 1030-1037 (2022).

51.	Aireddy, D. R. & Ding, K. Heterolytic dissociation of H2 in heterogeneous catalysis. ACS Catal. 12, 4707-4723 (2022).

52.	Du, S. & Zhang, F. General applications of density functional theory in photocatalysis. Chin. J. Catal. 61, 1-36 (2024).

53.	Hu, C. et al. Selective CO2 reduction to CH3OH over atomic dual-metal sites embedded in a metal-organic framework with high-energy radiation. Nat. Commun. 14, 4767 (2023).

54.	Kondo, J. N., Iizuka, M., Domen, K. & Wakabayashi, F. IR study of H2O adsorbed on H-ZSM-5. Langmuir 13, 747-750 (1997).

55.	Hack, J. H. et al. Structural characterization of protonated water clusters confined in HZSM-5 zeolites. J. Am. Chem. Soc. 143, 10203-10213 (2021).

56.	Lee, B., Kondo, J. N., Domen, K. & Wakabayashi, F. FT-IR study of H216O and H218O adsorption on H-ferrierite. J. Mol. Catal. A: Chem. 137, 269-272 (1999).

57.	Liu, Q. & van Bokhoven, J. A. Water structures on acidic zeolites and their roles in catalysis. Chem. Soc. Rev. 53, 3065-3095 (2024).

58.	Huo, J. et al. Microscopic mechanism of proton transfer in pure water under ambient conditions. J. Chem. Theory Comput. 19, 4243-4254 (2023).

59.	Wang, M. et al. Genesis and stability of hydronium ions in zeolite channels. J. Am. Chem. Soc. 141, 3444-3455 (2019).

60.	Wang, Y.-G. et al. CO oxidation on Au/TiO2: Condition-dependent active sites and mechanistic pathways. J. Am. Chem. Soc. 138, 10467-10476 (2016).

61.	Singh, A. K., Ribas, M. A. & Yakobson, B. I. H-spillover through the catalyst saturation: an ab initio thermodynamics study. ACS Nano 3, 1657-1662 (2009).

62.	Köck, E.-M., Kogler, M., Bielz, T., Klötzer, B. & Penner, S. In situ FT-IR spectroscopic study of CO2 and CO adsorption on Y2O3, ZrO2, and yttria-stabilized ZrO2. J. Phys. Chem. C 117, 17666-17673 (2013).

63.	Yu, J. et al. Stabilizing Cu+ in Cu/SiO2 catalysts with a shattuckite-like structure boosts CO2 hydrogenation into methanol. ACS Catal. 10, 14694-14706 (2020).

64.	Ben David, R., Ben Yaacov, A. & Eren, B. Hydrogen exchange through hydrogen bonding between methanol and water in the adsorbed state on Cu(111). J. Phys. Chem. Lett. 14, 2644-2650 (2023).

65.	Fan, B. et al. Quantitatively mapping the distribution of intrinsic acid sites in mordenite zeolite by high-field 23Na solid-state nuclear magnetic resonance. J. Phys. Chem. Lett. 13, 5186-5194 (2022).

66.	Jin, R., Easa, J. & O’Brien, C. P. Highly active CuOx/SiO2 dot core/rod shell catalysts with enhanced stability for the reverse water gas shift reaction. ACS Appl. Mater. Interfaces 13, 38213-38220 (2021).

67.	Pahija, E. et al. FeOx nanoparticle doping on Cu/Al2O3 catalysts for the reverse water gas shift. J. CO2 Util. 64, 102155 (2022).

68.	Bahmanpour, A. M. et al. Cu–Al spinel as a highly active and stable catalyst for the reverse water gas shift reaction. ACS Catal. 9, 6243-6251 (2019).

69.	Liu, H. X. et al. Partially sintered copper-ceria as excellent catalyst for the high-temperature reverse water gas shift reaction. Nat. Commun. 13, 867 (2022).

70.	Zhang, X. et al. Highly dispersed copper over beta-Mo2C as an efficient and stable catalyst for the reverse water gas shift (RWGS) reaction. ACS Catal. 7, 912-918 (2017).

71.	Yu, J. et al. Ultra-high thermal stability of sputtering reconstructed Cu-based catalysts. Nat. Commun. 12, 7209 (2021).

72.	Tarifa, P., González-Castaño, M., Cazaña, F., Monzón, A. & Arellano-García, H. Development of one-pot Cu/cellulose derived carbon catalysts for RWGS reaction. Fuel 319, 123707 (2022).

73.	Xu, N. et al. Structure and activity comparison of Cu/CeyZr1–yOx series catalysts in the reverse water–gas shift reaction. Energy & Fuels 38, 7158-7166 (2024).

74.	Zhang, J., Wang, Y., Tian, J. & Yan, B. Cu/LaFeO3 as an efficient and stable catalyst for CO2 reduction: Exploring synergistic effect between Cu and LaFeO3. AlChE J. 68, e17640 (2022).

75.	Li, Z.-X., Xu, K., Wang, W.-W., Fu, X.-P. & Jia, C.-j. Stabilized inverse Y2O3/Cu interfaces boost the performance of the reverse water–gas shift reaction. Catal. Sci. Technol. 14, 3483-3492 (2024).