Synthesis, characterization, and application of self-assembled safflower polysaccharide nanoparticles as liver targeting drug delivery carrier

Supplementary Material

Supplement 1

The protein was removed using the Sevage method. The anhydrous ethanol, acetone, and anhydrous ethanol were degreased successively, and purified SPS was obtained after drying. DEAE-52 cellulose and SephadexG-100 were successively used for elution.

Supplement 2

To put it briefly, 10 mL of DMSO was mixed with 100 mg of SPS until it entirely dissolved. Subsequently, under nitrogen protection, 100 mg CDI and 20 μL TMS were added one at a time for one hour. 200 mg of PEI was also added, and the mixture was stirred magnetically while it was incubated for 24 h at 40 °C in a water bath. After adding ethanol, a precipitate was formed. It was then cleaned with ethanol, redispersed in deionized water, dialyzed against deionized water, and lyophilized to produce the SPS-PEI conjugate.

Fig S1. Original protein blot.