Thermal conductive networks constructed by Sialon fibers in-situ synthesized in barium aluminosilicate glass-ceramic

Supporting Information

Fig. S1 (a)The powder sample in the crucible before sintering; (b)The sample in smaller rectangular shaped crucible after sintering; (c)The sample in cylindrical shaped crucible after sintering; (d)The sample in larger rectangular shaped crucible after sintering; (d)The sample in the crucible after sintering corresponding figure S1(a); (f) The sample has a certain degree of imitation to the cylindrical crucible.

,

Fig. S2 The density of samples with different Sialon contents

## Table S1 Detailed information of semi-quantitative calculataion

| ## Sample | ## ISialon | ## IBAS | ## KSialon(RIR) | ## K BAS(RIR) |
| --- | --- | --- | --- | --- |
| ## C2.5 | ## 56 | ## 589 | ## 1.3 | ## 1.18 |
| ## C3 | ## 96 | ## 706 |  |  |
| ## C3.5 | ## 251 | ## 687 |  |  |
| ## C4 | ## 187 | ## 829 |  |  |

Theoretical modeling of thermal conductivity in composites

The thermal conductivity of two-phase composites in parallel conductions can be estimated using the following equations:

Kc=Wfλf+1-Wfλp                      (Ⅰ)

The series conduction for two-phase system could be evaluated by:

Kc=1Wf/Kf+1-Wf/Kp                        (Ⅱ)

Where Kc is the thermal conductivity of the composite, Wf  is the weight fractions of filler phases in the composite, λp is the thermal conductivity of the matrix, and λfis thermal conductivity of the filler. In this work, based on the phase content, the composition of samples can be roughly divided into BAS and β-Sialon. Then BAS glass-ceramic were employed as matrix with the heat conductivity value of 2.52 W/mK and the β-Sialon phases as filler with the heat conductivity value of 16.48 W/mK.

The determined factor Xinterconnectivity and η could be calculated by following Eq. (Ⅲ) and (Ⅳ)[S1,S2],

Xinterconnectivity=Kc-KHS-KHS+-KHS-	(Ⅲ)

η=Kc-KmWfKm×100%	(Ⅳ)

Where Kc is the thermal conductivity of the composite, Km is the thermal conductivity of the matrix, KHS+is the upper boundary of The Hashin-Shtrikman model, KHS-is the lower boundary, Wf is the weight loading of thermal conductive fillers.

The lnp in Eq. (6) in the main body can be calculated by following equation[S3]:

lnp=ln⁡(p+p2-1)p(p2-1)3-1p2-1	(Ⅴ)

Where p is the aspect ratio of the Sialon fiber.

Table S2 Fitting parameters for model and contact thermal resistance model

| Agari model |  |  | Interfacial thermal resistance model |  |  | Contact thermal resistance model |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| C1 | C2 | R2 | t(p) | Kx | R2 | t(p) | K0 | R2 |
| 0.60592 | 1.04893 | 0.972 | 0.3209 | 16.8796 | 0.976 | 2.54465 | 15.4594 | 0.968 |

Table S3 Engineering data of the materials for finite element simulation

| Material | Density(g/cm3) | Young’s modulus(GPa) | Poisson’s ratio | Isotropic thermal conductivity(W m-1) |
| --- | --- | --- | --- | --- |
| BAS | 2.5 | 100 | 0.26 | 2.5 |
| Sialon | 2.2 | 100 | 0.22 | 16.48 |

Fig. S3 The deformation distribution of samples with different Sialon contents based on finite element method: (a) C2.5; (b) C3; (c) C3.5; (d) C4

Fig. S4 The thermal stress distribution of samples with different Sialon contents based on finite element method: (a) C2.5; (b) C3; (c) C3.5; (d) C4

References:

- Schilling FR, Partzsch GM. Quantifying partial melt fraction in the crust beneath the Central Andes and the Tibetan plateau. Physics and Chemistry of the Earth Part a-Solid Earth and Geodesy 2001;26(4-5): 239-46.

- Zhang X, Zheng J, Fang H, Zhang Y, Bai S, He G. Al2O3/graphene reinforced bio-inspired interlocking polyurethane composites with superior mechanical and thermal properties for solid propulsion fuel. Composites Science and Technology 2018;167: 42-52.

- Hu L, Desai T, Keblinski P. Thermal transport in graphene-based nanocomposite. J Appl Phys 2011;110(3):033517.