SupplementaryInformation for

Polarity- and molecular orbital-engineered host materials for stable and efficient blue thermally activated delayed fluorescence

Soo-Ghang Ihn,1* Daun Jeong,2 Eun Suk Kwon,1Sangmo Kim,1 Yeon Sook Chung,1 Myungsun Sim,1 Jun Chwae,1 Yasushi Koishikawa,1 Soon Ok Jeon,1Jong Soo Kim,1 Joonghyuk Kim,1 Sungho Nam,1 Hyeonho Choi,1Sunghan Kim1

1Organic Materials Laboratory, Materials Research Center,Samsung Advanced Institute of Technology, Samsung Electronics Co., LTD, 130 Samsung-ro, Yeongtong-gu, Suwon-si, Gyeonggi-do, 16678, the Republic of Korea.

2Data and Information Technology Center, Samsung Electronics Co., LTD, 1 Samsungjeonja-ro, Hwaseong-si, Gyeonggi-do 18448, the Republic of Korea.

Contents

Supplementary Figure 1	S2

Supplementary Figure 2	S3

Supplementary Figure 3	S4

Supplementary Figure 4	S5

Supplementary Figure 5	S6

Supplementary Figure 6	S6

Supplementary Figure 7	S7

Supplementary Figure 8	S7

Supplementary Figure 9	S8

Supplementary Figure 10	S8

Supplementary Figure 11	S9

Supplementary Figure 12	S9

Supplementary Figure 1. Ground-state dipole moments GS of hosts calculated from various conformer structures, related Figure 2. The representative value, corresponding to the minimum energy structure for each host, is marked with ablack solid line.

Supplementary Figure 2. PL stability of various host films with and without 1PCTrz doping, related to Figure 6.

Supplementary Figure 3. Analysis of the horizontal orientations of the transition dipolemoments, h/(h + v), related Figure 7. Angle-dependent PL intensities at peak wavelengths. The black open squares represent the PL intensities from a. H1:1PCTrz, b. H4:1PCTrz, c. mCBP:1PCTrz, and d. DPEPO:1PCTrz films. Inspection of the solid curves for the films of the four 15% TADF emitter (1PCTrz)-doped hosts (H1, H4, mCBP, and DPEPO) reveal that the horizontal orientations of (h/(h + v)) are 0.87, 0.88, 0.83, and 0.87, respectively. The blue and red lines correspond to theoretical curves constructed with h/(h + ν) values of 0.67 (isotropic orientation) and 1.0 (perfect parallel orientation), respectively.

Supplementary Figure 4. Synthetic route for H1, H2, H3, H4.

Supplementary Figure 5. 1H NMR spectra of H1.

Supplementary Figure 6. 13C NMR spectra of H1.

Supplementary Figure 7. 1H NMR spectra of H2.

Supplementary Figure 8. 13C NMR spectra of H2.

Supplementary Figure 9. 1H NMR spectra of H3.

Supplementary Figure 10. 13C NMR spectra of H3.

Supplementary Figure 11.1H NMR spectra of H4.

Supplementary Figure 12. 13C NMR spectra of H4.