Table 1. Structural parameters resulting from Rietveld refinement for the catalytic support and the heterogeneous systems.

| Samples | Cristalline system and Network Parameters (Å) | Percentage of fases (%) | Crystallite size (nm) | Crystallinity (%) |
| --- | --- | --- | --- | --- |
| Waste | Iron-Tschermakite – Monoclinic – C2/m (12); a = 10.1, b = 18.3 and c = 5.81. Biotite – Monoclinic - C2/m (12); a = 10.1, b = 18.3, c = 5.81. Albite – Triclinic – C-1 (2); a = 8.28, b = 12.9 and c = 7.18. Quartz – Hexagonal – P3221 (154); a = 4.99 and c = 5.46. Ferrosilite-magnsium – Orthorhombic – Pbca (61); a = 18.2, b = 8.83 and c = 5.18. | 1.49 50.14 18.26 2.07 28.03 | 207.5 2.0 24.1 23.1 8.30 | 36.4 |
| 30% σ-MoO3:Waste | Iron-Tschemakite -– Monoclinic – C2/m (12); a = 9.80, b= 18.0 and c = 5.31. Biotite – Monoclinic - C2/m (12); a = 5.41, b = 9.37 and c = 10.3. Albite – Triclinic – C-1 (2); a = 8.27, b = 12.9 and c = 7.18. σ-MoO3 – Orthorrombic – Pbnm; a = 3.96, b = 13.9 and c = 3.70. Quartz – Hexagonal – P3221 (154); a = 5.0, c = 5.46. Ferrosilite-magnsium – Orthorhombic – Pbca (61); a= 18.2, b = 8.83 and c = 5.18. | 2.15 6.74 30.61 28.45 27.86 2.15 | 8.90 7.40 5.30 0.70 0.50 0.40 | 28.4 |
| 40% σ-MoO3:Waste | Iron-Tschemakite -– Monoclinic – C2/m (12); a = 9.85, b = 17.0 and c = 5.02. Biotite – Monoclinic - C2/m (12); a = 5.41, b = 9.37 and c = 10.3. Albite – Triclinic – C-1 (2); a = 8.27, b = 12.9 and c = 7.18. σ-MoO3 – Orthorrombic – Pbnm; a = 3.33, b = 18.5 and c = 7.58. Quartz – Hexagonal – P3221 (154); a = 5.0 and c = 5.46. Ferrosilite-magnsium – Orthorhombic – Pbca (61); a = 18.2, b = 8.83 and c = 5.18. | 14.55 15.28 28.07 40.86 1.24 - | 0.30 0.30 0.30 0.30 0.30 200.0 | 39.4 |
| 50% σ-MoO3:Waste | Iron-Tschemakite -– Monoclinic – C2/m (12); a = 9.80, b = 18.0 and c = 5.31. Biotite – Monoclinic - C2/m (12); a = 5.41, b = 9.37 and c = 10.3. Albite – Triclinic – C-1 (2); a = 8.27, b = 12.9 and c = 7.18. σ-MoO3 – Orthorrombic – Pbnm; a = 3.96, b = 13.9 and c = 3.70. Quartz – Hexagonal – P3221 (154); a = 5.0 and c = 5.46. Ferrosilite-magnsium – Orthorhombic – Pbca (61); a = 19.7, b = 9.77 and c = 6.18 | 12.62 4.11 25.79 50.71 2.19 4.58 | 0.30 0.30 0.30 0.30 0.30 0.30 | 48.1 |