Supporting Information

Defect engineering of BCTZ–based piezoelectric ceramics with high piezoelectric properties

Xinjian Wang1, Yu Huan1*, Yixuan Zhu1, Peng Zhang1, Wenlong Yang1,  Peng Li2, Tao Wei1 & Longtu Li3, Xiaohui Wang3

1School of Material Science and Engineering, University of Jinan, Jinan 250022, China

2School of Materials Science and Engineering, Liaocheng University, Liaocheng, 252000, China

3State Key Laboratory of New Ceramics and Fine Processing, School of Materials Science and Engineering, Tsinghua University, Beijing 100084, China

Figure S1 Dielectric constant and loss of BCZT samples sintered in various atmospheres as a function of temperature: (a) 0Mn–N, (b) 0Mn–O, (c) 0.25Mn–N, (d) 0.25Mn–A, (e) 0.25Mn–O

Figure S2 XPS of Ca 2p, Ba 3d, Zr 3d, Ti 2p and survey scan for the BCZT ceramics sintered in different atmospheres

Table S1 Area of Mn2+, Mn3+, and Mn4+ fitting peaks for the Mn–doped BCTZ ceramic samples in different atmospheres

| sample | Mn2+ | Mn3+ | Mn4+ |
| --- | --- | --- | --- |
| 0.25Mn–N | 975 | 874 | 1170 |
| 0.25Mn–A | 1185 | 900 | 934 |
| 0.25Mn–O | 1230 | 1050 | 780 |

Table S2 Atomic coordinates of BCTZ ceramics

| element | 0Mn–A | 0.25Mn–N | 0.25Mn–A | 0.25Mn–O |
| --- | --- | --- | --- | --- |
| Ba | (0, 0, -0.04) | (0, 0, 0) | (0, 0, 0.043) | (0, 0, 0) |
| Ca | (0, 0, -0.04) | (0, 0, -0.0016) | (0, 0, 0) | (0, 0, 0.027) |
| Ti | (0.5, 0.5, 0.482) | (0.5, 0.5, 0.482) | (0.5, 0.5, 0.482) | (0.5, 0.5, 0.491) |
| Zr | (0.5, 0.5, 0.483) | (0.5, 0.5, 0.482) | (0.5, 0.5, 0.482) | (0.5, 0.5, 0.482) |
| O1 | (0.5, 0.5, 0.016) | (0.5, 0.5, -0.699) | (0.5, 0.5, 0.016) | (0.5, 0.5, 0.017) |
| O2 | (0.5, 0, 0.544) | (0.5, 0, 0.515) | (0.5, 0, 0.515) | (0.5, 0, 0.537) |
| Mn1 | (-, -, -) | (0.5, 0.5, 0.482) | (0.5, 0.5, 0.482) | (0.5, 0.5, 0.483) |

Table S3 Ionic radius and the corresponding coordination number

| ion | Ionic radius (Å) | coordination number (CN) |
| --- | --- | --- |
| Ba2+ | 1.61 | 12 |
| Ca2+ | 1.34 | 12 |
| Zr4+ | 0.72 | 6 |
| Ti4+ | 0.61 | 6 |
| Mn2+ | 0.83 | 6 |
| Mn3+ | 0.58 | 6 |
| Mn4+ | 0.53 | 6 |

*Corresponding authors: Yu Huan: mse_huany@ujn.edu.cn