Supporting Information

Boosted electrocatalytic activity on FeCoNi layered double hydroxide incorporating Cd deposition for label-free detection of Staphylococcus aureus via its biosorption of Cu2+ ions

Huamin Zhaoa, Xiaoxi Zhenga, Jihao Sub, Jun Wang a, Xinrui Wanga, Hang Lia*, Juan Wanga*, Kexin Shenc*, Chao Zhaoa*

a School of Public Health, Jilin University, Changchun, 130021, China,

b College of Physics, Qingdao University, Qingdao, 266071, China,

c China-Japan Union Hospital of Jilin University, 130021, China.

* Email: lihang21@mails.jlu.edu.cn (H. Li), jwang0723@jlu.edu.cn (J. Wang), shenkexin1314@jlu.edu.cn (K. Shen), czhao0529@jlu.edu.cn (C. Zhao).

Contents

Tables

Table S1 Bacterial strains employed in this work

Table S2 An overview for electrochemical detection of S. aureus

Figures

Fig. S1 SEM images of bimetallic LDHs

Fig. S2 FTIR and XRD spectra of LDHs

Fig. S3 SEM images of Cd deposite

Fig. S4 Optimization of the DPV current response to Cu2+

Fig. S5 Long-term stability

Fig. S6 TEM image of MNPs

Fig. S7 Magnetic measurements

Fig. S8 FTIR spectra of S. aureus and Cu2+-treated S. aureus

Fig. S9 Optimization of experimental conditions for the electrochemical sensing of S. aureus

Text

Experimental section

References

Tables

Table S1 Bacterial strains employed in this work.

| Bacteria | Abbreviation | ATCC No. |
| --- | --- | --- |
| Staphylococcus aureus | S. aureus | 25923 |
| Salmonella typhimurium | S. typhimurium | 13311 |
| Listeria monocytogenes | L. monocytogenes | 19111 |
| Escherichia coli O157:H7 | E. coli O157:H7 | 35150 |
| Vibrio parahaemolyticu | V. parahemolyticus | 17802 |
| Shigella flexneri | S. flexneri | 12022 |

Table S2 An overview for electrochemical detection of S. aureus.

| Substrate | Assay type | Detection range (CFU/mL) | LOD (CFU/mL) | Reference |
| --- | --- | --- | --- | --- |
| AgNPs | DPV | 101-106 | 1 | 1 |
| Gold electrode | EIS | 101-104 | 10 | 2 |
| rGO-AuNP/GCE | EIS | 101-106 | 10 | 3 |
| SWCNTs/SPE | DPV/CV | 101-107 | 13 | 4 |
| Cd/FeCoNi LDH | DPV | 100-106 | 5 | This work |

Figures

Fig. S1 SEM images of bimetallic LDHs. (a) FeNi LDH, (b) CoNi LDH and (c) FeCo LDH.

Fig. S2 The characterization of chemical composition of LDHs. (a) FTIR and (b) XRD spectra of LDHs. XPS spectra of (c) FeCoNi LDH, (d) C 1s, (e) O 1s, (f) Fe 2p, (g) Co 2p and (h) Ni 2p.

Fig. S3 SEM and EDS mapping of Cd deposite. SEM images at different scales, (a) 100 μm, (b) 2 μm. EDS elemental mapping of (a) Cd deposite, (b) C, (c) O and (d) Cd.

Fig. S4 Optimization of the DPV current response to 6 nM and 60 nM Cu2+ for Cd/FeCoNi LDH-modified electrodes. (a-c) Anodic preconcentration voltage for Cu2+; (d-f) electrode material modification mass; (g-i) Cd electrodeposition time; (j-l) anodic preconcentration time for Cu2+; and (m-o) pH of HAc/NaAc buffer solution. The optimal detection conditions are: -1.1 V of preconcentration voltage, 75 μg of FeCoNi LDH for electrode modification, 1200 s of the electro-deposition time of Cd, 160 s of preconcentration time and pH=4 of acetic acid buffer.

Fig. S5 Long-term stability. The DPASV signal of the Cd-FeCoNi LDH-modified electrode to 5 mM Cu2+ was recorded under optimal conditions.

Fig. S6 TEM image of MNPs at different scales. (a) 200 nm, (b) 20 nm. The as-synthesized Fe3O4 NPs showed a spherical morphology with sizes ranging from 100 to 200 nm. The enlarged image revealed the rough surface on the nanoparticles, providing more binding sites for aptamer.

Fig. S7 Magnetic measurements of MNPs (yellow curve), MNPs@apt (blue curve). MNPs and MNPs@apt showed good magnetic responsiveness with the saturation magnetization of 77.99 and 68.11 emu/g, respectively.

Fig. S8 FTIR spectra of S. aureus (yellow curve) and Cu2+-treated S. aureus (blue curve).

Fig. S9 Optimization of experimental conditions for the electrochemical sensing of S. aureus. (a) Cu2+ adsorption time, (b) the concentration of aptamer functionalized on the MNPs. The key experimental factors including the concentration of aptamer and the adsorption time of Cu2+ were explored. 102 CFU/ml of S. aureus was used to evaluate of the impact of experimental factors on the detection performance including the concentration of aptamer and the adsorption time of Cu2+. The findings indicated that the best detection parameters consisted of preparing the probes with the aptamer concentration of 60 nM and allowing a 45-minute Cu2+ adsorption per assay.

Text

Experimental section

Materials and reagents

Cadmium chloride hydrate (CdCl2·2.5H2O), Nickel chloride hexahydrate (NiCl2·6H2O), N-Hydroxysuccinimide (NHS) were bought from Sigma Company (USA). Ferric chloride hexahydrate (FeCl3·6H2O) and trisodium citrate dihydrate were purchased from Tianjin Damao Chemical Institute (Tianjin, China). Copper(II) chloride dihydrate (CuCl2·3H2O), potassium nitrate (KNO3), potassium ferricyanide (K3Fe(CN)6), 1-Hydroxy-2,5-pyrrolidinedione (NHS), 1-(3-Dimethylaminopropyl)-3-ethylcarbodiimide (EDC) were bought from Aladdin Chemistry Co. Ltd. (Shanghai, China). Phosphate buffered saline (PBS buffer) was obtained from Sangon Biotechnology Co. Ltd. (Shanghai, China). Cobaltous nitrate hexahydrate (Co(NO3)2·6H2O) was bought from Macklin Company (Shanghai, China). Aluminium oxide (Al2O3) was bought from Ecc Detecting Instroments Co. Ltd. (Shanghai, China). Ethanol absolute, ethylene glycol, N, N-Dimethylformamide (DMF) were bought from Jindong Tianzheng Precision Chemical Reagent Factory (Tianjin, China). Acetic acid/sodium acetate buffer and sodium chloride (NaCl) were purchased from Beijing Dingguo Changsheng Biotechnology Co., Ltd. (Beijing, China). Formaldehyde solution was purchased from Beijing Chemical Factory (Beijing, China). Sodium hydroxide (NaOH) was bought from Tiantai Precision Chemical Reagent Factory (Tianjin, China). The sequence of S. aureus aptamers was 5′-NH2-(CH2)6- CAC ACC GCA GCA GTG GGA ACG TTT CAG CCA TGC AAG CAT CAC GCC CGT -3′ and synthesized by Sangon Biotechnology Co. Ltd. (Shanghai, China). All chemicals and reagents employed were of analytical grade and were used without any further purification.

Apparatus

The X-ray diffraction (XRD) measurement in the range of 10°-80°(2θ) was performed on the DX-2700B X-ray diffractometer (Cu Kα radiation, λ = 1.5416 A). The microscopic morphology and crystal structure of the sample were analyzed by field emission electron microscope (SEM). The composition of the elements can be known by X-ray energy spectrum (EDS) analysis and element distribution diagram. Transmission electron microscopy (TEM) images of nanoparticles were performed on a JEM-2100F transmission electron microscope operated at an accelerating voltage of 200 kV. The zeta potential measurements were determined using a NanoBrook 90Plus Zeta. Magnetic hysteresis loops were measured with a 7410 vibrating sample magnetometer. The FT-IR measurements were conducted using a Bruker Vertex 70 spectrometer over the range of 4000-400 cm-1.

Bacteria culture

All the bacterial strains listed in Table S1 were stored at -80 °C with 15% glycerol and revived on Luria-Bertani (LB) agar plates. They were cultivated in ordinary LB medium at 37 °C for 18 h-24 h with shaking at 180 rpm except for the high salt medium for V. parahaemolyticus strain. Subsequently, the cultures were harvest at the exponential growth phase by centrifuging at 4000 rpm for 15 minutes at room temperature. 100 μL of the diluted suspensions was plated onto agar plates by spread plating, and bacterial counts were assessed and reported as cfu per mL (CFU/mL).

Synthesis of nanomaterials

Synthesis of magnetic Fe3O4 nanoparticles(MNPs)

The magnetic Fe3O4 nanoparticles (MNPs) were synthesized through a solvothermal method according to a previous study5. Briefly, 1.35 g FeCl3•6H2O and 3.6 g NaAc were dissolved in 40 mL ethylene glycol under ultrasonic condition. The obtained homogeneous dark yellow solution was transferred to a 100 mL Teflon-lined stainless-steel autoclave. Afterwards, the autoclave was sealed and maintained at 200 °C for 16 h. After cooling to room temperature naturally, the black products were magnetically separated, washed three times with deionized water and absolute ethanol, respectively. Finally, the products were collected using a permanent magnet and then dried in vacuum at 60 °C for 12 h.

Synthesis of Aptamer-Funtionalized MNPs (MNPs@apt)

The MNPs were conjugated with aptamer through EDC/NHS coupling chemistry 6. 1 mL MNPs (5 mg/mL) was treated with 10 mg EDC and 5 mg NHS at room temperature with continuous stirring for 30 minutes. Subsequently, the supernatant was removed by magnetic separation and the precipitated was washed three times with PBS. Then 100 μL aptamer (10 μM) against S.aureus was added and suspended overnight at room temperature. The final magnetic product was washed with PBS.

Calculation of electroactive surface area

Utilizing the Randles–Ševcík equation (Eq. (1)) 7, the electroactive surface area (A) of the modified electrodes can be calculated.

ip=2.69×105n3/2D1/2v1/2AC     (1)

where ip, n, D, υ, A, and C denote the peak current, the number of transferred electron, the diffusion coefficient of Fe(CN)63- (7.6×10-6 cm2/s), scan rate (V/s), electroactive surface area of modified electrodes (cm2), and concentration of Fe(CN)63- (mol/cm3), respectively.

References

1.	ABDOLKARIM, ABBASPOUR, FATEMEH, et al. Aptamer-conjugated silver nanoparticles for electrochemical dual-aptamer-based sandwich detection of Staphylococcus aureus. Biosensors & Bioelectronics. 149-55 (2015). https://doi.org/10.1016/j.bios.2014.12.040

2.	PEGGY, R. REGINA, S, BEATE, S. et al. Development of an impedimetric aptasensor for the detection of Staphylococcus aureus. International Journal of Molecular Sciences. 18, 12, 2484 (2017). https://doi.org/10.3390/ijms18112484

3.	FEI, J. NUO. et al. Impedimetric aptasensor for Staphylococcus aureus based on nanocomposite prepared from reduced graphene oxide and gold nanoparticles J. Microchimica Acta. 181, 967-74 (2014). https://doi.org/10.1007/s00604-014-1195-8

4.	BHARDWAJ, J. DEVARAKONDA, S. KUMAR, S. et al. Development of a paper-based electrochemical immunosensor using an antibody-single walled carbon nanotubes bio-conjugate modified electrode for label-free detection of foodborne pathogens. Sensors & Actuators B Chemical. 253, 115-123 (2017). https://doi.org/10.1016/j.snb.2017.06.108

5.	MA, Y. ZHAO, Y. XU, X. et al. Magnetic covalent organic framework immobilized gold nanoparticles with high-efficiency catalytic performance for chemiluminescent detection of pesticide triazophos. TALANTA. 235, 122798 (2021). https://doi.org/10.1016/j.talanta.2021.122798

6.	SONG, Y. XU, G. WEI, F. et al. Aptamer-based fluorescent platform for ultrasensitive adenosine detection utilizing Fe3O4 magnetic nanoparticles and silver nanoparticles. Microchimica Acta. 185, 2, 139 (2018). https://doi.org/10.1007/s00604-018-2681-1

7.	GONG, Z. LU, B. WANG, H. et al. Double-amplified electrochemiluminescence immunoassay sensor for highly sensitive detection of CA19-9 using a ternary semiconductor CdSSe. Analytical Chemistry. 96, 4, 1678-1685 (2024). https://doi.org/10.1021/acs.analchem.3c04690