Supporting Information

Isolated Single-Atomic Cu Catalyst Supported on P-doped Carbon for Hydrochlorination of Acetylene

Ting Wanga, Zhao Jianga, Qi Tanga, Bolin Wanga,b, Saisai Wanga, Mingde Yua, Renqin Changa,c, Yuxue Yuea, Jia Zhaoa,*, Xiaonian Lia,*

a Industrial Catalysis Institute of Zhejiang University of Technology, Hangzhou, 310014, People’s Republic of China

b College of Environment, Zhejiang University of Technology, Hangzhou, 310014, People’s Republic of China

c Research Center of Analysis Measurement, Zhejiang University of Technology,

Hangzhou, 310014, People’s Republic of China

* Corresponding author. Tel: +86 571 88871656. E-mail: jiazhao@zjut.edu.cn (Jia Zhao)

* Corresponding author. Tel: +86 571 88320002. E-mail: xnli@zjut.edu.cn (Xiaonian Li)

Table S1 C, Cu, P and O contents determined by XPS and EDS analysis over different samples.

| Sample | XPS (wt.%) |  |  |  | EDS (wt.%) |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | C | P | Cu | O | C | P | Cu | O |
| Cu/PC200 | 51.00 | 13.20 | 8.17 | 27.63 | 55.51 | 12.06 | 10.41 | 22.02 |
| Cu/PC400 | 46.00 | 13.81 | 9.17 | 31.02 | 54.04 | 12.38 | 8.14 | 25.44 |
| Cu/PC600 | 56.72 | 11.58 | 8.39 | 23.32 | 57.06 | 11.81 | 9.88 | 21.25 |
| Cu/PC800 | 76.51 | 5.25 | 9.33 | 8.91 | 74.95 | 6.32 | 10.37 | 8.36 |

Table S2 Textural properties of the phosphorus-doped carbon materials.

| Sample | SBET (m2 g-1) a | Volume (cm-3 g-1) b | Diameter (nm) c |
| --- | --- | --- | --- |
| AC | 1204 | 0.61 | 2.03 |
| PC200 | 186 | 0.12 | 2.40 |
| PC400 | 203 | 0.13 | 2.36 |
| PC600 | 910 | 0.47 | 2.04 |
| PC800 | 1005 | 0.58 | 2.19 |

a measured using the Brunauer-Emmett-Teller (BET) method; b calculated dependent on the adsorbed N2 volume; c determined by Barrett-Joyner-Halenda (BJH) method.

Table S3 X-ray photoelectron spectroscopy (XPS) data of Cu 2p spectra of fresh P-doped Cu-based catalysts from this work.

| Sample | Cu+/Cu0 a |  |  | Cu2+ a |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Position/ eV | FWHMb/ eV | Area/ % | Position/ eV | FWHMb/ eV | Area/ % |
| Cu/PC200 | 932.4 | 2.25 | 71.4 | 934.6 | 2.91 | 28.6 |
| Cu/PC400 | 932.4 | 2.20 | 67.7 | 934.5 | 2.91 | 32.3 |
| Cu/PC600 | 932.4 | 2.15 | 64.9 | 934.5 | 3.22 | 35.1 |
| Cu/PC800 | 932.3 | 2.15 | 27.4 | 934.6 | 2.41 | 72.6 |

a based on reference values; b FWHM = full width at half maximum.

Table S4 X-ray photoelectron spectroscopy (XPS) data of Cu XAES spectra of fresh P-doped Cu-based catalysts from this work.

| Sample | Cu0 a |  |  | Cu+ a |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Position/ eV | FWHMb/ eV | Area/ % | Position/ eV | FWHMb/ eV | Area/ % |
| Cu/PC200 | 918.6 | 3.78 | 19.2 | 916.6 | 4.13 | 52.2 |
| Cu/PC400 | 918.6 | 3.61 | 14.1 | 916.6 | 4.21 | 53.6 |
| Cu/PC600 | 918.7 | 3.63 | 10.0 | 916.6 | 4.22 | 54.9 |
| Cu/PC800 | 918.6 | 3.61 | 3.6 | 916.6 | 4.28 | 23.8 |

a based on reference values; b FWHM = full width at half maximum.

Table S5 X-ray photoelectron spectroscopy (XPS) data of P 2p spectra of fresh P-doped Cu-based catalysts from this work.

| Sample | P-C a |  |  | P-O a |  |  | P=O a |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Position/ eV | FWHMb/ eV | Area/ % | Position/ eV | FWHMb/ eV | Area/ % | Position/ eV | FWHMb/ eV | Area/ % |
| Cu/PC200 | 133.0 | 1.32 | 15.6 | 134.2 | 1.77 | 71.2 | 135.2 | 1.94 | 13.2 |
| Cu/PC400 | 133.0 | 1.50 | 27.4 | 134.3 | 1.96 | 59.9 | 135.2 | 1.96 | 12.7 |
| Cu/PC600 | 133.1 | 1.28 | 33.7 | 134.1 | 1.63 | 54.5 | 135.1 | 1.96 | 11.8 |
| Cu/PC800 | 133.0 | 1.52 | 41.6 | 134.3 | 1.60 | 48.3 | 135.1 | 1.95 | 10.1 |

a based on reference values; b FWHM = full width at half maximum.

Table S6 X-ray photoelectron spectroscopy (XPS) data of O 1s spectra of fresh P-doped Cu-based catalysts from this work.

| Sample | P=O a |  |  | P-O-Cu a |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Position/ eV | FWHMb/ eV | Area/ % | Position/ eV | FWHMb/ eV | Area/ % |
| Cu/PC200 | 531.5 | 1.62 | 29.6 | 532.7 | 2.29 | 70.4 |
| Cu/PC400 | 531.3 | 1.80 | 28.2 | 532.5 | 2.60 | 71.8 |
| Cu/PC600 | 531.4 | 1.73 | 26.2 | 532.6 | 2.40 | 73.8 |
| Cu/PC800 | 531.3 | 1.66 | 25.3 | 532.6 | 2.48 | 74.7 |

a based on reference values; b FWHM = full width at half maximu

Fig. S1 N2 gas adsorption / desorption isotherms of (a) PC200, (b) PC400 and (c) PC600.

Fig. S2 HRTEM image of (a) Cu/PC200, (b) Cu/PC400, (c) Cu/PC600 and (d) Cu/PC800 catalysts.

Fig. S3 (a) Representative HAADF-STEM images and (b) EDS elemental mapping of fresh Cu/PC200, (c) Representative HAADF-STEM images and (d) EDS elemental mapping of fresh Cu/PC400, (e) Representative HAADF-STEM images and (f) EDS elemental mapping of fresh Cu/PC600.

Fig. S4 Selectivity to VCM over P-doped Cu-based catalysts.

Fig. S5 (a) Corresponding-Cu contents and (b) O 1s XPS spectra of fresh P-doped Cu-based catalysts.

Fig. S6 Correlation diagram of (a-b) oxygen species content and productivity.

Fig. S7 (a) Structure and coordinate of C13H9 cluster, (b-f) optimized configurations of C2H2 adsorption on (b) C3P, (c) P=O, (d) (OH)2P=O, (e) P(OH)2, (f) (OH)P=O, respectively.