### Supplementary information

Single amino acid bionanozyme for environmental remediation

Pandeeswar Makam1, Sharma S. R. K. C. Yamijala2, Linda J. W. Shimon3, Bryan M. Wong2* & Ehud Gazit1,4*

Affiliations:

1Department of Molecular Microbiology and Biotechnology, George S. Wise Faculty of Life Sciences, Tel Aviv University, Tel Aviv 6997801, Israel.

2 Department of Chemical & Environmental Engineering and Materials Science & Engineering Program, University of California-Riverside, Riverside, CA, 92521, USA.

3 Chemical Research Support, The Weizmann Institute of Science, 7610001 Rehovot, Israel.

4 Department of Materials Science and Engineering, Iby and Aladar Fleischman Faculty of Engineering, Tel Aviv University, Tel Aviv 6997801, Israel.

*Correspondence to: Ehud Gazit (ehudg@post.tau.ac.il) and Bryan M. Wong (bmwong@engr.ucr.edu)

### Supplementary Table 1. Crystallographic Data collection and refinement statistics of F-Cu

| Compound | F-Cu |
| --- | --- |
| CCDC | 1871975 |
| Diffractometer | ESRF ID23-1 |
| Empirical formula | C18H20CuN2O4 |
| Formula weight (g/mol) | 391.90 |
| Crystal description | Blue plate |
| Temperature (K) | 100 |
| Wavelength (Å) | 0.70 |
| Crystal system | Monoclinic |
| Space group | P21 |
| a, b, c (Å) | 9.4800(19), 5.1500(10), 16.670(3) |
| α, β, γ (°) | 90, 98.93(3), 90 |
| Volume (Å3) | 804.0(3) |
| Z | 2 |
| Density calculated (mg/m3) | 1.619 |
| Absorption coefficient (mm-1) | 1.385 |
| F(000) | 406 |
| Crystal size (mm) | 0.15x0.10x0.01 |
| Theta range for data collection (°) | 1.218 to 31.926 |
| Reflections collected (unique) | 9071(5472) |
| R int | 0.0435 |
| Completeness (%) | 95.3 |
| Data\restraints\ parameters | 5472/1/242 |
| Goodness-of-fit on F2 | 1.105 |
| Final R [I>2σ(I)] | R1=0.0462, wR2=0.1234 |
| R (all data) | R1=0.0475, wR2=0.1256 |
| Largest diff. peak and hole (e. Å-3) | 1.416 and -0.548 |

ORTEP diagram of F-Cu crystal structure

Supplementary Fig. S1. Microscopic images of F-Cu crystals. a, Optical microscope images. inset enlarged single-crystal image b and c, HRSEM images

Supplementary Fig. S2. Spectroscopic characterization of F-Cu bionanozyme. a, UV-vis absorption spectra. b, FTIR spectra (3270–3040 (νN-H) and 580–540 cm–1 (νM-O) region) of phenylalanine (F) and F-Cu. c, EDS spectra. d, TGA of F-Cu bionanozyme (blue curve) revealing the high thermal stability (≤ 273 °c). The weight losses are depicted by the first derivative curve (red).

Supplementary Fig. S3. Catalytic activity in control experiments, a, Reaction progress in the presence of all the control building blocks of F-Cu bionanozyme. Only F-Cu bionanozyme can catalyze the oxidation of 2,4-DP into colored product absorbance at 510 nm. No significant oxidation was observed when omitting either the phenylalanine (F) molecule or Cu from the catalytic system. b, Reaction progress in the presence of different copper complexes of amino acids (glycine (G-Cu), histidine (H-Cu), cysteine (C-Cu), and phenylalanine (F-Cu)) and phenylalanine-zinc (F-Zn) complex

Supplementary Fig. S4. Relative catalytic activity of F-Cu bionanozyme in real water samples (tap water, river water, and seawater).

Supplementary Fig. S5. Evaluation of laccase-mimicking catalytic activity of F-Cu bionanozymes. a, UV-visible absorbance spectra of the control experiment testing the in-situ production of H2O2. b, UV-vis kinetic traces at 510 nm in the presence and absence of oxygen (O2), Solutions were made anaerobic (without O2) by bubbling water-vapor saturated nitrogen for 45 min.  c, EPR spectra of F-Cu bionanozyme before and after addition of substrate 2,4-DP.

References

1.	J. P. Perdew, K. Burke, M. Ernzerhof, Phys. Rev. Lett. 1996, 77, 3865.

2.	V. Blum, et al. Comput. Phys. Commun. 2009, 180, 2175.

3.	A.Tkatchenko, M. Scheffler, Phys. Rev. Lett. 2009, 102, 073005.

4.	G. Henkelman, B. P. Uberuaga, H. Jónsson, J. Chem. Phys. 2000, 113, 9901.

5.	W. E, W. Ren, E.Vanden-Eijnden, J. Chem. Phys. 2007, 126, 164103.

Supplementary Movie S1. In-situ monitoring of the F-Cu crystallization process under optical microscope.

Supplementary Movie S2. In-situ optical microscopy observation of phenylalanine-coordinated Copper ions (F–Cu) crystallization kinetics.

Supplementary Movie S3 in-situ reaction monitoring of 2,4-DP and 4-AP catalyzed by F-Cu crystals.

Supplementary Movie S4 Real-time monitoring of 2,4-DP and 4-AP oxidation in the presence and absence of F-Cu catalyst.