Rapid Dye Removal using MoO₃-Incorporated V₂O₅ Nanocomposites: Laboratory Experiments and Real-World Applications

Jaspreet Kaur, and Rajesh Kumar*

*rajeshphysicspu@gmail.com

Supplementary data

Contents:

Figure S1: Calibration plot of concentration of MB dye versus UV-Vis absorbance.

Figure S2: Removal percentage graph with different adsorbent dosage of MV-50.

Figure S3: Kinetic model fitting (A) Pseudo First Order Model (B) Pseudo Second order Model with different concentration of MV-50

Table S1:  First and second –order Kinetic Parameters for the adsorption of MB of MV-50 sample

Figure S1: Calibration plot of concentration of MB dye versus UV-Vis absorbance.

Figure S2: Removal percentage graph with different adsorbent dosage of MV-50

Figure S3: Kinetic model fitting (A) Pseudo First Order Model (B) Pseudo Second order Model with different concentration of MV-50

Table S1:  First and second –order Kinetic Parameters for the adsorption of MB of MV-50 sample

| Adsorbent | Co (mg/L) | qexp (mg/g) | PFO PSO |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | qth (mg/g) | k1 (min-1) | R2 | qth (mg/g) | k2(g/mg min) | R2 |  |
|  | 20 | 39.95 | 27.93 | 0.120 | 0.90 | 40.6 | 0.0073 | 0.99 |  |
|  | 40 | 99.95 | 39.29 | 0.011 | 0.68 | 80.6 | 0.0072 | 0.99 |  |
| MV-50 | 60 | 116.9 | 45.01 | 0.018 | 0.65 | 123.4 | 0.0006 | 0.99 |  |
|  | 80 | 157.0 | 195.19 | 0.059 | 0.88 | 188.6 | 0.0001 | 0.97 |  |
|  | 100 | 192.72 | 248.38 | 0.027 | 0.83 | 256.4 | 0.00003 | 0.91 |  |
|  | 150 | 216.96 | 257.23 | 0.020 | 0.74 | 333.3 | 0.00001 | 0.62 |  |