Synergistic effect of chitosan derivative and DOPO for simultaneous improvement of flame retardancy and mechanical property of epoxy resin

Junjie Wang a, Xuejun Yu b, Shengsong Dai a, Xinyu Wang a, Zhiquan Pan a,b,

Hong Zhoua,*

Supporting information

Fig. S1. FTIR spectra of char residues of neat EP and EP/2.66%CSA/5.34%DOPO

Fig. S2. Pyrolysis mass spectrum of neat EP

Fig. S3. The changes in the absorbance of EP and EP/2.66%CSA/5.34%DOPO pyrolysis products over time (a) and the curve obtained from the first derivative (b)

Table S1 Elemental analysis data of chitosan and CSA and the calculated values of H and N elements in CAS

| Elemental sample |  | C | H | N |
| --- | --- | --- | --- | --- |
| CS |  | 44.58 | 6.74 | 8.21 |
| CSA | Characterization data | 68.04 | 5.61 | 4.66 |
|  | Calculated data |  | 5.57 | 4.40 |

Table S2 Thermal decomposition parameters of CSA, DOPO and CSA/DOPO modified epoxy resins

| Sample | T5% (°C) | Tmax (°C) | Weight-loss rate at Tmax (wt%/min) | Residue at 750 °C (%) |
| --- | --- | --- | --- | --- |
| EP | 355 | 382 | 1.48 | 18.7 |
| CSA | 230 | 300 | 0.98 | 34.6 |
| EP/8%CSA | 352 | 391 | 1.46 | 20.3 |
| EP/8% DOPO | 303 | 381 | 1.33 | 12.9 |
| EP/2.66%CSA/5.34%DOPO | 328 | 378 | 1.22 | 17.6 |

Table S3 Element composition of the char residues

| Sample | C (wt %) | O (wt %) | N (wt %) | P (wt %) |
| --- | --- | --- | --- | --- |
| EP | 82.52 | 11.43 | 6.03 | 0 |
| EP/2.66%CSA/5.34%DOPO | 87.68 | 8.24 | 3.6 | 0.48 |

Table S4 XPS data of different chemical bonds for EP and EP/2.66%CSA/5.34%DOPO

| Samples | C1S (area (%)) |  |  | N1S (Area (%)) |  | O1S (Area (%)) |  |  | P2S (Area (%)) |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | - H, C-C | C-OH,C-N, C-O-P | C=C,C=O | C-N | C=N | C-O-C,C-OH, C-O-P | C=O P=O |  | C-O-P | P=O |
| EP | 54 | 25 | 21 | 22 | 78 | 69 |  | 31 | 0 | 0 |
| EP/2.66%CSA/5.34%DOPO | 63 | 28 | 9 | 26 | 74 | 83 |  | 17 | 65 | 35 |

Table S5 The main products of neat EP detected by Py-GC/MS

| Peaks | Times | m/z | Chemical structure | Peaks | Times | m/z | Chemical structure |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 1.63 | 44 |  | 7 | 21.15 | 211 |  |
| 2 | 9.04 | 94 |  | 8 | 22.72 | 227 |  |
| 3 | 10.36 | 107 |  | 9 | 23.69 | 213 |  |
| 4 | 12.81 | 121 |  | 10 | 24.69 | 254 |  |
| 5 | 14.02 | 135 |  | 11 | 27.92 | 213 |  |
| 6 | 20.22 | 196 |  |  |  |  |  |

Table S6 Comparison data of flame retardancy and mechanical properties for the CS containing flame retardants in EP

| Flame retardants | LOI | UL-94 | Flexural strength | Tensile strength | impact strength | Ref. |
| --- | --- | --- | --- | --- | --- | --- |
| EP/10 %CCD | 31.6% | V-0 | \ | \ | \ | (Chen et al. 2020) |
| EP/7%6BL@BF/3% EG-3 | 25.8% | V-0 | -11.8% | 2.4% | \ | (Chen et al. 2020) |
| EP/3HNT@ CSZFMOH | 28% | \ | \ | \ | \ | (Zhang et al. 2021) |
| EP/15%CMEP/1% OMMT | 30.6% | V-0 | \ | \ | \ | (Yu et al. 2020) |
| EP/15%CEUP/3% OMMT | 34.8% | V-0 | \ | \ | \ | (Yu et al. 2019) |
| EP/15%APP/5%CS/ 5%melamine/15% Boric Acid/3%ZrO2 NPs/ | 38.7% | V-0 | \ | \ | \ | (Rao et al. 2019) |
| EP/10wt%HNT@CS@Fe3O4 | 31.3% | \ | \ | -0.65% | \ | (Zhang et al. 2019) |
| EP/(PEC8.1@CF) | 30.4% | V-0 | \ | \ | \ | (Shi et al. 2018) |
| EP/APP Chitosan SiO2 NPs (Polyurethane coatings) | 35.7% | V-0 | \ | \ | \ | (Kong et al. 2019) |
| EP/2.66%CSA/5.34%DOPO | 36.4% | V-0 | 52.3% | 16.7% | 33.3% | this work |