Table 2 HVI quality statistics of unblended samples between GR 1 and GR 2 (adjusted intercept = intercept/average (Mean GR 1+ Mean GR 2))

| HVI quality | Mean±SD (GR 1) | Mean ±SD (GR 2) | Slope | Adjusted intercept | R2 | ANOVA p-value |
| --- | --- | --- | --- | --- | --- | --- |
| Micronaire (MIC) Upper-half mean length (UHML), in Uniformity index (UI), % Strength (STR), g/tex Reflectance (Rd) Yellowness (+b) Short fiber index (SFI), % Area% Particle count | 4.27±0.59 1.19±0.04 83.05±0.72 31.52±1.89 73.08±3.41 7.95±1.22 6.36±0.74 1.47±0.62 81.14±25.27 | 4.24±0.59 1.19±0.04 83.56±0.92 31.43±2.02 73.71±3.36 7.87±1.22 6.29±0.81 1.54±0.54 73.10±20.86 | 0.97 1.00 1.13 1.00 0.92 0.96 0.90 0.66 0.53 | 0.02 -0.01 -0.12 -0.01 0.09 0.03 0.08 0.37 0.39 | 0.93 0.89 0.77 0.87 0.86 0.93 0.68 0.56 0.41 | 0.83 0.88 0.03 0.88 0.51 0.82 0.75 0.69 0.22 |

Table 3 HVI quality statistics between unblended (x-axis) and blended (y-axis) samples at GR 1 and GR 2 (adjusted intercept = intercept/average (Mean Unblended + Mean Blended))

| HVI quality |  |  | Mean±SD (Unblended) | Mean±SD Blended | Slope | Adjusted Intercept | R2 | ANOVA p-value | ANCOVA p-value |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| MIC UHML UI STR Rd +b SFI Area% Particle count | GR 1 GR 2 GR 1 GR 2 GR 1 GR 2 GR 1 GR 2 GR 1 GR 2 GR 1 GR 2 GR 1 GR 2 GR 1 GR 2 GR 1 GR 2 | 4.27±0.59 4.24±0.59 1.19±0.04 1.19±0.04 83.05±0.72 83.56±0.92 31.52±1.89 31.43±2.02 73.08±3.41 73.71±3.36 8.17±1.30 7.87±1.21 6.36±0.74 6.29±0.81 1.47±0.62 1.54±0.55 81.14±25.27 73.10±20.86 |  | 4.28±0.59 4.22±0.57 1.18±0.04 1.18±0.04 83.41±0.82 83.68±0.78 32.08±2.04 31.64±1.75 77.10±2.90 76.86±3.03 8.70±1.37 8.30±1.29 6.58±0.72 5.89±0.76 0.69±0.34 0.92±0.48 40.16±16.73 45.14±19.67 | 0.99 0.96 0.88 0.92 0.96 0.76 1.04 0.81 0.82 0.80 1.04 1.03 0.84 0.64 0.44 0.56 0.50 0.59 | 0.01 0.04 0.10 0.07 0.04 0.24 -0.03 0.20 0.23 0.23 0.03 0.02 0.19 0.30 0.03 0.03 -0.01 0.04 | 0.97 0.96 0.91 0.94 0.71 0.80 0.94 0.87 0.92 0.80 0.97 0.94 0.76 0.47 0.65 0.41 0.58 0.39 | 1.00 0.93 0.12 0.39 0.10 0.62 0.32 0.70 <0.0001 <0.001 0.16 0.23 0.29 0.07 <0.0001 <0.0001 <0.0001 <0.0001 | 0.42 (Slope) 0.54 (Intercept) 0.67 (Slope) 0.17 (Intercept) 0.16 (Slope) 0.21 (Intercept) 0.01 (Slope) 0.05 (Intercept) 0.89 (Slope) 0.02 (Intercept) 1.00 (Slope) 0.26 (Intercept) 0.27 (Slope) <0.0001 (Intercept) 0.42 (Slope) 0.02 (Intercept) 0.63 (Slope) 0.02 (Intercept) |

Table 4 AFIS quality statistics of unblended samples between GR 1 and GR 2 (adjusted intercept = intercept/average (Mean GR 1+ Mean GR 2))

| AFIS quality | Mean±SD (GR 1) | Mean±SD (GR 2) | Slope | Adjusted intercept | R2 | p-value |
| --- | --- | --- | --- | --- | --- | --- |
| Nep size, µm Neps, /g Seed-coat nep (SCN) size, µm Seed-coat nep (SCN) count, /g L(w), in L(w) CV, % Upper quartile length (UQL(w)), in Short fiber content (SFC(w)), % L(n), in L(n) CV, % L5%(n), in Short fiber content (SFC(n)), % Fineness, mTex Immature fiber content (IFC), % Maturity ratio (MR) Total count, /g Trash size, µm Dust count, /g Particle count, /g Visible foreign matter (VFM), % | 678.60±18.77 239.94±83.87 1007.3±84.0 18.26±7.81 1.04±0.03 32.89±2.50 1.26±0.04 7.73±1.54 0.83±0.04 50.39±3.69 1.42±0.05 25.07±3.64 160.2±11.89 7.07±0.85 0.87±0.03 1645.7±639.5 371.64±25.54 1306.4±501.7 339.26±148.8 6.28±2.75 | 675.72±16.16 213.82±80.05 993.52±101.40 16.9±6.75 1.05±0.03 31.94±2.08 1.27±0.05 6.88±1.13 0.85±0.04 48.96±3.21 1.43±0.05 23.26±2.95 160.82±10.83 6.94±0.72 0.87±0.03 1638.2±631.6 373.62±25.97 1298.7±501.4 339.38±139.2 6.12±2.50 | 0.35 0.78 -0.14 0.40 0.70 0.71 0.91 0.54 0.59 0.71 0.95 0.60 0.84 0.74 0.76 0.60 0.83 0.59 0.65 0.64 | 0.65 0.12 1.14 0.55 0.31 0.26 0.09 0.37 0.43 0.27 0.05 0.34 0.16 0.25 0.25 0.38 0.18 0.42 0.35 0.34 | 0.16 0.67 0.01 0.21 0.52 0.74 0.76 0.54 0.44 0.66 0.73 0.56 0.85 0.74 0.79 0.37 0.66 0.35 0.49 0.48 | 0.56 0.26 0.60 0.51 0.09 0.15 0.48 0.03 0.04 0.15 0.50 0.06 0.84 0.57 0.40 0.97 0.79 0.96 0.99 0.83 |

Table 5 AFIS quality statistics between unblended (x-axis) and blended (y-axis) samples at GR 1 and 2 (adjusted intercept = intercept/average (Mean Unblended + Mean Blended))

| AFIS quality |  | Mean±SD (Unblended) | Mean±SD (Blended) | Slope | Adjusted intercept | R2 | ANOVA p-value | ANCOVA p-value |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Nep size Neps SCN size SCN count L(w) L(w) CV UQL(w) SFC(w) L(n) L(n) CV L5%(n) SFC(n) Fineness IFC MR Total count Trash size Dust count Particle count VFM | GR 1 GR 2 GR 1 GR 2 GR 1 GR 2 GR 1 GR 2 GR 1 GR 2 GR 1 GR 2 GR 1 GR 2 GR 1 GR 2 GR 1 GR 2 GR 1 GR 2 GR 1 GR 2 GR 1 GR 2 GR 1 GR 2 GR 1 GR 2 GR 1 GR 2 GR 1 GR 2 GR 1 GR 2 GR 1 GR 2 GR 1 GR 2 GR 1 GR 2 | 678.60±18.77 675.72±15.98 239.94±83.87 213.82±86.06 1007.3±84.0 993.52±101.4 18.26±7.81 16.90±6.75 1.04±0.03 1.06±0.03 32.89±2.50 31.94±2.08 1.27±0.04 1.28±0.05 7.73±1.54 6.88±1.13 0.83±0.04 0.85±0.04 50.39±3.69 48.96±3.21 1.42±0.05 1.43±0.05 25.07±3.64 23.26±2.95 160.20±11.89 160.82±10.83 7.07±0.85 6.94±0.72 0.87±0.03 0.88±0.03 1645.7±639.5 1638.2±631.6 371.65±25.54 373.62±25.97 1306.4±501.7 1298.7±501.4 339.26±148.8 339.38±139.2 6.28±2.75 6.12±2.50 | 695.86±14.58 690.42±16.54 401.74±156.08 307.70±111.76 1066.6±73.20 1026.6±87.2 22.66±8.58 23.76±8.86 1.04±0.03 1.06±0.04 32.47±2.18 31.75±2.38 1.27±0.04 1.28±0.05 7.32±1.44 6.80±1.43 0.84±0.04 0.86±0.05 49.68±3.44 48.95±4.06 1.42±0.04 1.43±0.05 24.1±3.48 23.21±3.87 165.14±9.03 164.44±11.04 6.73±0.61 6.86±0.68 0.88±0.03 0.88±0.03 894.4±450.6 1178.3±667.9 388.80±24.90 386.72±26.99 696.1±347.4 919.5±526.4 198.28±106.9 258.60±146.0 3.76±1.94 4.82±2.47 | 0.38 0.29 1.46 1.08 0.15 -0.13 0.64 0.76 0.87 0.99 0.68 1.05 0.75 0.99 0.75 1.08 0.83 1.10 0.68 1.12 0.84 0.94 0.72 1.12 0.55 0.95 0.60 0.78 0.83 0.97 0.56 0.75 0.70 0.75 0.54 0.73 0.60 0.79 0.60 0.77 | 0.63 0.72 0.16 0.28 0.88 1.15 0.53 0.50 0.13 0.06 0.31 -0.05 0.25 0.01 0.21 -0.09 0.18 -0.09 0.31 -0.13 0.16 0.06 0.25 -0.12 0.48 0.06 0.36 0.21 0.18 0.04 -0.02 -0.03 0.34 0.28 -0.01 -0.03 -0.02 -0.03 0.01 0.02 | 0.24 0.08 0.61 0.59 0.03 0.02 0.34 0.33 0.72 0.78 0.61 0.84 0.66 0.94 0.64 0.73 0.65 0.74 0.53 0.79 0.75 0.91 0.56 0.73 0.52 0.88 0.70 0.68 0.88 0.79 0.63 0.50 0.52 0.53 0.61 0.48 0.70 0.57 0.71 0.61 | <0.001 <0.01 <0.0001 <0.01 0.01 0.22 0.06 0.01 0.59 0.57 0.53 0.78 0.74 0.76 0.33 0.81 0.43 0.67 0.48 0.99 0.65 0.89 0.37 0.96 0.10 0.25 0.10 0.68 0.09 0.27 <0.0001 0.02 0.02 0.09 <0.0001 0.01 <0.001 0.06 <0.0001 0.07 | 0.70 (Slope) 0.29 (Intercept) 0.22 (Slope) 0.02 (Intercept) 0.28 (Slope) 0.09 (Intercept) 0.69 (Slope) 0.61 (Intercept) 0.47 (Slope) 0.99 (Intercept) 0.02 (Slope) 0.82 (Intercept) 0.04 (Slope) 0.99 (Intercept) 0.07 (Slope) 0.40 (Intercept) 0.15 (Slope) 0.69 (Intercept) 0.02 (Slope) 0.43 (Intercept) 0.12 (Slope) 0.53 (Intercept) 0.04 (Slope) 0.34 (Intercept) 0.01 (Slope) 0.487 (Intercept) 0.19 (Slope) 0.05 (Intercept) 0.21 (Slope) 0.14 (Intercept) 0.30 (Slope) 0.01 (Intercept) 0.79 (Slope) 0.50 (Intercept) 0.17 (Slope) 0.01 (Intercept) 0.26 (Slope) 0.01 (Intercept) 0.25 (Slope) 0.01 (Intercept) |

Table 6 Correlations between HVI and AFIS quality for GR 1 samples (x-axis) and GR 2 samples (y-axis) between unblended and blended samples

| HVI vs. AFIS quality |  | Unblended |  |  | Blended |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  | R2 | ANCOVA | R2 |  | ANCOVA |
| UHML vs. L(w) UHML vs. UQL(w) UHML vs. L(n) UHML vs. L5%(n) SFI vs. SFC(w) SFI vs. SFC(n) MIC vs. Fineness MIC vs. IFC MIC vs. MR L(w) vs. L(n) UQL(w) vs. L5%(n) SFC(w) vs. SFC(n) | GR 1 GR 2 GR 1 GR 2 GR 1 GR 2 GR 1 GR 2 GR 1 GR 2 GR 1 GR 2 GR 1 GR 2 GR 1 GR 2 GR 1 GR 2 GR 1 GR 2 GR 1 GR 2 GR 1 GR 2 | 0.41 0.70 0.83 0.94 0.02 0.13 0.83 0.91 0.16 0.12 0.09 0.07 0.92 0.84 0.68 0.56 0.60 0.55 0.66 0.62 0.95 0.96 0.97 0.97 | 0.47 (Slope) 0.01 (Intercept) 0.73 (Slope) 0.01 (Intercept) 0.52 (Slope) 0.03 (Intercept) 0.42 (Slope) 0.02 (Intercept) 0.47 (Slope) 0.03 (Intercept) 0.66 (Slope) 0.06 (Intercept) 0.19 (Slope) 0.28 (Intercept) 0.23 (Slope) 0.25 (Intercept) 0.32 (Slope) 0.11 (Intercept) 0.60 (Slope) 0.33 (Intercept) 0.26 (Slope) 0.92 (Intercept) 0.60 (Slope) 0.33 (Intercept) | 0.31 0.56 0.64 0.94 0.05 0.08 0.64 0.92 0.29 0.12 0.19 0.09 0.61 0.85 0.63 0.72 0.53 0.71 0.72 0.67 0.96 0.97 0.95 0.98 |  | 0.44 (Slope) 0.09 (Intercept) 0.10 (Slope) 0.50 (Intercept) 0.82 (Slope) 0.15 (Intercept) 0.13 (Slope) 0.99 (Intercept) 0.39 (Slope) 0.86 (Intercept) 0.66 (Slope) 0.79 (Intercept) 0.01 (Slope) 0.89 (Intercept) 0.33 (Slope) 0.46 (Intercept) 0.37 (Slope) 0.50 (Intercept) 0.99 (Slope) 0.75 (Intercept) 0.82 (Slope) 0.08 (Intercept) 0.07 (Slope) 0.20 (Intercept) |