Supporting Information

Unprecedented [Hg3Se2]2- cluster drives giant optical anisotropy and broad infrared transparency

Qixian Ren1,2, Chen Cui1,2, Xinchen Chen1,2, Yabo Wu1*, Ran An1, Zhihua Yang1, Shilie Pan1*

1Research Center for Crystal Materials, CAS Key Laboratory of Functional Materials and Devices for Special Environments, Xinjiang Technical Institute of Physics & Chemistry, CAS, Xinjiang Key Laboratory of Functional Crystal Materials, 40-1 South Beijing Road, Urumqi 830011, China. 2These authors contributed equally: Qixian Ren, Cui Chen, Xinchen Chen.

*e-mails: wyb@ms.xjb.ac.cn; slpan@ms.xjb.ac.cn

Supplementary Table 1. Crystal data and structure refinement for Hg9Ga4Se4Cl16 (298 K).

| Empirical formula | Hg9Ga4Se4Cl16 |
| --- | --- |
| Formula weight (Da) | 2967.23 |
| Temperature (K) | 298.00 |
| Crystal system | Monoclinic |
| Space group | C2/c |
| a (Å) | 12.3962(8) |
| b (Å) | 7.1340(5) |
| c (Å) | 42.127(3) |
| α (°) | 90 |
| β (°) | 93.799(2) |
| γ (°) | 90 |
| Volume (Å3) | 3717.3(4) |
| Z | 4 |
| Density (calc.) (g/cm3) | 5.302 |
| Absorption coefficient (mm-1) | 44.923 |
| F (000) | 5008.0 |
| Completeness to θ (%) | 99.7 |
| Radiation | MoKα (λ = 0.71073) |
| Theta range for data collection | 5.816 to 54.928 |
| Index ranges | -14 ≤ h ≤ 16, -9 ≤ k ≤ 9, -54 ≤ l ≤ 54 |
| Reflections collected | 34982 |
| Independent reflections | 4250 [Rint = 0.0605, Rsigma = 0.0386] |
| Data / restraints / parameters | 4250 / 0 / 150 |
| Goodness-of-fit on F2 | 1.095 |
| Final R indexes [I ≥ 2σ (I)] a | R1 = 0.0462, wR2 = 0.1114 |
| Final R indexes [all data] a | R1 = 0.0534, wR2 = 0.1149 |
| Largest diff. peak / hole (e/Å-3) | 1.17 / -1.25 |

a R1 = Fo - Fc/Fo and wR2 = [w (Fo2 – Fc2)2 / w Fo4]1/2 for Fo2 > 2( Fo2)

Supplementary Table 2. Fractional atomic coordinates (×104) and equivalent isotropic displacement parameters (Å2×103) for Hg9Ga4Se4Cl16 (298 K). Ueq is defined as 1/3 of the trace of the orthogonalized UIJ tensor.

| Atom | X | y | z | U(eq) |
| --- | --- | --- | --- | --- |
| Hg1 | 6325.1(5) | 3143.2(9) | 6103.5(2) | 45.56(16) |
| Hg2 | 3822.2(5) | 5631.8(9) | 6098.7(2) | 45.25(16) |
| Hg3 | 2666.4(5) | 7774.6(8) | 5299.4(2) | 45.51(16) |
| Hg4 | 4823.9(6) | 3210.3(11) | 6888.1(2) | 59.7(2) |
| Hg5 | 5000 | 3381.0(19) | 7500 | 77.8(4) |
| Ga1 | 3170.7(13) | 8067(2) | 6954.0(4) | 38.1(3) |
| Ga2 | 1198.1(12) | 3140(2) | 5565.9(3) | 33.9(3) |
| Se1 | 3103.0(11) | 8638(2) | 5883.7(3) | 38.6(3) |
| Se2 | 4509.9(11) | 2567.4(19) | 6279.4(3) | 38.3(3) |
| Cl1 | 4752(3) | 8046(6) | 6756.2(12) | 60.1(11) |
| Cl2 | 3274(6) | 7903(10) | 7458.5(11) | 95.4(19) |
| Cl3 | 2313(3) | 5657(5) | 6732.2(10) | 52.8(9) |
| Cl4 | 2287(3) | 10490(6) | 6762.1(11) | 56.3(10) |
| Cl5 | 2836(3) | 3152(6) | 5415.5(10) | 50.4(9) |
| Cl6 | 1300(3) | 3055(6) | 6084.5(9) | 53.2(9) |
| Cl7 | 333(3) | 639(5) | 5406.6(10) | 52.4(9) |
| Cl8 | 343(3) | 5666(5) | 5416.7(10) | 49.4(9) |

Supplementary Table 3. Anisotropic displacement parameters (Å2 × 103) for Hg9Ga4Se4Cl16 (298 K). The anisotropic displacement factor exponent takes the form: -2π2[h2a*2U11+2hka*b*U12+…].

| Atom | U11 | U22 | U33 | U23 | U13 | U12 |
| --- | --- | --- | --- | --- | --- | --- |
| Hg1 | 39.5(3) | 50.6(3) | 47.4(3) | 1.4(2) | 8.7(2) | 9.1(2) |
| Hg2 | 39.5(3) | 49.7(3) | 46.3(3) | 6.2(2) | 0.7(2) | 11.0(2) |
| Hg3 | 53.1(4) | 49.0(3) | 34.7(3) | 4.5(2) | 4.2(2) | -0.8(3) |
| Hg4 | 72.4(5) | 74.2(5) | 32.3(3) | 3.8(3) | 3.3(3) | 5.8(4) |
| Hg5 | 101.3(9) | 98.6(9) | 33.2(5) | 0 | 3.8(5) | 0 |
| Ga1 | 40.4(8) | 40.0(8) | 33.7(7) | -0.9(6) | 0.6(6) | 0.7(6) |
| Ga2 | 32.9(7) | 31.2(7) | 37.3(8) | 0.0(6) | 1.1(6) | -1.4(6) |
| Se1 | 37.7(7) | 38.3(7) | 39.7(7) | -1.7(6) | 1.9(6) | 1.7(6) |
| Se2 | 40.5(7) | 38.0(7) | 36.1(7) | -0.9(5) | 0.9(6) | -0.2(6) |
| Cl1 | 41(2) | 64(3) | 76(3) | 3(2) | 8.3(19) | 1.5(18) |
| Cl2 | 137(5) | 115(5) | 33(2) | 0(3) | -1(3) | 1(4) |
| Cl3 | 53(2) | 43.9(19) | 61(2) | -4.9(17) | -2.0(18) | -11.2(17) |
| Cl4 | 58(2) | 45(2) | 66(3) | 2.1(18) | 2.4(19) | 11.7(18) |
| Cl5 | 36.9(18) | 53(2) | 62(2) | 8.1(18) | 9.8(17) | 1.2(16) |
| Cl6 | 60(2) | 64(2) | 34.8(18) | -1.6(16) | 2.5(17) | -0.5(19) |
| Cl7 | 59(2) | 42.2(19) | 55(2) | -7.9(16) | -2.7(18) | -12.9(17) |
| Cl8 | 48(2) | 41.6(19) | 58(2) | 6.5(16) | 2.3(17) | 8.6(16) |

Supplementary Table 4. Bond lengths for Hg9Ga4Se4Cl16 (298 K).

| Atom | Atom | Length/Å |  | Atom | Atom | Length/Å |
| --- | --- | --- | --- | --- | --- | --- |
| Hg1 | Se11 | 2.4718(15) |  | Ga1 | Cl1 | 2.180(4) |
| Hg1 | Se2 | 2.4498(15) |  | Ga1 | Cl2 | 2.124(5) |
| Hg2 | Se1 | 2.4716(15) |  | Ga1 | Cl3 | 2.198(4) |
| Hg2 | Se2 | 2.4493(15) |  | Ga1 | Cl4 | 2.173(4) |
| Hg3 | Hg32 | 2.5595(11) |  | Ga2 | Cl5 | 2.167(4) |
| Hg3 | Se1 | 2.5600(15) |  | Ga2 | Cl6 | 2.181(4) |
| Hg4 | Hg5 | 2.5755(6) |  | Ga2 | Cl7 | 2.165(4) |
| Hg4 | Se2 | 2.6087(15) |  | Ga2 | Cl8 | 2.163(4) |

11/2+X,-1/2+Y,+Z; 21/2-X,3/2-Y,1-Z

Supplementary Table 5. Bond angles for Hg9Ga4Se4Cl16 (298 K).

| Atom | Atom | Atom | Angle/˚ |  | Atom | Atom | Atom | Angle/˚ |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Se2 | Hg1 | Se11 | 175.45(5) |  | Cl7 | Ga2 | Cl5 | 111.54(17) |
| Se2 | Hg2 | Se1 | 176.46(5) |  | Cl7 | Ga2 | Cl6 | 106.40(17) |
| Se1 | Hg3 | Hg32 | 174.01(5) |  | Cl8 | Ga2 | Cl5 | 111.26(16) |
| Hg5 | Hg4 | Se2 | 171.66(5) |  | Cl8 | Ga2 | Cl6 | 107.99(17) |
| Hg4 | Hg5 | Hg43 | 174.58(7) |  | Cl8 | Ga2 | Cl7 | 111.92(17) |
| Cl1 | Ga1 | Cl3 | 104.72(18) |  | Hg14 | Se1 | Hg3 | 100.89(5) |
| Cl2 | Ga1 | Cl1 | 112.7(3) |  | Hg2 | Se1 | Hg14 | 92.73(5) |
| Cl2 | Ga1 | Cl3 | 112.2(2) |  | Hg2 | Se1 | Hg3 | 101.06(5) |
| Cl2 | Ga1 | Cl4 | 114.3(2) |  | Hg1 | Se2 | Hg2 | 93.68(5) |
| Cl4 | Ga1 | Cl1 | 107.90(18) |  | Hg1 | Se2 | Hg4 | 100.81(5) |
| Cl4 | Ga1 | Cl3 | 104.26(17) |  | Hg2 | Se2 | Hg4 | 100.06(5) |
| Cl5 | Ga2 | Cl6 | 107.46(17) |  |  |  |  |  |

11/2+X,-1/2+Y,+Z; 21/2-X,3/2-Y,1-Z; 31-X,+Y,3/2-Z; 4-1/2+X,1/2+Y,+Z

Supplementary Figure 1. PXRD patterns of HGSC.

Supplementary Figure 2. The X-ray photoelectron spectra of HGSC: (a) survey spectrum, (b) gallium, (c) selenium, and (d) chlorine.

Supplementary Figure 3. Photoluminescence spectrum of HGSC.

Supplementary Figure 4. Pristine single crystal, crystal morphology change variation of HGSC under different laser output energies.

Supplementary Figure 5. The electron localization function for HGSC.

Birefringence measurement of HGSC.

Numerical fitting of the ellipticity tanχ (defined as the ratio of the short axis to the long axis) and ψ (representing the angle between the long axis of the ellipse and the x-axis).

Based on the Jones matrix theory, we established a complete polarization state characterization system: the horizontal linear polarization state under crystal-free conditions and the elliptical polarization states corresponding to crystal rotations of 30, 60, and 90 ° are represented as Jones vectors E0, E1, E2, and E3, respectively, with their mathematical expressions as follows:

E0=10#1

E1=0.231205260.972904994expi∙1.45631#2

E2=0.2336951360.972309921expi∙0.560412#3

E3=0.363708830.931512688expi∙0.481014#4

According to the above parameter relationships, the Jones matrix expressions corresponding to the three rotation angles (30, 60, and 90 °) can be derived as J1, J2, and J3

J1=cosφ2+icos2θsinφ2isin2θsinφ2isin2θsinφ2cosφ2-icos2θsinφ2#5

J2=cosφ2+icos2π6+θsinφ2isin2π6+θsinφ2isin2π6+θsinφ2cosφ2-icos2π6+θsinφ2#6

J3=cosϕ2+icos2π3+θsinφ2isin2π3+θsinφ2isin2π3+θsinφ2cosφ2-icos2π3+θsinφ2#7