Table. 2 Study on the catalytic performance of different catalysts in the DMR/ATH cascade reaction in THF/H2O v/v 8:1a

| Entry | Catalysts | Conversion%b | dr/%c | % ee c |
| --- | --- | --- | --- | --- |
| 1 | Poly(A-Ru1)-r-(B-Cu0) | 99 | 38:62 | 96/97 |
| 2 | Poly(A-Ru1)-b-(B-Cu2.7) | 99 | 86:14 | 40/62 |
| 3 | Poly(A-Ru1)-b-(B-Cu2.2) | 99 | 37:63 | 97/68 |
| 4 | Poly(A-Ru1)-r-(B-Cu5.6) | 99 | 95:5 | 59 |
| 5 | Poly(A-Ru1)-b-(B-Cu2.6) | 99 | 70:30 | 99/1 |
| 6 | Poly(A-Ru1)-b-(B-Cu5.0) | 99 | 98:2 | 55 |
| 7 | Poly(A-Ru1)-r-(B-Cu8) | 99 | 97:3 | 98 |
| 8 | Poly(A-Ru1)-r-(B-Cu1.5) | 99 | 43:57 | 99/77 |
| 9 | A-Ru/B-Cu 1:1 | 99 | 56:44 | 96/97 |
| 10 | Poly(A-Ru)/Poly-(B-Cu) 1:1 | 99 | 99:1 | 3 |
| 11 | Poly(A-Ru)/Poly-(B-Cu) 2:1 | 99 | 99:1 | 37 |
| 12 | Poly(A-Ru)/Poly-(B-Cu) 1:2 | 99 | 98:2 | 51 |
| 13 | Poly(A-Ru1-r-B1.3)d | 99 | 28:72 | 79/85 |
| 14 | Poly(A-Ru1)-r-(B-Cu8)d | 99 | 99:1 | 99 |
| 15 | Poly(A-Ru1)-r-(B-Cu1.5)d | 99 | 4:96 | -92 |

a. Reaction conditions: 0.0004 mmol of Ru, THF/H2O 8/1 1.2ml, 0.04 mmol of amine, 0.06 mmol of acid, S/C=1000, reaction at -20 ℃ for 5 hours, reaction at 60 ℃ for 18 hours; b. Conversion rate; c. Determination by high-performance liquid chromatography, AD-H, n-hexane/isopropanol=90/10, 1.0 mL/min; d. The reaction solvent is THF/H2O v/v 4:1.