Supporting information file

Fig. S1. Visible transmission of alumina with different sintering aids.

Fig. S2. Cross-sectional FESEM images of alumina with different sintering aids: (a) without sintering aid, (b) 100 ppm MgO, (c) 100 ppm MgO + 100 ppm La2O3, (d) 100 ppm MgO + 300 ppm ZrO2. Red arrows indicate porosity.

Figure S3: Light microscopic images of Vickers impact points and cracks observed for the 100M-100L-300Z (Z) sample: (a) impact point; (b) crack observed at higher magnification.

Figure S4: FESEM images of indentation impact points and crack length measurements for samples with varying amounts of sintering aids.

100ppm MgO 300 ppm ZrO2

100 ppm MgO

Without sintering aid

100ppm MgO 100 ppm La2O3

Fig. S1.

(a)

(b)

(c )

Alumina/1wt.% Si3N4

(d )

Fig. S2.

b

a

Crack

Figure S3.

100M100L50Z

100M100L100Z

100M100L300Z

200M100L100Z

Figure S4.