Supplemental Data

Electrocatalytic hydrogen evolution performance of RuO2 nanorods grown on top of WO3 nanotube arrays

Man Zhang,a, b Kefeng Wang,a* Jingxiao Ren,c Yong-hua Li,d Heng Jiang,b* Wei Weia*

a a School of Petrochemical Engineering, Liaoning Petrochemical University, Fushun, Liaoning 113001, China

b Henan Engineering Center of New Energy Battery Materials, College of Chemistry and Chemical Engineering, Shangqiu Normal University, Shangqiu 476000, Henan, China

c School of Surveying and Planning, Shangqiu Normal University, Shangqiu 476000, China

d North Huajin Chemical Industries Group Corporation, Panjin 124000, P. R. China

Figure S1 Photographs of blank W foil, anodized W foil (WO3 NTA), Ru(OH)3/WO3 NTA and RuO2 NRs/WO3 NTA.

Figure S2 SEM images of WO3 NTA fabricated through an anodization process using a piece of W foil as the substrate.

Figure S3 EDS elemental mapping images for RuO2 NRs/WO3 NTA: (a) overlay, (b) Ru, (c) W and (d) O

Figure S4 (a) HRTEM image of RuO2 nanorod in RuO2 NRs/WO3 NTA. (b) The fast Fourier transform (FFT) pattern of the selected area in (a). (c~e) Inverse FFT images taken from the square labeled in (b) correspond to the interplanar crystal spacings of (101), (211) and (112) planes of RuO2. (f-h) The corresponding interplanar spacings.

Figure S5 Calculation of the exchange current densities of different catalysts by extrapolating the linear fit of the Tafel plot to its interception.

Figure S6 Cyclic voltammetry (CV) curves with different scan rates of (a) RuO2 NRs/WO3 NRA, (b) Ru(OH)3/WO3 NRA, and (c) RuO2/W in the non-Faradaic regions in 1 M KOH.

Figure S7 Cyclic voltammetry (CV) curves with different scan rates of (a) RuO2 NRs/WO3 NRA, (b) Ru(OH)3/WO3 NRA, and (c) RuO2/W in the non-Faradaic regions in 0.5 M H2SO4.

Table S1 Comparison of alkaline HER performance of RuO2 NRs/WO3 NTA with other reported RuO2-based and Ru-based electrocatalysts

| Catalysts | η10 mV | η100 mV | Tafel slope (mV dec-1) | Reference |
| --- | --- | --- | --- | --- |
| RuO2 NRs/WO3 NTA | 33 | 83 | 35.2 | This work |
| RuO2@Ni-MWCNTs | 20.21 | 159 | 26.26 | J. Colloid Interface Sci., 2025, 679: 100-108 |
| Ru-RuO2/C-300A | 31 | >100 | 85.4 | Advanced science, 2025, 2414534. |
| Ru/NdOCl | 20 | >100 | 36 | Adv. Mater., 2025, 2417621. |
| RuO2@MoS2 | 114 | >400 | 62.9 | Appl. Surf. Sci., 2021, 538: 148019 |
| RuO2@Fe2O3/HrGO NSs | 239 | >300 | 97 | Int. J. Hydrogen Energy, 2023, 48: 1813-1830 |
| RuO2–Fe2O3 | 148 |  | 43 | Dalton Transactions, 2022, 51: 6314-6331. |
| Mn-RuO2 | 37 | >100 | 40.8 | Chin. Chem. Lett., 2024, 35: 109863. |
| RuO2@TiO2/TP | ~34 | 143 | 94 | Inorg. Chem. Frontiers, 2022, 9: 6602-6607 |
| Ni/Co(OH)2-Ru@NF | 28 | >100 | 23.81 | Small, 2025, 2410086. |
| Ru-RuO2@NPC | ~79 |  | 73 | Appl Catal B: Environ., 2022, 302, 120838. |
| Co-SAC/RuO2 | 45 |  | 58 | Angew Chem Int Ed, 2022, 61, e202114951 |
| Ru@RuO2 | 32 | 84 | 21.7 | Chem Eng J 2023, 460, 141672 |
| nanoporous RuO2 | 87 |  | 45.8 | J. Electroanal. Chem., 2021, 881: 114955 |
| ZIF-8/SnO2@RuO2 | ~198 |  | 55.6 | Mater. Today Commun., 2025, 43: 111769 |
| Ru-mCNFs-300 | 19 | 121 | 39 | Vacuum, 2024, 225: 113258. |
| Ru-RuO2/ MXene@CC | 43 | ~146 | 52.1 | Colloids Surf. Physicochem. Eng. Aspects, 2023, 679: 132638. |
| CoFe2O4/RuO2 | 58 | ~158 | 73.1 | Electrochim. Acta, 2024, 503, 144930 |
| h-RuO2/CNT | ~37 | ~125 | 43.5 | Appl Catal B: Environ., 2024, 365, 124220 |
| NiRuO2−x | 51 |  | 34.4 | J. Colloid Interface Sci., 2023, 630: 940-950. |
| Al doped Rux/RuO2 | 43.97 | 47.1 | 120.04 | J. Mater. Chem. A, 2025, 13: 5091-5105 |
| Ru/CeO2/C | 30 |  | 55.9 | ChemistrySelect, 2024, 9, e202404254 |
| Ir SA/RuO2 | 37 | 88 | 22.6 | Chem. Sci., 2024, 15, 16796–16803 |
| fcc Ru–RuO2/C | 30 | >150 | 21 | J. Mater. Chem. A, 2024, 12, 27540–27548 |

Table S2 Comparison of acidic HER performance of RuO2 NRs/WO3 NTA with other reported RuO2-based and Ru-based electrocatalysts

| Catalysts | η10 mV | Tafel slope (mV dec-1) | Reference |
| --- | --- | --- | --- |
| RuO2 NRs/WO3 NTA | 62 | 35.4 | This work |
| RuO2@Ni-MWCNTs | 73.7 | 48.86 | J. Colloid Interface Sci., 2025, 679: 100-108 |
| Ru-RuO2@NPC | 68 | 56 | Appl Catal B: Environ 2022, 302, 120838. |
| Al doped Rux/RuO2 | >100 | 57.9 | J. Mater. Chem. A, 2025, 13: 5091-5105 |
| Mn(SAs)-Ru/RuO2 | 39 | 14.31 | Adv. Funct. Mater., 2024, 2422166 |
| Ru NPs/Fe5Ni4S8 | 54 | 57 | Small, 2023, e2301721. |
| Mo2C-Ru/C | 64 | 67 | Adv. Funct. Mater., 2023, 2301925 |
| Ru1+NPs/N−C | 75 | 42.7 | ACS Appl. Mater. Interfaces, 2022, 14: 15250-15258. |
| RuFeP-NCs/CNF | 65.8 | 43.4 | Appl. Catal., B, 2021, 283: 119583 |
| Ru@Co/N-CNTs | 92 | 45 | ACS Sustainable Chem. Eng. 2020, 8, 9136−9144 |
| La-doped RuO2 | 71 | 49.3 | Chem. Eng. J., 2022, 439: 135699 |
| RuNi/CQDs | 58 | 55 | Angew. Chem. Int. Ed., 2020, 59: 1718-1726 |
| RuP3–CoP NS | 60 | 56 | Mater. Today Sustainability 2021, 13, 100074 |
| Ru-RuO2-NC | 112 |  | J. Alloys Compd., 2022, 902: 163787. |
| Ru-Ru2P | 48 | 41.2 | InfoMat, 2022, 4: e12287. |
| RuTe2/Graphene | 72 | 33 | Chem. Asian J. 2020, 15, 2886 |
| Ru/ZnRuO2 | 97 | 51.5 | Adv. Funct. Mater. 2024, 34, 2409306 |
| FeCoNiCrTi-RuO2 | ~50 | 69.1 | Small, 2024, 20: 2404019. |
| RuO2/CeO2@C | 120 | 83.1 | Chem. Eng. J., 2024, 479: 147939 |
| RuO2/Co3O4 | 100 | 85.1 | Adv. Energy Sustainability Res., 2023, 4: 2300057 |
| RuO2/C3N4 | 109 | 70.8 | Dalton Trans., 2023, 52, 10515–10521 |
| Pt-RuO2/Ti mesh | 49 | 51.2 | J. Electroanal. Chem., 2023, 932: 117221. |
| Ru@MoO(S)3 | 63 | 32 | Nano Energy, 2022, 100: 107445 |
| RuO2-WC NPs | 58 | 66 | Angew. Chem. 2022, 134, e202202519 |
| Ru/WO3-W2N/NC | 110 | 70 | J. Colloid Interface Sci., 2023, 636, 618–626 |