Supporting Information

Piezo-catalytic In-site H2O2 Generation and Activation Across Wide pH Range to Drive Hydroxyl Radical-Mediated Pollutant Degradation

Jing Xu et al

1. Experimental Procedures

1.1 Chemicals reagents

Bismuth nitrate (Bi(NO3)3·5H2O), potassium iodate (KIO3), nitric acid (65% HNO3), tert-butanol (TBA), sodium bromates (NaBrO3), 1,4-benzoquinone (p-BQ), triethanolamine (TEOA) were obtained from Sinopharm Chemical Reagent Co., Ltd. Iron triperchlorate (Fe(ClO4)3∙xH2O), Rhodamine B (RhB), benzophenone-3 (BP-3), atrazine (ATZ), phenol (PhOH) and ibuprofen (IBU) were supplied by Aladdin regent (Shanghai) Co., Ltd. , perchloric acid (HClO4) was obtained from Sigma-Aldrich. All chemicals used in this work are of analytical grade and utilized without further treatment.

1.2 Synthesis of piezo-catalysts

The BiOIO3 (BIO) nanosheets were synthesized via a one-step hydrolysis method as detailed in our earlier work [1]. Briefly, Bi (NO3)3·5H2O (2.1 mmol) and KIO3 (0.7 mmol) were dispersed in a mixture of deionized water (33 mL) and 65% HNO3 (2 mL), then stirred for 1h at room temperature. The resulting suspension was transferred into a 50 mL Teflon-lined stainless autoclave and hydrothermally treated at 453 K for 14 h in an electric heating oven. The sample was collected by centrifugation, washed alternately with ethanol and water, and subsequently dried at 333 K for 10 h, yielding the white BiOIO3 powder denoted as BIO.

BIOIO3/FeOOH (BF) was synthesized by a facile impregnation hydrolysis process in acidic aqueous solution. Specifically, 50 mL deionized water was added to a beaker, then the pH was adjusted to 2.5 with perchloric acid. Next, a certain amount of ferric perchlorate was added to the above solution, following which the pH was continued to be adjusted to 2 with perchloric acid. Subsequently, 150 mg of BiOIO3 catalyst was added to the above solution, dispersed homogeneously, and placed in an oil bath at 90 °C with stirring for 2 h. The powder obtained were washed to near neutrality by filtration and dried in a vacuum oven at 60 °C. The obtained samples are denoted as BF0.5, BF1.5 and BF2.5, where 0.5-2.5 indicated the mmol concentration of Fe(III) during the preparation of BF.

1.3 Characterization

The morphology and structure of the samples were analyzed employing scanning electron microscopy (SEM, Zeiss Supra 55) and transmission electron microscopy (TEM, JEOL, JEM-2100F). X-ray diffraction (XRD, Rigaku, Smart-Lab) was utilized to determine the crystalline phase. Fourier transform infrared (FTIR) spectroscopy (Thermo Scientific Nicolet iS20) was used to study the surface functional group structure. Surface-enhanced Raman spectroscopy (SERS, LabRAM HR Evolution) was employed to analyze the chemical structure, with 514 nm laser as the excitation source. To investigate the surface states, X-ray photoelectron spectroscopy (XPS, ESCALAB250XI) was employed. Steady-state photoluminescence (PL) was performed using a fluorescence spectrophotometer (Hitachi, F-7000) with an excitation wavelength of 300 nm. Electron spin resonance (ESR, JES-FA200 EER) with 5,5-dimethyl-1-pyrroline N-oxide (DMPO) acting as a spin trap was used to identify active species in the samples. The diffuse reflectance absorption spectra (DRS) of the samples were examined using a UV-visible spectrophotometer (UV-3600, Shimadzu Corporation, Tokyo, Japan), with BaSO4 as a reference. Additionally, surface potentials and piezoelectric properties of the produced samples were investigated using piezoelectric force microscopy (PFM) and a Kelvin probe force microscope (KPFM, Dimension Fast Scan, Bruker, America).

1.4 Quantification of Hydroxyl Radicals (·OH)

The ·OH was quantified using the terephthalic acid (TA) method. The procedure involves the reaction of TA with hydroxyl radicals to form 2-hydroxyterephthalic acid (HTA), which can be measured using fluorescence spectroscopy.

The specific steps are as follows: 20 mg of catalyst was dispersed in 50 mL mixed solution of terephthalic acid (TA) and sodium hydroxide (NaOH), with concentrations of 0.5 mM and 2 mM, respectively. The reaction was carried out under ultrasonic excitation for 20 minutes. At intervals, 2 mL of the supernatant was taken and tested using a fluorescence spectrophotometer, using 315 nm light for excitation. The relative content of ·OH was determined from the fluorescence intensity of the solution at 425 nm.

1.5 Piezo-catalytic H2O2 generation

For the piezo-catalyzed H₂O₂ synthesis, 20 mg of the piezo-catalyst was homogeneously dispersed in 50 mL of pure water and stirred for 20 minutes before the reaction. The mixture was then excited by ultrasonic waves at 200 W and 40 kHz, with temperature control maintained by circulating water during the reaction. At regular intervals, 2 mL of the clear reaction solution was withdrawn to measure the H₂O₂ yield.

The concentration of hydrogen peroxide was determined using a colorimetric method with spectrophotometry. Typically, 10 mg of peroxidase and 100 mg of N, N-diethyl-p-phenylenediamine are dissolved in 10 mL of deionized water, referred to as Solution A and Solution B, respectively. Solution C is a mixture of 10 mL of 0.1 M sodium dihydrogen phosphate (NaH2PO4) and 90 mL of 0.1 M disodium hydrogen phosphate (Na2HPO4). For the test, 1 mL of the centrifuged supernatant is added to a homogeneous mixture containing 3 mL of deionized water, 30 µL of Solution A, 30 µL of Solution B, and 300 µL of Solution C. The mixture is then shaken well, and the absorbance is measured at 551 nm using a UV-visible spectrophotometer.

1.6 Piezo-catalytic H2O2 generation in Ar

20 mg of piezo-catalyst was homogeneously dispersed in 50 mL of pure water and added to a sealed reactor. The reaction solution was evacuated by a vacuum pump for 30 minutes to remove dissolved oxygen completely. High-purity argon gas was then injected into the reactor until the pressure gauge read standard atmospheric pressure. Finally, the ultrasonic machine was turned on to activate the piezo-catalytic reaction.

1.7 Piezoelectric electrochemical measurements

The Piezoelectric electrochemical properties were tested on a CHI-660D electrochemical workstation using a standard three electrode system with Ag/AgCl electrode as the reference electrode, a Pt plate as the counter electrode, and an FTO glass covered with the prepared sample as the working electrode. Piezoelectric current, Mott-Schottky, cyclic voltammetry, and linear scanning voltammetry measurements were performed in a 0.5 M Na₂SO₄ aqueous solution.

The working electrode was prepared as follows: 8 mg of the sample was dispersed in a mixture of 960 µL of hydroalcohol (1:1) and 20 µL of naphthol (5 wt.%), and then sonicated for 60 minutes. Afterwards, 200 µL of the well-dispersed mixture was applied to the conductive side of the FTO glass and dried at room temperature.

1.8 Piezo-catalytic degradation of organic pollutants

20 mg of piezoelectric catalyst was homogeneously dispersed in 50 ml of contaminant solution and stirred for 30 min until adsorption-resolution equilibrium was reached. The catalyst was then excited by ultrasonic waves with 200 W at a frequency of 40 kHz for contaminant degradation. During the reaction the temperature was controlled to room temperature by circulating water. At intervals, 2 ml of the reaction solution was withdrawn and filtered through a 0.22 µm membrane, followed by ultraviolet spectrophotometry (UV) or high-performance liquid chromatography (HPLC) to detect changes in pollutant concentration during degradation, where the absorbance of RhB at 552 nm was detected by UV and the remaining several contaminants were detected by HPLC with the specific test methods shown in Table S2. The types and concentrations of pollutants used were: [RhB] = 5 ppm, [BP-3] = 5 ppm, [ATZ] = 5 ppm, [PhOH] = 5 ppm, [BIU] = 5 ppm.

Besides, water samples were collected from the banks of Mochou Lake and Yangtze River in Nanjing, Jiangsu Province, China, to simulate the impact of real water conditions on the degradation activity of catalysts. Tap water samples were taken from the laboratory of Nanjing Hohai University.

1.9 DFT calculation

Density functional theory (DFT) calculation was performed by using the Vienna Ab-initio Simulation Package (VASP).The energy and electronic structure analysis were carried out by using VASP [2-4] employing the projector augmented wave (PAW) method [5]. The generalized gradient approximation (GGA) of the Perdew-Burke-Ernzerh of (PBE) functional was used to treat the electronic exchange-functional [6]. Van der Waals (vdW) interaction was described using Grimme's semi-empirical dispersion-corrected DFT-D3 method. A plane-wave basis set with k point of 1×1×1, cutoff energy with 450 eV, and energy convergence criteria with 10-5 eV, and the forces on each atom were less than 0.03 eV A-1. The following formula was used to calculate the free energy (ΔG) of the piezo-catalytic reaction step:

G(T) = Eele + Gcorr(T) = Eele + ZPE + ∆G0→T

where Eele, Gcorr(T), ZPE and G0→T stand for electronic energy, thermal corrections to Gibbs free energy, zero-point energy and contribution by heating the system from 0 K to 298.15 K, respectively.

Figure S1. (a) SEM image, (b)TEM image, (c) HRTEM image (with the left inset showing the SAED pattern and the right inset displaying the corresponding inverse FFT) and (d) EDS elements mapping of BIO.

Electron diffraction pattern of selected areas (SAED) (inset of Figure S1c) and the corresponding inverse fast Fourier transform (FFT) (inset of Figure S1c) reflects the superior single-crystal structure of BIO.

Figure S2. (a) TEM images of BF1.5. (b) XRD spectra of as-prepared samples.

In X-ray diffraction (XRD) spectra, BIO exhibits standard and sharp peaks of ICSD # 262019 (Figure S2b), indicating its pure-phase crystal structure. Noteworthily, the characteristic peaks in the prepared BF samples remained unshifted compared to BIO, indicating that the load of FeOOH did not alter the lattice structure of BIO.

Figure S3. XPS survey spectra of (a) BIO and (b) BF1.5. (c) Fe 2p core-level XPS spectrum of BF1.5.

Figure S4. O 1s XPS spectra of BIO and BF1.5.

Figure S5. The optimized electronic structure of the BF.

Figure S6. The (a) phase, (b) amplitude images, and (c) corresponding phase hysteresis loop and amplitude-voltage curves of BIO.

Figure S7. The (a) phase, (b) amplitude images of BF1.5. (c) d33 of BIO and BF1.5.

Figure S8. Piezo-catalytic H2O2 yield of BF1.5 under different reaction conditions (TEOA, TBA, NaBrO3 and p-BQ for piezo-holes, ·OH, piezo-electrons and ·O2- capture, respectively).

Figure S9. Pseudo-first-order kinetic curve fitting for the RhB degradation by different catalysts within 15 min.

Figure S10. (a) Standard curves for different concentration of 2-Hydroxyterephthalic acid (HTA) and (b) The linear relationship of concentration of HTA vs. UV-vis absorption intensity.

Figure S11. Time profiles of HTA concentration in different catalytic systems.

Figure S12. (a) UV-vis DRS of BIO and BF1.5. Plots of transformed Kubelka-Munk function versus photon energy of (b) BIO and (c) BF1.5. (d) The estimated energy band structures of BIO and BF1.5.

The energy band structure of BIO was analyzed with UV-vis DRS (Figure S12a) and Mott-Schottky diagrams (Figure S15). Figure S12b shows that BIO has a broad band gap of 3.03 eV. Additionally, the Fermi flat band potential (EFB) of BIO was estimated from the Mott-Schottky diagram (Figure S15a) to be -1.23 V (vs. Ag/AgCl), which can be converted to -0.68 V (vs. RHE). For n-type semiconductors of BIO, EFB is approximately 0.1 V below the conduction band (CB). Therefore, the CB position of BIO is evaluated to be -0.78 V and the VB position of BIO is assessed to be 2.25 V, which does not meet the requirements for 1e- WOR. Similarly, it can be inferred from Mott-Schottky diagram that the CB of BF1.5 shifts negatively, and the band gap narrows after modification of BIO with FQDs. Thus, the energy band structure of BF1.5 still cannot support 1e- WOR (Figure S12d).

Figure S13. The ·OH yield of pure water cavitation without catalyst, BF1.5 in pure water/air and BF1.5 in pure water/Ar in sealable reactor.

Figure S14. Cyclic voltammetry for (a) BIO and (b) BF1.5. (c) Negative sweep J–V curve of BF1.5 (with/without ultrasonic).

Figure S15. The PL spectra of BIO and BF1.5.

Figure S15. Mott-Schottky plots of the samples.

The charge densities (Nd) can be calculated by Mott–Schottky measurements from the following formula:

Nd=2e0ε0εd1C2dV-1

where C denotes charge capacitance, V is the applied potential, e0 represents the electron charge (1.6 × 10-19 C), ε0 (8.85 × 10–14 F/cm) and ε are the vacuum permittivity and dielectric constant of BiOIO3, respectively [7-9]. From the above equation, it can be inferred that Nd is negatively correlated with the slope of the Mott-Schottky plot.

Figure S16. Piezo-current response of BIO and BF1.5 under ultrasonic.

Figure S17. Intermediate configurations for H2O2 activation on (a-b) BIO and (c-d) BF.

Figure S18. (a-c) Time-dependent UV–vis absorption spectra for RhB degradation and (d) Time profiles of RhB degradation by BF1.5 in different water quality.

Figure S19. Time profiles of multiple emerging pollutants (5 ppm) degradation by BF1.5.

Figure S20. Cyclic stability for RhB degradation by BF1.5.

Figure S21. (a-b) Piezo-catalytic H2O2 yield and (c-d) RhB degradation properties of BF1.5 when integrated onto nonwoven fabric substrates.

Table S1.  Comparison of catalytic performances for RHB degradation of catalysts in recently reported works and this study.

| Catalyst， dosages | Catalytic type | [Pollutant] (mg/L) | k (min−1) | Degradation efficiency | Year, Ref. |
| --- | --- | --- | --- | --- | --- |
| BF1.5 | Piezo | RHB, 5 | 0.311 | 99.6%, 15 min | This work |
| Fe3O4-BT | Piezo | RHB, 5 | 0.017 | 86.3%, 120 min | 2024 [10] |
| KNNS-BxNZ-Fe | Piezo | RHB, 5 | 0.092 | 93.0%, 40 min | 2023 [11] |
| CoOx/BiFeO3 | Piezo | RHB, 5 | 0.039 | 96.0%, 90 min | 2021 [12] |
| PVDF/Fe2O3 | Piezo | RHB, 5 | 0.050 | 94.8%, 60 min | 2024 [13] |
| BiFeO3 | Piezo | RHB, 5 | 0.079 | 92.0%, 30 min | 2024 [14] |
| Ag2O@BFO | Piezo-photo | RHB, 5 | 0.025 | 79.0%, 60 min | 2023 [15] |
| BaTiO3/CuPbSbS3 | Piezo-photo | RHB, 5 | 0.093 | 90.5%, 60 min | 2024 [16] |
| BT@TiO2 | Piezo-photo | RHB, 5 | 0.080 | 89.0%, 30 min | 2022 [17] |
| BaTiO3/ZnO | Piezo-photo | RHB, 5 | 0.052 | 99.0%, 90 min | 2022 [18] |
| Bi0.5Na0.5TiO3 | Piezo-photo | RHB, 5 | 0.094 | 95.0%, 30 min | 2021 [19] |

Reference

[1] J. Xu, Q. Zhang, X. Gao, P. Wang, H. Che, C. Tang, Y. Ao, Highly Efficient Fe (III)‐initiated Self‐cycled Fenton System in Piezo‐catalytic Process for Organic Pollutants Degradation, Angewandte Chemie, (2023) e202307018.

[2] G. Kresse, J. Hafner, Ab initio molecular dynamics for liquid metals, Physical review B, 47 (1993) 558.

[3] G. Kresse, J. Hafner, Ab initio molecular-dynamics simulation of the liquid-metal–amorphous-semiconductor transition in germanium, Physical Review B, 49 (1994) 14251.

[4] W. Kohn, L.J. Sham, Self-consistent equations including exchange and correlation effects, Physical review, 140 (1965) A1133.

[5] P.E. Blöchl, Projector augmented-wave method, Physical review B, 50 (1994) 17953.

[6] J.P. Perdew, K. Burke, M. Ernzerhof, Generalized gradient approximation made simple, Phys. Rev. Lett., 77 (1996) 3865.

[7] M. Ran, B. Du, W. Liu, Z. Liang, L. Liang, Y. Zhang, L. Zeng, M. Xing, Dynamic defects boost in-situ H2O2 piezocatalysis for water cleanup, Proceedings of the National Academy of Sciences, 121 (2024) e2317435121.

[8] G. Di Liberto, S. Tosoni, G. Pacchioni, Nature and role of surface junctions in BiOIO3 photocatalysts, Advanced Functional Materials, 31 (2021) 2009472.

[9] S.-H. Chiou, H.-C. Ho, H.-T. Liao, F.-Y. Tsai, C.-W. Tsao, Y.-J. Hsu, C.-H. Hsueh, Plasmonic gold nanoplates-decorated ZnO branched nanorods@ TiO2 nanorods heterostructure photoanode for efficient photoelectrochemical water splitting, Journal of Photochemistry and Photobiology A: Chemistry, 443 (2023) 114816.

[10] J. Xie, Q. Liu, L. Huang, X. Chen, C. Zhao, X. Wu, T. Lin, Y. Wu, M. Gao, C. Lin, Piezo-Fenton catalysis in Fe3O4-BaTiO3 nanocomposites: A low-cost and highly efficient degradation method without the additive of H2O2 or Fe (II) ions, Chemical Engineering Journal, 487 (2024) 150685.

[11] J. Liao, X. Lv, X.x. Sun, J. Li, H. Wang, Q. Chen, H. Lu, D. Wang, J. Bi, J. Wu, Boosting piezo‐catalytic activity of KNN‐based materials with phase boundary and defect engineering, Advanced Functional Materials, 33 (2023) 2303637.

[12] L. Wang, J. Wang, C. Ye, K. Wang, C. Zhao, Y. Wu, Y. He, Photodeposition of CoOx nanoparticles on BiFeO3 nanodisk for efficiently piezocatalytic degradation of rhodamine B by utilizing ultrasonic vibration energy, Ultrasonics Sonochemistry, 80 (2021) 105813.

[13] X. Yang, F. Ye, Z. Li, X. Liu, J. Chu, B. Xie, L. Ji, P. Hu, J. Wang, J. Du, Largely enhanced Piezoelectric-Fenton capability in rationally designed PVDF/Fe2O3 flexible porous film, Journal of Environmental Chemical Engineering, 12 (2024) 113013.

[14] H. Zeng, C. Yu, C. Liu, M. Tan, Y. Su, L. Qiao, Y. Bai, Boost piezocatalytic H2O2 production in BiFeO3 by defect engineering enabled dual-channel reaction, Materials Today Energy, 39 (2024) 101475.

[15] V.-T. Tran, D.-H. Chen, Ag2O@ BiFeO3 heterostructure composite coupling built-in electric field with piezopotential for enhanced photocatalytic pollutant degradation and photoelectrochemical water splitting, Applied Surface Science, 625 (2023) 157175.

[16] Z. Chen, G. Li, X. Zheng, Y. Liu, J. Dai, B. Huang, M. Xia, L. Yan, Q. Chen, Y. Shen, Facile synthesis of advanced BaTiO3/CuPbSbS3 heterostructure photocatalyst with enhanced piezo-photocatalytic degradation performance, Nano Energy, 124 (2024) 109463.

[17] Q. Liu, D. Zhai, Z. Xiao, C. Tang, Q. Sun, C.R. Bowen, H. Luo, D. Zhang, Piezo-photoelectronic coupling effect of BaTiO3@ TiO2 nanowires for highly concentrated dye degradation, Nano Energy, 92 (2022) 106702.

[18] W. Zheng, Y. Tang, Z. Liu, G. Xing, K. Zhao, Enhanced charge carrier separation by bi-piezoelectric effects based on pine needle-like BaTiO 3/ZnO continuous nanofibers, Journal of Materials Chemistry A, 10 (2022) 13544-13555.

[19] X. Zhou, Q. Sun, D. Zhai, G. Xue, H. Luo, D. Zhang, Excellent catalytic performance of molten-salt-synthesized Bi0.5Na0.5TiO3 nanorods by the piezo-phototronic coupling effect, Nano Energy, 84 (2021) 105936.