Supporting Information

Integrated and sustainable preparation of functional nanocellulose via formic acid/choline chloride solvents pretreatment

Meiyan Wu • Keyu Liao • Chao Liu • Guang Yu • Mehdi Rahmaninia • Haiming Li • Bin Li

Meiyan Wu • Keyu Liao • Chao Liu • Guang Yu • Bin Li ()

CAS Key Laboratory of Biofuels, Qingdao Institute of Bioenergy and Bioprocess Technology, Chinese Academy of Sciences, Qingdao, Shandong, 266101, China

Tel: +86-532-80662725, Fax: +86-532-80662725, Postal address: No. 189 Songling Road, Qingdao, Shandong 266101, China. E-mail: libin@qibebt.ac.cn (B. Li)

Keyu Liao • Haiming Li ()

School of Light Industry and Chemical Engineering, Dalian Polytechnic University, Dalian, Liaoning, 116034, China

E-mail: charley1114@163.com (H. Li)

Meiyan Wu • Chao Liu

Key Laboratory of Pulp and Paper Science & Technology of Ministry of Education/Shandong Province, Qilu University of Technology (Shandong Academy of Sciences), Jinan, Shandong, 250353, China

Mehdi Rahmaninia

Wood and Paper Science and Technology Department, Faculty of Natural Resources, Tarbiat Modares University, Noor 46417-76489, Iran

# The first two authors contributed equally.

Including Pages S1-S9, Tables S1 and S2, Figures S1-S13, References.

Tab. S1 Summary of the preparation method of NC using DES pretreatment

| Raw materials | Composition of the DES | Mechanical treatment | Products |
| --- | --- | --- | --- |
| Cotton (Ling et al. 2018; Liu et al. 2017) | ChCl/oxalic acid | Ultrasonication | CNCs |
| Softwood dissolving pulp (Laitinen et al. 2017a) | ChCl/oxalic acid | Microfluidization | CNCs |
| Beached eucalyptus kraft pulp (Yang et al. 2019) | FeCl3-catalyzed ChCl/oxalic acid | - | CNCs |
| Spruce groundwood pulp (Sirvio 2018) | Imidazole/triethylmethylammonium chloride | Homogenization | CNFs |
| Softwood dissolving pulp (Sirvio et al. 2016) | ChCl/oxalic acid, p-toluenesulfonic acid, levulinic acid | Homogenization | CNCs |
| Waste-board/fluting/waste container board (Laitinen et al. 2017b; Suopajarvi et al. 2017) | ChCl/urea | Microfluidization | CNFs |
| Bleached birch pulp (Sirviö et al. 2015) | ChCl/urea | Microfluidization | CNFs |
| Groundwood pulp (Sirviö and Visanko 2017) | Triethylmethylammonium chloride/imidazole | Homogenization | CNFs |
| Bleached kraft birch pulp (Li et al. 2018) | Aminoguanidine hydrochloride/glycerol | Microfluidization | CNFs |
| Bleached kraft birch pulp (Li et al. 2017) | Ammonium thiocyanate/urea or guanidine hydrochloride/urea | Microfluidization | CNFs |
| Softwood dissolving pulp (Sirviö et al. 2019) | Sulfamic acid/urea | Microfluidization | CNFs |
| Softwood dissolving pulp (Selkala et al. 2016) | Urea/LiCl | Microfluidization | CNFs |
| Poplar kraft Pulp (Ma et al. 2019) | ChCl/oxalic acid | Ultrasonication | CNCs/CNFs |
| Ramie fiber (Yu et al. 2019) | ChCl/oxalic acid or ChCl/urea | Ball milling | CNFs |

Note: ChCl-Choline chloride, CNCs-cellulose nanocrystals, CNFs-cellulose nanofibrils.

Tab. S2 List of abbreviations

| Abbreviation | Definition |
| --- | --- |
| F-DES | Formic acid/choline chloride |
| U-DES | Urea/choline chloride |
| MCC | Microcrystalline cellulose |
| U-MCC | Pretreated microcrystalline cellulose with U-DES |
| F-MCC | Pretreated microcrystalline cellulose with F-DES |
| NC | Nanocellulose |
| F-NC | Nanocellulose prepared via F-DES pretreatment plus ball-milling |
| U-NC | Nanocellulose prepared via U-DES pretreatment plus ball-milling |
| CNCs | Cellulose nanocrystals |
| CNFs | Cellulose nanofibrils |
| B-CNCs1/B-CNFs1 | CNCs or CNFs prepared via direct ball-milling for 8 h |
| B-CNCs2/B-CNFs2 | CNCs or CNFs prepared via direct ball-milling for 16 h |
| F-CNCs1/F-CNFs1 | CNCs or CNFs prepared via F-DES pretreatment plus ball-milling for 8 h |
| F-CNCs2/ F-CNFs2 | CNCs or CNFs prepared via F-DES pretreatment plus ball-milling for 16 h |
| U-CNCs1/U-CNFs1 | CNCs or CNFs prepared via U-DES pretreatment plus ball-milling for 8 h |
| U-CNCs2/U-CNFs2 | CNCs or CNFs prepared via U-DES pretreatment plus ball-milling for 16 h |
| U-DES (R1/R2/R3) | Recycled U-DES after the first/second/third cycle |
| F-DES (R1/R2/R3) | Recycled F-DES after the first/second/third cycle |

Fig. S1 Digital images of the prepared U-DES and F-DES

Fig. S2 Digital images of U-MCC and F-MCC after DES pretreatment for 2 h

Fig. S3 Crystallinity index of MCC and the pretreated MCC samples

Fig. S4 The dispersion of MCC after ball milling with different milling time (0.1 wt% in water, standing for 2 h)

Fig. S5 The dispersion of U-MCC after ball milling with different milling time (0.1 wt% in water, standing for 2 h)

Fig. S6 The dispersion of F-MCC after ball milling with different milling time (0.1 wt% in water, standing for 2 h)

Fig. S7 TEM images of the CNCs and CNFs separated from B-NC1, U-NC1 and F-NC1 after ball milling for 8 h

Fig. S8 Diameter distribution and mean diameter (d) of CNCs and CNFs separated from B-NC2, U-NC2 and F-NC2 samples after ball milling for 16 h

Fig. S9 Equivalent volume size of MCC and U-MCC samples after ball milling for different milling time

Fig. S10 Dispersibility of F-NC2 suspension (0.1 wt%) in various solvents (after standing for 3 months)

Fig. S11 DTG curves of MCC and NC samples after ball milling for 16 h

Fig. S12 TEM images and mean diameter (d) of the CNCs and CNFs prepared using the recycled U-DES (R3) and F-DES (R3)

Fig. S13 Diameter distribution of droplets in F-CNCs2 stabilized Pickering emulsions

References

Laitinen O, Ojala J, Sirviö JA, Liimatainen H (2017a) Sustainable stabilization of oil in water emulsions by cellulose nanocrystals synthesized from deep eutectic solvents Cellulose 24:1679-1689 https://doi:10.1007/s10570-017-1226-9

Laitinen O, Suopajarvi T, Osterberg M, Liimatainen H (2017b) Hydrophobic, superabsorbing aerogels from choline chloride-based deep eutectic solvent pretreated and silylated cellulose nanofibrils for selective oil removal ACS Appl Mater Interfaces 9:25029-25037 https://doi:10.1021/acsami.7b06304

Li P, Sirvio JA, Asante B, Liimatainen H (2018) Recyclable deep eutectic solvent for the production of cationic nanocelluloses Carbohydr Polym 199:219-227 https://doi:10.1016/j.carbpol.2018.07.024

Li P, Sirvio JA, Haapala A, Liimatainen H (2017) Cellulose nanofibrils from nonderivatizing urea-based deep eutectic solvent pretreatments ACS Appl Mater Interfaces 9:2846-2855 https://doi:10.1021/acsami.6b13625

Ling Z, Edwards JV, Guo Z, Prevost NT, Nam S, Wu Q, French AD, Xu F (2018) Structural variations of cotton cellulose nanocrystals from deep eutectic solvent treatment: Micro and nano scale Cellulose 26:861-876 https://doi:10.1007/s10570-018-2092-9

Liu Y, Guo B, Xia Q, Meng J, Chen W, Liu S, Wang Q, Liu Y, Li J, Yu H (2017) Efficient cleavage of strong hydrogen bonds in cotton by deep eutectic solvents and facile fabrication of cellulose nanocrystals in high yields ACS Sustain Chem Eng 5:7623-7631 https://doi:10.1021/acssuschemeng.7b00954

Ma Y, Xia Q, Liu Y, Chen W, Liu S, Wang Q, Liu Y, Li J, Yu H (2019) Production of nanocellulose using hydrated deep eutectic solvent combined with ultrasonic treatment ACS omega 4:8539-8547 https://doi:10.1021/acsomega.9b00519

Selkala T, Sirvio JA, Lorite GS, Liimatainen H (2016) Anionically stabilized cellulose nanofibrils through succinylation pretreatment in urea-lithium chloride deep eutectic solvent ChemSusChem 9:3074-3083 https://doi:10.1002/cssc.201600903

Sirviö JA, Ukkola J, Liimatainen H (2019) Direct sulfation of cellulose fibers using a reactive deep eutectic solvent to produce highly charged cellulose nanofibers Cellulose 26:2303-2316 https://doi:10.1007/s10570-019-02257-8

Sirviö JA, Visanko M (2017) Anionic wood nanofibers produced from unbleached mechanical pulp by highly efficient chemical modification J Mater Chem A 5:21828-21835 https://doi:10.1039/c7ta05668k

Sirviö JA, Visanko M, Liimatainen H (2015) Deep eutectic solvent system based on choline chloride-urea as a pre-treatment for nanofibrillation of wood cellulose Green Chemistry 17:3401-3406 https://doi:10.1039/c5gc00398a

Sirvio JA (2018) Cationization of lignocellulosic fibers with betaine in deep eutectic solvent: Facile route to charge stabilized cellulose and wood nanofibers Carbohydr Polym 198:34-40 https://doi:10.1016/j.carbpol.2018.06.051

Sirvio JA, Visanko M, Liimatainen H (2016) Acidic deep eutectic solvents as hydrolytic media for cellulose nanocrystal production Biomacromolecules 17:3025-3032 https://doi:10.1021/acs.biomac.6b00910

Suopajarvi T, Sirvio JA, Liimatainen H (2017) Nanofibrillation of deep eutectic solvent-treated paper and board cellulose pulps Carbohydr Polym 169:167-175 https://doi:10.1016/j.carbpol.2017.04.009

Yang X, Xie H, Du H, Zhang X, Zou Z, Zou Y, Liu W, Lan H, Zhang X, Si C (2019) Facile extraction of thermally stable and dispersible cellulose nanocrystals with high yield via a green and recyclable FeCl3-catalyzed deep eutectic solvent system ACS Sustain Chem Eng 7:7200-7208 https://doi:10.1021/acssuschemeng.9b00209

Yu W, Wang C, Yi Y, Zhou W, Wang H, Yang Y, Tan Z (2019) Choline chloride-based deep eutectic solvent systems as a pretreatment for nanofibrillation of ramie fibers Cellulose 26:3069-3082 https://doi:10.1007/s10570-019-02290-7