# Synthesis and self-assembly of a novel block copolymer poly(N-vinylcaprolactam)-b-poly(3-hydroxybutyrate-co-3-hydroxyvalerate) (PNVCL-b-PHBHV) by the combination of RAFT/MADIX and click chemistry techniques

Rodolfo Minto de Moraes*, Layde Teixeira de Carvalho, Gizelda Maria Alves, Simone de Fátima Medeiros, Amilton Martins dos Santos

Engineering School of Lorena, University of São Paulo, EEL-USP, Laboratory of Polymers, Department of Chemical Engineering, Estrada Municipal do Campinho, 100, 12602-810, Lorena, SP, Brazil.

* Correspondence: rodolfommoraes@hotmail.com

Supporting Information

Table S1 Monitoring of Mn SEC and Đ of alkyne-PHBHV during the transesterification reaction of PHBHV with propargyl alcohol: ReT(1) reaction

| ReT(1) |  |  |
| --- | --- | --- |
| t (h) | Mn SEC a (g.mol-1) | Đ a |
| 0 | 114873 | 2.86 |
| 2 | 22461 | 2.49 |
| 4 | 11682 | 2.17 |
| 6 | 8412 | 1.83 |
| 8 | 5855 | 1.76 |
| 10 | 4736 | 1.64 |
| 12 | 4049 | 1.54 |

a Determined by SEC in chloroform

Fig. S1 Plots of (a) reaction time vs monomer conversion, and (b) number-average molar mass (Mn) and dispersity (Ð) vs monomer conversion in the RAFT/MADIX polymerization of NVCL in 1.4-dioxane using [NVCL]:[CTA]:[AIBN] molar ratio = 300:1:0.25 at 70 °C. The Mn and Đ values were determined by HPLC in THF and TEA (3% v/v).

Fig. S2 SEC chromatogram of PNVCL-N3 (1)

Fig. S3 SEC chromatogram of (a) alkyne-PHBHV (1) and (b) alkyne-PHBHV (2)