Supporting Information

Design and catalytic performance of a novel 2D copper MOF for green synthesis of tetrahydrobenzo[b]pyrans

Ehsan Joukar Bahaderania, Khosro Mohammadi*a, Payam Hayati*b, Jan Janczakc

a Chemistry Department, Faculty of Nano and Bio Sciences and Technology, Persian Gulf University, Bushehr 75169, Iran

b Department of Biotechnology and Life Sciences, University of Insubria, Via Jean Henry Dunant, 3, 21100 Varese, Italy

c Institute of Low Temperature and Structure Research, Polish Academy of Sciences, P. O. Box 1410, Okólna 2 Str., 50-422 Wroclaw, Poland

Email: khmohammadi@pgu.ac.ir; khmohammadi@yahoo.com

Table S1. Crystallographic data for (1).

| Compound | [Cu(H2O)(m-PO3CH2C6H4CO2H)]n (1) |
| --- | --- |
| Chemical formula | C8H9CuO6P |
| Mr | 295.66 |
| Crystal system, space group | Monoclinic, P21/n |
| Temperature (K) | 295(2) |
| a, b, c (Å) | 5.7362 (5), 4.7509 (4), 34.635 (3) |
| β (°) | 92.327 (7) |
| V (Å3) | 943.09 (14) |
| Z | 4 |
| Dcalc (g·cm–3) | 2.082 |
| Radiation type, wavelength, λ (Å) | Mo Kα , 0.71073 |
| µ (mm−1) | 2.50 |
| F(000) | 596 |
| Crystal size (mm) | 0.24 × 0.20 × 0.15 |
| Tmin, Tmax | 0.794, 1.000 |
| θ range(°) | 3.5-27.4 |
| Absorption correction | multi-scan |
| Reflections collected / unique / observed | 26181, 2167, 1913 |
| Rint | 0.064 |
| Refinement on | F2 |
| R[F2 > 2σ(F2)] | 0.0745 |
| wR(F2 all reflections) | 0.1655 |
| Goodness-of-fit, S | 1.001 |
| Δρmax, Δρmin (e Å−3) | +1.442, -0.844 |

wR={Σ [w(Fo2–Fc2)2]/ΣwFo4}½; w = 1/[σ2(Fo2) + (0.0549P)2 + 16.5039P] where P = (Fo2 + 2Fc2)/3

Figure S1

Figure S1. IR spectrum of nanoparticle (1′).

Figure S2

Figure S2. TGA/DTA of nanoparticle (1′).