Effects of Crystal Defects on the Electronic and Magnetic properties of Bulk and 2D monolayer MoS2: A Density Functional Theoretical study

aOlha Shyiko, aVenkateswara Rao Penugonda, bPeter Nattaniel Nelson*

aDepartment of Physics, The University of the West Indies Mona, Kingston 7, St. Andrew, Jamaica

bDepartment of Chemistry, The University of the West Indies Mona, Kingston 7, St. Andrew, Jamaica

Supporting Information

# Table S1. Formulae for calculating defect formation energies.

| Type of defect | Formation energy formula |
| --- | --- |
| MoV Mo-rich | Eform=Edef-EMoS2+μMo+qEF+Ecorr |
| MoV S-rich | Eform=Edef-EMoS2+μMo+∆μMo+qEF+Ecorr |
| SV Mo-rich | Eform=Edef-EMoS2+μS+∆μS+qEF+Ecorr |
| SV S-rich | Eform=Edef-EMoS2+μS+qEF+Ecorr |
| MoS Mo-rich | Eform=Edef-EMoS2+μS+∆μS-μMo+qEF+Ecorr |
| MoS S-rich | Eform=Edef-EMoS2+μS-μMo+qEF+Ecorr |
| SMo Mo-rich | Eform=Edef-EMoS2+μMo-μS+qEF+Ecorr |
| SMo S-rich | Eform=Edef-EMoS2+μMo+∆μMo-μS+qEF+Ecorr |
| Sinter Mo-rich | Eform=Edef-EMoS2-μS+∆μS+qEF+Ecorr |
| Sinter S-rich | Eform=Edef-EMoS2-μS+qEF+Ecorr |
| Mointer Mo-rich | Eform=Edef-EMoS2-μMo+qEF+Ecorr |
| Sinter S-rich | Eform=Edef-EMoS2-μMo+∆μMo+qEF+Ecorr |

Where μMo and μS are chemical potentials of isolated Mo and S respectively. To calculate these chemical potentials, consideration was given to stable cubic structure of Mo with 2 atoms, and stable α structure of S, which consists of 16 S clusters each having 8 atoms of S. For Mo-rich case, ∆μMo=0, ∆μS=∆Hf(MoS2)/2. For S-rich case ∆μMo=∆Hf(MoS2) and ∆μS=0. The energy needed to form monolayer MoS2, ∆Hf(MoS2) ,is calculated as:

∆HfMoS2=Etot(MoS2)unit formula-EtotMonumber of atoms-2×Etot(S)number of atoms

Where Etot(MoS2) is the total energy of unit cell monolayer MoS2 obtained from SCF calculations, EtotMo EtotS and are the total energies of unit cell Mo  and S respectively obtained from SCF calculations.

# Table S2. Calculated defect formation energies.

| Type of defect | Charge state | Formation energy of defect with correction term included for Mo-rich condition, eV |  | Formation energy of defect with correction term included for S-rich condition, eV | Correction term, eV |
| --- | --- | --- | --- | --- | --- |
| Vacancy S | -1 | 2.67 |  | 4.30 | -1.15 |
|  | 0 | 1.32 |  | 2.95 | 0.00 |
|  | 1 | 4.03 |  | 5.66 | -1.19 |
|  | 2 | 10.87 |  | 12.50 | -4.79 |
| Vacancy Mo | -3 | 4.55 |  | 1.29 | -10.70 |
|  | -2 | 7.53 |  | 4.27 | -4.99 |
|  | -1 | 8.68 |  | 5.42 | -1.15 |
|  | 0 | 7.89 |  | 4.63 | 0.00 |
|  | 1 | 10.70 |  | 7.44 | -0.91 |
| Mo in S | 0 | 3.96 |  | 8.85 | 0.00 |
|  | 1 | 5.59 |  | 10.48 | -1.08 |
|  | 2 | 11.61 |  | 16.50 | -4.47 |
|  | 3 | 22.24 |  | 27.12 | -10.17 |
| S in Mo | -2 | 9.49 |  | 4.61 | -4.67 |
|  | -1 | 10.07 |  | 5.18 | -1.23 |
|  | 0 | 9.04 |  | 4.15 | 0.00 |
|  | 1 | 11.71 |  | 6.83 | -0.92 |
|  | 2 | 18.78 |  | 13.90 | -4.03 |
| Mo interstitial | -2 | 4.63 |  | 7.89 | -4.63 |
|  | -1 | 4.91 |  | 8.16 | -1.17 |
|  | 0 | 3.31 |  | 6.57 | 0.00 |
|  | 1 | 5.45 |  | 8.71 | -1.11 |
|  | 2 | 8.81 |  | 12.06 | -7.41 |
|  | 3 | 17.70 |  | 20.96 | -14.69 |
| S interstitial | -2 | 5.16 |  | 3.53 | -4.31 |
|  | -1 | 5.45 |  | 3.82 | -1.06 |
|  | 0 | 4.32 |  | 2.69 | 0.00 |
|  | 1 | 6.41 |  | 4.78 | -1.17 |
|  | 2 | 12.51 |  | 10.88 | -4.55 |
| V in Mo | -2 | 0.35 |  | -2.90 | -4.49 |
|  | -1 | 1.05 |  | -2.21 | -1.14 |
|  | 0 | 0.42 |  | -2.83 | 0.00 |
|  | 1 | 3.30 |  | 0.04 | -1.10 |
|  | 2 | 10.41 |  | 7.16 | -4.45 |
|  | 3 | 21.87 |  | 18.62 | -10.03 |
| V in S | -1 | 4.13 |  | 5.76 | -1.20 |

Table S2 Continued

| Type of defect | Charge state | Formation energy of defect with correction term included for Mo-rich condition, eV | Formation energy of defect with correction term included for S-rich condition, eV | Correction term, eV |
| --- | --- | --- | --- | --- |
|  | 0 | 2.63 | 4.26 | 0.00 |
|  | 1 | 4.21 | 5.84 | -1.12 |
|  | 2 | 10.75 | 12.38 | -4.57 |
|  | 3 | 21.45 | 23.08 | -10.34 |
| V interstitial 1 | -2 | 3.47 | 3.47 | -4.41 |
|  | -1 | 3.92 | 3.92 | -1.08 |
|  | 0 | 2.78 | 2.78 | 0.00 |
|  | 1 | 4.98 | 4.98 | -1.16 |
|  | 2 | 11.38 | 11.38 | -4.57 |
|  | 3 | 22.05 | 22.05 | -10.22 |
| V interstitial 2 | -2 | 4.42 | 4.43 | -4.76 |
|  | -1 | 4.77 | 4.77 | -1.22 |
|  | 0 | 3.37 | 3.37 | 0.00 |
|  | 1 | 4.77 | 4.77 | -1.08 |
|  | 2 | 10.39 | 10.39 | -4.47 |
|  | 3 | 20.14 | 20.14 | -10.17 |
|  | 0 | 2.63 | 4.26 | 0.00 |

# S3

PDOS of substitutional defect Mo in position of S with the contribution of Mo and S atomic orbitals.

# S4

PDOS of S interstitial defect with the contribution of Mo and S atomic orbitals.

# S5

PDOS of substitutional defect V in position of S with the contribution from Mo, S and V atomic orbitals.

# S6

PDOS of substitutional defect V in position of Mo with the contribution from Mo, S and V atomic orbitals.

# S7

PDOS of V interstitial defect in atomic position #2 with the contribution from Mo, S and V atomic orbitals.

# S8

TDOS of Mo and S vacancies: (a) divacancy of Mo (b) three vacancies of Mo (c) divacancy of S (d) three vacancies of S

# S9

PDOS of Mo vacancies with the contribution from Mo and S atomic orbitals: (a) divacancy (b) three vacancies.