Supporting information

Extrapolative-machine-learning-guided discovery of multi-elemental heterogeneous catalysts for low-temperature NO reduction by H2

Yuan Jing,1† Chenyang Zhang,1† Shinya Mine,2† Xiupeng Zhang,1 Chenxi He,1 Ningqiang Zhang,1 Xu Guo,1 Akihiko Anzai,1 Kohei Oka,3 Ryo Toyoshima,4 Hiroshi Kondoh,5 Ichigaku Takigawa,*6,7

Ken-ichi Shimizu,*1 Takashi Toyao*1

1 Institute for Catalysis, Hokkaido University, N-21, W-10, Sapporo 001-0021, Japan

2 Research Institute for Chemical Process Technology, National Institute of Advanced Industrial Science and Technology (AIST), 4-2-1 Nigatake, Miyagino-ku, Sendai 983-8551, Japan

3 Isuzu Advanced Engineering Center, Ltd., 8 Tsuchidana, Fujisawa 252-0881, Japan

4 Department of Materials Engineering, The University of Tokyo, Bunkyo, Tokyo 113-8656, Japan

5 Department of Chemistry, Keio University, 3-14-1 Hiyoshi, Kohoku-ku, Yokohama 223-8522, Japan

6 Center for Innovative Research and Education in Data Science (CIREDS), Institute for Liberal Arts and Scieneces, Kyoto University, Kyoto 606-8315, Japan

7 Institute for Chemical Reaction Design and Discovery (WPI-ICReDD), Hokkaido University, N-21, W-10, Sapporo 001-0021, Japan

†These authors contributed equally to this work.

Table S1. Sources and purity of chemicals used to prepare catalysts.

| AN | Symbol | Chemical formula | Purity/concentration | Company name |
| --- | --- | --- | --- | --- |
| 3 | Li | LiNO3 | 99.99% | Kanto Chemical |
| 11 | Na | NaNO3 | 99.99% | Aldrich |
| 12 | Mg | Mg(NO3)2 | 99.99% | Kanto Chemical |
| 13 | Al | Al(NO3)3・9H2O | 99.99% | Wako Chemical |
| 14 | Si | Si(OCH2CH3)4 | 97% | Tokyo Chemical Industry |
| 15 | P | (NH4)2HPO4 | 99% | Wako Chemical |
| 16 | S | NH4HSO4 | 99.99% | Wako Chemical |
| 19 | K | KNO3 | 99.99% | Wako Chemical |
| 20 | Ca | Ca(NO3)2・4H2O | 98.5% | Wako Chemical |
| 21 | Sc | Sc(OOCCH3)3・nH2O | 98% | Tokyo Chemical Industry |
| 22 | Ti | C4H10N2O10Ti | 99.99% | Alfa Aesar |
| 23 | V | NH4VO3 | 99.99% | Wako Chemical |
| 24 | Cr | Cr(NO3)3・9H2O | 98.5% | Aldrich |
| 25 | Mn | Mn(NO3)2・6H2O | 99.99% | Wako Chemical |
| 26 | Fe | Fe(NO3)3・9H2O | 98% | Aldrich |
| 27 | Co | Co(NO3)2・6H2O | 99.99% | Wako Chemical |
| 28 | Ni | Ni(NO3)2・6H2O | 98% | Wako Chemical |
| 29 | Cu | Cu(NO3)2・3H2O | 99.99% | Aldrich |
| 30 | Zn | Zn(NO3)2・6H2O | 99.99% | Kanto Chemical |
| 31 | Ga | Ga(NO3)3・8H2O | 99.99% | Wako Chemical |
| 32 | Ge | (NH4)2GeF6 | 99.99% | Wako Chemical |
| 34 | Se | H2SeO3 | 97% | Wako Chemical |
| 37 | Rb | RbNO3 | 99.99% | Wako Chemical |
| 38 | Sr | Sr(NO3)2 | 98% | Kanto Chemical |
| 39 | Y | Y(NO3)3・6H2O | 99.99% | Mitsuwa Chemical |
| 40 | Zr | Zr(NO3)2O・2H2O | 99.99% | Mitsuwa Chemical |
| 41 | Nb | Nb(HC2O4)5・5H2O | 95% | Mitsuwa Chemical |
| 42 | Mo | (NH4)6Mo7O24・4H2O | 99.99% | Wako Chemical |
| 44 | Ru | Ru(NO)(NO3)3 | 1.5 wt% Ru aqueous solution | Strem Chemical |
| 45 | Rh | Rh(NO3)3 | 50 g/L Rh aqueous solution | Tanaka Chemical |
| 46 | Pd | Pd(NH3)2(NO2)2 | 50.5 g/L Pd aqueous solution | Kojima Chemical |
| 47 | Ag | AgNO3 | 99.99% | Wako Chemical |
| 48 | Cd | Cd(NO3)2・4H2O | 99% | Aldrich |
| 49 | In | In(NO3)3・3H2O | 99.99% | Kanto Chemical |
| 50 | Sn | SnCl2 | 99.99% | Kishida Chemical |
| 51 | Sb | Sb(OOCCH3)3 | 99.99% | Aldrich |
| 52 | Te | H6TeO6 | 99% | Mitsuwa Chemical |
| 53 | I | HIO3 | 99.5% | Aldrich |
| 55 | Cs | CsNO3 | 99.99% | Wako Chemical |
| 56 | Ba | Ba(NO3)2 | 99.99% | Kanto Chemical |
| 57 | La | La(NO3)3・6H2O | 99.99% | Mitsuwa Chemical |
| 58 | Ce | Ce(NO3)3・6H2O | 99.99% | Wako Chemical |
| 59 | Pr | Pr(NO3)3・6H2O | 99.99% | Aldrich |
| 60 | Nd | Nd(NO3)3・6H2O | 99.5% | Wako Chemical |
| 62 | Sm | Sm(NO3)3・6H2O | 99.5% | Mitsuwa Chemical |
| 63 | Eu | Eu(NO3)3・6H2O | 99.99% | Alfa Aesar |
| 64 | Gd | Gd(NO3)3・6H2O | 99.5% | Wako Chemical |
| 65 | Tb | Tb(NO3)3・6H2O | 99.9% | Strem Chemicals |
| 66 | Dy | Dy(NO3)3・6H2O | 99.5% | Wako Chemical |
| 67 | Ho | Ho(NO3)3・nH2O | 99.5% | Wako Chemical |
| 68 | Er | Er(NO3)3・nH2O | 99.99% | Wako Chemical |
| 69 | Tm | Tm(NO3)3・5H2O | 99.99% | Mitsuwa Chemical |
| 70 | Yb | Yb(NO3)3・nH2O | 99.99% | Wako Chemical |
| 71 | Lu | Lu(NO3)3・nH2O | 99.99% | Wako Chemical |
| 72 | Hf | HfCl4 | 99.5% | Wako Chemical |
| 73 | Ta | TaCl5 | 99.8% | Aldrich |
| 74 | W | (NH4)10W12O41・5H2O | 99.99% | Wako Chemical |
| 75 | Re | NH4ReO4 | 99.99% | Aldrich |
| 77 | Ir | IrCl3・3H2O | 99.99% | Kanto Chemical |
| 78 | Pt | Pt(NH3)(NO2)2 | 50 g/L Pt aqueous solution | Tanaka Chemical |
| 79 | Au | HAuCl14・4H2O | 27.8 g/L Au aqueous solution | Wako Chemical |
| 82 | Pb | Pb(NO3)2 | 99.99% | Wako Chemical |
| 83 | Bi | Bi(NO3)3・5H2O | 99.99% | Wako Chemical |

Table S2. Sources and purity of chemicals used to prepare catalysts.

| Support name | SBETa (m2/g) | SBETb (m2/g) | Company name | Code name | Comment |
| --- | --- | --- | --- | --- | --- |
| g-Al2O3 | 142 | 162 | Sasol | Puralox | Gamma phase |
| Al2O3_AKP-G07 | 80 | 91 | Sumitomo Chemical | AKP-G07 | Theta phase |
| TiO2_P25 | 43 | 41 | Evonik (formerly Degussa) | P25 | Anatase + rutile |
| SiO2 | 332 | 300 | Fuji Silysia Chemical | CARiACT Q-10 |  |
| ZrO2_JRC3_RC-100 | 113 | 42 | Daiichi Kigenso Kagaku Kogyo | RC-100 (JRC-ZRO-3) | Tetragonal + monoclinic |
| ZrO2_JRC4_EP | 33 | 33 | Daiichi Kigenso Kagaku Kogyo | EP (JRC-ZRO-4) | Tetragonal + monoclinic |
| CeO2_JRC2 | 78 | 85 | Daiichi Kigenso Kagaku Kogyo | Type A (JRC-CEO-2) |  |
| Nb2O5 | 76 | 10 | Companhia Brasileira de Metalurgia e Mineração | HY-340 | Prepared by calcining (500 °C for 3 h) niobic acid (Nb2O5∙nH2O, HY-340) |
| Co3O4 | 41 | 3 | US Research Nanomaterials |  | >99.5%, 30–50 nm |
| MgO | 94 | 36 | Ube Material Industries | 500A (JRC-MGO-4 500A) |  |
| CeO2(50%)-ZrO2 | 56 | 53 | Daiichi Kigenso Kagaku Kogyo | Z-1119 | CeO2 = 50 wt.% |
| SiO2-Al2O3_JRC-SAL-6 | 718 | 533 | Nikki-Shokubai Kasei | JRC-SAL-6 | Al2O3 = 13 wt.% |
| SiO2-Al2O3_JRC-SAH-7 | 568 | 492 | Nikki-Shokubai Kasei | JRC-SAH-7 | Al2O3 = 28 wt.% |
| H-ZSM-5_11 | 402 | 340 | Tosoh | HSZ-820NHA (JRC-Z-HM20) | Si/Al ratio = 11.5 |
| H-ZSM-5_45 | 411 | 375 | Clariant | JRC-Z-HM90 | Si/Al ratio = 45 |
| H-Y_15 | 785 | 786 | Tosoh | HSZ-372HUA | Si/Al ratio = 15 |
| H-BEA_20 | 556 | 631 | Tosoh | HSZ-940HOA | Si/Al ratio = 20 |
| H-MOR_10 | 521 | 433 | Tosoh | JRC-Z-HM20 | Si/Al ratio = 10 |
| H-CHA_11 | 707 | 207 | Tosoh |  | Si/Al ratio = 11 |

N2 adsorption was performed after pretreatment at 300 °C for 1 h under vacuum. a as received/prepared. b measured after calcination 700 °C for 1 h.

Table S3. Descriptors used in ML-based catalyst exploration and statistical analysis.a

| Type | Descriptors |
| --- | --- |
| PGM | ・Electronegativity according to the Allred’s definition (EN(Allred)) ・Group ・Melting point (m.p.) ・Electron affinity (EA) ・Adsorption energy of H2 on metallic surfaces (Eads(H2)) |
| Add | ・ Electronegativity according to the Allen’s definition (EN(Allen)) ・ Thermal expansion (Therm. exp.) ・ Group ・ Oxidation number of the precursor (metal) salt used for catalyst preparation (Prec. ox. num.) ・ Density in the most stable oxide form (Density oxide) ・ Enthalpy of formation (∆Hfus) ・ Thermal conductivity (Therm. Cond.) ・ Atomic radius (Atom. rad.) ・ Adsorption energy of an O atom on metallic surfaces (Eads(O)) |
| Support | ・ Band gap energy (Eband gap) ・ Formation energy (Eform) ・ SBET for the support materials calcined at 700 °C for 3 h in the air (SSA@700 °C) ・ Peak intensities around 1550–1540 cm−1, corresponding to Brønsted acid sites, observed during pyridine adsorption IR measurements for samples calcined at 700 °C (IR B-acid intensity (@700 °C)) ・ Wavenumber values around 1550-1540 cm−1 observed during pyridine adsorption IR measurements of samples calcined at 700 °C (IR B-acid cm−1 (@700 °C)) ・ Eads of H2 (Eads(H2)) |

a Descriptors for PGMs shown in this table were used for the initial catalyst exploration (prediction of catalysts tested at iteration = 1), whereas descriptors for Add and Support shown in this table were used in the post-analysis of the final dataset, consisting of 425 points.

Figure S1. Correlation map for the five selected descriptors for the PGM elements.

Figure S2. Correlation map for the nine selected descriptors for the Additive elements.

Figure S3. Correlation map for the six selected descriptors for the Supports.

Scheme S1. Schematic representation of ML-assisted H2-SCR catalysts discovery.

Figure S4. Visualization of the number PGMs, additives, and supports appeared for the first time in each iteration. Elements/supports appearing for the first time are shown in color, while those already present are shown in gray. The numbers above indicate the total count of elements/supports present at each iteration, while the numbers in parentheses below represent the count of elements/supports appeared for the first time in that iteration.

Figure S5. Comparison of prediction accuracy (RMSE, MSE, MAE, and R2) at each iteration for the H2-SCR activity (average N2 yield in the temperature range between 50–150 °C) using ML models based on 27 types of descriptor representation.

Supplementary text for ML-based analysis on the final dataset (425 datapoints) and comparison of the ML model

For hyperparameter tuning, we tested a reasonable range of candidate values in an exhaustive way (grid search) shown in Table S4, chose the best hyperparameter by 10-fold cross validation (CV) on the training set, and used the model for calculating the predicted values for the test set (the hyperparameters not explicitly indicated in the table were set to the scikit-learn defaults). Namely, to avoid data leakage, we strictly followed a standard practice of "nested" CV, also known as double CV, to estimate the prediction accuracies; we used 5-fold CV for the internal CV, and used Monte Carlo CV (also known as repeated random subsampling CV) with 100-times of random leave-20%-out trials for the external CV to increase the statistical reliability for validating the test prediction accuracies with fixing the number of training data.

In addition to our base ML model, Extra-Trees regression (ETR)1, five well-established ML models were used: least absolute shrinkage and selection operator regression (Lasso)2, ridge regression (Ridge)3, Gaussian process regression (GPR)4, support vector regression (SVR)5, and random forest regression (RFR)6. Two of these methods involve linear regression methods (Lasso, Ridge), and the other four methods including ETR involve nonlinear regression methods. More specifically, two kernel methods (GPR, SVR) and two types of decision tree ensemble methods (RFR, ETR). Among the ML models tested, the ETR combined with the 012 descriptor representation gave the best prediction accuracy to predict the average N2 yield in the temperature range between 50-150 °C of the 425 H2-SCR catalysts (Figures S6-8).

Table S4. Ranges used in the hyperparameter searches for the ML methods (if not specified, the default values of scikit-learn were used).

| Type |  | Method | Hyperparameters [Tested range] |
| --- | --- | --- | --- |
| Linear |  | Lasso | alpha ∈ [10-2,10-1,1.0,101,102] |
|  |  | Ridge | alpha ∈ [10-2,10-1,1.0,101,102] |
| Nonlinear | Kernel methods | GPR | kernel=Matern 2.5, alpha ∈ [1, 10-1, 10-2, 10-3, 10-4, 10-5], n_restarts_optimizer = 10, normalize_y = True |
|  |  | SVR | kernel=’rbf’, C ∈ [1.0,10,102,…, 105], gamma ∈ [1, 10-1, 10-2, 10-3, 10-4, 10-5], epsilon ∈ [10-2,10-1,1.0,101,102] |
|  | Tree ensemble methods | RFR | n_estimators ∈ [100, 500, 1000, 1500], bootstrap ∈ [True or False] |
|  |  | ETR | n_estimators ∈ [100, 500, 1000, 1500], bootstrap ∈ [True or False] |

Figure S6. Comparison of the prediction accuracy for the average N2 yield in the temperature range between 50–150 °C of the 425 H2-SCR catalysts using ML models based on the best descriptor representation (012).

Figure S7. Effect of the descriptor representation on the prediction accuracy for the average N2 yield in the temperature range between 50–150 °C of the 425 H2-SCR catalysts. The three numbers in each bar graph represent the descriptor representations for PGM, Additive, and Support, respectively, from left to right. 0 represents a direct input representation, which uses only elemental compositions or support name; 1 represents an exploitative representation, which uses both elemental compositions/support name and elemental/support properties; and 2 represents an explorative representation, which uses only elemental/support properties.

Figure S8.  Experimental and predicted values of the average N2 yield in the temperature range between 50–150 °C of the 425 H2-SCR catalysts. Cross validation was performed using ETR combined with the best descriptor representation (012). (A) 90%/10% training-test error plots and (B) 100% test error plots. Blue points represent training data, while red points represent test data. Numbers in the right Fig. correspond to the catalyst ID.

Figure S9. Visualization of H2-SCR catalyst datasets. Boxplots for each PGM, Additive, and Support component. The boxes represent the interquartile range, spanning from the first quartile to the third quartile, with a horizontal line indicating the median. Whiskers extend up to 1.5 times the interquartile range, encompassing the largest and smallest observed data points falling within this range. Individual data points are displayed as dots.

Figure S10. Effects of the loading amount of PGM elements on the average N2 yield in the temperature range between 50–150 °C in the H2-SCR reaction.

Figure S11. Effects of the loading amount of Additive elements on the average N2 yield in the temperature range between 50–150 °C in the H2-SCR reaction.

Figure S12. Correlation between the average N2 yield in the temperature range between 50–150 °C and each descriptor value for the Additive elements.

Figure S13. Correlation between the average N2 yield in the temperature range between 50–150 °C and each descriptor value for the Supports.

Figure S14. H2-SCR reaction over Pt(1.3)-Ir(0.2)/Ba(1.5)-Co(1)/H-ZSM-5(11) and related catalysts for comparison. Catalyst weight: 15 mg; total flow rate: 100 mL/min; heating rate: 1 °C/min; Gas composition: 0.1% NO, 0.6% H2, 6% O2, 1% H2O, 5% CO2, He balance. The reaction was initiated at 50 °C and ramped to 200 °C at a rate of 1 °C/min after conditioning at 300 °C for 30 min under the reaction atmosphere.

Figure S15. H2-SCR reaction over Pt(1.3)-Ir(0.2)/Ba(1.5)-Co(1)/H-ZSM-5(11) and related catalysts for comparison. Catalyst weight: 15 mg; total flow rate: 100 mL/min; heating rate: 1 °C/min; Gas composition: 0.1% NO, 0.6% H2, 6% O2, 1% H2O, 5% CO2, He balance. The reaction was initiated at 50 °C and ramped to 200 °C at a rate of 1 °C/min after conditioning at 300 °C for 30 minutes under the reaction atmosphere.

Figure S16.  Correlation of the average NO conversion, H2 conversion, N2 yield, N2O yield, NH3 yield, NO2 yield, and N2 selectivity in the temperature range between 50–150 °C of the 425 H2-SCR catalysts.

Figure S17.  Correlation of the (average) N2 yield in the different temperature range of the 425 H2-SCR catalysts.

Figure S18. XRD patterns of Pt(1.3)-Ir(0.2)/Ba(1.5)-Co(1)/H-ZSM-5(11) and related catalysts for comparison.

Figure S19. (a) Particle size distribution obtained from the HADDF-STEM images and the STEM EDX-spectrum of Pt(1.3)-Ir(0.2)/Ba(1.5)-Co(1)/H-ZSM-5(11).

Table S5. Results of the curve-fitting analysis of Pt L3-edge EXAFS spectra of Pt(1.3)-Ir(0.2)/Ba(1.5)-Co(1)/H-ZSM-5(11).

| Sample | shell | CNa | R (Å) b | σ2 (Å2) c | R (%) d |
| --- | --- | --- | --- | --- | --- |
| Pt foil | Pt–Pt | 12 (fixed) | 2.77 | 0.004 | 0.1 |
| Pt(1.3)-Ir(0.2)/Ba(1.5)-Co(1)/H-ZSM-5(11) | Pt–Pt | 11.8 | 2.75 | 0.006 | 0.2 |

a Coordination number. b Bond distance. c Debye-Waller factor. d Residual factor.

Table S6. Results of the curve-fitting analysis of Ba K-edge EXAFS spectra of Pt(1.3)-Ir(0.2)/Ba(1.5)-Co(1)/H-ZSM-5(11).

| Sample | shell | CNa | R (Å) b | σ2 (Å2) c | R (%) d |
| --- | --- | --- | --- | --- | --- |
| BaO | Ba–O | 6 (fixed) | 2.80 | 0.014 | 3.2 |
| Pt(1.3)-Ir(0.2)/Ba(1.5)-Co(1)/H-ZSM-5(11) | Ba–O | 3.8 | 2.76 | 0.014 | 2.4 |

a Coordination number. b Bond distance. c Debye-Waller factor. d Residual factor.

Table S6. Results of the curve-fitting analysis of Co K-edge EXAFS spectra of Pt(1.3)-Ir(0.2)/Ba(1.5)-Co(1)/H-ZSM-5(11).

| Sample | shell | CN | R(A) | σ2 (Å2) c | R / % |
| --- | --- | --- | --- | --- | --- |
| Co3O4 | Co–O | 4 (fixed) | 1.92 | 0.003 | 2.3 |
| Pt(1.3)-Ir(0.2)/Ba(1.5)-Co(1)/H-ZSM-5(11) | Co–O | 5.7 | 2.07 | 0.011 | 0.4 |

a Coordination number. b Bond distance. c Debye-Waller factor. d Residual factor.

1

Figure S20. (a) Experimental conditions during AP-XPS studies. (b) Co 2p and (c) N 1s AP-XPS spectra of Pt(1.3)-Ir(0.2)/Ba(1.5)-Co(1)/H-ZSM-5(11) under (a) vacuum at room temperature, (ii) 0.1 Torr NO, (iii) 0.1 Torr H2 after exposure to 0.1 Torr NO (iv) 0.1 Torr NO + 0.1 Torr O2, and (iii*) H2 after exposure to 0.1 Torr NO + 0.1 Torr O2 at 150 °C. blue dots: raw spectrum; black line: sum; purple: adsorbed atomic nitrogen (Nads); light blue: adsorbed molecular NO (NOads); green: nitrite species; light yellow: NH3 adsorbed on Brønsted acid sites of zeolite (NH4+); red: residual nitrate species from metal nitrate precursors used in catalyst preparation; blue: surface nitrate species (NO3-).

Table S7. Peak concentration in the Co 2p AP-XPS spectra of Pt(1.3)-Ir(0.2)/Ba(1.5)-Co(1)/H-ZSM-5(11) under different conditions.

| Gas condition | Co2+ / % | Co3+ / % |
| --- | --- | --- |
| Vacuum | 69 | 31 |
| 0.1 Torr NO | 36 | 64 |
| 0.1 Torr H2 | 67 | 33 |
| 0.1 Torr NO + 0.1 Torr O2 | 17 | 83 |
| 0.1 Torr H2 | 67 | 33 |

Figure S21. Experimental conditions during operando FT-IR spectroscopic studies for Figure 6a and 6b.

Figure S22. Experimental conditions during operando FT-IR spectroscopic studies for Figure 6c

Figure S23. Operando IR spectra presenting the evolution of surface species adsorbed on Pt(1.3)-Ir(0.2)/Ba(1.5)-Co(1)/H-ZSM-5(11) after the introduction of (a) O2 and (c) NO2 following the introduction of 0.5% NO + 1% H2 for 30 min at 150 °C. (b, d) Corresponding concentration of products in the effluent gases. Conditions: catalyst weight: 40 mg, total flow rate: 100 mL/min.

Figure S24. Experimenetal conditions during the in situ FT-IR spectroscopic measurements. (a) Experimental conditions during in situ FT-IR spectroscopic studies Evolution of the surface species after the introduction of 1% H2 following the introduction of 0.5% NO for 15 min over various control catalysts without the addtion of (b) Ba, (c) Co, (d) Pt, and (e) Ir. Conditions: catalyst weight: 40 mg, total flow rate: 100 mL/min.

Supplementary References

(1) 	Geurts, P.; Ernst, D.; Wehenkel, L. Extremely Randomized Trees. Mach Learn 2006, 63, 3–42.

(2) 	Shrinkage, R. Regression Shrinkage and Selection via the Lasso. Journal of the Royal Statistical Society B 1996, 58 (1), 267–288.

(3) 	Hoerl, A. E.; Kennard, R. W. Ridge Regression: Applications to Nonorthogonal Problems. Technometrics 1970, 12 (1), 69–82.

(4) 	R. H. Myers, D. C. Montgomery, C. M. A.-C. Response Surface Methodology: Process and Product Optimization Using Designed Experiments; 1985; Vol. 001.

(5) 	Drucker, H.; Burges, C. J. C. C.; Kaufman, L.; Smola, A.; Vapnik, V. Support Vector Regression Machines. Adv Neural Inf Process Syst 1997, 9, 155–161.

(6) 	Breiman, L. Random Forests. Mach Learn 2001, 45, 5–32.