Analysis of electrolyte degradation products in cylindrical automotive lithium-ion cells during thermal aging

Sabrina Schönemeier1,2, Verena Peters2, Fabian Horsthemke2, Frank-Michael Matysik1

Frank-Michael Matysik

Frank-Michael.Matysik@chemie.uni-regensburg.de

[1] University Regensburg, Institute of Analytical Chemistry, Universitätsstrasse 31, 93053 Regensburg, Germany

[2] BMW Group, Battery Cell Competence Center, Lemgostrasse 7, 80935 Munich, Germany

Supplementary Data

Table S1: Specific conductivity results of the LiPF6 electrolytes in EC/EMC for different conductive salt concentrations. The measurements were performed in a microcell with a platinum beaker and a glassy carbon electrode at 25 °C.

| LiPF6 electrolyte in EC/EMC – original - measurement at 25 °C |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Electrolyte concentration | 1. [mS/cm] | 2. [mS/cm] | 3. [mS/cm] | Average [mS/cm] | Deviation [mS/cm] |
| 0.6 M | 8.28 | 8.27 | 8.26 | 8.27 | ± 0.01 |
| 1.0 M | 8.74 | 8.74 | 8.74 | 8.74 | ± 0.00 |
| 1.1 M | 9.13 | 9.12 | 9.13 | 9.12 | ± 0.01 |
| 1.2 M | 8.76 | 8.76 | 8.75 | 8.76 | ± 0.01 |
| 1.3 M | 8.47 | 8.47 | 8.46 | 8,47 | ± 0.01 |
| 1.4 M | 7.77 | 7.77 | 7.78 | 7.77 | ± 0.01 |
| 1.5 M | 7.35 | 7.30 | 7.46 | 7.37 | ± 0.09 |
| 1.7 M | 6.84 | 6.80 | 6.89 | 6.84 | ± 0.05 |
| 1.8 M | 5.23 | 5.23 | 5.23 | 5.23 | ± 0.00 |

Table S2: Specific conductivity results of the LiPF6 electrolytes in EC/EMC for different conductive salt concentrations after the storage at 55 °C for 7 days. The measurements were performed in a microcell with a platinum beaker and a glassy carbon electrode at 25 °C.

| LiPF6 electrolyte in EC/EMC – 7 days - measurement at 25 °C |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Electrolyte concentration | 1. [mS/cm] | 2. [mS/cm] | 3. [mS/cm] | Average [mS/cm] | Deviation [mS/cm] |
| 0.6 M | 8.23 | 8.28 | 8.24 | 8.25 | ± 0.03 |
| 1.0 M | 8.62 | 8.64 | 8.62 | 8.63 | ± 0.01 |
| 1.1 M | 8.68 | 8.61 | 8.62 | 8.64 | ± 0.04 |
| 1.2 M | 8.29 | 8.29 | 8.28 | 8.29 | ± 0.01 |
| 1.3 M | 8.10 | 8.10 | 8.09 | 8.10 | ± 0.01 |
| 1.4 M | 7.43 | 7.43 | 7.44 | 7.43 | ± 0.01 |
| 1.5 M | 7.21 | 7.19 | 7.26 | 7.22 | ± 0.04 |
| 1.7 M | 6.28 | 6.17 | 6.21 | 6.22 | ± 0.06 |
| 1.8 M | 5.20 | 5.28 | 5.23 | 5.23 | ± 0.05 |

Table S3: Specific conductivity results of the LiPF6 electrolytes in EC/EMC for different conductive salt concentrations after the storage at 55 °C for 14 days. The measurements were performed in a microcell with a platinum beaker and a glassy carbon electrode at 25 °C.

| LiPF6 electrolyte in EC/EMC – 14 days - measurement at 25 °C |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Electrolyte concentration | 1. [mS/cm] | 2. [mS/cm] | 3. [mS/cm] | Average [mS/cm] | Deviation [mS/cm] |
| 0.6 M | 8.21 | 8.20 | 8.19 | 8.20 | ± 0.01 |
| 1.0 M | 8.55 | 8.55 | 8.58 | 8.56 | ± 0.02 |
| 1.1 M | 8.64 | 8.65 | 8.66 | 8.65 | ± 0.01 |
| 1.2 M | 8.26 | 8.26 | 8.25 | 8.26 | ± 0.01 |
| 1.3 M | 7.97 | 7.97 | 7.98 | 7.97 | ± 0.01 |
| 1.4 M | 7.19 | 7.18 | 7.19 | 7.19 | ± 0.01 |
| 1.5 M | 7.09 | 7.12 | 7.08 | 7.10 | ± 0.01 |
| 1.7 M | 6.13 | 6.23 | 6.15 | 6.17 | ± 0.06 |
| 1.8 M | 5.11 | 5.16 | 5.10 | 5.12 | ± 0.04 |

Table S4: Specific conductivity results of the LiPF6 electrolytes in EC/EMC for different conductive salt concentrations after the storage at 55 °C for 28 days. The measurements were performed in a microcell with a platinum beaker and a glassy carbon electrode at 25 °C.

| LiPF6 electrolyte in EC/EMC – 28 days - measurement at 25 °C |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Electrolyte concentration | 1. [mS/cm] | 2. [mS/cm] | 3. [mS/cm] | Average [mS/cm] | Deviation [mS/cm] |
| 0.6 M | 8.11 | 8.04 | 8.05 | 8.07 | ± 0.04 |
| 1.0 M | 8.50 | 8.45 | 8.48 | 8.47 | ± 0.03 |
| 1.1 M | 8.57 | 8.59 | 8.66 | 8.61 | ± 0.05 |
| 1.2 M | 8.20 | 8.21 | 8.19 | 8.20 | ± 0.01 |
| 1.3 M | 7.84 | 7.85 | 7.86 | 7.84 | ± 0.02 |
| 1.4 M | 6.93 | 6.94 | 6.94 | 6.94 | ± 0.01 |
| 1.5 M | 6.75 | 6.81 | 6.72 | 6.76 | ± 0.05 |
| 1.7 M | 6.04 | 5.99 | 6.04 | 6.02 | ± 0.03 |
| 1.8 M | 4.85 | 4.87 | 4.84 | 4.85 | ± 0.02 |

Table S5: Specific conductivity results of the LiPF6 electrolytes in EC/EMC for different conductive salt concentrations after the storage at 55 °C for 42 days. The measurements were performed in a microcell with a platinum beaker and a glassy carbon electrode at 25 °C.

| LiPF6 electrolyte in EC/EMC – 42 days - measurement at 25 °C |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Electrolyte concentration | 1. [mS/cm] | 2. [mS/cm] | 3. [mS/cm] | Average [mS/cm] | Deviation [mS/cm] |
| 0.6 M | 8.10 | 8.05 | 8.05 | 8.07 | ± 0.03 |
| 1.0 M | 8.14 | 8.15 | 8.12 | 8.14 | ± 0.02 |
| 1.1 M | 8.48 | 8.47 | 8.54 | 8.50 | ± 0.04 |
| 1.2 M | 8.01 | 8.02 | 8.03 | 8.02 | ± 0.01 |
| 1.3 M | 7.64 | 7.65 | 7.63 | 7.64 | ± 0.01 |
| 1.4 M | 6.92 | 6.92 | 6.93 | 6.92 | ± 0.01 |
| 1.5 M | 6.27 | 6.33 | 6.28 | 6.29 | ± 0.04 |
| 1.7 M | 5.94 | 5.91 | 5.91 | 5.92 | ± 0.02 |
| 1.8 M | 4.55 | 4.55 | 4.55 | 4.55 | ± 0.00 |

Table S6: Specific conductivity results of the LiFSI electrolytes in EC/EMC for different conductive salt concentrations. The measurements were performed in a microcell with a platinum beaker and a glassy carbon electrode at 25 °C.

| LiFSI electrolyte in EC/EMC – original - measurement at 25 °C |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Electrolyte concentration | 1. [mS/cm] | 2. [mS/cm] | 3. [mS/cm] | Average [mS/cm] | Deviation [mS/cm] |
| 0.6 M | 8.49 | 8.50 | 8.49 | 8.49 | ± 0.01 |
| 1.0 M | 9.52 | 9.53 | 9.51 | 9.52 | ± 0.01 |
| 1.1 M | 9.73 | 9.70 | 9.76 | 9.73 | ± 0.03 |
| 1.2 M | 9.36 | 9.37 | 9.36 | 9.36 | ± 0.01 |
| 1.3 M | 9.21 | 9.20 | 9.22 | 9.21 | ± 0.01 |
| 1.4 M | 8.82 | 8.82 | 8.83 | 8.82 | ± 0.01 |
| 1.5 M | 8.36 | 8.47 | 8.39 | 8.41 | ± 0.06 |
| 1.7 M | 8.04 | 8.04 | 8.04 | 8.04 | ± 0.00 |
| 1.8 M | 7.33 | 7.36 | 7.31 | 7.34 | ± 0.03 |

Table S7: Specific conductivity results of the LiPF6 electrolytes in EC/EMC for different conductive salt concentrations after the storage at 55 °C for 7 days . The measurements were performed in a microcell with a platinum beaker and a glassy carbon electrode at 25 °C.

| LiFSI electrolyte in EC/EMC – 7 days - measurement at 25 °C |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Electrolyte concentration | 1. [mS/cm] | 2. [mS/cm] | 3. [mS/cm] | Average [mS/cm] | Deviation [mS/cm] |
| 0.6 M | 9.15 | 9.09 | 9.11 | 9.12 | ± 0.03 |
| 1.0 M | 9.46 | 9.50 | 9.47 | 9.48 | ± 0.02 |
| 1.1 M | 9.59 | 9.61 | 9.60 | 9.60 | ± 0.01 |
| 1.2 M | 9.26 | 9.27 | 9.28 | 9.27 | ± 0.01 |
| 1.3 M | 9.14 | 9.14 | 9.14 | 9.14 | ± 0.00 |
| 1.4 M | 8.63 | 8.63 | 8.62 | 8.63 | ± 0.01 |
| 1.5 M | 7.69 | 7.73 | 7.68 | 7.70 | ± 0.03 |
| 1.7 M | 7.43 | 7.48 | 7.44 | 7.45 | ± 0.03 |
| 1.8 M | 7.24 | 7.28 | 7.24 | 7.25 | ± 0.03 |

Table S8: Specific conductivity results of the LiFSI electrolytes in EC/EMC for different conductive salt concentrations after the storage at 55 °C for 14 days. The measurements were performed in a microcell with a platinum beaker and a glassy carbon electrode at 25 °C.

| LiFSI electrolyte in EC/EMC – 14 days - measurement at 25 °C |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Electrolyte concentration | 1. [mS/cm] | 2. [mS/cm] | 3. [mS/cm] | Average [mS/cm] | Deviation [mS/cm] |
| 0.6 M | 9.05 | 9.05 | 9.05 | 9.05 | ± 0.00 |
| 1.0 M | 9.39 | 9.42 | 9.38 | 9.40 | ± 0.02 |
| 1.1 M | 9.56 | 9.59 | 9.56 | 9.57 | ± 0.02 |
| 1.2 M | 9.25 | 9.24 | 9.25 | 9.25 | ± 0.01 |
| 1.3 M | 8.83 | 8.83 | 8.82 | 8.83 | ± 0.00 |
| 1.4 M | 8.33 | 8.34 | 8.34 | 8.34 | ± 0.01 |
| 1.5 M | 7.52 | 7.54 | 7.62 | 7.56 | ± 0.06 |
| 1.7 M | 7.27 | 7.18 | 7.20 | 7.22 | ± 0.04 |
| 1.8 M | 7.26 | 7.16 | 7.19 | 7.20 | ± 0.06 |

Table S9: Specific conductivity results of the LiFSI electrolytes in EC/EMC for different conductive salt concentrations after the storage at 55 °C for 28 days. The measurements were performed in a microcell with a platinum beaker and a glassy carbon electrode at 25 °C.

| LiFSI electrolyte in EC/EMC – 28 days - measurement at 25 °C |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Electrolyte concentration | 1. [mS/cm] | 2. [mS/cm] | 3. [mS/cm] | Average [mS/cm] | Deviation [mS/cm] |
| 0.6 M | 9.01 | 9.03 | 9.03 | 9.02 | ± 0.01 |
| 1.0 M | 9.21 | 9.24 | 9.21 | 9.22 | ± 0.02 |
| 1.1 M | 9.45 | 9.43 | 9.45 | 9.45 | ± 0.02 |
| 1.2 M | 9.23 | 9.22 | 9.24 | 9.23 | ± 0.01 |
| 1.3 M | 8.83 | 8.84 | 8.83 | 8.83 | ± 0.01 |
| 1.4 M | 8.26 | 8.26 | 8.27 | 8.26 | ± 0.01 |
| 1.5 M | 7.56 | 7.45 | 7.48 | 7.50 | ± 0.06 |
| 1.7 M | 7.05 | 6.95 | 6.92 | 6.97 | ± 0.08 |
| 1.8 M | 6.75 | 6.82 | 6.72 | 6.76 | ± 0.06 |

Table S10: Specific conductivity results of the LiFSI electrolytes in EC/EMC for different conductive salt concentrations after the storage at 55 °C for 42 days. The measurements were performed in a microcell with a platinum beaker and a glassy carbon electrode at 25 °C.

| LiFSI electrolyte in EC/EMC – 42 days - measurement at 25 °C |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Electrolyte concentration | 1. [mS/cm] | 2. [mS/cm] | 3. [mS/cm] | Average [mS/cm] | Deviation [mS/cm] |
| 0.6 M | 9.00 | 9.03 | 9.04 | 9.02 | ± 0.02 |
| 1.0 M | 9.19 | 9.14 | 9.16 | 9.16 | ± 0.02 |
| 1.1 M | 9.33 | 9.32 | 9.33 | 9.33 | ± 0.01 |
| 1.2 M | 9.08 | 9.06 | 9.09 | 9.08 | ± 0.02 |
| 1.3 M | 8.74 | 8.76 | 8.76 | 8.76 | ± 0.02 |
| 1.4 M | 8.22 | 8.23 | 8.25 | 8.23 | ± 0.02 |
| 1.5 M | 7.46 | 7.51 | 7.46 | 7.48 | ± 0.03 |
| 1.7 M | 6.98 | 6.89 | 6.91 | 6.93 | ± 0.05 |
| 1.8 M | 6.78 | 6.74 | 6.72 | 6.75 | ± 0.03 |

Table S11: LiPF6 containing electrolytes were mixed in the glovebox in the following concentrations. For the validation of the mixing procedure IC-CD-MS was measured.

| LiPF6 electrolytes in EC/EMC |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Electrolyte concentr. | LiPF6 |  | EC |  | EMC |  | Real concentr. |
| [mol/L] | [g] | [mL] | [g] | [mL] | [g] | [mL] | [mol/L] |
| 0.6 M | 1.932 | 1.29 | 11.644 | 8.75 | 11.546 | 11.43 | 0.63 |
| 1.0 M | 3.136 | 2.09 | 10.918 | 8.27 | 11.190 | 11.08 | 0.99 |
| 1.1 M | 3.486 | 2.32 | 10.830 | 8.20 | 10.888 | 10.78 | 1.15 |
| 1.2 M | 3.857 | 2.57 | 10.597 | 8.03 | 10.695 | 10.59 | 1.23 |
| 1.3 M | 4.179 | 2.79 | 10.449 | 7.92 | 10.859 | 10.75 | 1.31 |
| 1.4 M | 4.497 | 3.00 | 10.274 | 7.78 | 10.272 | 10.17 | 1.38 |
| 1.5 M | 4.877 | 3.25 | 10.172 | 7.71 | 10.320 | 10.22 | 1.54 |
| 1.7 M | 5.318 | 3.55 | 9.818 | 7.44 | 9.981 | 9.88 | 1.68 |
| 1.8 M | 5.698 | 3.80 | 9.696 | 7.35 | 9.646 | 9.55 | 1.84 |

Table S11: LiFSI containing electrolytes were mixed in the glovebox in the following concentrations. For the validation of the mixing procedure IC-CD-MS was measured.

| LiFSI electrolytes in EC/EMC |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Electrolyte concentr. | LiFSI |  | EC |  | EMC |  | Real concentr. |
| [mol/L] | [g] | [mL] | [g] | [mL] | [g] | [mL] | [mol/L] |
| 0.6 M | 2.55 | 2.42 | 11.314 | 8.57 | 11.385 | 11.67 | 0.65 |
| 1.0 M | 3.93 | 3.74 | 10.654 | 8.07 | 10.862 | 10.57 | 1.02 |
| 1.1 M | 4.46 | 4.24 | 10.353 | 7.84 | 10.336 | 10.23 | 1.06 |
| 1.2 M | 4.88 | 4.64 | 10.414 | 7.89 | 10.299 | 10.20 | 1.19 |
| 1.3 M | 5.14 | 4.89 | 9.927 | 7.52 | 9.938 | 9.84 | 1.29 |
| 1.4 M | 5.90 | 5.61 | 9.701 | 7.35 | 9.694 | 9.60 | 1.44 |
| 1.5 M | 6.31 | 5.99 | 9.473 | 7.18 | 9.551 | 9.46 | 1.51 |
| 1.7 M | 7.18 | 6.83 | 9.261 | 7.02 | 9.227 | 9.13 | 1.72 |
| 1.8 M | 7.47 | 7.10 | 9.036 | 6.85 | 9.086 | 8.99 | 1.85 |