Reactive cement pellet media including drinking water treatment and mine drainage residuals for phosphorus removal in agricultural runoff

### Beth Kondro*1, Michael A. Holly1,

1University of Wisconsin-Green Bay, 2420 Nicolet Dr, Green Bay, WI, 54311, United States

*kondrob@uwgb.edu, (920) 465-2503

Figure S1 Source of drinking water treatment residual at Green Bay Water Utility (Green Bay, WI)

Table S1. Different binder ratios (wt/wt) for two binder types. PC = Portland cement. * Denotes the binder ratio that was most effective.

| Binder Type | Binder Ratio |
| --- | --- |
| AlCl3 | 1 AlCl3 : 9 DWTR/AMD |
|  | 2 AlCl3 : 23 DWTR/AMD |
|  | 1 AlCl3 : 4 DWTR/AMD |
| Cement Mixture | 1 PC : 4 DWTR/AMD |
|  | 1 Lime : 4 DWTR/AMD |
|  | 1 PC : 2 Sand : 3 DWTR/AMD |
|  | 1 Lime : 2 Sand : 3 DWTR/AMD |
|  | 1 Lime : 1 PC : 2 Sand : 4 DWTR/AMD |
|  | 1 Lime : 1 PC : 2 Sand : 2 DWTR/AMD* |

Figure S2 Dried test pellets after compression and soaking.

Figure S3. Stability diagram of HPO42- ([HPO42-] = 5.21x10-6 in 6a and 6b) in the presence of Ca ([Ca] = 1x10-3 in 6a and [Ca] = 1x10-6 in 6b).

Calculations for cost estimate:

Using the cement pellet (CEM) as an example.

- Mass of CEM required to treat a P load of 7 kg:

- P removal capacity of CEM = 1,397 mg P/kg

  - P removal capacity of CEM adjusting for inefficiency of P removal from agricultural runoff (18% for CEM) =1,397mg Pkg1.18 =1,184 mg Pkg

- P load after 3 years = 7x106 mg P

  - Mass required = 7x106 mg P x kg1,184 mg P =5,912 kg CEM

- Cost of materials required to make 5,912 kg CEM:

  - Cost of Portland cement = $0.36/kg

  - Cost of lime = $0.72/kg

  - Cost of sand = $0.41/kg

  - Cost of pyrolysis = $0.08/kg

  - Pellet ratio = 1 cement : 1 lime : 2 sand

    - Mass of cement in pellet =  5,912 kg4 = 1,478 kg

      - Cost of cement = 1,478 kg x $0.36 = $532

    - Mass of lime in pellet = 5,912 kg4  = 1,478 kg

      - Cost of lime = 1,478 kg x $0.72/kg = $1,064

    - Mass of sand = 5,912 kg2  = 2,956 kg

      - Cost of sand = 2,956 kg x $0.41/kg = $1,212

  - Total cost:

    - Cement + lime + sand = total cost

    - $532 + $1,064 + $1,212 = $2,808

Using the pyrolyzed cement pellet (CEMC) as an example.

- Mass of CEM-P required to treat P load of 7 kg:

- P removal capacity of CEM-P = 2,270 mg P/kg

  - P removal capacity of CEM-P adjusting for inefficiency of P removal from agricultural runoff (13% for CEM) =2,270mg Pkg1.13=2,009 mg Pkg

- P load after 3 years = 7x106 mg P

  - Mass required = 7x106 mg P x kg2,009 mg P =3,484 kg CEMC

- Cost of materials required to make 3,484 kg CEM-P:

  - Cost of Portland cement = $0.36/kg

  - Cost of lime = $0.72/kg

  - Cost of sand = $0.41/kg

  - Cost of pyrolysis = $0.08/kg

  - Pellet ratio = 1 cement : 1 lime : 2 sand

    - Mass of cement in pellet = 3,484 kg4 = 871 kg

      - Cost of cement = 871 kg x $0.36 = $314

    - Mass of lime in pellet = 3,484 kg4  = 871 kg

      - Cost of lime = 871 kg x $0.72/kg = $627

    - Mass of sand = 3,484 kg2  = 1,742 kg

      - Cost of sand = 1,742 kg x $0.41/kg = $714

    - Mass of CEMC pyrolyzed = 3,484 kg

      - Cost of pyrolysis = 3,484 kg x $0.08/kg = $279

  - Total cost:

    - Cement + lime + sand + pyrolysis = total cost

    - $314 + $627 + $714 + $279 = $1,934