Supplementary Information

Enhancing stability by trapping palladium inside N-heterocyclic carbene-functionalized hypercrosslinked polymers for heterogeneous C-C bond formations

Yue et al.

Supplementary Figures

Supplementary Figure 1. FT-TR spectrum of KAP-Pd-PEPPSI. The characteristic peaks are labelled in the spectra (from left to right: 2959, 2918, 2867, 1667, 1465 and 1447 cm-1).

Supplementary Figure 2. Solid-state 13C CP/MAS NMR spectrum of KAP-Pd-PEPPSI. The characteristic peaks are labelled in the spectra.

Supplementary Figure 3. Pd 3d XPS spectra of KAP-Pd-PEPPSI. (a) KAP-Pd-PEPPSI-1, (b) KAP-Pd-PEPPSI-2, (c) KAP-Pd-PEPPSI-3, and (d) molecular Pd-PEPPSI.

Supplementary Figure 4. SEM images of KAP-Pd-PEPPSI. (a, d) KAP-Pd-PEPPSI-1, (b, e) KAP-Pd-PEPPSI-2 and (c, f) KAP-Pd-PEPPSI-3. (a-c): KAP-Pd-PEPPSI. (d-f): KAP-Pd-PEPPSI after swelling in DMF. Scale bars: 500 nm

Supplementary Figure 5. STEM images of KAP-Pd-PEPPSI. (a-b) KAP-Pd-PEPPSI-1, (c-d) KAP-Pd-PEPPSI-2, (e-f) KAP-Pd-PEPPSI-2 after being reduced by NaBH4 and (g-h) KAP-Pd-PEPPSI-3.

Supplementary Figure 6. Textural properties of catalysts. (a) N2 sorption isotherms collected at 77 K and (b) pore size distributions of KAP-Pd-PEPPSI. The BET surface area in KAP-Pd-PEPPSI-1 is 227 cm3 g-1, which decreases to 10 cm3 g-1 and 7 cm3 g-1, respectively, in KAP-Pd-PEPPSI-2 and KAP-Pd-PEPPSI-3.

Supplementary Figure 7. STEM images of reference catalysts. (a) Fresh Pd@C, (b) Pd@NC, (c) Pd@PC, (d) Pd@SiO2, (e) KAP-Pd-PPh3 and (f) POP-Pd-PEPPSI. The STEM morphologies of fresh Pd@C, Pd@NC, Pd@PC, Pd@SiO2 (a-d, supported Pd catalysts) show uniform distributed nanoparticles with sizes ranging from several nanometers to tens of nanometers, whereas KAP-Pd-PPh3 and POP-Pd-PEPPSI (e-f, polymer supported Pd complex precatalysts) show even more uniform distributed Pd species without formation of nanoparticles.

Supplementary Figure 8. STEM images of different catalysts after a single cycle. (a) Pd-PEPPSI, (b) Pd@C, (c) Pd@NC, (d) Pd@PC, (e) Pd@SiO2, (f) KAP-Pd-PEPPSI-1, (g) KAP-Pd-PEPPSI-2, (h) KAP-Pd-PEPPSI-3, (i) POP-Pd-PEPPSI, (j) KAP-Pd-PPh3.

Supplementary Figure 9. STEM images of different catalysts after a single cycle. (a) KAP-Pd-PEPPSI-1, (b) KAP-Pd-PEPPSI-2, (c) KAP-Pd-PEPPSI-3, (d) POP-Pd-PEPPSI, (e) KAP-Pd-PPh3.

Supplementary Figure 10. STEM images of (a-b) KAP-Pd-PPh3 after 5 cycles and (c-d) POP-Pd-PEPPSI after 5 cycles.

Supplementary Figure 11. STEM images of KAP-Pd-PEPPSI-2. (a-b) fresh catalyst, (c-d) after 1 cycles, (e-f) after 3 cycles, (g-h) after 5 cycles, (i-j) after 7 cycles, (k-l) after 9 cycles (m-p) STEM-EDS mapping of the catalyst after 5 cycles.

Supplementary Figure 12. STEM images of the spent catalysts in control experiment. (a-b) KAP-2/PdCl2 and (c-d) KAP-4/PdCl2.

Supplementary Figure 13. Recyclability of KAP-Pd-PEPPSI-3 in Suzuki coupling reaction. Reaction conditions: catalyst 0.4 mol%, iodobenzene 1.0 mmol, phenylboronic acid 1.5 mmol, K3PO4 3.0 mmol, EtOH/H2O 4 mL, 60 oC, 2 h.

Supplementary Figure 14. STEM images of the spent catalysts in Suzuki coupling reaction. (a-b) Pd@C after 6 cycles and (c-d) KAP-Pd-PEPPSI-3 after 21 cycles in Suzuki coupling reaction.

Supplementary Figure 15. Pd 3d XPS spectra of recycled KAP-Pd-PEPPSI-2 after the 21th cycle in Suzuki coupling reaction.

Supplementary Tables

Supplementary Table 1. Pd content in different catalysts and the corresponding ligand-to-metal ratio a

| Cat. | Pd loading wt% | L/Pd |
| --- | --- | --- |
| Pd@C | 5.6 | - |
| Pd@NC | 2.1 | 56 |
| Pd@PC | 1.2 | 19 |
| Pd@SiO2 | 2.1 | - |
| KAP-Pd-PPh3 | 2.2 | 5.34 |
| POP-Pd-PEPPSI | 2.5 | 4.22 |
| KAP- Pd-PEPPSI-1 | 2.5 | 6.32 |
| KAP- Pd-PEPPSI-2 | 2.4 | 5.79 |
| KAP- Pd-PEPPSI-3 | 2.9 | 5.50 |

a The Pd content in catalysts were determined by ICP-MS using In as a reference and ligand-to-metal ratios were calculated from the XPS results.

Supplementary Table 2. Optimization of fluorocarbonylation of indoles a

| Entry | Solvent | [F-] | Base | Yield (%) |
| --- | --- | --- | --- | --- |
| 1 | DMF | CsF | Cs2CO3 | 24 |
| 2 | DMF | CsF | K2CO3 | 12 |
| 3 | DMF | CsF | K3PO4 | 8 |
| 4 | DMF | CsF | DBU | trace |
| 5b | DMF | CsF | DABCO | 89(79) |
| 6 | DMF | KF | DABCO | 74 |
| 7 | DMF | NH4F | DABCO | trace |
| 8 | DMF | NBu4F | DABCO | 32 |
| 9 | Toluene | CsF | DABCO | trace |
| 10 | Dioxane | CsF | DABCO | trace |
| 11c | DMF | CsF | DABCO | trace |

a Conditions: 1a (0.25 mmol), CsF (1 mmol), catalyst (5 mol%), I2 (0.5 mmol), base (0.5 mmol), DMF (2 mL), 80 oC, 24 h. bIsolated yield in bracket. cMecury test.

Supplementary Table 3. Pd leaching conditions of different catalyst in washing test a

| Entry | Catalyst | Pd leaching (%) |
| --- | --- | --- |
| 1 | Pd@C | 39.6 |
| 2 | Pd@NC | 19.6 |
| 3 | Pd@PC | 12.4 |
| 4 | Pd@SiO2 | 27.4 |
| 5 | KAP-Pd-PPh3 | 60.4 |
| 6 | POP-Pd-PEPPSI | 41.3 |
| 7 | KAP-Pd-PEPPSI-1 | 39.6 |
| 8 | KAP-Pd-PEPPSI-2 | 16.1 |
| 9 | KAP-Pd-PEPPSI-3 | 7.0 |
| 10b | KAP-Pd-PEPPSI-3 | 5.5 |
| 11c | KAP-Pd-PEPPSI-3 | 91.0 |

a The washing test was performed to determine the extent of Pd leaching from the catalysts upon treatment with the reactants for 4 h at 80 oC in the absence of CsF. bAfter reaction for 4 h in the presence of CsF (3% yield). cCatalyst 0.6 mol% (21% yield).

Supplementary Table 4. The time-course analyses of Pd distribution as well as the corresponding reaction activity in flurocarbonylation of indole

| Time h | Pd@C |  | KAP-Pd-PEPPSI |  |
| --- | --- | --- | --- | --- |
|  | Yield % | Pd in solution wt% | Yield % | Pd in solution wt% |
| 2 | 45 | 37.3 | 0 | 2 |
| 4 | 67 | 40.7 | 3 | 5.5 |
| 6 | 74 | 35.1 | 55 | 1.9 |
| 8 | 81 | 28.8 | 69 | 0.6 |
| 10 | 84 | 16.4 | 78 | 0.5 |
| 24 | 89 | 2 | 86 | 0.2 |

Supplementary Table 5. Aminocarbonylation of indole with weakly nucleophilic aromatic amines using various catalyst systems a

| Entry | Reaction Conditions | Yield % |
| --- | --- | --- |
| 1 | (Arndtsen's Conditions)1a 0.37 mmol, 2a 0.25 mmol, Pd(PtBu3)2 5 mol% EtN(iPr)2 0.74 mmol, I2 0.37 mmol, Bu4NCl 0.25 mmol, CH3CN 0.4 mL, 80 oC, 24 h | 14 |
| 2 | (Manabe's Conditions)1a 0.25 mmol, 2a 0.37 mmol, Pd(OAc)2 5 mol% Xantphos 10 mol%, Et3N 1 mmol, I2 0.47 mmol, KF 0.625 mmol, DMF 3 mL, 80 oC, 24 h | 11 |
| 3 | (This Work)1a 0.25 mmol, 2a 1.25 mmol, KAPs-Pd-PEPPSI 5 mol%, DABCO 0.5 mmol, I2 0.5 mmol, CsF 1 mmol, DMF 2 mL, 80 oC, 24 h | 74 |

a Isolated yield.

Supplementary Table 6. Control reactions to investigate the role of fluoride a

| Halides | Yield % | Halides | Yield % | Yield % |
| --- | --- | --- | --- | --- |
| - | n.d. | - | n.d. | 84 |
| CsF | 78 | CsF | 89 |  |
| CsCl | n.d. | CsCl | n.d. |  |
| CsBr | n.d. | CsBr | n.d. |  |
| CsI | n.d. | CsI | n.d. |  |

a Conditions: 1a (0.25 mmol), CsX (1 mmol), KAP-Pd-PEPPSI-2 (5 mol%), I2 (0.5 mmol), base (0.5 mmol), DMF (2 mL), 80 oC, 24 h. HPLC yield.

Supplementary Note 1

Detailed Descriptions for Products

1-methyl-1H-indole-3-carbonyl fluoride

Purified by column chromatography (10:1 PE/EA); white solid; 79% yield; Rf = 0.28 (5:1 PE/EA). 1H NMR (400 MHz, CDCl3) δ 7.99 – 7.97 (m, 1H), 7.70 (s, 1H), 7.29 – 7.23 (m, 3H), 3.75 (s, 3H). 13C NMR (100 MHz, CDCl3) δ 156.3, 153.0, 137.8, 137.5, 136.5, 126.8, 123.9, 123.1, 121.1, 110.4, 109.9, 33.8, 33.6. The spectral data obtained agree with those reported in the literature.9

(1-methyl-1H-indol-3-yl)(1H-pyrazol-1-yl)methanone

Purified by column chromatography (10:1 PE/EA); light red solid; 74% yield; Rf = 0.36 (5:1 PE/EA). 1H NMR (400 MHz, CDCl3) δ 8.82 (s, 1H), 8.50 (s, 2H), 7.75 (s, 1H), 7.35 (s, 3H), 6.45 (s, 1H), 3.86 (d, J = 2.3 Hz, 3H). 13C NMR (100 MHz, CDCl3) δ 160.9, 143.1, 140.1, 136.8, 129.7, 128.9, 123.4, 122.8, 122.4, 109.8, 108.0, 106.1, 33.7. HRMS (ESI) m/z: calculated for C13H11N3ONa [M + Na]+ 248.0800, found 248.0797.

(1,4-dimethyl-1H-indol-3-yl)(1H-pyrazol-1-yl)methanone

Purified by column chromatography (10:1 then 5:1 PE/EA); light red solid; 83% yield; Rf = 0.29 (5:1 PE/EA). 1H NMR (400 MHz, CDCl3) δ 8.45 (d, J = 2.6 Hz, 1H), 8.12 (s, 1H), 7.75 (s, 1H), 7.18 (m, 3H), 6.48 (dd, J = 2.6, 1.5 Hz, 1H), 3.78 (s, 3H), 2.75 (s, 3H). 13C NMR (100 MHz, CDCl3) δ 161.2, 143.2, 139.7, 137.6, 132.7, 129.9, 126.6, 124.6, 123.6, 108.5, 107.6, 107.2, 33.7, 22.0. HRMS (ESI) m/z: calculated for C14H13N3ONa [M + Na]+ 262.0956, found 262.0954.

(1,5-dimethyl-1H-indol-3-yl)(1H-pyrazol-1-yl)methanone

Purified by column chromatography (10:1 PE/EA); light red solid; 81% yield; Rf = 0.38 (5:1 PE/EA). 1H NMR (400 MHz, DMSO) δ 8.89 (s, 1H), 8.55 (dd, J = 2.7, 0.5 Hz, 1H), 8.12 (s, 1H), 7.94 (d, J = 0.8 Hz, 1H), 7.50 (d, J = 8.3 Hz, 1H), 7.18 (dd, J = 8.4, 1.3 Hz, 1H), 6.64 (dd, J = 2.7, 1.5 Hz, 1H), 3.93 (s, 3H), 2.47 (s, 3H). 13C NMR (100 MHz, DMSO) δ 160.1, 143.5, 140.5, 135.1, 131.5, 129.6, 128.3, 124.6, 121.0, 110.7, 108.5, 103.9, 33.4, 21.3. HRMS (ESI) m/z: calculated for C14H13N3ONa [M + Na]+ 262.0956, found 262.0957.

(1,6-dimethyl-1H-indol-3-yl)(1H-pyrazol-1-yl)methanone

Purified by column chromatography (10:1 PE/EA); light red solid; 91% yield; Rf = 0.40 (5:1 PE/EA). 1H NMR (400 MHz, DMSO) δ 8.85 (s, 1H), 8.56 (d, J = 2.7 Hz, 1H), 8.18 (d, J = 8.1 Hz, 1H), 7.94 (d, J = 0.7 Hz, 1H), 7.40 (s, 1H), 7.15 (d, J = 8.1 Hz, 1H), 6.63 (dd, J = 2.7, 1.5 Hz, 1H), 3.91 (s, 3H), 2.46 (s, 3H). 13C NMR (100 MHz, DMSO) δ 160.1, 143.6, 140.2, 137.0, 132.6, 129.6, 125.9, 124.1, 120.9, 110.8, 108.5, 104.4, 33.3, 21.3. HRMS (ESI) m/z: calculated for C14H13N3ONa [M + Na]+ 262.0956, found 262.0952.

(1,7-dimethyl-1H-indol-3-yl)(1H-pyrazol-1-yl)methanone

Purified by column chromatography (10:1 then 5:1 PE/EA); light red solid; 69% yield; Rf = 0.31 (5:1 PE/EA). 1H NMR (400 MHz, DMSO) δ 8.82 (s, 1H), 8.59–8.52 (m, 1H), 8.19 (d, J = 7.9 Hz, 1H), 7.98–7.88 (m, 1H), 7.16 (t, J = 7.6 Hz, 1H), 7.03 (d, J = 7.1 Hz, 1H), 6.63 (dd, J = 2.7, 1.5 Hz, 1H), 4.19 (s, 3H), 2.77 (s, 3H). 13C NMR (100 MHz, DMSO) δ 160.0, 143.5, 142.0, 135.2, 129.7, 129.2, 125.8, 122.6, 119.2, 108.5, 103.8, 37.5, 19.0. HRMS (ESI) m/z: calculated for C14H13N3ONa [M + Na]+ 262.0956, found 262.0954.

(1,2-dimethyl-1H-indol-3-yl)(1H-pyrazol-1-yl)methanone

Purified by column chromatography (10:1 then 5:1 PE/EA); light red solid; 57% yield; Rf = 0.13 (5:1 PE/EA). 1H NMR (400 MHz, DMSO) δ 8.45 (d, J = 2.7 Hz, 1H), 7.86 (s, 1H), 7.56 (d, J = 8.2 Hz, 1H), 7.37 (d, J = 7.9 Hz, 1H), 7.22 (t, J = 7.6 Hz, 1H), 7.12 (t, J = 7.5 Hz, 1H), 6.64 (s, 1H), 3.78 (s, 3H), 2.47 (s, 3H). 13C NMR (100 MHz, DMSO) δ 163.3, 146.2, 143.1, 136.3, 130.2, 126.3, 122.0, 121.3, 120.0, 110.1, 109.0, 105.3, 29.9, 12.4. HRMS (ESI) m/z: calculated for C14H13N3ONa [M + Na]+ 262.0956, found 262.0957.

(6-chloro-1-methyl-1H-indol-3-yl)(1H-pyrazol-1-yl)methanone

Purified by column chromatography (10:1 PE/EA); light red solid; 69% yield; Rf = 0.35 (5:1 PE/EA). 1H NMR (400 MHz, DMSO) δ 8.94 (s, 1H), 8.56 (d, J = 2.8 Hz, 1H), 8.27 (d, J = 8.5 Hz, 1H), 7.96 (s, 1H), 7.77 (d, J = 1.7 Hz, 1H), 7.33 (dd, J = 8.5, 1.8 Hz, 1H), 6.65 (dd, J = 2.7, 1.5 Hz, 1H), 3.95 (s, 3H). 13C NMR (100 MHz, DMSO) δ 160.0, 143.9, 141.4, 137.2, 129.7, 127.9, 126.7, 122.7, 122.5, 111.2, 108.8, 104.7, 33.6. HRMS (ESI) m/z: calculated for C13H10ClN3ONa [M + Na]+ 282.0410, found 282.0408.

(6-bromo-1-methyl-1H-indol-3-yl)(1H-pyrazol-1-yl)methanone

Purified by column chromatography (10:1 PE/EA); light red solid; 64% yield; Rf = 0.34 (5:1 PE/EA). 1H NMR (400 MHz, DMSO) δ 8.96 (s, 1H), 8.60 (dd, J = 2.8, 0.6 Hz, 1H), 8.25 (d, J = 8.5 Hz, 1H), 8.02–7.97 (m, 1H), 7.94 (d, J = 1.6 Hz, 1H), 7.49 (dd, J = 8.5, 1.8 Hz, 1H), 6.68 (dd, J = 2.8, 1.5 Hz, 1H), 3.98 (s, 3H). 13C NMR (100 MHz, DMSO) δ 160.0, 143.9, 141.3, 137.6, 129.7, 127.0, 125.4, 122.8, 115.9, 114.1, 108.8, 104.7, 33.6. HRMS (ESI) m/z: calculated for C13H10BrN3ONa [M + Na]+ 325.9904, found 325.9912.

(5-methoxy-1-methyl-1H-indol-3-yl)(1H-pyrazol-1-yl)methanone

Purified by column chromatography (10:1 then 5:1 PE/EA); white solid; 73% yield; Rf = 0.30 (5:1 PE/EA). 1H NMR (400 MHz, DMSO) δ 8.89 (s, 1H), 8.55 (d, J = 2.7 Hz, 1H), 7.95 (d, J = 0.6 Hz, 1H), 7.83 (d, J = 2.5 Hz, 1H), 7.53 (d, J = 8.9 Hz, 1H), 6.98 (dd, J = 8.9, 2.5 Hz, 1H), 6.64 (dd, J = 2.4, 1.7 Hz, 1H), 3.93 (s, 3H), 3.84 (s, 3H). 13C NMR (100 MHz, DMSO) δ 160.1, 156.0, 143.6, 140.5, 131.6, 129.6, 129.1, 112.7, 111.9, 108.5, 104.0, 103.2, 55.3, 33.6. HRMS (ESI) m/z: calculated for C14H13N3O2Na [M + Na]+ 278.0905, found 278.0902.

(1-methyl-1H-pyrrolo[2,3-b]pyridin-3-yl)(1H-pyrazol-1-yl)methanone

Purified by column chromatography (10:1 then 5:1 PE/EA); light red solid; 70% yield; Rf = 0.16 (5:1 PE/EA). 1H NMR (400 MHz, CDCl3) δ 8.98 (s, 1H), 8.72 (dd, J = 7.9, 1.6 Hz, 1H), 8.49 (dd, J = 2.8, 0.5 Hz, 1H), 8.44 (dd, J = 4.7, 1.6 Hz, 1H), 7.78 (d, J = 0.7 Hz, 1H), 7.33–7.23 (m, 1H), 6.48 (dd, J = 2.8, 1.5 Hz, 1H), 4.00 (s, 3H). 13C NMR (100 MHz, CDCl3) δ 160.5, 147.9, 144.6, 143.5, 140.0, 130.7, 129.6, 121.3, 118.7, 108.4, 104.8, 32.1. HRMS (ESI) m/z: calculated for C12H10N4ONa [M + Na]+ 249.0752, found 249.0750.

(1-allyl-1H-indol-3-yl)(1H-pyrazol-1-yl)methanone

Purified by column chromatography (10:1 PE/EA); light red solid; 56% yield; Rf = 0.47 (5:1 PE/EA). 1H NMR (400 MHz, DMSO) δ 8.98 (s, 1H), 8.58 (d, J = 2.7 Hz, 1H), 8.40–8.28 (m, 1H), 7.96 (d, J = 0.7 Hz, 1H), 7.67–7.58 (m, 1H), 7.39–7.30 (m, 2H), 6.65 (dd, J = 2.7, 1.5 Hz, 1H), 6.08–6.04 (m, 1H), 5.24 (dd, J = 10.3, 1.3 Hz, 1H), 5.18–5.13 (m, 1H), 5.04 (d, J = 5.5 Hz, 2H). 13C NMR (100 MHz, DMSO) δ 160.2, 143.8, 139.8, 135.9, 133.4, 129.7, 128.2, 123.2, 122.6, 121.4, 117.9, 111.4, 108.7, 104.9, 48.8. HRMS (ESI) m/z: calculated for C15H13N3ONa [M + Na]+ 274.0956, found 274.0956.

(1-benzyl-1H-indol-3-yl)(1H-pyrazol-1-yl)methanone

Purified by column chromatography (10:1 PE/EA); white solid; 56% yield; Rf = 0.40 (5:1 PE/EA). 1H NMR (400 MHz, CDCl3) δ 8.97 (s, 1H), 8.52 (t, J = 5.1 Hz, 2H), 7.74 (s, 1H), 7.37–7.25 (m, 6H), 7.19–7.11 (m, 2H), 6.46 (dd, J = 2.5, 1.4 Hz, 1H), 5.41 (s, 2H). 13C NMR (100 MHz, CDCl3) δ 160.9, 143.2, 139.8, 136.3, 135.8, 129.7, 129.1, 129.0, 128.1, 126.8, 123.6, 122.9, 122.5, 110.5, 108.1, 106.7, 51.1. HRMS (ESI) m/z: calculated for C19H15N3ONa [M + Na]+ 324.1112, found 324.1111.

(1-methyl-1H-pyrrol-3-yl)(1H-pyrazol-1-yl)methanone

Purified by column chromatography (10:1 PE/EA); light red solid; 62% yield; Rf = 0.49 (5:1 PE/EA). 1H NMR (400 MHz, CDCl3) δ 8.38 (d, J = 2.4 Hz, 1H), 7.80–7.63 (m, 2H), 6.96 (s, 1H), 6.46 (dd, J = 2.7, 1.5 Hz, 1H), 6.24 (dd, J = 4.2, 2.5 Hz, 1H), 4.01 (s, 3H). 13C NMR (100 MHz, CDCl3) δ 157.7, 143.5, 132.3, 129.9, 124.6, 122.6, 109.0, 108.3, 37.7. HRMS (ESI) m/z: calculated for C9H9N3ONa [M + Na]+ 198.0643, found 198.0632.

(1-methyl-1H-indol-3-yl)(3-methyl-1H-pyrazol-1-yl)methanone

Purified by column chromatography (10:1 PE/EA); white solid; 72% yield; Rf = 0.36 (5:1 PE/EA). 1H NMR (400 MHz, CDCl3) δ 8.84 (s, 1H), 8.54–8.45 (m, 1H), 8.39 (d, J = 2.5 Hz, 1H), 7.44–7.29 (m, 3H), 6.26 (d, J = 2.5 Hz, 1H), 3.89 (s, 3H), 2.40 (s, 3H). 13C NMR (100 MHz, CDCl3) δ 160.8, 153.0, 139.8, 136.8, 130.4, 128.9, 123.3, 122.7, 122.4, 109.7, 108.6, 106.3, 33.7, 14.1. HRMS (ESI) m/z: calculated for C14H13N3ONa [M + Na]+ 262.0956, found 262.0954.

(3,5-dimethyl-1H-pyrazol-1-yl)(1-methyl-1H-indol-3-yl)methanone

Purified by column chromatography (10:1 PE/EA); light red solid; 63% yield; Rf = 0.35 (5:1 PE/EA). 1H NMR (400 MHz, CDCl3) δ 8.60 (s, 1H), 8.46 (dd, J = 6.1, 2.7 Hz, 1H), 7.33 (dt, J = 5.5, 3.9 Hz, 3H), 6.01 (s, 1H), 3.86 (s, 3H), 2.66 (s, 3H), 2.32 (s, 3H). 13C NMR (100 MHz, CDCl3) δ 163.2, 150.9, 144.7, 139.7, 136.8, 128.9, 123.1, 122.5, 122.4, 110.0, 109.6, 107.6, 33.6, 14.7, 13.9. HRMS (ESI) m/z: calculated for C15H15N3ONa [M + Na]+ 276.1112, found 276.1092.

(1H-imidazol-1-yl)(1-methyl-1H-indol-3-yl)methanone

Purified by column chromatography (2:1 PE/EA); white solid; 85% yield; Rf = 0.06 (2:1 PE/EA). 1H NMR (400 MHz, CDCl3) δ 8.19 – 8.02 (m, 2H), 7.55 (d, J = 26.8 Hz, 2H), 7.36 – 7.22 (m, 3H), 7.07 (s, 1H), 3.80 (s, 3H). 13C NMR (101 MHz, CDCl3) δ 160.73 (s), 137.38 (d, J = 7.5 Hz), 136.05 (s), 130.31 (s), 127.29 (s), 124.26 (s), 123.10 (s), 121.72 (s), 118.02 (s), 110.22 (s), 107.94 (s), 33.86 (s). HRMS (ESI) m/z: calculated for C13H11N3ONa [M + Na]+ 248.0800, found 248.0802.

(1H-benzo[d]imidazol-1-yl)(1-methyl-1H-indol-3-yl)methanone

Purified by column chromatography (2:1 PE/EA); white solid; 68% yield; Rf = 0.14 (2:1 PE/EA). 1H NMR (400 MHz, CDCl3) δ 8.39 (s, 1H), 8.08 (dd, J = 6.4, 2.5 Hz, 1H), 8.03 (d, J = 7.5 Hz, 1H), 7.75 (dd, J = 6.2, 2.3 Hz, 1H), 7.57 (s, 1H), 7.36–7.21 (m, 5H), 3.80 (s, 3H). 13C NMR (100 MHz, CDCl3) δ 160.7, 143.1, 141.7, 136.4, 134.8, 131.5, 127.8, 124.1, 123.5, 123.1, 121.9, 120.5, 119.3, 113.9, 109.2, 107.7, 32.8. HRMS (ESI) m/z: calculated for C17H13N3ONa [M + Na]+ 298.0956, found 298.0954.

(1H-benzo[d][1,2,3]triazol-1-yl)(1-methyl-1H-indol-3-yl)methanone

Purified by column chromatography (10:1 then 5:1 PE/EA); white solid; 71% yield; Rf = 0.20 (5:1 PE/EA). 1H NMR (400 MHz, CDCl3) δ 8.76 (s, 1H), 8.57–8.52 (m, 1H), 8.49 (d, J = 8.3 Hz, 1H), 8.12 (d, J = 8.3 Hz, 1H), 7.63 (dd, J = 11.4, 4.0 Hz, 1H), 7.53–7.44 (m, 1H), 7.43–7.31 (m, 3H), 3.90 (d, J = 1.3 Hz, 3H). 13C NMR (100 MHz, CDCl3) δ 160.9, 145.6, 139.8, 137.0, 132.6, 129.8, 128.6, 125.7, 123.8, 123.2, 122.3, 119.8, 115.1, 110.0, 106.4, 33.8. The spectral data obtained agree with those reported in the literature.10

(1H-indazol-1-yl)(1-methyl-1H-indol-3-yl)methanone

Purified by column chromatography (10:1 PE/EA); light red solid; 67% yield; Rf = 0.30 (5:1 PE/EA). 1H NMR (400 MHz, CDCl3) δ 8.74 (s, 1H), 8.70 (dd, J = 8.5, 0.7 Hz, 1H), 8.63–8.57 (m, 1H), 8.18 (d, J = 0.5 Hz, 1H), 7.76 (d, J = 8.0 Hz, 1H), 7.58 (ddd, J = 8.3, 7.1, 1.1 Hz, 1H), 7.39–7.31 (m, 4H), 3.90 (s, 3H). 13C NMR (100 MHz, CDCl3) δ 163.3, 140.4, 138.9, 138.7, 136.7, 129.1, 129.0, 125.6, 123.9, 123.2, 122.5 (two peaks overlapped), 120.7, 116.1, 109.7, 107.4, 33.6. HRMS (ESI) m/z: calculated for C17H13N3ONa [M + Na]+ 298.0956, found 298.0956.

1-methyl-N-phenyl-1H-indole-3-carboxamide

Purified by column chromatography (10:1 then 5:1 PE/EA); white solid; 64% yield; Rf = 0.38 (2:1 PE/EA). 1H NMR (400 MHz, CDCl3) δ 8.05 (dd, J = 6.3, 2.5 Hz, 1H), 7.74 (d, J = 10.5 Hz, 2H), 7.66 (d, J = 7.7 Hz, 2H), 7.40–7.28 (m, 5H), 7.11 (t, J = 7.4 Hz, 1H), 3.80 (s, 3H). 13C NMR (100 MHz, CDCl3) δ 163.2, 138.5, 137.4, 132.6, 130.9, 129.1, 128.9, 125.4, 123.9, 122.8, 121.8, 120.1 (two peaks overlapped), 111.1, 110.3, 33.4. The spectral data obtained agree with those reported in the literature.11

N-(4-methoxyphenyl)-1-methyl-1H-indole-3-carboxamide

Purified by column chromatography (10:1 then 5:1 PE/EA); white solid; 70% yield; Rf = 0.05 (5:1 PE/EA). 1H NMR (400 MHz, CDCl3) δ 8.05 (dd, J = 6.5, 1.9 Hz, 1H), 7.71 (s, 2H), 7.55 (d, J = 8.9 Hz, 2H), 7.44–7.27 (m, 3H), 6.93–6.86 (m, 2H), 3.80, 3.79 (6H). 13C NMR (100 MHz, CDCl3) δ 163.3, 156.3, 137.3, 132.5, 131.5, 130.9, 128.9, 125.5, 122.8, 122.1, 121.7, 120.2, 114.2, 111.0, 110.2, 55.5, 33.3. The spectral data obtained agree with those reported in the literature.12

N-(4-chlorophenyl)-1-methyl-1H-indole-3-carboxamide

Purified by column chromatography (10:1 then 5:1 PE/EA); white solid; 59% yield; Rf = 0.06 (5:1 PE/EA). 1H NMR (400 MHz, CDCl3) δ 8.03 (dd, J = 6.4, 2.0 Hz, 1H), 7.76–7.68 (m, 2H), 7.61 (d, J = 8.8 Hz, 2H), 7.42–7.37 (m, 1H), 7.37–7.28 (m, 4H), 3.82 (s, 3H). 13C NMR (100 MHz, CDCl3) δ 163.1, 137.4, 137.1, 132.7, 130.9, 129.0, 128.9, 128.8, 125.3, 122.9, 121.9, 121.2, 120.1, 110.8, 110.3, 33.4. HRMS (ESI) m/z: calculated for C16H13ClN2ONa [M + Na]+ 307.0614, found 307.0593.

1-methyl-1H-indole-3-carbonyl azide

Purified by column chromatography (10:1 PE/EA); light red solid; 86% yield; Rf = 0.30 (5:1 PE/EA). 1H NMR (400 MHz, CDCl3) δ 8.20–8.09 (m, 1H), 7.63 (s, 1H), 7.29–7.20 (m, 3H), 3.68 (s, 3H). 13C NMR (100 MHz, CDCl3) δ 167.8, 137.6, 136.5, 126.5, 123.5, 122.7, 121.7, 110.1, 108.4, 33.6. The spectral data obtained agree with those reported in the literature.12

1,5-dimethyl-1H-indole-3-carbonyl azide

Purified by column chromatography (10:1 PE/EA); light red solid; 85% yield; Rf = 0.35 (5:1 PE/EA). 1H NMR (400 MHz, CDCl3) δ 7.93 (s, 1H), 7.57 (s, 1H), 7.07 (dd, J = 26.7, 8.4 Hz, 2H), 3.64 (s, 3H), 2.39 (s, 3H). 13C NMR (100 MHz, CDCl3) δ 167.8, 136.4, 136.0, 132.5, 126.7, 125.0, 121.4, 109.7, 107.9, 33.7, 21.6. HRMS (ESI) m/z: calculated for C11H11N2O [M + H – N2]+ 187.0871, found 187.0869.

1,6-dimethyl-1H-indole-3-carbonyl azide

Purified by column chromatography (10:1 PE/EA); light red solid; 68% yield; Rf = 0.31 (5:1 PE/EA). 1H NMR (400 MHz, DMSO) δ 8.13 (s, 1H), 7.93 (d, J = 8.1 Hz, 1H), 7.37 (s, 1H), 7.12 (d, J = 8.1 Hz, 1H), 3.83 (s, 3H), 2.45 (s, 3H). 13C NMR (100 MHz, DMSO) δ 166.7, 137.9, 137.5, 132.6, 124.1, 123.6, 120.2, 110.9, 106.6, 33.2, 21.3. HRMS (ESI) m/z: calculated for C11H11N2O [M + H – N2]+ 187.0871, found 187.0868.

1,7-dimethyl-1H-indole-3-carbonyl azide

Purified by column chromatography (10:1 PE/EA); light red solid; 92% yield; Rf = 0.38 (5:1 PE/EA). 1H NMR (400 MHz, DMSO) δ 8.12 (s, 1H), 7.93 (d, J = 7.9 Hz, 1H), 7.12 (t, J = 7.6 Hz, 1H), 7.00 (d, J = 7.2 Hz, 1H), 4.10 (s, 3H), 2.72 (s, 3H). 13C NMR (100 MHz, DMSO) δ 166.6, 139.3, 136.1, 127.0, 125.7, 122.8, 122.6, 118.6, 106.1, 37.3, 18.8. HRMS (ESI) m/z: calculated for C11H11N2O [M + H – N2]+ 187.0871, found 187.0868.

1,2-dimethyl-1H-indole-3-carbonyl azide

Purified by column chromatography (10:1 PE/EA); light red solid; 71% yield; Rf = 0.39 (5:1 PE/EA). 1H NMR (400 MHz, DMSO) δ 8.12–8.03 (m, 1H), 7.59–7.50 (m, 1H), 7.27–7.18 (m, 2H), 3.72 (s, 3H), 2.73 (s, 3H). 13C NMR (100 MHz, DMSO) δ 167.7, 147.9, 136.5, 125.5, 122.3, 122.0, 120.5, 110.4, 104.0, 29.8, 12.0. HRMS (ESI) m/z: calculated for C11H10N2ONa [M + Na – N2]+ 209.0690, found 209.0684.

5-methoxy-1-methyl-1H-indole-3-carbonyl azide

Purified by column chromatography (10:1 PE/EA); light red solid; 66% yield; Rf = 0.23 (5:1 PE/EA). 1H NMR (400 MHz, DMSO) δ 8.12 (s, 1H), 7.53 (d, J = 2.4 Hz, 1H), 7.47 (d, J = 8.9 Hz, 1H), 6.94 (dd, J = 8.9, 2.5 Hz, 1H), 3.83 (s, 3H), 3.81 (s, 3H). 13C NMR (100 MHz, DMSO) δ 166.7, 155.9, 137.8, 132.5, 126.7, 112.8, 112.1, 106.2, 102.3, 55.3, 33.4. HRMS (ESI) m/z: calculated for C11H11N2O2 [M + H – N2]+ 203.0820, found 203.0809.

5-cyano-1-methyl-1H-indole-3-carbonyl azide

Purified by column chromatography (10:1 PE/EA); light red solid; 49% yield; Rf = 0.11 (5:1 PE/EA). 1H NMR (400 MHz, DMSO) δ 8.46 (s, 1H), 8.40 (d, J = 0.7 Hz, 1H), 7.82 (d, J = 8.6 Hz, 1H), 7.72 (dd, J = 8.6, 1.2 Hz, 1H), 3.93 (s, 3H). 13C NMR (100 MHz, DMSO) δ 166.9, 140.2, 139.2, 126.0, 125.4 (two peaks overlapped), 119.8, 112.9, 107.3, 104.7, 33.6. HRMS (ESI) m/z: calculated for C11H8N3O [M + H – N2]+ 198.0667, found 198.0662.

6-bromo-1-methyl-1H-indole-3-carbonyl azide

Purified by column chromatography (10:1 PE/EA); light red solid; 61% yield; Rf = 0.43 (5:1 PE/EA). 1H NMR (400 MHz, DMSO) δ 8.21 (s, 1H), 7.94 (d, J = 8.5 Hz, 1H), 7.85 (d, J = 1.5 Hz, 1H), 7.40 (dd, J = 8.5, 1.7 Hz, 1H), 3.85 (s, 3H). 13C NMR (100 MHz, DMSO) δ 166.8, 138.6, 138.4, 125.3, 124.7, 122.1, 115.9, 114.2, 106.8, 33.5. HRMS (ESI) m/z: calculated for C10H8BrN2O [M + H – N2]+ 250.9820, found 250.9821.

6-chloro-1-methyl-1H-indole-3-carbonyl azide

Purified by column chromatography (10:1 PE/EA); light red solid; 68% yield; Rf = 0.30 (5:1 PE/EA). 1H NMR (400 MHz, DMSO) δ 8.24 (s, 1H), 8.01 (d, J = 8.5 Hz, 1H), 7.73 (d, J = 1.4 Hz, 1H), 7.30 (dd, J = 8.5, 1.5 Hz, 1H), 3.86 (s, 3H). 13C NMR (100 MHz, DMSO) δ 166.8, 138.8, 138.0, 127.9, 124.4, 122.7, 121.8, 111.3, 106.8, 33.5. HRMS (ESI) m/z: calculated for C10H8BrN2O [M + H – N2]+ 207.0325, found 207.0316.

1-methyl-1H-pyrrolo[2,3-b]pyridine-3-carbonyl azide

Purified by column chromatography (10:1 PE/EA); light red solid; 69% yield; Rf = 0.15 (5:1 PE/EA). 1H NMR (400 MHz, DMSO) δ 8.48–8.39 (m, 2H), 8.36 (dd, J = 7.9, 1.3 Hz, 1H), 7.35 (dd, J = 7.9, 4.7 Hz, 1H), 3.90 (s, 3H). 13C NMR (100 MHz, DMSO) δ 166.8, 148.0, 144.3, 138.1, 129.0, 118.6, 118.1, 105.2, 31.6. HRMS (ESI) m/z: calculated for C9H7N3ONa [M + Na – N2]+ 196.0487, found 196.0486.

1-allyl-1H-indole-3-carbonyl azide

Purified by column chromatography (10:1 PE/EA); light red solid; 66% yield; Rf = 0.6 (5:1 PE/EA). 1H NMR (400 MHz, DMSO) δ 8.26 (s, 1H), 8.09 (dt, J = 5.0, 2.8 Hz, 1H), 7.59 (dd, J = 6.0, 2.8 Hz, 1H), 7.36–7.23 (m, 2H), 6.03 (dq, J = 10.5, 5.6 Hz, 1H), 5.22 (dd, J = 10.3, 1.3 Hz, 1H), 5.11 (dd, J = 17.1, 1.5 Hz, 1H), 4.95 (d, J = 5.5 Hz, 2H). 13C NMR (100 MHz, DMSO) δ 166.9, 137.2, 136.8, 133.2, 125.9, 123.2, 122.6, 120.7, 117.9, 111.6, 107.1, 48.7. HRMS (ESI) m/z: calculated for C12H11N2O [M + H – N2]+ 199.0871, found 199.0869.

1-allyl-5-methyl-1H-indole-3-carbonyl azide

Purified by column chromatography (10:1 PE/EA); light red solid; 83% yield; Rf = 0.34 (5:1 PE/EA). 1H NMR (400 MHz, DMSO) δ 8.19 (s, 1H), 7.89 (s, 1H), 7.45 (d, J = 8.4 Hz, 1H), 7.12 (dd, J = 8.4, 1.2 Hz, 1H), 6.02 (m, 1H), 5.20 (dd, J = 10.3, 1.3 Hz, 1H), 5.09 (dd, J = 17.1, 1.4 Hz, 1H), 4.91 (d, J = 5.5 Hz, 2H), 2.43 (s, 3H). 13C NMR (100 MHz, DMSO) δ 166.8, 137.0, 135.2, 133.3, 131.6, 126.2, 124.7, 120.4, 117.7, 111.3, 106.7, 48.7, 21.2. HRMS (ESI) m/z: calculated for C13H13N2O [M + H – N2]+ 213.1028, found 213.1027.

1-allyl-6-bromo-1H-indole-3-carbonyl azide

Purified by column chromatography (10:1 PE/EA); light red solid; 61% yield; Rf = 0.44 (5:1 PE/EA). 1H NMR (400 MHz, DMSO) δ 8.30 (s, 1H), 8.18 (d, J = 1.9 Hz, 1H), 7.57 (d, J = 8.8 Hz, 1H), 7.44 (dd, J = 8.8, 2.0 Hz, 1H), 6.02 (qd, J = 10.6, 5.5 Hz, 1H), 5.22 (dd, J = 10.3, 1.3 Hz, 1H), 5.09 (dd, J = 17.1, 1.4 Hz, 1H), 4.95 (d, J = 5.5 Hz, 2H). 13C NMR (100 MHz, DMSO) δ 166.9, 138.1, 135.6, 133.0, 127.5, 125.8, 122.8, 118.0, 115.4, 113.8, 106.7, 48.9. HRMS (ESI) m/z: calculated for C12H10BrN2O [M + H – N2]+ 276.9976, found 276.9971.

methyl 1-allyl-3-(azidocarbonyl)-1H-indole-5-carboxylate

Purified by column chromatography (10:1 then 5:1 PE/EA); light red solid; 47% yield; Rf = 0.29 (5:1 PE/EA). 1H NMR (400 MHz, DMSO) δ 8.76–8.70 (m, 1H), 8.38 (s, 1H), 7.90 (dd, J = 8.7, 1.7 Hz, 1H), 7.69 (d, J = 8.7 Hz, 1H), 6.04 (qd, J = 10.6, 5.5 Hz, 1H), 5.23 (dd, J = 10.3, 1.3 Hz, 1H), 5.11 (dd, J = 17.1, 1.4 Hz, 1H), 4.99 (d, J = 5.5 Hz, 2H), 3.89 (s, 3H). 13C NMR (100 MHz, DMSO) δ 167.0, 166.6, 139.2, 138.9, 133.0, 125.4, 123.9 (two peaks overlapped), 122.7, 118.1, 111.8, 108.2, 52.0, 48.9. HRMS (ESI) m/z: calculated for C14H13N2O3 [M + H – N2]+ 257.0926, found 257.0923.

1-benzyl-1H-indole-3-carbonyl azide

Purified by column chromatography (10:1 PE/EA); light red solid; 81% yield; Rf = 0.42 (5:1 PE/EA). 1H NMR (400 MHz, DMSO) δ 8.46 (s, 1H), 8.09 (dd, J = 6.4, 2.8 Hz, 1H), 7.60 (dd, J = 6.7, 2.6 Hz, 1H), 7.42–7.20 (m, 7H), 5.55 (s, 2H). 13C NMR (100 MHz, DMSO) δ 167.0, 137.4, 136.7, 136.6, 128.7, 127.8, 127.4, 126.1, 123.3, 122.6, 120.7, 111.7, 107.3, 49.8. The spectral data obtained agree with those reported in the literature.13

1-methyl-1H-indole-3-carbonyl cyanide

Purified by column chromatography (10:1 then 5:1 PE/EA); light red solid; 82% yield; Rf = 0.24 (5:1 PE/EA). 1H NMR (400 MHz, DMSO) δ 8.69 (s, 1H), 8.05 (d, J = 7.3 Hz, 1H), 7.67 (d, J = 7.9 Hz, 1H), 7.47–7.34 (m, 2H), 3.97 (s, 3H). 13C NMR (100 MHz, DMSO) δ 157.8, 144.2, 138.3, 124.9, 124.5, 124.2, 121.0, 115.0, 114.3, 111.9, 33.9. The spectral data obtained agree with those reported in the literature.14

1,4-dimethyl-1H-indole-3-carbonyl cyanide

Purified by column chromatography (10:1 then 5:1 PE/EA); light red solid; 81% yield; Rf = 0.23 (5:1 PE/EA). 1H NMR (400 MHz, CDCl3) δ 8.06 (s, 1H), 7.29–7.20 (m, 1H), 7.14 (d, J = 8.2 Hz, 1H), 7.07 (d, J = 7.3 Hz, 1H), 3.84 (s, 3H), 2.78 (s, 3H). 13C NMR (100 MHz, CDCl3) δ 158.2, 144.4, 139.4, 134.1, 126.3, 125.5, 124.4, 117.6, 115.0, 107.9, 34.4, 22.8. GCMS (EI): m/z for C12H10N2O [M]+ 198.1.

1,5-dimethyl-1H-indole-3-carbonyl cyanide

Purified by column chromatography (10:1 PE/EA); light red solid; 85% yield; Rf = 0.25 (5:1 PE/EA). 1H NMR (400 MHz, DMSO) δ 8.63 (s, 1H), 7.86 (s, 1H), 7.56 (d, J = 8.4 Hz, 1H), 7.26 (d, J = 8.3 Hz, 1H), 3.94 (s, 3H), 2.44 (s, 3H). 13C NMR (100 MHz, DMSO) δ 162.89 (s), 149.22 (s), 141.94 (s), 138.93 (s), 131.53 (s), 130.10 (s), 126.12 (s), 119.98 (s), 119.63 (s), 116.82 (s), 45.20 (s), 44.99 (s), 44.78 (s), 44.57 (s), 44.36 (s), 26.34 (s). GCMS (EI): m/z for C12H10N2O [M]+ 198.1.

1,6-dimethyl-1H-indole-3-carbonyl cyanide

Purified by column chromatography (10:1 then 5:1 PE/EA); light red solid; 71% yield; Rf = 0.27 (5:1 PE/EA). 1H NMR (400 MHz, DMSO) δ 8.57 (s, 1H), 7.88 (d, J = 8.0 Hz, 1H), 7.44 (s, 1H), 7.19 (d, J = 8.0 Hz, 1H), 3.91 (s, 3H), 2.45 (s, 3H). 13C NMR (100 MHz, DMSO) δ 157.6, 143.8, 138.6, 134.6, 125.6, 122.3, 120.7, 115.0, 114.3, 111.6, 33.7, 21.3. GCMS (EI): m/z for C12H10N2O [M]+ 198.1.

1,7-dimethyl-1H-indole-3-carbonyl cyanide

Purified by column chromatography (10:1 then 5:1 PE/EA); light red solid; 83% yield; Rf = 0.22 (5:1 PE/EA). 1H NMR (400 MHz, DMSO) δ 8.56 (s, 1H), 7.89 (d, J = 7.7 Hz, 1H), 7.21 (t, J = 7.6 Hz, 1H), 7.11 (d, J = 7.2 Hz, 1H), 4.18 (s, 3H), 2.73 (s, 3H). 13C NMR (100 MHz, DMSO) δ 157.5, 145.2, 136.8, 127.5, 125.7, 124.3, 123.6, 119.1, 114.5, 114.3, 37.8, 18.6. GCMS (EI): m/z for C12H10N2O [M]+ 198.1.

1,2-dimethyl-1H-indole-3-carbonyl cyanide

Purified by column chromatography (10:1 then 5:1 PE/EA); light red solid; 60% yield; Rf = 0.17 (5:1 PE/EA). 1H NMR (400 MHz, DMSO) δ 8.13 (dd, J = 5.9, 3.0 Hz, 1H), 7.67 (dd, J = 6.1, 2.9 Hz, 1H), 7.39–7.31 (m, 2H), 3.80 (s, 3H), 3.36 (s, 3H). 13C NMR (100 MHz, CDCl3) δ 163.0, 157.0, 142.1, 130.2, 129.2, 129.1, 124.8, 120.8, 116.5, 35.6, 17.3. GCMS (EI): m/z for C12H10N2O [M]+ 198.1.

5-methoxy-1-methyl-1H-indole-3-carbonyl cyanide

Purified by column chromatography (10:1 then 5:1 PE/EA); light red solid; 79% yield; Rf = 0.16 (5:1 PE/EA). 1H NMR (400 MHz, DMSO) δ 8.59 (s, 1H), 7.57 (d, J = 8.9 Hz, 1H), 7.49 (s, 1H), 7.03 (dd, J = 8.8, 1.6 Hz, 1H), 3.93 (s, 3H), 3.81 (s, 3H). 13C NMR (100 MHz, DMSO) δ 157.5, 157.1, 143.6, 133.0, 125.6, 114.8, 114.3, 114.2, 112.9, 103.1, 55.4, 34.0. GCMS (EI): m/z for C12H10N2O2 [M]+ 214.1.

6-bromo-1-methyl-1H-indole-3-carbonyl cyanide

Purified by column chromatography (10:1 then 5:1 PE/EA); light red solid; 63% yield; Rf = 0.23 (5:1 PE/EA). 1H NMR (400 MHz, DMSO) δ 8.72 (s, 1H), 7.98–7.93 (m, 2H), 7.52 (dd, J = 8.4, 1.6 Hz, 1H), 3.96 (s, 3H). 13C NMR (100 MHz, DMSO) δ 158.0, 144.7, 139.1, 127.0, 123.5, 122.5, 117.5, 115.0, 114.8, 114.1, 34.0. GCMS (EI): m/z for C11H7BrN2O [M]+ 262.0.

6-chloro-1-methyl-1H-indole-3-carbonyl cyanide

Purified by column chromatography (10:1 then 5:1 PE/EA); light red solid; 71% yield; Rf = 0.20 (5:1 PE/EA). 1H NMR (400 MHz, DMSO) δ 8.73 (s, 1H), 7.99 (d, J = 8.4 Hz, 1H), 7.84 (d, J = 1.7 Hz, 1H), 7.39 (dd, J = 8.4, 1.8 Hz, 1H), 3.95 (s, 3H). 13C NMR (100 MHz, DMSO) δ 158.0, 144.9, 138.8, 129.5, 124.4, 123.2, 122.2, 114.8, 114.1, 112.2, 34.0. GCMS (EI): m/z for C11H7ClN2O [M]+ 218.0.

1-methyl-1H-pyrrolo[2,3-b]pyridine-3-carbonyl cyanide

Purified by column chromatography (10:1 then 5:1 PE/EA); light red solid; 55% yield; Rf = 0.12 (5:1 PE/EA). 1H NMR (400 MHz, DMSO) δ 8.95 (s, 1H), 8.52 (dd, J = 4.7, 1.3 Hz, 1H), 8.39 (dd, J = 7.8, 1.3 Hz, 1H), 7.45 (dd, J = 7.8, 4.7 Hz, 1H), 3.98 (s, 3H). 13C NMR (100 MHz, DMSO) δ 158.4, 148.8, 145.9, 144.3, 129.7, 120.1, 117.1, 113.9, 113.1, 32.2. GCMS (EI): m/z for C10H7N3O [M]+ 185.1.

1-allyl-1H-indole-3-carbonyl cyanide

Purified by column chromatography (10:1 PE/EA); light red solid; 67% yield; Rf = 0.36 (5:1 PE/EA). 1H NMR (400 MHz, DMSO) δ 8.73 (s, 1H), 8.12–7.99 (m, 1H), 7.67 (d, J = 7.7 Hz, 1H), 7.42–7.38 (m, 2H), 6.11–6.04 (m, 1H), 5.31–5.16 (m, 2H), 5.06 (d, J = 5.6 Hz, 2H). 13C NMR (100 MHz, DMSO) δ 158.1, 143.4, 137.5, 132.7, 125.0, 124.7, 124.2, 121.2, 118.5, 115.4, 114.3, 112.3, 49.3. GCMS (EI): m/z for C13H10N2O [M]+ 210.1.

1-allyl-5-methyl-1H-indole-3-carbonyl cyanide

Purified by column chromatography (10:1 PE/EA); light red solid; 75% yield; Rf = 0.34 (5:1 PE/EA). 1H NMR (400 MHz, CDCl3) δ 8.06, 8.02 (s, 2H), 7.33–7.18 (m, 2H), 6.07–6.00 (m, 1H), 5.40 (d, J = 10.2 Hz, 1H), 5.27 (d, J = 17.1 Hz, 1H), 4.81 (d, J = 5.6 Hz, 2H), 2.49 (s, 3H). 13C NMR (100 MHz, CDCl3) δ 158.7, 140.5, 136.0, 134.6, 130.8, 126.8, 125.6, 122.4, 120.1, 116.6, 114.1, 110.6, 50.1, 21.5. GCMS (EI): m/z for C14H12N2O [M]+ 224.1.

1-allyl-6-bromo-1H-indole-3-carbonyl cyanide

Purified by column chromatography (10:1 PE/EA); light red solid; 57% yield; Rf = 0.40 (5:1 PE/EA). 1H NMR (400 MHz, CDCl3) δ 8.41 (d, J = 1.9 Hz, 1H), 8.06 (s, 1H), 7.49 (d, J = 8.8 Hz, 1H), 7.29 (dd, J = 8.8, 2.0 Hz, 1H), 6.07–6.00 (m, 1H), 5.44 (dd, J = 10.3, 1.3 Hz, 1H), 5.30 (dd, J = 17.1, 1.4 Hz, 1H), 4.83 (d, J = 5.6 Hz, 2H). 13C NMR (100 MHz, CDCl3) δ 158.7, 140.7, 136.3, 130.4, 128.5, 126.8, 125.2, 120.5, 118.3, 116.3, 113.7, 112.3, 50.3. GCMS (EI): m/z for C13H9BrN2O [M]+ 288.0.

1-benzyl-1H-indole-3-carbonyl cyanide

Purified by column chromatography (10:1 PE/EA); light red solid; 77% yield; Rf = 0.36 (5:1 PE/EA). 1H NMR (400 MHz, DMSO) δ 8.98 (s, 1H), 8.14–8.02 (m, 1H), 7.66 (dd, J = 6.2, 2.7 Hz, 1H), 7.42–7.28 (m, 7H), 5.66 (s, 2H). 13C NMR (100 MHz, DMSO) δ 158.3, 143.6, 137.4, 136.0, 128.8, 128.0, 127.5, 125.0, 124.9, 124.3, 121.3, 115.5, 114.3, 112.5, 50.3. GCMS (EI): m/z for C17H12N2O [M]+ 260.1.

1H-indole-3-carbonyl cyanide

Purified by column chromatography (10:1 then 5:1 PE/EA); light red solid; 59% yield; Rf = 0.51 (2:1 PE/EA). 1H NMR (400 MHz, DMSO) δ 12.93 (s, 1H), 8.65 (s, 1H), 8.10–8.00 (m, 1H), 7.59 (d, J = 7.2 Hz, 1H), 7.39–7.32 (m, 2H). 13C NMR (100 MHz, CDCl3) δ 163.8, 146.7, 142.8, 130.2, 129.4, 129.1, 126.2, 121.4, 119.6, 118.6. The spectral data obtained agree with those reported in the literature.14

Supplementary Note 2

1H NMR and 13C NMR Copies of Products

Supplementary Figure 15. 1H and 13C NMR spectrum for A

Supplementary Figure 16. 1H and 13C NMR spectrum for 3aa

Supplementary Figure 17. 1H and 13C NMR spectrum for 3ba

Supplementary Figure 18. 1H and 13C NMR spectrum for 3ca

Supplementary Figure 19. 1H and 13C NMR spectrum for 3da

Supplementary Figure 20. 1H and 13C NMR spectrum for 3ea

Supplementary Figure 21. 1H and 13C NMR spectrum for 3fa

Supplementary Figure 22. 1H and 13C NMR spectrum for 3ga

Supplementary Figure 23. 1H and 13C NMR spectrum for 3ha

Supplementary Figure 24. 1H and 13C NMR spectrum for 3ia

Supplementary Figure 25. 1H and 13C NMR spectrum for 3ja

Supplementary Figure 26. 1H and 13C NMR spectrum for 3ka

Supplementary Figure 27. 1H and 13C NMR spectrum for 3la

Supplementary Figure 28. 1H and 13C NMR spectrum for 3ma

Supplementary Figure 29. 1H and 13C NMR spectrum for 3ab

Supplementary Figure 30. 1H and 13C NMR spectrum for 3ac

Supplementary Figure 31. 1H and 13C NMR spectrum for 3ad

Supplementary Figure 32. 1H and 13C NMR spectrum for 3ae

Supplementary Figure 33. 1H and 13C NMR spectrum for 3af

Supplementary Figure 34. 1H and 13C NMR spectrum for 3ag

Supplementary Figure 35. 1H and 13C NMR spectrum for 3ah

Supplementary Figure 36. 1H and 13C NMR spectrum for 3ai

Supplementary Figure 37. 1H and 13C NMR spectrum for 3aj

Supplementary Figure 38. 1H and 13C NMR spectrum for 4a

Supplementary Figure 39. 1H and 13C NMR spectrum for 4b

Supplementary Figure 40. 1H and 13C NMR spectrum for 4c

Supplementary Figure 41. 1H and 13C NMR spectrum for 4d

Supplementary Figure 42. 1H and 13C NMR spectrum for 4e

Supplementary Figure 43. 1H and 13C NMR spectrum for 4f

Supplementary Figure 44. 1H and 13C NMR spectrum for 4g

Supplementary Figure 45. 1H and 13C NMR spectrum for 4h

Supplementary Figure 46. 1H and 13C NMR spectrum for 4i

Supplementary Figure 47. 1H and 13C NMR spectrum for 4j

Supplementary Figure 48. 1H and 13C NMR spectrum for 4k

Supplementary Figure 49. 1H and 13C NMR spectrum for 4l

Supplementary Figure 50. 1H and 13C NMR spectrum for 4m

Supplementary Figure 51. 1H and 13C NMR spectrum for 4n

Supplementary Figure 52. 1H and 13C NMR spectrum for 4o

Supplementary Figure 53. 1H and 13C NMR spectrum for 5a

Supplementary Figure 54. 1H and 13C NMR spectrum for 5b

Supplementary Figure 55. 1H and 13C NMR spectrum for 5c

Supplementary Figure 56. 1H and 13C NMR spectrum for 5d

Supplementary Figure 57. 1H and 13C NMR spectrum for 5e

Supplementary Figure 58. 1H and 13C NMR spectrum for 5f

Supplementary Figure 59. 1H and 13C NMR spectrum for 5g

Supplementary Figure 60. 1H and 13C NMR spectrum for 5h

Supplementary Figure 61. 1H and 13C NMR spectrum for 5i

Supplementary Figure 62. 1H and 13C NMR spectrum for 5j

Supplementary Figure 63. 1H and 13C NMR spectrum for 5k

Supplementary Figure 64. 1H and 13C NMR spectrum for 5l

Supplementary Figure 65. 1H and 13C NMR spectrum for 5m

Supplementary Figure 66. 1H and 13C NMR spectrum for 5n

Supplementary Figure 67. 1H and 13C NMR spectrum for 5o

References

- Li B, Guan Z, Wang W, Yang X, Hu J, Tan B, Li T. Highly Dispersed Pd Catalyst Locked in Knitting Aryl Network Polymers for Suzuki–Miyaura Coupling Reactions of Aryl Chlorides in Aqueous Media. Adv. Mater. 24, 3390-3395 (2012).

- Bukhryakov KV, Mugemana C, Vu KB, Rodionov VO. Palladium N-Heterocyclic Carbene Precatalyst Site Isolated in the Core of a Star Polymer. Org. Lett. 17, 4826-4829 (2015).

- Sashuk V, Schoeps D, Plenio H. Fluorophore Tagged Cross-Coupling Catalysts. Chem. Commun. 770-772 (2009).

- Wang W, Zheng A, Zhao P, Xia C, Li F. Au-NHC@Porous Organic Polymers: Synthetic Control and Its Catalytic Application in Alkyne Hydration Reactions. ACS Catal. 4, 321-327 (2014).

- Medri V, Martelli S, Landi E, Esposito L. Alkali Inorganic Binders for The Production of Fibre Based Foams. Ceram. Int. 40, 10131-10136 (2014).

- Patel MA, Luo F, Khoshi MR, Rabie E, Zhang Q, Flach CR, Mendelsohn R, Garfunkel E, Szostak M, He H. P-Doped Porous Carbon as Metal Free Catalysts for Selective Aerobic Oxidation with an Unexpected Mechanism. ACS Nano 10, 2305-2315 (2016).

- Koh K, Jeon M, Chevrier DM, Zhang P, Yoon CW, Asefa T. Novel Nanoporous N-Doped Carbon-Supported Ultrasmall Pd Nanoparticles: Efficient Catalysts for Hydrogen Storage and Release. Appl. Catal. B: Environ. 203, 820-828 (2017).

- Cheng T, Chen J, Cai A, Wang J, Liu H, Hu Y, Bao X, Yuan P. Synthesis of Pd/SiO2 Catalysts in Various HCl Concentrations for Selective NBR Hydrogenation: Effects of H+ and Cl– Concentrations and Electrostatic Interactions. ACS Omega 3, 6651-6659 (2018).

- Ogiwara Y, Sakurai Y, Hattori H, Sakai N. Palladium-Catalyzed Reductive Conversion of Acyl Fluorides via Ligand-Controlled Decarbonylation. Org. Lett. 20, 4204-4208 (2018).

- Agarwal PK, Dathi MD, Saifuddin M and Kundu B. Engineering of indole-based tethered biheterocyclic alkaloid meridianin into β-carboline-derived tetracyclic polyheterocycles via amino functionalization/6-endo cationic π-cyclization. Beilstein J. Org. Chem. 8, 1901–1908 (2012).

- Sauer DR, Kalvin D, Phelan KM. Microwave-Assisted Synthesis Utilizing Supported Reagents:  A Rapid and Efficient Acylation Procedure. Org. Lett. 5, 4721-4724 (2003).

- Reekie TA, Wilkinson SM, Law V, Hibbs DE, Ong JA, Kassiou M. Rapid access to N-(indol-2-yl)amides and N-(indol-3-yl)amides as unexplored pharmacophores. Org. Biomol. Chem. 15, 576-580 (2017).

- Abdel R, Farghaly AH. Synthesis, Reactions and Antimicrobial Activity of Some New Indolyl-1,3,4-Oxadiazole, Triazole and Pyrazole Derivatives. J. Chin. Chem. Soc. 51, 147-156 (2004).

- Veale CGL. A new synthesis of versatile indolyl-3-carbonylnitriles. Tetrahedron Lett. 56, 5287-5290 (2015).