Table 2  Optimization of the reaction conditions for the synthesis of 1,4-dihydropyridines under the catalysis of the UiO-66-NH2-CC@Cu(II) nanocatalyst a

| Entry | Catalyst (g) | Solvent | Temperature (°C) | Time (min) | Yield (%)b |
| --- | --- | --- | --- | --- | --- |
| 1 | UiO-66-NH2-CC@Cu(II) (0.02) | Solvent free | 80 | 20 | 89 |
| 2 | UiO-66-NH2-CC@Cu(II) (0.02) | H2O | 80 | 30 | 49 |
| 3 | UiO-66-NH2-CC@Cu(II) (0.02) | DMF | 80 | 20 | 75 |
| 4 | UiO-66-NH2-CC@Cu(II) (0.02) | CH3CN | 80 | 20 | 56 |
| 5 | UiO-66-NH2-CC@Cu(II) (0.02) | THF | 66 | 20 | 35 |
| 6 | UiO-66-NH2-CC@Cu(II) (0.02)) | Toluene | 80 | 60 | 30 |
| 7 | UiO-66-NH2-CC@Cu(II) (0.02) | MeOH | 64.7 | 20 | 55 |
| 8 | UiO-66-NH2-CC@Cu(II) (0.02) | EtOH | 80 | 20 | 96 |
| 9 | UiO-66-NH2-CC@Cu(II) (0) | EtOH | 80 | 2880 | trace |
| 10 | UiO-66-NH2-CC@Cu(II) (0.007) | EtOH | 80 | 20 | 65 |
| 11 | UiO-66-NH2-CC@Cu(II) (0.01) | EtOH | 80 | 20 | 73 |
| 12 | UiO-66-NH2-CC@Cu(II) (0.015) | EtOH | 80 | 20 | 84 |
| 13 | UiO-66-NH2-CC@Cu(II) (0.02) | EtOH | 25 | 20 | 35 |
| 14 | UiO-66-NH2-CC@Cu(II) (0.02) | EtOH | 60 | 20 | 78 |
| 15 | UiO-66-NH2 (0.02) | EtOH | 80 | 20 | 31 |
| 16 | Cu(II) pincer complex (0.02) | EtOH | 80 | 20 | 59 |

aReaction condition: benzaldehyde (1 mmol), ethyl acetoacetate (2 mmol), ammonium acetate (1 mmol), 2 mL of solvent, and catalyst. bIsolated yield

Table 3  Synthesis of 1,4-dihydropyridine derivatives catalyzed by the UiO-66-NH2-CC@Cu(II) nanocatalyst a

| Entry | Aldehyde | Product | Time | Yield (%)b | MP (°C) |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | Observed | Literature |
| 1 |  |  | 15 | 95 | 146-147 | 145–147 [49] |
| 2 |  |  | 20 | 93 | 115-117 | 115-117 [50] |
| 3 |  |  | 15 | 95 | 159-161 | 160-162 [51] |
| 4 |  |  | 25 | 90 | 156-158 | 156–158 [51] |
| 5 |  |  | 15 | 93 | 128-130 | 127‐129 [52] |
| 6 |  |  | 20 | 90 | 136-138 | 135–137 [53] |
| 7 |  |  | 25 | 93 | 156-158 | 155–157 [51] |
| 8 |  |  | 25 | 92 | 227-228 | 226-228 [51] |
| 9 |  |  | 20 | 89 | 162-164 | 161–163 [54] |
| 10 |  |  | 25 | 90 | 167-170 | 168–170 [49] |
| 11 |  |  | 20 | 96 | 156-158 | 156–158 [53] |

a Reaction conditions: aldehyde (1 mmol), ethyl acetoacetate (2 mmol), ammonium acetate (1 mmol), UiO-66-NH2-CC@Cu(II) nanocatalyst (0.02 g), EtOH (2 mL), and temperature (80 °C). b Isolated yield

Table 4  Optimization of the reaction conditions for the synthesis of  3,4-dihydropyrimidinones under the catalysis of the UiO-66-NH2-CC@Cu(II) nanocatalyst a

| Entry | Catalyst (g) | Solvent | Temperature (°C) | Time (min) | Yield (%)b |
| --- | --- | --- | --- | --- | --- |
| 1 | UiO-66-NH2-CC@Cu(II) (0.007) | EtOH | 70 | 90 | 65 |
| 2 | UiO-66-NH2-CC@Cu(II) (0.01) | EtOH | 70 | 40 | 75 |
| 3 | UiO-66-NH2-CC@Cu(II) (0.02) | EtOH | 70 | 35 | 86 |
| 4 | UiO-66-NH2-CC@Cu(II) (0.025) | EtOH | 70 | 35 | 95 |
| 5 | UiO-66-NH2-CC@Cu(II) (0.03) | EtOH | 70 | 35 | 95 |
| 6 | UiO-66-NH2-CC@Cu(II) (0.025) | EtOH | 25 | 60 | 50 |
| 7 | UiO-66-NH2-CC@Cu(II) (0.025) | EtOH | 60 | 35 | 80 |
| 8 | UiO-66-NH2-CC@Cu(II) (0.025) | EtOH | reflux | 35 | 95 |
| 9 | UiO-66-NH2-CC@Cu(II) (0.025) | EtOH | 70 | 20 | 75 |
| 10 | UiO-66-NH2-CC@Cu(II) (0.025) | EtOH | 70 | 60 | 95 |
| 11 | UiO-66-NH2-CC@Cu(II) (0.025) | H2O | 90 | 35 | 40 |
| 12 | UiO-66-NH2-CC@Cu(II) (0.025) | EtOH/H2O | 70 | 35 | 75 |
| 13 | UiO-66-NH2-CC@Cu(II) (0.025) | DMF | 70 | 35 | 88 |
| 14 | UiO-66-NH2-CC@Cu(II) (0.025) | PEG | 70 | 35 | 65 |
| 15 | UiO-66-NH2-CC@Cu(II) (0.025g) | MeOH | reflux | 35 | 55 |
| 16 | UiO-66-NH2-CC@Cu(II) (0.025) | Toluene | 70 | 5h | 20 |
| 17 | UiO-66-NH2-CC@Cu(II) (0.025) | Solvent free | 70 | 35 | 69 |
| 18 | UiO-66-NH2 (0.025) | EtOH | 70 | 35 | 65 |
| 19 | UiO-66-NH2-CC@Cu(II) (0.025) | EtOH | 70 | 35 | 33 |

aReaction condition: 4-chlorobenzaldhyde (1mmol), urea (1mmol), ethlacetoacetate (1 mmol), 2 ml solvent, and       catalyst. bIsolated yield.

Table 5  Synthesis of 3,4-dihydropyrimidinone derivatives catalyzed by the UiO-66-NH2-CC@Cu(II) nanocatalyst a

| Entry | Aldehyde | Product | Time | Yield (%)b | MP (°C) |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | Observed | Literature |
| 1 |  |  | 35 | 95 | 212-214 | 212-214 [56] |
| 2 |  |  | 30 | 90 | 200-201 | 198‐200 [57] |
| 3 |  |  | 40 | 93 | 210-212 | 211-213 [56] |
| 4 |  |  | 25 | 91 | 225-227 | 225–226 [58] |
| 5 |  |  | 35 | 93 | 208-210 | 207‐209 [58] |
| 6 |  |  | 50 | 90 | 211-213 | 212–214 [56] |
| 7 |  |  | 40 | 93 | 203-205 | 203-204 [54] |
| 8 |  |  | 40 | 93 | 210-211 | 208-210 [56] |
| 9 |  |  | 35 | 90 | 209-211 | 209-211 [59] |
| 10 |  |  | 30 | 90 | 216-218 | 215-217 [60] |
| 11 |  |  | 40 | 95 | 203-204 | 202–204 [56] |
| 12 |  |  | 40 | 91 | 237-239 | 236-238 [56] |
| 13 |  |  | 45 | 90 | 177-178 | 173-176 [61] |

a Reaction conditions: aldehyde (1 mmol), urea (1 mmol), ethylacetoacetate (1 mmol), the UiO-66-NH2-CC@Cu(II) nanocatalyst (0.025 g), temperature (70 °C), EtOH (2 mL). bIsolated yield