Supplementary Information

Living microbial cement supercapacitors with reactivatable energy storage

Qi Luo1✉, Zhongmin Li2, Yongxin Li2, Mikhail Petrov3

1Department of Civil and Architectural Engineering, Aarhus University, Aarhus C 8000, Denmark.

2School of Civil Engineering, Chongqing Jiaotong University, Chongqing 400074, PR China.

3Department of Biological and Chemical Engineering, Aarhus University, Aabogade 40, Aarhus, N 8200, Denmark.

✉e-mail: qluo@cae.au.dk

This Supplementary Information contains Supplementary Tables, Supplementary Methods, and Supplementary Figures.

Supplementary Table

Table 1. Chemical composition of P.I 42.5 cement measured by X-ray fluorescence (XRF).

| Composition | CaO | SiO2 | Al2O3 | Fe2O3 | TiO2 | SO3 | K2O | P2O5 | MnO | Na2O | Others |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Wt. % | 57.386 | 20.793 | 6.044 | 3.528 | 1.477 | 0.33 | 2.806 | 0.154 | 0.334 | 0.206 | 6.263 |

Supplementary Method

Electrochemical characterization of S. oneidensis

To evaluate the electrochemical activity of S. oneidensis, we performed DCPIP (2,6-dichlorophenol indophenol sodium salt) reduction, TTC (2,3,5-triphenyltetrazolium chloride) reductionn, cyclic voltammetry (CV), and electrochemical impedance spectroscopy (EIS). For the DCPIP reduction assay, a 0.01 g/100 mL DCPIP solution was prepared. One milliliter of S. oneidensis MR-1 culture was mixed with 100 μL of the DCPIP solution, and the absorbance at 600 nm was measured every 10 minutes using a spectrophotometer until stable. A color change from blue to colorless indicated successful electron transfer via outer membrane proteins. For the TTC reduction assay, EAMs cultures were centrifuged, and the resulting pellet was resuspended in phosphate-buffered saline (PBS). A 100 μL aliquot of 0.5 mg/mL TTC solution was added, and the mixture was incubated at 37°C for 1–2 hours. The absorbance was measured at 485 nm, where a color change from colorless to red confirmed active bacterial metabolism. CV was conducted by coating the bacterial suspension onto carbon cloth electrodes, allowing it to sit for 10 minutes, and then placing the electrodes in a three-electrode electrochemical cell containing PBS buffer. The voltage range was set from -0.6 V to +0.6 V, with a scan rate of 10–100 mV/s. The recorded CV curves were used to identify redox peaks indicative of extracellular electron transfer activity. For EIS, the coated electrodes were connected to an electrochemical workstation, and measurements were performed over a frequency range of 1 Hz to 1000 kHz with open-circuit potential (OCP) as the perturbation and a perturbation amplitude of 0.01 V. The Nyquist plots were used to evaluate charge transfer resistance and the electrochemical activity of the EAMs.

Supplementary Figures

Fig. 1 Growth characterization of S. oneidensis. a, DCPIP and TTC reduction assays confirming the EET activity of S. oneidensis. The decrease in OD600 of DCPIP and the increase in OD485 of TTC over time indicate microbial reduction processes. b, Growth curve of S. oneidensis measured by OD600 over time. The bacterial culture exhibits an exponential growth phase followed by a stationary phase, suggesting stable microbial activity under the tested conditions.

Fig. 2 GCD curves of EAM-cement composites at different current densities at 28d. a, GCD curves of EAM-cement composites at 0.5 A. b, GCD curves of EAM-cement composites at 0.75 A. c, GCD curves of EAM-cement composites at 1 A.

Fig. 3 CV evolution of EAM-cement composites over time. CV curves of EAM-cement composites with different EAM incorporations measured at 10 mV/s over various curing periods (1, 7, 28, 56, and 90 days). The progressive increase in current density over time indicates the development of electroactive microbial networks within the cement matrix. a-e, EAMs-0% (control), EAMs-0.3%, EAMs-0.9%, EAMs-1.5%, and EAMs-3%, respectively.

Fig. 4 Effect of scan rate on the electrochemical performance of EAM-cement composites at 56d. Cyclic voltammetry (CV) curves of EAM-cement composites with different EAM incorporations at 56 days, tested at varying scan rates (10, 20, 30, 50, and 100 mV/s). a-e, EAMs-0% (control), EAMs-0.3%, EAMs-0.9%, EAMs-1.5%, and EAMs-3%, respectively.

Fig. 5 Impact of W/C ratio and curing conditions on the electrochemical performance of EAM-cement composites. a, Composites with W/C = 0.3, 0.4, and 0.5 under ambient curing conditions. Higher W/C ratios result in enhanced electrochemical activity due to increased porosity, facilitating ion transport and microbial viability. b, Comparison between water curing, ambient curing, and nutrient solution curing for samples with W/C = 0.4. Nutrient solution curing enhances electrochemical performance, by sustaining microbial metabolism and EET activity.