Supplementary Information

Flexible Units in Covalent Organic Frameworks Promote Photocatalytic Uranium Extraction from Wastewater

Mengjie Hao1, Ming Lei1, Juyao Zhang1, Yinghui Xie1, He Gu1, Zhongshan Chen1, Hui Yang1*, Geoffrey I. N. Waterhouse2, Shengqian Ma3*, and Xiangke Wang1*

1 College of Environmental Science and Engineering, North China Electric Power University, Beijing 102206, P.R. China;

2 School of Chemical Sciences, The University of Auckland, Auckland 1142, New Zealand;

3 Department of Chemistry, University of North Texas, Denton, Texas 76201, United States

Email: h.yang@ncepu.edu.cn (H.Y.); shengqian.ma@unt.edu (S.M.); xkwang@ncepu.edu.cn (X.W.)

# Chemicals and Instrumentation

Chemicals

All chemicals were sourced from commercial suppliers and used without further purification. 1,3,5-tris(4-formylphenyl) benzene (TFPB), carbohydrazide (CHYD), oxalyl dihydrazide (ODH), and hydrazine hydrate were purchased from Jilin Chinese Academy of Sciences-Yanshen Technology Co., Ltd. The groundwater was collected in Mentougou District, Beijing, China.

Instrumentation

Powder X-ray diffraction (PXRD) patterns were collected on a Rigaku SmartLab SE X-ray diffractometer equipped with a Cu Kα source. Small angle X−ray scattering (SAXS) data were collected on a Bruker D8 Advance. Brunauer-Emmett-Teller (BET) surface areas and pore size distributions were determined from N2 adsorption/desorption isotherms collected at 77 K using a Micromeritics TriStar II. Samples were heated under a vacuum at 75 °C for 12 h before the measurements. Scanning electron microscopy (SEM) images were recorded on Hitachi SU8010 and ZEISS GeminiSEM 300 microscope. High-resolution transmission electron microscopy (HRTEM) images were recorded on a JEOL JEM-F200 transmission electron microscope. Fourier transform infrared spectra (FTIR) were recorded on a Shimadzu high-resolution IRTracer-100. Solid-state 13C CP/MAS NMR spectra were collected on a Bruker Avance Neo 400WB spectrometer. X-ray photoelectron spectroscopy (XPS) analyses were performed using a Thermo ESCALAB 250Xi spectrometer, equipped with a monochromatic Al Kα X−ray source. All binding energies were calibrated against the C 1s peak at 284.6 eV of neutral hydrocarbons. UV−vis spectra were recorded in diffuse reflectance (DR) mode at room temperature on a Shimadzu UV−2700 spectrophotometer equipped with an integrating sphere attachment. Inductively coupled plasma mass spectrometry (ICP−MS) analyses were performed on an Agilent 7800 spectrometer. Time-resolved photoluminescence (TRPL) spectra were obtained at room temperature on an Edinburgh FLS1000 spectrofluorometer operating at an excitation wavelength of 375 nm. Zeta potentials at different pH values were measured on a Malvern Zetasizer Nano ZSE analyzer. Thermogravimetric analyses (TGA) were carried out on a Taber discovery SDT650/Netzsch STA 409PC instrument. Samples were heated under a N2 atmosphere from 25 to 600 °C at a heating rate of 10 °C/min. Photoelectrochemical experiments were carried out using an electrochemical workstation (CHI 760E) with a three-electrode electrochemical cell. Mott-Schottky plots were recorded at a frequency of 3000 Hz. Electrochemical impedance spectroscopy (EIS) data were collected in the frequency range of 1-1000000 Hz. The applied potential vs. Ag/AgCl was converted to a normal hydrogen electrode (NHE) potential using the following equation: ENHE = EAg/AgCl + EθAg/AgCl (EθAg/AgCl = 0.199 V). Photocurrent tests were carried out under visible light irradiation, which was generated by a 300 W xenon lamp (PerfectLight, PLS-SXE300).

# Photocatalytic H2O2 production tests

Briefly, COF-3 photocatalyst (5 mg) was added to groundwater, or tap water (100 mL). Adsorption-desorption equilibrium was achieved by stirring the dispersion under dark conditions for 2 h. The dispersion in photoreactor was then irradiated using a 300 W Xe lamp under magnetic stirring at 25 °C. At regular intervals, an aliquot of the solution was collected and filtered through a 0.45 μm filter to remove any photocatalyst. The concentration of H2O2 in the filtrate liquid was then determined spectrophotometrically by the method described below.

# H2O2 detection

The concentration of H2O2 was determined by iodometry according to a previously reported method1. Briefly, potassium iodide (KI) solution (1 mL, 0.4 mol/L) and potassium hydrogen phthalate (C8H5KO4) solution (1 mL, 0.1 mol/L) were added to a diluted sample solution (0.5 mL) along with 2.5 mL deionized water. H2O2 reacts with I- under acidic conditions to form I3- (H2O2 + 3I- + 2H+ → I3- + 2H2O), which has a strong absorption maximum at about 350 nm by UV–vis spectroscopy. The total amount of H2O2 produced during the photocatalytic reaction was then calculated using a calibration graph of absorbance at 350 nm versus H2O2 concentration constructed using standard H2O2 solutions of known concentration.

In order to investigate the influence of different sacrificial agents on the H2O2 generation activity of COF-3, AgNO3 (1 mM), CH3OH (5%), isopropyl alcohol (IPA, 5%) and p-benzoquinone (p-BQ, 2.5 mM) were used as radical scavengers for electrons (e-), holes (h+), ·OH, and ·O2- radicals, respectively. To explore the influence of O2 on the photocatalytic H2O2 generation activity, additional experiments were conducted by purging N2 or O2 into the reaction solution under dark conditions. After purging for a sufficient period, the photocatalysis test was carried out under the condition of a continuous N2 or O2 flow. A 300 W Xe lamp was used as the light source. The H2O2 generated in all these experiments was quantified spectrophotometrically using iodometry. The concentration of U(VI) in the filtrates was measured by UV–vis spectrophotometry at a wavelength of 650 nm using the Arsenazo III method.

| Supplementary Table 1. Fractional atomic coordinates for the unit cell of COF-1. |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| space group P6/M, a = b = 29.88 Å, c = 3.52 Å; α = β = 90°, γ = 120° Pawley refined, Rwp = 3.97%, Rp = 3.04% |  |  |  |  |  |  |  |
| Atom | x | y | z | Atom | x | y | z |
| C1 | 2.38681 | -1.31215 | 0 | C9 | 2.44122 | -1.50045 | 0 |
| C2 | 2.366 | -1.27923 | 0 | N10 | 2.50951 | -1.51714 | 0 |
| C3 | 2.37728 | -1.4003 | 0 | H11 | 2.43057 | -1.29468 | 0 |
| C4 | 2.34518 | -1.45425 | 0 | H12 | 2.30139 | -1.47199 | 0 |
| C5 | 2.36641 | -1.48663 | 0 | H13 | 2.33998 | -1.53037 | 0 |
| C6 | 2.41998 | -1.4656 | 0 | H14 | 2.49607 | -1.39438 | 0 |
| C7 | 2.45231 | -1.41182 | 0 | H15 | 2.4575 | -1.33572 | 0 |
| C8 | 2.43109 | -1.37946 | 0 | H16 | 2.4141 | -1.54408 | 0 |

| Supplementary Table 2. Fractional atomic coordinates for the unit cell of COF-2. |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| space group P-6, a = b = 30.82 Å, c = 3.51 Å; α = β = 90°, γ = 120° Pawley refined, Rwp = 3.25%, Rp = 2.60% |  |  |  |  |  |  |  |
| Atom | x | y | z | Atom | x | y | z |
| C1 | 0.66722 | 0.66743 | 0 | C20 | 0.16449 | 0.50169 | 0 |
| N2 | 0.65285 | 0.70478 | 0 | C21 | 0.17564 | 0.46285 | 0 |
| O3 | 0.71152 | 0.68006 | 0 | C22 | 0.2256 | 0.47433 | 0 |
| N4 | 0.62993 | 0.61557 | 0 | C23 | 0.26422 | 0.52424 | 0 |
| C5 | 0.61696 | 0.32231 | 0 | C24 | 0.13585 | 0.41018 | 0 |
| C6 | 0.62752 | 0.28304 | 0 | H25 | 0.68194 | 0.74506 | 0 |
| C7 | 0.64381 | 0.41358 | 0 | H26 | 0.58961 | 0.60424 | 0 |
| C8 | 0.68243 | 0.46382 | 0 | H27 | 0.57643 | 0.31372 | 0 |
| C9 | 0.67138 | 0.50259 | 0 | H28 | 0.72322 | 0.47325 | 0 |
| C10 | 0.62146 | 0.49167 | 0 | H29 | 0.70302 | 0.54326 | 0 |
| C11 | 0.58282 | 0.44178 | 0 | H30 | 0.5421 | 0.43259 | 0 |
| C12 | 0.59389 | 0.403 | 0 | H31 | 0.56195 | 0.36248 | 0 |
| C13 | 0.60882 | 0.53162 | 0 | H32 | 0.56791 | 0.52179 | 0 |
| N14 | 0.64324 | 0.57832 | 0 | H33 | 0.35336 | 0.59632 | 0 |
| N15 | 0.30862 | 0.91089 | 0 | H34 | 0.19349 | 0.58281 | 0 |
| C16 | 0.34458 | 0.62813 | 0 | H35 | 0.12376 | 0.49248 | 0 |
| C17 | 0.38369 | 0.67804 | 0 | H36 | 0.23498 | 0.44293 | 0 |
| C18 | 0.25341 | 0.56343 | 0 | H37 | 0.30481 | 0.53302 | 0 |
| C19 | 0.2031 | 0.55158 | 0 | H38 | 0.14586 | 0.37923 | 0 |

| Supplementary Table 3. Fractional atomic coordinates for the unit cell of COF-3. |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| space group P-6, a = b = 28.20 Å, c = 3.50 Å; α = β = 90°, γ = 120° Pawley refined, Rwp=2.87%, Rp=2.24% |  |  |  |  |  |  |  |
| Atom | x | y | z | Atom | x | y | z |
| C1 | 0.27032 | 0.27383 | 0 | C21 | 0.5434 | 0.75732 | 0 |
| C2 | 0.33113 | 0.30651 | 0 | C22 | 0.564 | 0.81382 | 0 |
| O3 | 0.24743 | 0.22404 | 0 | C23 | 0.52769 | 0.83411 | 0 |
| N4 | 0.23709 | 0.29906 | 0 | C24 | 0.47123 | 0.79806 | 0 |
| N5 | 0.36443 | 0.2814 | 0 | C25 | 0.62341 | 0.85084 | 0 |
| O6 | 0.35402 | 0.3563 | 0 | N26 | 0.25923 | 0.35589 | 0 |
| C7 | 0.63484 | 0.27641 | 0 | H27 | 0.19178 | 0.27331 | 0 |
| C8 | 0.69206 | 0.30114 | 0 | H28 | 0.40973 | 0.30723 | 0 |
| C9 | 0.54861 | 0.28128 | 0 | H29 | 0.60843 | 0.22988 | 0 |
| C10 | 0.52285 | 0.31287 | 0 | H30 | 0.54852 | 0.35946 | 0 |
| C11 | 0.46583 | 0.28771 | 0 | H31 | 0.44528 | 0.31373 | 0 |
| C12 | 0.43339 | 0.2305 | 0 | H32 | 0.43318 | 0.15233 | 0 |
| C13 | 0.45894 | 0.19892 | 0 | H33 | 0.53604 | 0.19752 | 0 |
| C14 | 0.516 | 0.224 | 0 | H34 | 0.34858 | 0.15489 | 0 |
| C15 | 0.37291 | 0.20155 | 0 | H35 | 0.37086 | 0.76917 | 0 |
| N16 | 0.34282 | 0.22455 | 0 | H36 | 0.4707 | 0.67525 | 0 |
| C17 | 0.35373 | 0.72301 | 0 | H37 | 0.57282 | 0.74065 | 0 |
| C18 | 0.29697 | 0.68731 | 0 | H38 | 0.5442 | 0.88017 | 0 |
| C19 | 0.4502 | 0.74122 | 0 | H39 | 0.44216 | 0.81515 | 0 |
| C20 | 0.48691 | 0.72126 | 0 | H40 | 0.6522 | 0.83342 | 0 |

Supplementary Fig. 1 | FT-IR spectra for linkers.

Supplementary Fig. 2 | Top and side view of the eclipsed AA stacking crystal structure of COF-1. The C, N, and H atoms are represented by gray, blue, and white spheres, respectively.

Supplementary Fig. 3 | Top and side view of the eclipsed AA stacking crystal structure of COF-2. The C, N, O, and H atoms are represented by gray, blue, red, and white spheres, respectively.

Supplementary Fig. 4 | Top and side view of the eclipsed AA stacking crystal structure of COF-3. The C, N, O, and H atoms are represented by gray, blue, red, and white spheres, respectively.

Supplementary Fig. 5 | PXRD patterns of COF-1 before and after treatment in different solvents.

Supplementary Fig. 6 | SEM images of COF-1 (left) and COF-2 (right).

Supplementary Fig. 7 | TGA curves for COF-1, COF-2, and COF-3. Samples were heated at 10 oC/min in flowing N2.

Supplementary Fig. 8 | UV−visible diffuse reflectance spectra for COF-1, COF-2, and COF-3.

DFT calculations

All calculations were carried out using Gaussian 16 A.03 software2. The PBE03 functional was adopted for all calculations in combination with the Grimme’s D3(BJ)4, 5 dispersion correction. For geometry optimization and frequency calculations, the def2-SVP6, 7 basis set was used for all atoms. The vertical transition energies of the first 50 excited states were calculated at the TD-PBE0-D3(BJ)/def2-TZVP calculation level using time-dependent density functional theory (TD-DFT). The hole-electron excited analysis8 was performed using Multiwfn 3.8(dev) software9, 10, Some isosurface maps were rendered by means of the VMD11 visualization program based on the files exported by Multiwfn 3.8(dev).

Supplementary Fig. 9 | The electrostatic potential distributions for COF-1, COF-2, and COF-3. The blue regions represent positive electrostatic potential (electron-deficient areas), and the red regions indicate negative electrostatic potential (electron-rich areas).

Supplementary Fig. 10 | The excited state oscillator strength for COF-1, COF-2, and COF-3.

Supplementary References

1.	Wei Z., Liu M., Zhang Z., Yao W., Tan H., Zhu Y. Efficient visible-light-driven selective oxygen reduction to hydrogen peroxide by oxygen-enriched graphitic carbon nitride polymers. Energy Environ. Sci. 11, 2581-2589 (2018).

2.	Frisch M. J., et al. Gaussian 16 rev. A.03. Wallingford, CT (2016).

3.	Adamo C., Barone V. Toward reliable density functional methods without adjustable parameters: The pbe0 model. J. Chem. Phys. 110, 6158-6170 (1999).

4.	Grimme S. Density functional theory with london dispersion corrections. WIREs Comput. Mol. Sci. 1, 211-228 (2011).

5.	Grimme S., Ehrlich S., Goerigk L. Effect of the damping function in dispersion corrected density functional theory. J. Comput. Chem. 32, 1456-1465 (2011).

6.	Weigend F., Ahlrichs R. Balanced basis sets of split valence, triple zeta valence and quadruple zeta valence quality for H to Rn: Design and assessment of accuracy. Phys. Chem. Chem. Phys. 7, 3297-3305 (2005).

7.	Weigend F. Accurate coulomb-fitting basis sets for H to Rn. Phys. Chem. Chem. Phys. 8, 1057-1065 (2006).

8.	Liu Z., Lu T., Chen Q. An sp-hybridized all-carboatomic ring, cyclo[18]carbon: Electronic structure, electronic spectrum, and optical nonlinearity. Carbon 165, 461-467 (2020).

9.	Lu T., Chen F. Multiwfn: A multifunctional wavefunction analyzer. J. Computat. Chem. 33, 580-592 (2012).

10.	Lu T. A comprehensive electron wavefunction analysis toolbox for chemists, multiwfn. J. Chem. Phys. 161, 082503 (2024).

11.	Humphrey W., Dalke A., Schulten K. Vmd: Visual molecular dynamics. J. Mol. Graph. Model. 14, 33-38 (1996).