Extended Data Figure 1| 1H NMR characterization of [Fe(ImP)2][PF6]. The spectrum was recorded in deuterated acetonitrile on a scan range from -50 – 50 ppm. The spectrum shows the expected number of resonances and integrals of 1 (26 H nuclei in total) and resonances of the residual solvents.

Extended Data Figure 2| ESI mass spectrometry measurement of [Fe(ImP)2][PF6]. a, Fullfull spectrum over the whole measurement range, showing [M-PF6]+ at 530.1685 m/z and the ESI-oxidized [M-PF6]2+ species at 265.0824 m/z. b, enlargement on the [M-PF6]+ range. c, simulation of [M-PF6]+ showing the good agreement to the experimental isotopic pattern.

Extended Data Figure 3| Magnetic characterization of [Fe(ImP)2] [PF6]. Magnetic susceptibility data as temperature dependence of χMT in the range of 2 – 300 K at 0.5 T, showing the typical behavior of metal complexes with (t2g)5 electron configuration (2T2) with significantly higher χMT values than expected for a conventional S = ½ spin system (spin-only) due to spin-orbit coupling.

Extended Data Figure 4| Further electrochemical and spectroelectrochemical investigations. a, Square wave voltammogram of 1 in CH3CN/[nBu4N][PF6] of the reduction up to -2.85 V vs FcH0/+ in comparison with the blind current during that process at a scan rate of 100 mV s-1. This indicates that the ligand reduction is observed at around -2.7 V. b, UV-Vis absorption spectrum of 1 (grey) in comparison with that of 1- (red) and 1+ (blue) obtained by spectro-electrochemical measurements in CH3CN/[nBu4N][PF6].

Extended Data Table 1: Main contributions to molecular orbitals in 1-, 1 and 1+.

| Orb. Nr. | 1- FeII (singlet) |  | 1 FeIII (doublet) |  |  |  | 1+ FeIV (triplet) |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Orbital (↑↓) |  | Orbital (α, ↑)* |  | Orbital (β, ↓) |  | Orbital (α, ↑)** |  | Orbital (β, ↓) |  |
| 136 | HOMO-2 | Fe (t2g) | SOMO-2 | Fe (t2g) | SOMO-1 | Fe (t2g) | SOMO-2 | Ligand | SOMO | Fe (t2g) |
| 137 | HOMO-1 | Fe (t2g) | SOMO-1 | Fe (t2g) | SOMO | Fe (t2g) | SOMO-1 | Ligand | SUMO | Fe (t2g) |
| 138 | HOMO | Fe (t2g) | SOMO | Fe (t2g) | SUMO | Fe (t2g) | SOMO | Fe (t2g) | SUMO+1 | Fe (t2g) |
| 139 | LUMO | Ligand | SUMO | Ligand | SUMO+1 | Ligand | SUMO+1 | Ligand | SUMO+2 | Ligand |
| 140 | LUMO+1 | Ligand | SUMO+1 | Ligand | SUMO+2 | Ligand | SUMO+2 | Ligand | SUMO+3 | Ligand |

The main contributions to molecular orbital were extracted from the respective DFT calculation of the optimized structure (1-, 1 and 1+ as singlet, doublet and triplet, respectively). The comparison of the three structures and their iron orbital densities show the consecutive removal of electrons from the t2g-orbitals upon oxidizing from 1- to 1 to 1+ as seen in the β-orbitals. This proves that reduction and oxidation are metal-centered. (*) Strong mixing of Fe-orbitals and Ligand orbitals leads to a significant ligand-orbital proportion in the t2g α-orbitals. (**) The α-orbitals in 1+ do not show localized t2g-orbitals. The Fe-fraction is delocalized over the different SOMOs and just the highest SOMO shows signs of a t2g-orbital (with a fraction of ligand orbitals). The proportion of Fe in the β-orbitals is much higher for both 1 and 1+ than in the α-orbitals.

Extended Data Figure 5| Theoretical investigations of [Fe(ImP)2][PF6]. a,b, Tuning of the LC-BLYP functional for DFT calculations. a, functional J*(α,ω)=J02+J12, J0=εHOMON+IP(N) and J1=εHOMON+1+EA(N)  showing the deviation from Koopman's theorem for ionization potential (IP) and electron affinity (EA) for the system with N electrons. The red points denote minima of the J*-functional at constant α values. b, The deviation from linearity of energy dependence between integer number of electrons. As a result of tuning, the parameters α=0.0 and ω=0.15 Bohr-1 were found. c, Huang-Rhys factors for lowest 40 doublet and 20 quartet states as calculated using TDDFT. The mode shown in Fig. 4 of the main text corresponds to mode with index 7 (ω/(2πc)=126 cm-1). It has the largest Huang-Rhys factor among the lowest 15 doublet states.

Extended Data Figure 6| Extended Luminescence Spectroscopy. a, Excitation spectra of 1 in CH3CN for the MCLT (420 nm, red) and LMCT (675 nm, black) emission in comparison to the absorption spectrum (blue). The peak (*) arises from the second order diffraction of the excitation (2l). b, Excitation-emission plot for 1. The plot shows the clear separation between the MLCT luminescence and the LMCT emission. Excitation in the MLCT-absorption band (310 – 410 nm) shows both MLCT and LMCT emission. Above this wavelength, the LMCT emission is visible. The narrow diagonal features below 600 nm are caused by Raman signals from the solvent.

Extended Data Figure 7| Variable Temperature Emission. The spectra of 1 were collected in butyronitrile with an excitation wavelength of 400 nm, showing the intensity increase upon cooling of both MLCT and LMCT bands and the blue shift of the LMCT band upon cooling. The peak at 800 nm (*) arises from the second order diffraction of the excitation (2).

Extended Data Figure 8| Transient absorption (TA) spectra with pump pulses centered at 600 nm and 330 nm, respectively. a, b, c TA data for excitation of complex 1 at 600 nm and corresponding fits. A degassed acetonitrile solution of 1 was used as sample. A global fit, as described in the manuscript, was applied and a pure monoexponential decay with a time constant of τ1 = 240 ps was found. a, TA spectra at the given times after excitation at 600 nm. b, Time traces of the transient absorption of 1 at three selected detection wavelengths together with the time curves resulting from the global fit. c, Decay associated amplitude spectrum of the single exponential decay in comparison with the ground state bleach, i. e., the scaled negative absorption spectrum. d, e, f TA data for excitation of complex 1 at 330 nm and corresponding fits. d, TA spectra obtained at the given times after excitation of a degassed solution of 1 in acetonitrile at 330 nm. e, Time traces of the transient absorption of 1 at three selected detection wavelengths together with the time curves resulting from the global fit. f, Decay associated amplitude spectra for the three components with τ1 = 236 ps, τ2 = 6.1 ps, and τ3 = 0.5 ps in comparison with the ground state bleach, i. e., the scaled negative absorption spectrum.

Extended Data Figure 9| TRES Data after excitation at 346 nm and 374 nm. a, b, c, measurements between 380 and 450 nm for 1 h per data point after 346 nm excitation. a, Decay of the fluorescence signal over time. b, Decay curves (points) at 380, 395 and 450 nm with the corresponding fits (line). c, Amplitude spectra of the lifetimes τ1 = 0.4 ns, τ2 = 2.1 ns and τ3 = 10.3 ns obtained from global fitting. d, e, f, Measurements between 390 and 455 nm for 10k Counts per data point after 374 nm excitation. d, Decay of the fluorescence signal over time. e, Decay curves (points) at 390 nm, 405 nm and 455 nm with the respective fits (line). f, Amplitude spectra of the lifetimes τ1 = 0.01 ns, τ2 = 0.3 ns, τ3 = 2.2 ns and τ4 = 9.1 ns obtained from global fitting of the decay curves.