Table 1. Summary of microplastic particles sampled across different locations with a 0.10mm sieve employed.

| Location | Weather | Collected water | Colour | Plastic identifiedb | Microscope image |
| --- | --- | --- | --- | --- | --- |
| Matilda Bay (Crawley) | Sunny | 230 L | Blue | PP |  |
|  | Sunny | 1500 L | Blue | Blend of PE and HDPE |  |
|  |  |  | Grey | PLA |  |
|  | Sunny | 1200 L | Blue | Blend of PP and PE |  |
|  |  |  | Green | PP |  |
|  | Sunny | 2000 L | Blue (1) | Blend of PP and PE |  |
|  |  |  | Blue (2) | PP |  |
|  |  |  | Green | Blend of PP and PE |  |
|  | Sunny | 1500 L | Blue (1) | PP |  |
|  |  |  | Blue (2) | PP |  |
|  |  |  | Blue (3) | Blend of PE and HDPE with a small fraction of PP |  |
|  |  |  | Blue (4) | Blend of PP and PE |  |
|  |  |  | Blue (5) | Predominantly PP with traces of PE |  |
|  |  |  | Turquoise (1) | Blend of PP and PE with traces of PVC |  |
|  |  |  | Turquoise (2) | PP |  |
|  |  |  | Turquoise (3) | PP |  |
|  |  |  | Turquoise (4) | PP |  |
|  |  |  | Turquoise (5) | Blend of PP, PE, and HDPE |  |
|  |  |  | Turquoise (6) | Blend of PP, PE, and HDPE |  |
|  |  |  | Turquoise (7) | Blend of PP, PE, and HDPE |  |
|  |  |  | Turquoise (8) | Blend of PP and PE |  |
| Deep Water Point Reserve (Mount Pleasant) | Rainy | 2000 L | Blue | Blend of PE, PP, HDPE |  |
| Bardon Park (Maylands)a | Rainy | 2000 L | Blue | PP |  |

aA 0.074 mm (200 mesh) sieve was used instead of a 0.10 mm (150 mesh).

bAbbreviations: polypropylene: PP; polyethylene: PE; high-density polyethylene: HDPE; polylactic acid: PLA; polyvinyl chloride: PVC.