Supporting Information

Core-shell magnetic Fe3O4/CNC@MOF composites with peroxidase-like activity for colorimetric detection of phenol

Chen Hou a,*, Linhui Fu a, Yang Wang a,*, Wenqiang Chen a, Fang Chen a, Sufeng Zhang a,*, Jianzhi Wang b

a College of Bioresources Chemical and Materials Engineering, Shaanxi University of Science and Technology, Shaanxi Provincial Key Laboratory of Papermaking Technology and Specialty Paper Development, Key Laboratory of Paper Based Functional Materials of China National Light Industry, National Demonstration Center for Experimental Light Chemistry Engineering Education, Xi’an 710021, China

b Key Laboratory for Green Chemical Process of Ministry of Education, School of Chemical Engineering and Pharmacy, Wuhan Institute of Technology, Wuhan 430205, P.R. China

⁎ Corresponding authors.

E-mail addresses: houchen@sust.edu.cn (C. Hou), wangyang@sust.edu.cn (Y. Wang), sufengzhang@126.com (S. Zhang)

Fig.S1 EDS analysis of Fe3O4/CNC@ZIF-8

Fig.S2 High resolution XPS spectra of Zn 2p

Fig. S3 Absorbance spectrum of OPD oxidation at (a) different catalyst dosage; (b) different pH; (b) different temperatures

Fig. S4 Study on effects of (a) 4-AAP concentration; (b) H2O2 concentration; (c) varying temperature on colorimetric detection of phenol

Table S1 Comparison of this work with other papers for the specific surface area of different detection Materials

| Materials | SBET(N2) (m2/g) | Total pore volume (cm3/g) | Pore size (nm) | Ref. |
| --- | --- | --- | --- | --- |
| Fe3O4@SiO2 | 114.60 | 0.16 | 2.45 | (Mir et al. 2019) |
| Fe3O4@CNT | 188 | 0.55 | - | (Liu et al. 2021) |
| Fe3O4/N-PCNC | 187.10 | 0.49 | 2-50 | (Nsabimana et al. 2019) |
| h-CNT/Fe3O4/ZrO2 | 324.90 | 0.69 | 15.51 | (Shi et al. 2020) |
| g-C3N4/Fe3O4 | 111.4 | 0.42 | - | (Duan et al. 2019) |
| Fe3O4/CNC@ZIF-8 | 463.63 | 0.31 | 5.1 | This work |

Table S2 Comparison of this work with other papers for the detection of phenol

| Materials | Detection Limit(μM) | detection range(μM) | Ref. |
| --- | --- | --- | --- |
| Fe3O4NPs | 3.79 | 1.67 μM-1.2 mM | (Wu et al. 2020) |
| RGO/Cu8S5/PPy | 1.78 | 5-200 | (Jiang et al. 2017) |
| Au@Ni/rGO | 1.68 | 1-300 | (Darabdhara and Das 2019) |
| H-MOFs | 1.0 | 0-200 | (Yin et al. 2016) |
| HRP@H-ZIF-8-GOx | 0.86 | 0-100 | (Liu et al. 2019) |
| Fe3O4/CNC@ZIF-8 | 0.316 | 2-200 | This work |

References

Darabdhara G, Das MR (2019) Dual responsive magnetic Au@Ni nanostructures loaded reduced graphene oxide sheets for colorimetric detection and photocatalytic degradation of toxic phenolic compounds. J Hazard Mater 368:365-377. https://doi.org/10.1016/j.jhazmat.2019.01.010

Duan J, Zhao L, Lv W, Li Y, Zhang Y, Ai S, Zhu L (2019) Facile synthesis of g-C3N4/Fe3O4 nanocomposites for fluorescent detection and removal of Cr(VI). Microchemical Journal 150. https://doi.org/10.1016/j.microc.2019.104105

Jiang Y et al. (2017) Synthesis of RGO/Cu8S5/PPy Composite Nanosheets with Enhanced Peroxidase-Like Activity for Sensitive Colorimetric Detection of H2O2and Phenol. Particle & Particle Systems Characterization 34. https://doi.org/10.1002/ppsc.201600233

Liu B et al. (2021) Fe3O4@CNT as a high-effective and steady chainmail catalyst for tetracycline degradation with peroxydisulfate activation: Performance and mechanism. Separation and Purification Technology 273. https://doi.org/10.1016/j.seppur.2021.118705

Liu H et al. (2019) Compartmentalization of Biocatalysts by Immobilizing Bienzyme in Hollow ZIF-8 for Colorimetric Detection of Glucose and Phenol. Industrial & Engineering Chemistry Research 59:42-51. https://doi.org/10.1021/acs.iecr.9b04391

Mir N, Karimi P, Castano CE, Norouzi N, Rojas JV, Mohammadi R (2019) Functionalizing Fe3O4@SiO2 with a novel mercaptobenzothiazole derivative: Application to trace fluorometric and colorimetric detection of Fe3+ in water. Applied Surface Science 487:876-888. https://doi.org/10.1016/j.apsusc.2019.05.156

Nsabimana A et al. (2019) Multifunctional magnetic Fe3O4/nitrogen-doped porous carbon nanocomposites for removal of dyes and sensing applications. Applied Surface Science 467-468:89-97. https://doi.org/10.1016/j.apsusc.2018.10.119

Shi J, Zhang S, Deng Q, Li Y, Geng Z, Zheng L, Tang B (2020) A versatile biocatalytic nano-platform based on Fe3O4-filled and zirconia shrunk holey carbon nanotubes. Chemical Engineering Journal 402. https://doi.org/10.1016/j.cej.2020.125737

Wu S, Guo D, Xu X, Pan J, Niu X (2020) Colorimetric quantification and discrimination of phenolic pollutants based on peroxidase-like Fe3O4 nanoparticles. Sensor Actuat B-Chem 303:127225. https://doi.org/10.1016/j.snb.2019.127225

Yin Y, Gao C, Xiao Q, Lin G, Lin Z, Cai Z, Yang H (2016) Protein-Metal Organic Framework Hybrid Composites with Intrinsic Peroxidase-like Activity as a Colorimetric Biosensing Platform. ACS Appl Mater Interfaces 8:29052-29061. https://doi.org/10.1021/acsami.6b09893