Photodegradation behavior of nanosilica-filled PMMA composite: synergistic effect of mixed solvents and interfacial functional groups

Supplementary Material

Zhiping Xu1, Liangchen Li1†, Ying Liu1, Rui Yang1*

- Department of Chemical Engineering, Tsinghua University, Beijing, China

*Corresponding author(s), E-mail(s): yangr@mail.tsinghua.edu.cn

†These authors contributed equally to this work

Table S1 lists the specific feeding information of Nano-SiO2 with different surface chemical modifications. According to the literature, the maximum density of hydroxyl groups that can be accommodated on the surface of silica is about 5 hydroxyl groups/nm1. Therefore, in this work, the required silane coupling agent additions were all calculated based on the molar ratio of surface silica hydroxyl groups to coupling agent molecules of 1:4.

Table S1 Feeding information of silane coupling agents for SiO2 surfaces chemical modification

| Silanes | Feed | Products |
| --- | --- | --- |
| APTES | 12.6 mmol (2.95 ml) | SiO2@NH2 |
| EPPTMS | 12.6 mmol (2.78ml) | SiO2@Ep |
| MAPTMS | 12.6 mmol (2.84 ml) | SiO2@MA |
| MPTMS | 12.6 mmol (2.34 ml) | SiO2@SH |
| PhTMS | 12.6 mmol (2.36 ml) | SiO2@Ph |
| PTES | 12.6 mmol (2.91 ml) | SiO2@Propyl |
| OTMS | 12.6 mmo (3.26 ml) | SiO2@Octyl |

Fig. S1 Thermogravimetric curves of PMMA and its SiO2 filled composite films before and after photooxidative aging: (a) before photooxidative aging; (b) after photooxidative aging for 283h

Fig. S2 Surface morphology changes of the film during photooxidative aging: (a) PMMA; (b) PMMA/SiO2; (c) PMMA/SiO2@NH2; (d) PMMA/SiO2@Ep; (e) PMMA/SiO2@MA; (f) PMMA/SiO2@SH; (g) PMMA/SiO2@Ph; (h) PMMA/SiO2@Propyl; (i) PMMA/SiO2@Octyl

References

1.	Zhuravlev LT (2000) The surface chemistry of amorphous silica. Zhuravlev model. Colloids Surf Physicochem Eng Asp 173(1):1-38. https://doi.org/10.1016/S0927-7757(00)00556-2