Electronic Supplementary

Eco-Friendly Synthesis and Enhanced Photocatalytic Performance of CeO2/Porphyrin Nanocomposites for Organic Pollutant Degradation under Visible Light

Kieu Anh Thi Vo1,2+, Duy Van Lai3,+, Nam Thi Pham1,2, Lam Dai Tran1,2, Thanh Tung Nguyen3, Dinh Ngo Vu4, Duong Duc La5,*

1Institute for Tropical Technology, Vietnam Academy of Science and Technology, Hanoi, Vietnam

2Graduate University of Science and Technology-VAST, Cau Giay, Hanoi, Vietnam

3Institute of Materials Science, Vietnam Academy of Science and Technology, 18 Hoang Quoc Viet Street, Cau Giay District, Hanoi City, Vietnam.

4Electric Power University, 235 Hoang Quoc Viet St, Bac Tu Liem Dist, Hanoi, Vietnam

5Institute of Chemistry and Materials, 17 Hoang Sam, Nghia Do, Cau Giay, Hanoi, Vietnam

+ These authors contributed equally

* Corresponding authors: duc.duong.la@gmail.com

Figure S1. SEM image of pure CeO2 nanoparticles.

Figure S2. (a) Adsorption kinetics over time, (b) Photocatalytic degradation performance, and (c) First-order kinetic analysis for the control sample, CeO2 nanoparticles, and TCPP nanofibers under simulated sunlight exposure for 120 minutes.

Figure S3. (a) Time-dependent removal of Rhodamine B (RhB) using CeO2/TCPP nanocomposite, (b) Adsorption and photodegradation kinetics of RhB, and (c) Kinetic study under simulated sunlight over a 120-minute period.