SUPPLEMENTARY INFORMATION for
 Nanomesh-patterning on multilayer MoS2 field-effect transistors for ultra-sensitive detection of cortisol

Heekyeong Park1,2†, Seungho Baek1†, Bongjin Jung2, Anamika Sen1, Sehwan Kim1, Yun Chang Park3, Sunkook Kim1*, and Young Jun Kim2*

1Department of Advanced Materials and Science Engineering, Sungkyunkwan University (SKKU), Suwon, 16419, Republic of Korea

2Electronics and Telecommunications Research Institute (CTRI), Daejeon, 34129, Republic of Korea

3Measurement and Analysis Division, National Nanofab Center (NNFC), Daejeon, 16229, Republic of Korea

*Corresponding authors. Email: seonkuk@skku.edu (S. Kim), junkin@etri.re.kr

† These authors contributed equally to this work.

Supplementary Fig. 1 | SEM images of the surface of multilayer MoS2 for each process. a, after BCP patterning, b, after O2, c, SF6, and d, BCl3 plasma RIE treatments.

Supplementary Fig. 2 | XPS spectra of multilayer MoS2 before and after nanomesh patterning. a, S 2p and b, Cl 2p.

Supplementary Table 1 | Statistical distribution of electrical performances for 20 different MoS2 nanomesh FETs.

| # of device | L (m) | W (m) | Thickness (nm) |  (cm2 V-1 s-1) | Ion/Ioff |
| --- | --- | --- | --- | --- | --- |
| 1 | 8.47 | 23.3 | 26.50 | 1.80 | 1.4 × 104 |
| 2 | 9.05 | 5.84 | 20.69 | 0.66 | 2.9 × 105 |
| 3 | 8.99 | 5.14 | 24.88 | 3.48 | 2.7 × 104 |
| 4 | 9.44 | 2.5 | 19.10 | 3.40 | 3.1 × 104 |
| 5 | 9.12 | 25.68 | 27.80 | 6.08 | 7.0 × 104 |
| 6 | 8.92 | 3.66 | 25.86 | 8.03 | 6.3 × 104 |
| 7 | 8.92 | 9.37 | 28.94 | 1.45 | 7.3 × 104 |
| 8 | 8.15 | 10.09 | 32.63 | 3.11 | 4.6 × 104 |
| 9 | 9.31 | 26.32 | 23.09 | 1.20 | 5.8 × 104 |
| 10 | 10.21 | 5.84 | 16.55 | 8.50 | 4.3 × 106 |
| 11 | 6.8 | 21.12 | 19.47 | 0.39 | 1.5 × 103 |
| 12 | 7.19 | 24.26 | 27.80 | 0.90 | 1.7 × 105 |
| 13 | 7.32 | 25.22 | 23.99 | 0.86 | 7.0 × 103 |
| 14 | 6.61 | 10.21 | 29.55 | 3.99 | 1.4 × 105 |
| 15 | 6.74 | 26.44 | 14.99 | 3.19 | 4.8 × 104 |
| 16 | 7.77 | 21.5 | 21.04 | 1.17 | 5.3 × 104 |
| 17 | 7.64 | 33.06 | 28.56 | 3.06 | 1.5 × 104 |
| 18 | 8.6 | 1.86 | 16.72 | 1.74 | 9.0 × 104 |
| 19 | 10.34 | 4.24 | 6.66 | 6.07 | 1.2 × 107 |
| 20 | 6.74 | 6.35 | 20.47 | 0.58 | 4.2 × 105 |

Supplementary Fig. 3 | XPS spectra of MoS2 nanomesh after O2 plasma RIE treatment.

In XPS analysis on the MoS2 nanomesh before and after the O2 plasma treatment (Supplementary Fig. 3), the reduction of the atomic ratio of S2- 2p to Mo4+ 3d is observed from 2.04 to 1.87 because of the formation of MoOx on the edge area. For comparison, we also conducted same treatment on the pristine MoS2 having less edge area. The stability of MoS2 bonds upon O2 plasma treatment is confirmed by few variations in the atomic ratio from 2.06 to 2.01. This verifies that the O2 plasma condition we treated can only oxidize the exposed edge area, not the basal plane of the MoS2. However, MoOx peaks (Mo6+ 3d and Mo5+ 3d) were also observed in the pristine MoS2 since it is derived from the temporary formation on unstable oxide layer on the basal plane (MoS2-xOx)1.

Supplementary Fig. 4 | Sensing characteristics of MoS2 pristine bio-FET for different cortisol concentrations.

Supplementary Fig. 5 | Detection characteristics of MoS2 nanomesh bio-FET in human serum.

Reference

1.	Jadwiszczak, J. et al. Oxide-mediated recovery of field-effect mobility in plasma-treated MoS2. Sci. Adv. 4, eaao5031 (2018).