Supplementary Materials for

Study on thermal-storage stability

of polyurethane dispersions prepared via prepolymer method

Hongmei Jiang, Lijuan Sun *

Shanghai Huafeng New Material R&D Technology Co., Ltd. Pudong New Area, Shanghai, China

*Correspondence: sun.lijuan@huafeng.com

Table S1 Sample designations of WPU dispersions

| Sample no. | Synthesis of WPU |  |  |  | parameters |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Acetone (g) | Hyhy (mmol) | Emulsified Water (g) | NCO content of prepolymer (%) |  | Acetone content (%) a | Ratio of [NCO] to [H] | Solid content (%) |  | Ratio of Hyhy : H2O |  | Time of adding Hyhy solution (min) |
| WPU1-1 | / | 124.10 | 264.27 |  | 3.85 | / | 1.03 | 50 | 1:4 |  | 1 |  |
| WPU2-1 | / | 212.50 | 240.67 |  | 6.58 | / | 1.03 | 50 | 1:4 |  | 1 |  |
| WPU2-2 | / | 243.10 | 235.27 |  | 6.58 | / | 0.95 | 50 | 1:4 |  | 1 |  |
| WPU2-3 | / | 263.50 | 231.67 |  | 6.58 | / | 0.90 | 50 | 1:4 |  | 1 |  |
| WPU2-4 | / | 212.50 | 215.67 |  | 6.58 | / | 1.03 | 50 | 1:6 |  | 1 |  |
| WPU2-5 | / | 212.50 | 165.67 |  | 6.58 | / | 1.03 | 50 | 1:10 |  | 1 |  |
| WPU2-6 | / | 212.50 | 240.67 |  | 6.58 | / | 1.03 | 50 | 1:4 |  | 2 |  |
| WPU2-7 | / | 212.50 | 24.067 |  | 6.58 | / | 1.03 | 50 | 1:4 |  | 3 |  |
| WPU2-8 | 122.43 | 212.50 | 240.67 |  | 6.58 | 40 | 1.03 | 50 | 1:4 |  | 1 |  |
| WPU2-9 | 188.64 | 212.50 | 240.67 |  | 6.58 | 60 | 1.03 | 50 | 1:4 |  | 1 |  |
| WPU2-10 | / | 212.50 | 308.64 |  | 6.58 | / | 1.03 | 42 | 1:4 |  | 1 |  |
| WPU2-11 | / | 212.50 | 503.1 |  | 6.58 | / | 1.03 | 38 | 1:4 |  | 1 |  |

a the mass of acetone accounts for the total mass of the solid.

Table S2 Size and distribution of WPU dispersions

|  | WPU 1-1 | WPU 2-1 | WPU 2-2 | WPU 2-3 | WPU 2-4 | WPU 2-5 | WPU 2-6 | WPU 2-7 | WPU 2-8 | WPU 2-9 | WPU 2-10 | WPU 2-11 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Size (nm) | 165.0 | 224.1 | 229.8 | 189.3 | 201.9 | 224.1 | 190.0 | 197.3 | 199.6 | 179.2 | 171.9 | 190.7 |
| Distribution | 0.335 | 0.380 | 0.381 | 0.267 | 0.367 | 0.254 | 0.266 | 0.356 | 0.228 | 0.317 | 0.304 | 0.316 |