Supplementary Materials

Table S1. Recent research on ZnAlMg alloy coatings focusing on chemical composition (C), microstructure (M), corrosion products (CP), atmospheric corrosion (AC), and conversion coating (CC).

| Reference | Material | Category | Methods | Main results |
| --- | --- | --- | --- | --- |
| Elvins et al.77 (2008) | Zn4.5Al(0.01-0.05)Mg | C, M | SVET; 5 wt.% NaCl | Zn dendritic phase increased with Mg addition. Microstructural change increased cut-edge corrosion. |
| Li et al.78 (2012) | Zn0.2Al(0-3)Mg | C, M | SEM, XRD, FTIR; Echem; 5 wt.% NaCl | Mg enhanced grain corrosion resistance. 2 wt.% Mg addition would be optimal. |
| Shimoda et al.79 (2015) | Zn(1-11)Al1Mg | C | XRD, SST, mass loss; 5 wt.% NaCl | Better corrosion resistance with increasing %Al. 6-8% or above Al and 3 wt.% Mg would be optimal. |
| Li et al.80 (2016) | Zn11Al3MgxSi (x = 0.1, 0.2, 0.4, 0.6) | C, M | SEM | Si could affect the phase constitution of Fe-Al intermetallic layer and restrain its growth. |
| Wint et al.81 (2021) | Zn(1-6)Al(1-3)Mg Zn1.5Al1.5Mg | C, M | SEM, FFC; 0.1 mol dm-3 CH3COOH | FFC decreased with increasing %Al and thickness. |
| Duchoslav et al.82 (2019) | Zn1.5Al1.5Mg Zn2.5Al1.5Mg Zn3.7Al3.0Mg | C, M | XPS, AES, FIB-TEM | Outmost several nanometers of different composition samples showed similar chemical composition. |
| Sullivan et al.83 (2015) | Zn(1-2)Al(1-2)Mg Zn3.7Al3Mg | C, M | TLM, SVET; 1% NaCl, 0.01 mol dm-3 Na3PO4 | Corrosion attack initiated at MgZn2 by subsequent Zn-rich phase dissolution. |
| Duchoslav et al.84 (2014) | Zn2Al2Mg | M, AC | SST, XPS, AES; 5% NaCl | Initial corrosion attack at MgO. Selective dissolution on binary and ternary phases. |
| Prosek et al.45 (2016) | Zn3Al2Mg Zn2Al2Mg | C, M | CCT, XRF, SEM, XRD, Echem, IRRAS; 4.6 M NaCl (pH 4, 7, and 10) 0.01 M NaCl (pH 7) | Same chemical composition but different microstructure samples were obtained. Finer microstructure showed better corrosion resistance by rapidly blocking the cathodic sites. |
| Truglas et al.85 (2020) | Zn2.5Al1.5Mg | M | SEM, TEM-FIB | In situ monitoring of eutectic phase change during temperature change. |
| Prosek et al.86 (2016) | Zn-X, ZnAl-X, ZnMg-X, ZnAlMg-X | C, M, AC | XRD, XRF, SST, mass loss; Exposure in marine atmosphere; 1 wt.% NaCl pH 4 | Al and Mg showed beneficial effect on corrosion. Fourth element improved corrosion resistance. X = Ti, Zr, Mo, Cr, Ga, In, Cu, Ni, Ca, B, Si, Mn |
| Wint et al.87 (2021) | Zn1.6Al1.6MgxGe (x = 0.19-1.8) | C, M | SEM, XRD, SKPFM, TLM, SVET, Echem, mass loss; 0.17 mol dm-3 NaCl | The addition of Ge resulted in Mg2Ge formation and decreased in fractional area of eutectic phase. Mg2Ge crystals served as reservoirs of Mg2+. |
| Reference | Material | Category | Methods | Main results |
| Gablacová et al.88 (2021) | Zn1.6Al1.6MgxSn (x = 0, 0.5, 1, 2, 3) | C, M | SST, SEM, XRD, mass loss; 5 wt.% NaCl | 0.5 wt.% Sn showed best corrosion resistance. |
| Britton et al.89 (2024) | ZnAlMgxSb (x = 0.45-1.8) | C, M | SEM, DSC, XPS, XRM, SVET, TLM, Echem; 1 wt.% NaCl | Sb addition resulted in Mg3Sb2 intermetallic phase, reducing MgZn2 eutectic, decreasing both anodic and cathodic electrochemical reactivity. |
| Lee et al.90 (2022) | Zn2Al3Mg0.04Si | C, M | CCT, SEM, TEM-FIB, XPS, XRD, Echem; 5 wt.% NaCl | 0.04 wt.% Si addition refined the microstructure in the outer alloy coating by precipitating Mg2Si and Zn-Al intermetallic phases, which preferentially dissolve. |
| Sung et al.91 (2025) | Zn15Al6Mg0.4Si Zn6Al2Mg | C, M | XRD, SEM, TEM, Echem; 3.5 wt.% NaCl | Zn15Al6Mg0.4Si showed high hardness and low corrosion rate. |
| Duchoslav et al.92 (2015) | Zn2Al2Mg | CP | SST, XPS; 5 wt.% NaCl | Rapid formation of LDH stabilized the surface pH, hindered further alkalization. |
| Volovitch et al.71 (2011) | Zn(3-4)Al(3-4)Mg | CP | SEM, FTIR, XRD, AESEC; NaCl and Na2SO4 | Mg2+ enhanced simonkolleite stability by removing carbonate and buffering pH, LDH formation. |
| Azevedo et al.93 (2015) | Zn3.7Al3Mg | CP | SST, XRD, SEM, Raman, titration, Echem; NaCl, Na2SO4, ARW | Presence of Mg2+ delayed the transformation of basic zinc salts to ZnO. Al3+ formed LDH, stable at pH > 12.5. |
| Schuerz et al.94 (2009) | Zn2Al2Mg | CP | SST, SEM-FIB; 5 wt.% NaCl | Corrosion resistant Al-rich oxide layer formation. |
| Schürz et al.70 (2010) | Zn2Al2Mg | CP | SST, SEM, XRD, XPS, Raman; 5 wt.% NaCl | Corrosion resistant Zn6Al2(CO3)(OH)16·4H2O layer formation. |
| Persson et al.28 (2013) | Zn2Al2Mg | CP, AC | IRRAS, XRD, SEM, ATR-FTIR; CO2 and RH controlled | MgAl and Zn/Al LDH formation due to anodic Zn-MgZn2 dissolution and cathodic oxygen reduction on Zn-Al-MgZn2 and Al-phases. |
| Ueda et al.95 (2012) | Zn11Al3Mg0.2Si (pre-painted) | CP, AC | Field exposure (9.5 years) in marine atmosphere, SEM, XRD | Zn5(OH)8Cl2·H2O; NaZn4(SO4)Cl(OH)6·H2O; Zn6Al2(OH)16CO3·4H2O at underpaint, Mg-rich corrosion products at cut-edge. |
| LeBozec et al.96 (2013) | Zn2Al2Mg | CP, AC | SST, SEM, GD-OES, IRRAS, XRD; CO2 and RH controlled | LDH and simonkolleite formation in low CO2; hydroxylcarbonate and simonkolleite in ambient air. |
| Diler et al.97 (2014) | Zn1.5Al1.5Mg | CP, AC | SEM, FTIR, XRD, XPS; 6 months marine exposures | Zn4SO4(OH)6·nH2O and NaZn4Cl(OH)6SO4·6H2O formation; Mg2+ and Al3+ induced quenching of corrosion activity. |
| Stoulil et al.72 (2015) | Zn1.5Al1.5Mg Zn11Al3Mg0.2Si | CP | SKP, EIS, PL, GD-OES; NaCl drop, RH controlled | Formation of compact corrosion products with lower electric conductivity and better barrier properties. |
| Reference | Material | Category | Methods | Main results |
| Yao et al.98 (2016) | Zn5Al(0-2)Mg | C, M, CP | SST, XRD, SEM, Echem; 3.5 wt.% NaCl | Refined Zn grain size and increased eutectic areas at Zn grain boundary with increasing %Mg. Formation of simonkolleite reduces corrosion process. |
| Azevedo et al.99 (2015) | Zn3.7Al3Mg | CP, AC | SST, XRD, SEM, titration; NaCl, Na2SO4, ARW | Presence of NH4+ and HCO3- delays LDH formation and Al dissolution by buffering pH. |
| Azevedo et al.100 (2015) | Zn3.7Al3Mg | Electrolyte | AESEC active-passive cycle, XRD; Cl-, NH4+, HCO3- | Mg(OH)2 formation rather than LDH. NH4+: increased anodic Zn reactivity, suppressed Zn-corrosion product, inhibited Al dissolution; HCO3-: increased insoluble Zn-corrosion product. |
| Tokuda et al.101 (2024) | Zn11Al3Mg0.2Si Zn0.18Al | CP | XRF, XRD, SEM, Echem; ASW | Mg-based corrosion product served as a barrier. |
| Holzner et al.102 (2022) | Zn2.5Al1.5Mg | CC (LDH) | SST, XEM, XRD, mass loss, Echem (0.5 M NaCl) | Enhanced corrosion resistance after 30 s of LDH formation. |
| Tanguy et al.103 (2019) | Zn(≤5%)Al(≤3%)Mg | M, CP, PCC | XPS, SEM, Echem, mass loss; PCC bath at 60 °C | Effect of Ti-activation on PCC. Fine microstructure was completely covered by PCC. |
| Lostak et al.104 (2014) | Zn3.97Al5.78Mg | ZrCC | SKPFM, XPS, SEM | CC formation initiated at Zn-rich sites for t < 40 s. For t > 40 s, CC formed at Mg-rich phases. |
| Ponomareva et al.105 (2024) | Zn2.5Al1.5Mg | ZrCC | XPS, LEIS, AFM, AES; Na2B4O7 (pH 9), NaH2PO4 (pH 9), NaOH (pH 12.7), H2SO4 (pH 2) | ZrO2-ZrOxFy layer and an underlying MgAlF layer formation after alkaline pretreatment. Zr oxide layer formation in acidic solution. |
| Chen et al.106 (2024) | Zn6Al3Mg | ZrCC | SEM, mass loss; SO2 and NH3 gas environments | Lower corrosion rate than Zn-Al alloys in SO2 but higher corrosion rate in NH3 environment. |

Techniques: scanning vibrating electrode technique (SVET); electrochemistry (Echem); scanning electron microscope (SEM); X-ray photoelectron spectroscopy (XPS); Auger electron spectroscopy (AES); focused ion beam - transmission electron microscopy (FIB-TEM); X-ray diffraction (XRD); scanning Kelvin probe forced microscopy (SKPFM); time lapse microscopy (TLM); infrared reflection absorption spectroscopy (IRRAS); Fourier transformed infrared spectroscopy (FTIR); low-energy ion scattering (LEIS); atomic force microscopy (AFM); glow-discharge optical emission spectroscopy (GD-OES); differential scanning calorimetry (DSC); X-ray microscopy (XRM).

Others: salt spray test (SST); cyclic corrosion test (CCT); filiform corrosion (FFC); artificial rain water (ARW); artificial sea water (ASW); relative humidity (RH); hot-dip galvanized steel (HDG); layered double hydroxide (LDH).

Table S2. pH = 8.4, 30 mM NaCl, Ar deaerated.

| V vs. SCE | Zn | Al | Mg | Zn0.7Al | Zn22Al | Zn68Al | MgZn2 | Zn5Al | Zn55Al | ZnAlMg |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Eoc | -1.00 | -1.20 | -1.61 | -1.11 | -1.10 | -1.10 | -1.09 | -0.99 | -1.12 | -1.13 |
| Ej=0 | -1.15 | -1.13 | -1.59 | -1.16 | -1.20 | -1.17 | -1.25 | -1.17 | -1.17 | -1.30 |
| EcZn | -1.21 | - | - | -1.20 | -1.12 | -1.17 | -1.15 | -1.18 | -1.17 | -1.13 |
| ba, jZn / mV decade-1 | 75 | - | - | 56 | 48 | 47 | 104 | 57 | 52 | 55 |
| jsZn / A cm-2 | 3.8 | - | - | 5.4 | 2.3 | 0.1 | 0.6 | 2.5 | 0.5 | 0.5 |
| jsAl / A cm-2 | - | 2.3 | - | 0 | 3.2 | 4.7 | - | 0 | 2.7 | 0.5 |
| jsMg / A cm-2 | - | - | 194 | - | - | - | 1.7 | - | - | 0.7 |

Table S3. pH = 8.4, 30 mM NaCl, O2 saturated.

| V vs. SCE | Zn | Al | Mg | Zn0.7Al | Zn22Al | Zn68Al | MgZn2 | Zn5Al | Zn55Al | ZnAlMg |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Eoc | -0.93 | -0.71 | -1.60 | -0.94 | -1.05 | -0.99 | -0.99 | -0.93 | -0.98 | -0.95 |
| Ej=0 | -0.85 | -0.75 | -1.58 | -0.90 | -1.00 | -0.91 | -0.87 | -0.91 | -0.89 | -0.90 |
| EcZn | -0.90 | - | - | -1.01 | -1.08 | -0.94 | -0.87 | -1.05 | -0.91 | -0.93 |
| ba, jZn / mV decade-1 | 28 | - | - | 51 | 13 | 82 | 21 | 55 | 35 | 11 |
| jsZn / A cm-2 | 2.1 | - | - | 8.2 | 1.5 | 0 | 0.3 | 10 | 0.6 | 12 |
| jsAl / A cm-2 | - | 5 | - | 0 | 7.5 | 2.9 | - | 0 | 1.1 | 3 |
| jsMg / A cm-2 | - | - | 165 | - | - | - | 4.3 | - | - | 1.7 |

Table S4. pH = 10.1, 30 mM NaCl, Ar deaerated.

| V vs. SCE | Zn | Al | Mg | Zn0.7Al | Zn22Al | Zn68Al | MgZn2 | Zn5Al | Zn55Al | ZnAlMg |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Eoc | -0.98 | -1.44 | -1.65 | -0.96 | -1.30 | -1.31 | -1.06 | -1.12 | -1.22 | -1.07 |
| Ej=0 | -1.21 | -1.41 | -1.64 | -1.27 | -1.29 | -1.28 | -1.21 | -1.31 | -1.30 | -1.31 |
| EcZn | -1.10 | - | - | -1.12 | -1.13 | -1.14 | -0.96 | -1.12 | -1.10 | -1.14 |
| ba, jZn / mV decade-1 | 71 | - | - | 54 | 39 | 27 | 20 | 59 | 54 | 55 |
| jsZn / A cm-2 | 0.7 | - | - | 1.3 | 0.35 | 0 | 0.1 | 1.0 | 0.3 | 0.3 |
| jsAl / A cm-2 | - | 20.7 | - | 0 | 12.6 | 36.9 | - | 3.8 | 2.0 | 1.9 |
| jsMg / A cm-2 | - | - | 93 | - | - | - | 2.2 | - | - | 0.29 |

Table S5. pH = 10.1, 30 mM NaCl, O2 saturated.

| V vs. SCE | Zn | Al | Mg | Zn0.7Al | Zn22Al | Zn68Al | MgZn2 | Zn5Al | Zn55Al | ZnAlMg |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Eoc | -0.95 | -1.29 | -1.63 | -0.93 | -1.01 | -1.11 | -0.98 | -0.93 | -1.10 | -0.95 |
| Ej=0 | -0.96 | -1.25 | -1.42 | -0.90 | -0.96 | -0.91 | -0.96 | -0.91 | -0.90 | -0.89 |
| EcZn | -0.96 | - | - | -0.91 | -1.06 | -0.94 | -0.88 | -0.93 | -0.91 | -0.90 |
| ba, jZn / mV decade-1 | 45 | - | - | 14 | 105 | 49 | 20 | 7 | 31 | 12 |
| jsZn / A cm-2 | 17 | - | - | 11 | 0.29 | 0 | 0 | 2.2 | 0.9 | 6 |
| jsAl / A cm-2 | - | 20 | - | 0.3 | 20 | 27.5 | - | 1.5 | 4.2 | 5.9 |
| jsMg / A cm-2 | - | - | 82 | - | - | - | 1.7 | - | - | 0.84 |

Table S6. pH = 12.8, 0.1 M NaOH, Ar deaerated.

| V vs. SCE | Zn | Al | Mg | Zn0.7Al | Zn22Al | Zn68Al | MgZn2 | Zn5Al | Zn55Al | ZnAlMg |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Eoc | -1.51 | -1.62 | -1.65 | -1.51 | -1.53 | -1.60 | -1.41 | -1.58 | -1.66 | -1.59 |
| Ej=0 | -1.52 | -1.62 | -1.59 | -1.51 | -1.51 | -1.59 | -1.41 | -1.52 | -1.64 | -1.58 |
| EcZn | -1.45 | - | - | -1.56 | -1.36 | -1.39 | -1.45 | -1.45 | -1.33 | -1.55 |
| ba, jZn / mV decade-1 | 36 | - | - | 33 | 47 | 102 | 96 | 31 | 30 | 34 |
| jsZn / A cm-2 | 22 | - | - | 20 | 0 | 0.1 | 3.2 | 0 | 0.2 | 0.01 |
| jsAl / A cm-2 | - | 4 | - | 0.007 | 1.4 | 1.6 | - | 0.086 | 2 | 0.048 |
| jsMg / A cm-2 | - | - | 0.1 | - | - | - | 0.05 | - | - | 0 |

Table S7. pH = 12.8, 0.1 M NaOH, O2 saturated.

| V vs. SCE | Zn | Al | Mg | Zn0.7Al | Zn22Al | Zn68Al | MgZn2 | Zn5Al | Zn55Al | ZnAlMg |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Eoc | -0.92 | -1.61 | -1.68 | -1.01 | -1.49 | -0.15 | -1.24 | -1.15 | -1.56 | -1.22 |
| Ej=0 | -0.79 | -1.61 | -1.66 | -0.94 | -1.43 | -1.57 | -1.13 | -0.98 | -1.47 | -1.12 |
| EcZn | -1.73 | - | - | -1.71 | -1.72 | -1.53 | -1.70 | -1.76 | -1.65 | -1.77 |
| ba, jZn / mV decade-1 | 76 | - | - | 109 | 45 | 24 | 104 | 92 | 44 | 111 |
| jsZn / A cm-2 | 64 | - | - | 77 | 721 | 0.4 | 25 | 232 | 1 | 121 |
| jsAl / A cm-2 | - | 3.7 | - | 0.006 | 0.77 | 1.8 | - | 0.33 | 2 | 0.15 |
| jsMg / A cm-2 | - | - | 0.054 | - | - | - | 0.1 | - | - | 0.06 |