Theoretical investigation on the complexation characteristics and spectral properties of CdTe QDs with four capping agents

Qinghong Yang. Xujiang Wan .Yang Chen .Hui Luo . Yan Zheng* . Laicai Li*

College of Chemistry and Material Science, Sichuan Normal University, Chengdu, 610068, China.

E-mail: zhengyanchem@163.com; lilcmail@163.com

Table of Contents

Fig. S1. The stable complexation configurations of GSH、TG and MES on (CdTe)n(n=6,9) respectively

Fig. S2. The electron density maps of stable complexation structures of MPA、GSH、TG and MES

on (CdTe)n(n=6,9)

Table S1. The milliken charge values of MPA、GSH、TG、MES、(CdTe)n(n=6,9) before complexation and the stable configurations after complexation

Fig. S1 The stable complexation configurations of GSH、TG and MES on (CdTe)n(n=6,9) respectively

Fig. S2. The electron density maps of stable complexation structures of MPA、GSH、TG and MES on (CdTe)n (n = 6, 9)

Table S1.  The Milligan charge values of MPA、GSH、TG、MES、(CdTe)n(n=6,9) before complexation and the stable configurations after complexation

| complexes | q/e | complexes | q/e | complexes | q/e | complexes | q/e |
| --- | --- | --- | --- | --- | --- | --- | --- |
| (CdTe)6 | Cd1=0.24 Te1=-0.24 | MPA | S1=-0.82 | TG | S1=-0.77 |  |  |
| (CdTe)9 | Cd1=0.10 Cd4=0.37 Te1=-0.24 Te4=-0.33 | GSH | S1=-0.64 | MES | S1=-0.95 |  |  |
| A1-MPA | S1=0.23 Cd1=0.22 Cd2=0.19 | A1-GSH | S1=0.43 Cd1=0.18 Cd2=0.20 | A1-TG | S1=0.09 Cd1=0.35 Cd2=0.23 | A1-MES | S1=0.39 Cd1=0.19 Cd2=0.19 |
| A2-MPA | S1=-0.20 Cd1=0.47 | A2-GSH | S1=-0.21 Cd1=0.40 | A2-TG | S1=-0.22 Cd1=0.52 | A2-MES | S1=-0.20 Cd1=0.38 |
| A3-MPA | S1=0.19 Cd1=0.17 Cd2=0.19 | A3-GSH | S1=0.30 Cd1=0.18 Cd2=0.23 | A3-TG | S1=0.22 Cd1=0.21 Cd2=0.15 | A3-MES | S1=0.38 Cd1=0.17 Cd2=0.18 |
| A4-MPA | S1=-0.14 Cd1=0.36 | A4-GSH | S=-0.17 Cd1=0.39 | A4-TG | S1=-0.16 Cd1=0.36 | A4-MES | S1=-0.21 Cd1=0.42 |
| A5-MPA | S1=-0.06 Cd4=0.42 | A5-GSH | S=-0.23 Cd1=0.47 | A5-TG | S1=-0.08 Cd4=0.44 | A5-MES | S1=-0.37 Cd4=0.50 |