Extended Data Fig. 1 | Generic fabrication of high-phase-purity TMDs. a,e XPS spectra of exfoliated WS2 NSs (a) and MoSe2 NSs (e). b,f AFM images and measured thicknesses of exfoliated 1T’-WS2 NSs (b) and 1T’-MoSe2 NSs (f). c,d,g,h Atomic-resolution HAADF-STEM image of 1T’-WS2 NSs (c), 2H-WS2 NSs (d), 1T’-MoSe2 NSs (g) and 2H-MoSe2 NSs (h) (inset: the corresponding fast Fourier transform pattern) and panels share the same scale bar.

Extended Data Fig. 2 | AFM images of exfoliated 1T’/2H-MoS2 heterophase NSs. Heterophase MoS2 with 1T’ ratio of 13% (a), 45% (b), 78% (c) and 92% (d).

Extended Data Fig. 3 | The energy difference between 1T’-MoS2 and 2H-MoS2.

Extended Data Fig. 4 | Post-process and characterization of exfoliated 1T’ MoS2. a, Photographs of 1T’-MoS2 NSs after drying from ink solutions. b,c Photo of a 1T’-MoS2 membrane (diameter=11 cm) fabricated onto a polyvinylidene difluoride (PVDF) substrate by vacuum filtration (b) and good flexibility of the membrane (c). d, Cross-section SEM view and corresponding EDS elemental mappings of 1T’-MoS2 membrane.

Extended Data Fig. 5 | Electrochemical NO3−RR stability test and performance comparison of 1T’-TMDs flakes. a, Long-term electrocatalytic stability test of the NO3−RR over 1T’-WS2 at 1.0 A cm−2 in a H-cell. Arrows indicate the renewal of fresh electrolytes (the measured potentials were not iR-compensated). b, NO3− RR performance of 1T’-MoS2, 1T’-WS2, 1T’-MoSe2 and 2H/1T mixed MoS2 comparison with reported electrocatalyst.