Supporting information

A surface-imprinting lanthanide fluorescent hybrid probe on the SiO2 microspheres for the detection of the enrofloxacin

Xiao-Qing Huang1,†，Mao-Yu Wang1,†, Xiao-Chen Wang2,†, Xin Shi1, Rui-Wen Li1, Shuang Wu1 and Ying Li1, *

1 School of Materials and Chemistry, University of Shanghai for Science and Technology, Shanghai 200093, P. R. China

2 Shandong Center for Food and Drug Evaluation&Inspection, Shandong 250014, P. R. China

†  These two authors contributed equally to this work

*  Correspondence: liying@usst.edu.cn. (Y.L)

Fig S1. XPS wide-scan high-resolution full spectrum of SiO2@Eu(DBM)3Phen/SMIP (a); XPS narrow-scan maps of C1s (b), Eu3d (c), N1s (d), O1s (e) and Si2p (f)

Fig S2. (a) Emission spectra of pure Eu(DBM)3Phen complexes (a) and SiO2@Eu(DBM)3Phen(b)

Fig S3. Effect of incubation time (a) and concentration (b) on the fluorescence burst value (F/F0) of SiO2@Eu(DBM)3Phen/SMIP

Fig S4. MIP and NIP dynamic adsorption curves of 0.3 mg/ml SiO2@Eu(DBM)3Phen/SNIP/SMIP incubated with an initial concentration of 100 mg/ml enrofloxacin at 500 rpm stirring speed for 30 min

Fig S5. Static adsorption curves of MIP and NIP on different concentrations of ENFX (0, 50, 75, 150, 300, 400, 500 mg/L) in 1h

Fig S6. Ion immunity detection for MIP

Table S1 Detection of ENFX content in real samples using the probe.

| Sample | Spiked concentration (μmol/L) | Detectable limit (μmol/L) | Recovery rate (%) | RSD (%) |
| --- | --- | --- | --- | --- |
| Milk | 5 | 5.81 | 116.18% | 1.03% |
|  | 10 | 10.53 | 105.31% | 1.36% |
|  | 25 | 24.35 | 97.40% | 1.01% |
|  | 50 | 47.32 | 94.64% | 1.27% |
|  | 80 | 79.29 | 99.11% | 0.89% |
|  | 100 | 96.35 | 96.35% | 0.83% |
| Drinking water | 5 | 5.22 | 104.4% | 0.97% |
|  | 10 | 10.16 | 101.6% | 1.03% |
|  | 25 | 25.59 | 102.36% | 1.16% |
|  | 50 | 48.59 | 97.18% | 0.99% |
|  | 80 | 79.48 | 99.35% | 1.06% |  |
|  | 100 | 96.96 | 96.96% | 1.05% |  |