Supporting Information

Structural and Mechanistic Insights into a Cu-Adenine MOF for Selective Fluorescence Sensing of Antibiotics: Experimental and TDDFT Approaches

Tanin Nanok1, Tontrakarn  Pongpai1, Kittinan  Ketsrisung1, Jiraporn Singhophon1, Kittipong Chainok2, and Tanwawan Duangthongyou1,3*

1Faculty of Science, Kasetsart University, Bangkok 10900, Thailand.

2Thammasat University Research Unit in Multifunctional Crystalline Materials and Applications (TU-MCMA), Faculty of Science and Technology, Thammasat University, Pathum Thani 12120, Thailand.

3The Center of Excellence for Innovation in Chemistry (PERCH-CIC), Department of Chemistry, Faculty of Science, Kasetsart University, Bangkok 10900

*Correspondence should be addressed to Tanwawan Duangthongyou: fscitwd@ku.ac.th

Table S1 Selected bond lengths (Å) of [Cu(adenine)(succinate)]ₙ.

| Atom-Atom | Length (Å) | Atom-Atom | Length (Å) |
| --- | --- | --- | --- |
| Cu1-O1 Cu1-N1 Cu1-O2 Cu1-N2 Cu1-N5 O1-C1 O2-C1 C1-C2 | 2.002(2) 1.970(1) 2.011(3) 2.160(1) 2.030(1) 1.247(4) 1.247(4) 1.492(5) | N4-C5 N4-H4A N4-H4B C2-H2A C2-H2B C3-H3 C6-H6 | 1.340(2) 0.860 0.860 0.969 0.970 0.930 0.930 |

Table S2 Selected bond angles (º) of [Cu(adenine)(succinate)]ₙ.

| Atom-Atom-Atom | Angle (º) | Atom-Atom-Atom | Angle (º) |
| --- | --- | --- | --- |
| O1-Cu1-N1 O1-Cu1-O2 O1-Cu1-N2 O1-Cu1-N5 N1-Cu1-O2 N1-Cu1-N2 N1-Cu1-N5 O2-Cu1-N2 | 87.1(5) 160.6(1) 105.2(3) 93.9(4) 91.9(5) 100.8(6) 165.9(6) 94.0(3) | O2-Cu1-N5 N2-Cu1-N5 Cu1-O1-C1 C1-O2-Cu1 Cu1-N1-C7 C1-C2-C2 C7-N5-Cu1 | 82.5(4) 92.6(5) 125.3(2) 127.3(2) 127(1) 110.9(3) 119.1(9) |