Supplementary Information

Enhanced Hydrogen Evolution Reaction Kinetics by Sulfur Incorporation in Transition Metal-Based Oxyhydroxide Electrodes

Jun Seok Haa,b,i, Seung Hun Leea,i, Sung Jun Leec, In Tae Kimc, Seo Hyun Parkc, Woo Jae Leed, Kyeong-Ho Kime, Jooyoung Leeb, Yangdo Kima*, Sung Mook Choib,f*, Yoo Sei Parkg,h*

AUTHOR ADDRESS.

a Department of Materials Science and Engineering, Pusan National University, Busan, 46241, Republic of Korea

b Department of Energy & Environment Materials Research Division, Korea Institute of Materials Science (KIMS), Changwon 51508, Republic of Korea

c Department of Urban, Energy, and Environmental Engineering, Chungbuk National University, Chungdae-ro 1, Seowon-Gu, Cheongju, Chungbuk 28644, Republic of Korea

d Division of Nanotechnology and Semiconductor Engineering, Pukyong National University, 45 Yongso-ro, Busan 48513, Republic of Korea

e Department of Materials Science and Engineering, Pukyong National University, Busan 48513, Republic of Korea

f Advanced Materials Engineering, University of Science and Technology (UST), Yuseong-gu, Daejeon 34113, Republic of Korea

g Department of Nanoenergy Engineering, Pusan National University, 50, Busandaehak-ro 63 beon-gil 2, Geumjeong-gu, Busan 46241, Republic of Korea

h Department of Nano Fusion Technology, Pusan National University, Busandaehak-ro 63 beon-gil 2, Geumjeong-gu, Busan 46241, Republic of Korea

i These authors contributed equally: Jun Seok Ha, Seung Hun Lee

*E-mail: yoosei@pusan.ac.kr (Prof. Yoo Sei Park), akyzaky@kims.re.kr (Dr. Sung Mook Choi), yangdo@pusan.ac.kr (Prof. Yangdo Kim)

Figure S1. Photographs of NiFeCo/NF and S-NiFeCo/NF.

Figure S2. SEM image of NiFeCo/NF.

Figure S3. (a) TEM image of NiFeCo/NF. (b) EDS elemental mapping images of the NiFeCo/NF : Ni(red), Fe(blue), Co(green), O(yellow).

Figure S4. EDS elemental mapping images of the S-NiFeCo/NF : Ni(green), Fe(red), Co(blue), S(purple).

Figure S5. XPS spectrum Co 2p.

Figure S6. XPS spectrum O 1s.

Figure S7. LSV curves of (a) NiFeCo/NF and (b) S-NiFeCo/NF at different temperatures.

Figure S8. ln(i/mAcm-2) vs. overpotential plots of (a) NiFeCo/NF, (b) S-NiFeCo/NF at different temperatures.

Figure S9. Arrhenius plots of (a) NiFeCo/NF and (b) S-NiFeCo/NF at different overpotentials.