Support information

Theoretical study of novel B2CO compounds with high hardness

Chao LIUa,b *, Lingyu LIUc, Pan YINGd

a College of Rare Earths, Faculty of Materials Metallurgy and Chemistry, Jiangxi University of Science and Technology, Ganzhou 341000, China

b State Key Laboratory of Metastable Materials Science and Technology, Yanshan University, Qinhuangdao 066004, China

c School of Physics and Optoelectronic Engineering, Guangdong University of Technology, Guangzhou 510006, China

d Hebei Key Laboratory of Microstructural Material Physics, School of Science, Yanshan University, Qinhuangdao 066004, China

Author to whom correspondence should be addressed. E-mail address: liuchao198967@126.com.

Table S1	The elastic matrix of two reported B2CO phases at different pressure, the numerical unit is unified with GPa.

| oP8’ |  |  |  |  |  | mP16 |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 792.2 | 52.4 | 98.7 |  |  |  | 566.1 | 182.9 | 134.3 |  | -3.5 |  |
| …… | 358.7 | 141.7 |  |  |  | …… | 561.4 | 123.6 |  | -1.5 |  |
| …… | …… | 258.1 |  |  |  | …… | …… | 704.7 |  | 45.7 |  |
|  |  |  | 208.2 |  |  |  |  |  | 253.1 |  | 9.3 |
|  |  |  |  | 204.5 |  | …… | …… | …… |  | 239.8 |  |
|  |  |  |  |  | 163.4 |  |  |  | …… |  | 193.5 |
| 10 GPa |  |  |  |  |  | 10 GPa |  |  |  |  |  |
| 1045.2 | 121.6 | 243.3 |  |  |  | 808.8 | 230.7 | 201.4 |  | -7.5 |  |
| …… | 399.5 | 230.6 |  |  |  | …… | 839.1 | 250.3 |  | 15.6 |  |
| …… | …… | 531.3 |  |  |  | …… | …… | 949.5 |  | 36.2 |  |
|  |  |  | 320.7 |  |  |  |  |  | 318.6 |  | 26.0 |
|  |  |  |  | 327.3 |  | …… | …… | …… |  | 284.6 |  |
|  |  |  |  |  | 212.7 |  |  |  | …… |  | 204.4 |
| 50 GPa |  |  |  |  |  | 50 GPa |  |  |  |  |  |
| 1262.1 | 192.7 | 430.6 |  |  |  | 1022.3 | 337.8 | 300.1 |  | -15.3 |  |
| …… | 860.4 | 384.9 |  |  |  |  | 1080.8 | 395.9 |  | 24.4 |  |
| …… | …… | 871.4 |  |  |  |  |  | 1197.0 |  | 35.8 |  |
|  |  |  | 471.0 |  |  |  |  |  | 361.1 |  | 41.1 |
|  |  |  |  | 490.6 |  |  |  |  |  | 315.6 |  |
|  |  |  |  |  | 255.0 |  |  |  |  |  | 207.8 |
| 100 GPa |  |  |  |  |  | 100 GPa |  |  |  |  |  |

Fig S1 Phonon dispersion spectra (left panel) and phonon DOS (right panel) at different HP, a, c and e represent oP8’-B2CO, b, d and f represent mP16-B2CO, respectively.

Fig. S2	Calculated formation enthalpies ΔHf via pressure of several IED B-C-O with the critical pressures all below 30 GPa, a and b represents B2CO and B2CXO (x=2, 3, 5), respectively.

Fig. S3	The relationship of (a) pressure and volume per formula, (b) pressure and band gap of all B2CXO (X=2, 3, 5) phases at AP to 100 GPa.

Table S2	The independent elastic constant Cijs of oP8’ at HP, the numerical units of pressure P and Cijs are unified with GPa.

| P Cij | 20 | 30 | 40 | 60 | 70 | 80 | 90 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| C11 | 865.0 | 931.7 | 993.0 | 1093.3 | 1136.9 | 1175.7 | 1218.6 |
| C22 | 376.4 | 391.1 | 410.0 | 416.2 | 489.0 | 615.2 | 749.7 |
| C33 | 325.9 | 395.2 | 466.8 | 611.9 | 691.3 | 761.7 | 822.1 |
| C44 | 236.6 | 268.0 | 296.3 | 346.1 | 372.4 | 407.3 | 442.5 |
| C55 | 229.3 | 258.5 | 290.4 | 370.0 | 409.6 | 441.1 | 468.5 |
| C66 | 177.0 | 189.4 | 202.0 | 224.9 | 235.8 | 243.0 | 249.2 |
| C12 | 69.0 | 88.9 | 109.2 | 136.7 | 151.6 | 163.9 | 177.5 |
| C13 | 131.8 | 169.6 | 207.5 | 285.8 | 326.9 | 363.7 | 398.4 |
| C23 | 168.7 | 198.7 | 226.9 | 237.9 | 259.5 | 299.0 | 344.5 |

Table S3	The elastic matrix of mP16 B2CO phases at different pressure, the numerical unit is unified with GPa.

| 638.9 | 184.5 | 147.5 |  | -4.2 |  | 701.1 | 196.1 | 163.9 |  | -5.4 |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| …… | 650.2 | 158.5 |  | 4.8 |  | …… | 720.2 | 190.1 |  | 9.4 |  |
| …… | …… | 773.6 |  | 41.4 |  | …… | …… | 836.5 |  | 38.9 |  |
|  |  |  | 275.8 |  | 14.5 |  |  |  | 292.9 | 0 | 18.9 |
| …… | …… | …… |  | 254.0 |  | …… | …… | …… |  | 265.6 |  |
|  |  |  | …… |  | 197.1 |  |  |  | …… |  | 200.0 |
| 20 GPa |  |  |  |  |  | 30 GPa |  |  |  |  |  |
| 758.3 | 212.3 | 182.3 | 0 | -6.4 | 0 | 856.6 | 250.7 | 221.4 |  | -8.5 |  |
| …… | 782.9 | 220.5 |  | 13.0 |  | …… | 891.5 | 280.1 |  | 18.2 |  |
| …… | …… | 894.8 |  | 37.3 |  | …… | …… | 1002.8 |  | 36.0 |  |
|  |  |  | 306.9 |  | 22.7 |  |  |  | 329.0 |  | 29.4 |
| …… | …… | …… |  | 275.8 |  | …… | …… | …… |  | 292.5 |  |
|  |  |  | …… |  | 202.6 |  |  |  | …… |  | 205.7 |
| 40 GPa |  |  |  |  |  | 60 GPa |  |  |  |  |  |
| 901.6 | 271.4 | 241.3 |  | -10.4 |  | 942.6 | 292.9 | 260.7 |  | -11.2 |  |
| …… | 941.5 | 308.7 |  | 19.7 |  | …… | 989.4 | 338.4 |  | 21.6 |  |
| …… | …… | 1053.5 |  | 35.4 |  | …… | …… | 1102.5 |  | 35.4 |  |
|  |  |  | 337.1 |  | 32.6 |  |  |  | 345.5 |  | 35.4 |
| …… | …… | …… |  | 299.3 |  | …… | …… | …… |  | 305.3 |  |
|  |  |  | …… |  | 206.6 |  |  |  | …… |  | 207.3 |
| 70 GPa |  |  |  |  |  | 80 GPa |  |  |  |  |  |
| 984.0 | 315.7 | 280.7 |  | -13.3 |  |  |  |  |  |  |  |
| …… | 1036.4 | 367.8 |  | 23.1 |  |  |  |  |  |  |  |
| …… | …… | 1151.2 |  | 35.5 |  |  |  |  |  |  |  |
|  |  |  | 354.3 |  | 38.3 |  |  |  |  |  |  |
| …… | …… | …… |  | 311.1 |  |  |  |  |  |  |  |
|  |  |  | …… |  | 207.9 |  |  |  |  |  |  |
| 90 GPa |  |  |  |  |  |  |  |  |  |  |  |