Table.1 Results of electrochemical impedance and Warburg coefficient of MoS2/NC  electrode.

Table.1 Results of electrochemical impedance and Warburg coefficient of MoS2/NC electrode.

| Cell | Rs , Ω | Rct , Ω | Aw , Ω s−1/2 |
| --- | --- | --- | --- |
| Before 500 cycles | 12.82 | 91.28 | 103.74 |
| After 500 cycles | 4.152 | 137 | 115.64 |