Supporting Information

Optimizing Electron Transport in Crystalline Silicon Solar Cells with Oxygen-Doped Titanium Carbide Layers

Lei He1, Kuiwen Guan1,  Biao Sun4, Zhiping Huang2,3, Ying Xu4, Huaidong Yin2*,  Deyuan Wei5*, Yang Ding,2,4*

To investigate the structural characteristics of ultra-thin TiCxOy films, a 5 nm TiCxOy layer was deposited on monocrystalline silicon substrates with a resistivity of 1–5 Ω·cm and (100) orientation for transmission electron microscopy (TEM) analysis. As shown in Figure S1a, the TiCxOy film forms a continuous, relatively uniform layer approximately 6 nm thick, slightly exceeding the expected thickness by about 1 nm. Small protruding particles, measuring 0.9–2.4 nm in width and 0.8–1.2 nm in height, were observed on the film surface, indicating a surface roughness of around 1–2 nm.

Figure S1b shows a  TEM image of the TiCxOy film, with dark regions representing the silicon substrate, revealing a clear lattice structure. The intermediate dark band represents the TiCxOy film, which displays a mixed amorphous and microcrystalline structure. As highlighted by the orange contour in Figure S1c, nano-crystalline grains are embedded within the continuous amorphous phase, confirming the presence of nanocrystallites in an overall amorphous matrix. Figure S1c provides a magnified view of these nanocrystallites, showing partially ordered atomic arrangements in polygonal structures. Red circles highlight the irregular distribution of carbon vacancies.

The TEM findings corroborate the crystallization observed in X-ray diffraction (XRD) analysis and the carbon vacancies indicated in Raman spectra, demonstrating that TiCxOy films consist of coexisting crystalline and amorphous phases with abundant defect sites.

Figure S1. Cross-Sectional TEM Images of EBE-TiCxOy Thin Film; (a) Cross-sectional TEM image; (b) High-resolution TEM image; (c) Grain distribution map.

Figure S2. a) device structure diagram of TLM test. b) calculation principle for contact resistivity using TLM method.

Figure S3. UPS Spectra of TiCxOy Films at Different Evaporation Rates.

Figure S4. XPS Spectra of TiCxOy Films at Different Evaporation Rates.

Figure S5. Correspondence between Growth Rate and (a) Carrier Concentration; (b) Mobility.

Figure S6.  Minority Carrier Lifetime of 50 nm EBE-TiCxOy prepared at Evaporation Rate of 1.0 Å/s.