Table 2: Recommended practices of RSW joint in low carbon steel sheets

| Sl. No. | TH (mm) | Ep (bar) | Tsq (Cycles) | IW (kA) | TW (Cycles) | Tq/c (Cycles) |
| --- | --- | --- | --- | --- | --- | --- |
| 01 | 1 – 1.5 | 3.5 | 40 | 12 | 12 | 15 |
| Thickness (TH), Electrode pressure (Ep), Squeeze Time (Tsq), Weld Current (IW), Weld Time (TW), WN dia. (Dn), quench/cool time (Tq/c) |  |  |  |  |  |  |